# ELE 717 Solid State Electronics

A week-by-week course following the 15-week Lecture 2 plan

Table of Contents

Orientation · Course

# Start Here

Course: ELE 717 Solid State Electronics (3 credits, compulsory), Postgraduate Diploma, Nigerian Defence Academy. Lecturer: Engr. Mrs Ruby Chinyere Beremeh Onyesoh.

This course follows the lecturer's own 15-week plan (Lecture 2). There is one page per week, grouped into the five modules of the plan. Week 1 follows the issued lecture notes slide by slide. Weeks 2–15 teach each topic on the plan from scratch, because the notes for those weeks have not been issued yet.

Each week ends with solved questions:

- the lecturer's own revision and calculation questions (Week 1);

- every one of the 50 PGD examination questions (Q1–Q50), filed under the week that teaches it;

- CAT practice tests with answers in Weeks 6 and 12.

## The 15-week plan

| Week | Topic (from the lecture plan) | Exam questions |
| --- | --- | --- |
| Module 1 | Material Physics & Semiconductor Growth (Weeks 1–3) |  |
| 1 | Introduction to semiconductor materials: elemental vs compound (Si, Ge, GaAs); crystal structures, Miller indices and bonding | Q1–Q8 |
| 2 | Material growth: purification of silicon (metallurgical to electronic grade); Czochralski bulk growth; epitaxy (VPE, LPE, MBE) | Q9–Q13 |
| 3 | Impurity control and doping: diffusion and ion implantation; controlled doping profiles and evaluation of impurity distribution | Q14–Q21 |
| Module 2 | Energy Bands & Carrier Statistics (Weeks 4–6) |  |
| 4 | Energy bands and carrier concentrations: quantum mechanics (Schrödinger, Kronig–Penney); band gaps; intrinsic and extrinsic concentrations | Q22–Q29, Q34 |
| 5 | Carrier statistics: Fermi–Dirac function; density of states; Fermi level against temperature and doping | Q30–Q33 |
| 6 | Continuous Assessment Test 1 and review: crystal structures and carrier statistics | CAT 1 practice |
| Module 3 | Carrier Transport & Injection Phenomena (Weeks 7–9) |  |
| 7 | Drift and diffusion currents: mobility, scattering, conductivity; diffusion, Fick's law, Einstein relation | Q35–Q40 |
| 8 | High-field effects and excess carriers: velocity saturation, hot carriers; generation and recombination (SRH); lifetime and steady-state injection | Q41–Q44 |
| 9 | Continuity equation and surface phenomena: minority-carrier continuity equation; surface states and surface recombination velocity | Q45–Q46 |
| Module 4 | Junctions, Interfaces & Characterisation (Weeks 10–12) |  |
| 10 | The p-n junction: built-in potential, depletion width, field profile; Shockley equation under forward and reverse bias | Q47–Q48 |
| 11 | Metal–semiconductor interfaces: Schottky barrier vs Ohmic contact; band diagrams in equilibrium and under bias | Q49 |
| 12 | Interface characterisation: C-V profiling, I-V analysis; CAT 2 | Q50, CAT 2 practice |
| Module 5 | Advanced Device Technology (Weeks 13–15) |  |
| 13 | Bipolar junction transistors: operation, minority-carrier profiles, emitter efficiency, base transport factor, α and β | — |
| 14 | MOSFETs: ideal MOS capacitor (accumulation, depletion, inversion), threshold voltage, linear and saturation regions | — |
| 15 | Revision and final exam preparation: formula sheet, problem-solving clinic, past-question review | All |

After Week 15 there are two more pages: the answer key for all 50 exam questions, and the laboratory practicals.

## Laboratory and practical component (3 hours/week)

The plan requires at least four practical or simulation experiments. Each one has its own section in the Laboratory page:

- Simulation of carrier transport: modelling Fermi-level shifts in MATLAB or Python.

- I-V characterisation: measuring and plotting the forward and reverse characteristics of a p-n junction and a Schottky diode.

- C-V profiling: finding doping concentration and built-in potential from capacitance measurements.

- MOSFET parameter extraction: measuring threshold voltage Vth and channel mobility.

## Assessment

- CAT 1 (Week 6): crystal structures and carrier statistics (Weeks 1–5).

- CAT 2 (Week 12): transport, junctions and interfaces (Weeks 7–12).

- Final examination: the whole course. The 50-question PGD paper is the best guide to its style.

## How to study each week

- Read the week's Symbols and abbreviations table first. Every week has one near the top, listing every symbol, constant and abbreviation used on that page with its meaning and units, so you can start at any week. The Glossary page at the end lists all of them.

- Read the week's notes once, straight through.

- Cover the answers and attempt every question on paper.

- For derivations, check you stated the assumptions; marks are given for them.

- Tick the week as read (the button at the bottom of each page) to track your progress.

Numbers to know without looking (Eg is the band-gap energy, ni the intrinsic carrier concentration, kT/q the thermal voltage, q the electronic charge, μn the electron mobility): Eg = 1.12 eV (Si), 0.66 eV (Ge), 1.42 eV (GaAs); ni(Si) ≈ 1×1010 cm−3; kT/q = 0.0259 V at 300 K; q = 1.6×10−19 C; Si lattice constant 5.43 Å; μn(Si) ≈ 1350 cm2/V·s.

## Textbooks

Fundamentals of Solid State Electronics (C.-T. Sah, World Scientific, 1991); Solid State Electronic Circuits (Edward W. Maby); Solid State Electronic Devices (B. G. Streetman and S. K. Banerjee). Further reading: Sze and Ng, Physics of Semiconductor Devices; Neamen, Semiconductor Physics and Devices; Pierret, Semiconductor Device Fundamentals.

Week 1 · Module 1 · Material Physics & Semiconductor Growth

# Introduction to Semiconductor Materials

Plan: elemental vs compound semiconductors (Si, Ge, GaAs); crystal structures, Miller indices and bonding mechanisms. This page follows the issued Lecture 2 notes in their own order, then goes to the depth the examination needs.

## Learning objectives

By the end of this week you should be able to:

- Define a semiconductor and distinguish it from a conductor and an insulator.

- Describe the atomic structure of Si, Ge, Ga and As and identify their valence electrons.

- Explain covalent bonding in silicon and electron–hole pair generation.

- Distinguish intrinsic, n-type and p-type semiconductors, and donors from acceptors.

- Compare elemental and compound semiconductors, and Si, Ge and GaAs.

- Explain the energy-band picture, the band gap and direct versus indirect gaps.

- Describe crystal lattices, unit cells and the diamond and zinc-blende structures.

- Determine Miller indices of planes and the spacing between planes.

How to read this page. Read it in order: each section builds on the one before. The tables and boxed equations are the parts to memorise; the paragraphs around them explain why they are true. The key points at the end summarise the week, and the solved revision and exam questions show how to write the answers.

## Symbols and abbreviations used this week

Every symbol, constant and abbreviation on this page is listed here, even if an earlier week already defined it, so you can study this page on its own.

Constants and units

| Symbol | Meaning | Units / typical value |
| --- | --- | --- |
| q | Magnitude of the electronic charge | 1.6×10−19 C |
| k | Boltzmann constant | 8.617×10−5 eV/K = 1.381×10−23 J/K |
| kT | Thermal energy | 0.0259 eV (often 0.02585 eV) at 300 K |
| T | Absolute temperature | kelvin (K); room temperature = 300 K |
| h | Planck constant | 6.626×10−34 J·s |
| m0 | Free-electron mass | 9.11×10−31 kg |
| eV | Electron-volt, a unit of energy | 1 eV = 1.6×10−19 J |
| Å | Ångström, a unit of length | 1 Å = 10−10 m = 0.1 nm |
| μm | Micrometre (micron) | 1 μm = 10−4 cm = 10−6 m |

Symbols

| Symbol | Meaning | Units / typical value |
| --- | --- | --- |
| Ec (EC) | Energy of the bottom of the conduction band | eV |
| Ev (EV) | Energy of the top of the valence band | eV |
| Eg | Band-gap energy, Ec − Ev | eV; Si 1.12, Ge 0.66, GaAs 1.42 at 300 K |
| EF | Fermi level: the energy at which a state has a 50 % chance of being occupied | eV |
| n | Electron concentration (free electrons per cm3) | cm−3 |
| p | Hole concentration (holes per cm3) | cm−3 |
| ni | Intrinsic carrier concentration (n = p = ni in pure material) | cm−3; Si ≈ 1×1010 at 300 K |
| ND | Donor concentration | cm−3 |
| NA | Acceptor concentration | cm−3 |
| k (wave vector) | Wave vector, 2π/λ; measures the electron's momentum, p = ħk | m−1 or cm−1 |
| λ | Wavelength | μm or nm; λ(μm) = 1.24/E(eV) |
| ν, hν | Frequency of light, and photon energy | Hz; eV |
| a | Lattice constant: edge length of the cubic unit cell | Å; Si 5.43, Ge and GaAs 5.65 |
| (h k l), {h k l} | Miller indices of a plane; family of equivalent planes | integers |
| [u v w], ⟨u v w⟩ | A crystal direction; family of equivalent directions | integers |
| dhkl | Spacing between neighbouring (h k l) planes, a/√(h2 + k2 + l2) | Å |
| μ, μn, μp | Mobility: drift velocity per unit field (electrons, holes) | cm2/(V·s); Si μn 1350, μp 480 |
| vd | Drift velocity | cm/s |
| σ | Conductivity, q(nμn + pμp) (in Week 8, σ is also a capture cross-section) | S/cm (siemens per cm) |
| ρ | Resistivity, 1/σ | Ω·cm |
| α, β, γ (cell) | Angles between the edges of a unit cell | degrees; 90° for cubic |
| fT | Transition (cut-off) frequency | Hz |
| λmax | Longest wavelength a material absorbs, 1.24/Eg (μm, Eg in eV) | μm |
| σi, ρi | Conductivity and resistivity of intrinsic (undoped) material; σdoped after doping | S/cm; Ω·cm |

Abbreviations

| Abbreviation | Meaning |
| --- | --- |
| Si | Silicon |
| Ge | Germanium |
| GaAs | Gallium arsenide |
| GaN | Gallium nitride |
| SiC | Silicon carbide |
| InP | Indium phosphide |
| GaP | Gallium phosphide |
| SiO2 | Silicon dioxide (silica), the oxide insulator |
| FCC | Face-centred cubic lattice |
| BCC | Body-centred cubic lattice |
| SC | Simple cubic lattice |
| APF | Atomic packing factor |
| III–V | Compound of Group III and Group V elements (e.g. GaAs) |
| MOS | Metal–oxide–semiconductor |
| MOSFET | Metal–oxide–semiconductor field-effect transistor |
| MESFET | Metal–semiconductor field-effect transistor |
| HEMT | High-electron-mobility transistor |
| BJT | Bipolar junction transistor |
| HBT | Heterojunction bipolar transistor |
| IC | Integrated circuit |
| VLSI | Very-large-scale integration |
| LED | Light-emitting diode |
| RF | Radio frequency |
| IGBT | Insulated-gate bipolar transistor |
| MEMS | Micro-electro-mechanical systems |
| LCM | Lowest common multiple |
| KOH | Potassium hydroxide (an anisotropic silicon etchant) |
| UV | Ultraviolet |

## Key terms

Every important word used this week is defined here, so you can read this week on its own.

Semiconductor. A material whose ability to carry electric current lies between that of a metal (conductor) and that of an insulator, and can be changed enormously by temperature, light and, above all, by adding tiny amounts of selected impurities. Silicon, germanium and gallium arsenide are the main examples.

Why it matters: this controllability is what lets us build diodes, transistors and integrated circuits.

Valence electrons. The electrons in the outermost shell of an atom. They take part in chemical bonding and decide the electrical behaviour of the material: silicon and germanium have 4, gallium and boron 3, arsenic and phosphorus 5.

Covalent bond. A bond in which two neighbouring atoms share a pair of valence electrons, one from each atom. In silicon each atom forms four covalent bonds with four neighbours, so every atom has a full outer shell of eight electrons.

Crystal lattice. A regular, repeating three-dimensional arrangement of atoms. A single crystal has the same arrangement and orientation throughout the whole piece.

Unit cell. The smallest block of a crystal lattice that, repeated over and over in three directions, rebuilds the whole crystal. Silicon's unit cell is a cube containing 8 atoms (the diamond-cubic structure).

Lattice constant (a). The edge length of the cubic unit cell, measured in ångströms (1 Å = 10−10 m). Si: 5.43 Å; Ge and GaAs: 5.65 Å.

Why it matters: a thin crystal layer can only be grown without defects on a substrate with almost the same lattice constant.

Miller indices (h k l). Three whole numbers, found from the reciprocals of the points where a plane cuts the crystal axes, that name the orientation of a crystal plane. Wafers are described by them, e.g. (100) wafers for MOS chips.

dhkl = a / √(h2 + k2 + l2)

Where:

- dhkl = spacing between neighbouring (h k l) planes in a cubic crystal (Å)

- a = lattice constant (Å)

- h, k, l = Miller indices of the plane (integers)

Energy band. When many atoms join to form a solid, each sharp atomic energy level spreads into a wide range of closely spaced allowed energies, called a band. The valence band holds the electrons that form the bonds; the conduction band above it holds electrons that are free to move and carry current.

Band gap (Eg). The range of energies between the top of the valence band and the bottom of the conduction band in which no electron states exist. It is the minimum energy needed to free an electron from a bond.

Eg = Ec − Ev

Where:

- Eg = band-gap energy (eV); Si 1.12, Ge 0.66, GaAs 1.42 at 300 K

- Ec = energy of the bottom of the conduction band (eV)

- Ev = energy of the top of the valence band (eV)

Why it matters: the band gap sets how many carriers exist at a given temperature, how much a device leaks, how hot it can run, and which colour of light it absorbs or emits.

Direct and indirect band gap. In a direct-gap material (GaAs, GaN, InP) an electron can drop from the conduction band to the valence band without changing its momentum, so it gives out its energy as light efficiently. In an indirect-gap material (Si, Ge) the drop also needs a lattice vibration (phonon), so light emission is very weak.

Free electron and hole. When a covalent bond breaks, the released electron can wander through the crystal (a free electron, in the conduction band), and the empty place it leaves in the bond (a hole, in the valence band) behaves as a mobile positive charge. Breaking one bond creates one electron–hole pair.

Intrinsic semiconductor. A pure semiconductor with no impurities deliberately added, in which every free electron comes from a broken bond and so is matched by a hole. The number of each per cm3 is the intrinsic carrier concentration, ni.

n = p = ni

Where:

- n = free-electron concentration (cm−3)

- p = hole concentration (cm−3)

- ni = intrinsic carrier concentration, 1×1010 cm−3 for Si at 300 K

Doping. The deliberate addition of a small, controlled amount of an impurity element (the dopant) to a pure semiconductor, to set whether electrons or holes carry the current and to raise the conductivity.

Donor and acceptor. A donor is a dopant atom with five valence electrons (P, As, Sb in Si) that gives one free electron to the crystal and becomes a fixed positive ion. An acceptor is a dopant with three valence electrons (B, Al, Ga, In in Si) that takes an electron from a neighbouring bond, creating a hole, and becomes a fixed negative ion.

n-type and p-type semiconductor; majority and minority carriers. Silicon doped with donors is n-type: electrons are the majority carriers (the more numerous) and holes the minority carriers. Silicon doped with acceptors is p-type: holes are the majority and electrons the minority. In either case the product of the two concentrations is fixed (the mass-action law):

n · p = ni2

Where:

- n, p = electron and hole concentrations (cm−3)

- ni = intrinsic carrier concentration (cm−3)

Why it matters: this one rule lets you find the minority-carrier concentration as soon as you know the doping, e.g. p = ni2/ND in n-type material.

Fermi level (EF). The energy at which an electron state has exactly a 50 % chance of being occupied. It sits near the middle of the gap in intrinsic material, near the conduction band in n-type material and near the valence band in p-type material.

Mobility (μ). How easily a carrier moves through the crystal: the average drift velocity it gains per unit electric field.

μ = vd / E

Where:

- μ = mobility (cm2/V·s); Si: μn = 1350 for electrons, μp = 480 for holes

- vd = drift velocity of the carriers (cm/s)

- E = applied electric field (V/cm)

Conductivity (σ) and resistivity (ρ). Conductivity measures how well a material carries current; resistivity is its inverse. In a semiconductor both electrons and holes contribute.

σ = q(nμn + pμp), ρ = 1/σ

Where:

- σ = conductivity (S/cm)

- ρ = resistivity (Ω·cm)

- q = electronic charge, 1.6×10−19 C

- n, p = electron and hole concentrations (cm−3)

- μn, μp = electron and hole mobilities (cm2/V·s)

Why it matters: doping raises n or p by many orders of magnitude, and σ rises in proportion; this is how the resistivity of every region of a device is set.

## Introduction

Semiconductor materials are the foundation of modern electronic and electrical systems. Almost every modern electronic device depends on them, including computers, mobile phones, solar cells, sensors, communication systems, power converters and control systems.

A semiconductor is a material whose electrical conductivity lies between that of a good conductor and an insulator. More importantly, its conductivity can be controlled by temperature, light, electric fields, magnetic fields, and the intentional addition of impurities known as dopants.

The most important semiconductor materials used in electronics are:

| Material | Type | Where you meet it |
| --- | --- | --- |
| Silicon (Si) | Elemental | ICs, microprocessors, solar cells, power devices |
| Germanium (Ge) | Elemental | Early transistors, infrared, SiGe high-speed transistors |
| Gallium arsenide (GaAs) | Compound (III–V) | Microwave, RF, LEDs, lasers |
| Gallium nitride (GaN) | Compound (III–V), wide gap | Blue/white LEDs, power and RF transistors |
| Silicon carbide (SiC) | Compound (IV–IV), wide gap | High-voltage, high-temperature power electronics |
| Indium phosphide (InP) | Compound (III–V) | Fibre-optic lasers and detectors, very high-speed circuits |
| Gallium phosphide (GaP) | Compound (III–V) | Red, yellow and green indicator LEDs |

## What is a semiconductor?

A semiconductor is a material whose electrical conductivity lies between that of a conductor and an insulator, and can be significantly controlled by temperature, impurities, light or applied electric fields. Examples: silicon (Si), germanium (Ge) and gallium arsenide (GaAs).

Its conductivity is not fixed, and that is exactly what makes it useful for electronic devices. Pure silicon at room temperature conducts poorly. When a small, controlled quantity of an impurity such as phosphorus or boron is introduced, its conductivity rises dramatically: one phosphorus atom per million silicon atoms (5×1016 cm−3) raises the conductivity more than a million times. This process is called doping.

## Classification of materials by electrical conductivity

Materials can broadly be classified into conductors, semiconductors and insulators.

Conductors have a large number of free electrons available for electrical conduction. Examples: copper, aluminium, silver, gold, iron. Copper is widely used in electrical wiring because of its high conductivity. Characteristics:

- high electrical conductivity (σ ≈ 105–106 S/cm);

- low electrical resistivity (Cu: 1.7×10−6 Ω·cm);

- large number of free charge carriers (about 1022 cm−3);

- small, or effectively overlapping, energy gap.

Insulators have very few free charge carriers under normal conditions. Examples: glass, rubber, plastic, ceramic, mica. They strongly resist the flow of electric current. Characteristics:

- very high resistivity (1010–1018 Ω·cm);

- very low conductivity;

- large energy band gap (more than about 4 eV; SiO2 ≈ 9 eV);

- electrons strongly bound to their atoms.

Semiconductors have conductivity between conductors and insulators. Examples: silicon, germanium, gallium arsenide, silicon carbide, gallium nitride. Their conductivity can be modified through temperature, doping, illumination, electric field, magnetic field and mechanical stress. This controllability is one of the most important characteristics of semiconductor materials.

Band pictures at room temperature. In a metal the highest band is partly filled; in a semiconductor a small gap lets some electrons cross by thermal excitation; in an insulator the gap is too wide.

### Comparison of conductors, semiconductors and insulators

| Property | Conductor | Semiconductor | Insulator |
| --- | --- | --- | --- |
| Conductivity | Very high | Moderate, controllable | Very low |
| Resistivity | Very low | Intermediate | Very high |
| Band gap | Approximately zero | Small (≈ 0.5–3.5 eV) | Large (> 4 eV) |
| Free electrons | Many | Moderate, controllable | Very few |
| Temperature effect | Conductivity usually decreases | Conductivity usually increases | Small effect under normal conditions |
| Examples | Cu, Ag, Al | Si, Ge, GaAs | Glass, rubber, plastic |
| Main application | Wiring | Electronic devices | Electrical isolation |

Why the temperature effect is opposite. In a metal the number of free electrons is fixed; heating only makes the lattice vibrate more, which scatters electrons, so resistance rises. In a semiconductor heating breaks covalent bonds and creates many more carriers (roughly as e−Eg/2kT); the extra carriers far outweigh the extra scattering, so resistance falls.

## Atomic structure of semiconductor materials

An atom consists of a nucleus containing protons (positive) and neutrons (neutral), with electrons (negative) occupying different energy levels (shells) around it, as in the Bohr model. The electrons in the outermost shell are the most important in determining the electrical properties of a material. These are the valence electrons.

Bohr model of silicon (Z = 14): shells hold 2, 8 and 4 electrons. The four outer electrons are the valence electrons.

### Valence electrons

The electrons in the outermost energy level of an atom are its valence electrons. They take part in chemical bonding.

| Atom | Z | Electron configuration | Valence electrons | Group |
| --- | --- | --- | --- | --- |
| Silicon (Si) | 14 | 1s22s22p63s23p2 (shells 2, 8, 4) | 4 | IV (14) |
| Germanium (Ge) | 32 | 1s22s22p63s23p64s23d104p2 (shells 2, 8, 18, 4) | 4 | IV (14) |
| Gallium (Ga) | 31 | [Ar]3d104s24p1 | 3 | III (13) |
| Arsenic (As) | 33 | [Ar]3d104s24p3 | 5 | V (15) |

Silicon's atomic mass is 28.085. The difference in valence electrons between Ga (3) and As (5) is what allows them to combine into a compound semiconductor (average 4 per atom), and the difference between Si (4) and P (5) or B (3) is what makes doping work.

## Covalent bonding in silicon

Silicon atoms form a covalent bonding structure. Each silicon atom has four valence electrons and shares them with four neighbouring silicon atoms, so each atom forms four covalent bonds and is surrounded by eight shared electrons (a full outer shell).

Two-dimensional picture of the silicon crystal. Each Si atom shares one electron pair with each of four neighbours. One bond has been broken by thermal energy, creating a free electron and a hole.

- The shared electrons hold the crystal structure together.

- At very low temperatures nearly all electrons stay in the covalent bonds, so electrical conductivity is very low (pure Si is an insulator at 0 K).

- When sufficient energy is supplied (heat, light), some electrons break away from their bonds and become mobile.

## Electron–hole pair generation

When a valence electron receives sufficient energy (at least Eg = 1.12 eV in Si) from thermal excitation, it can leave its covalent bond:

- the electron becomes a free electron;

- the vacancy it leaves behind in the bond is called a hole.

Energy supplied → electron–hole pair

- The electron carries negative charge, q = −1.6×10−19 C.

- The hole behaves as if it has positive charge, q = +1.6×10−19 C. A neighbouring bond electron can jump into the hole, so the hole moves in the opposite direction to that electron.

- Both electrons and holes contribute to electrical conduction in semiconductors. This two-carrier conduction is what separates semiconductors from metals.

The reverse process, a free electron falling back into a hole, is recombination (Week 8).

## Intrinsic semiconductor

An intrinsic semiconductor is a pure semiconductor without intentionally introduced impurities. Examples: pure silicon, pure germanium. Every free electron came from a broken bond that also left a hole, so

n = p = ni

Where:

- n = electron concentration (cm−3)

- p = hole concentration (cm−3)

- ni = intrinsic carrier concentration (cm−3): Si about 1×1010 cm−3 at 300 K; Ge 2.4×1013 cm−3

The number of electrons equals the number of holes. In thermal equilibrium the product is constant:

n · p = ni2 (mass-action law, true for doped material too)

Where:

- n, p = electron and hole concentrations (cm−3), in pure or doped material

- ni = intrinsic carrier concentration of the material at that temperature (cm−3)

## Extrinsic semiconductor

An extrinsic semiconductor is one whose electrical properties have been deliberately modified by adding controlled impurities. This process is doping. There are two major types: n-type and p-type.

### N-type semiconductor

Produced by adding a pentavalent impurity (five valence electrons): phosphorus (P), arsenic (As) or antimony (Sb). Suppose phosphorus is added to silicon. Four of its five valence electrons form covalent bonds with neighbouring Si atoms; the fifth is only weakly bound (about 0.045 eV) and easily becomes a free electron. The phosphorus atom is called a donor, and it is left as a fixed positive ion.

- Majority carriers = electrons; minority carriers = holes.

- n ≈ ND (donor concentration), p = ni2/ND.

### P-type semiconductor

Produced by adding a trivalent impurity (three valence electrons): boron (B), aluminium (Al), gallium (Ga) or indium (In). When boron is introduced into silicon, only three covalent bonds can be completed. An electron is missing from the fourth bond; this missing electron is a hole. A neighbouring electron easily moves in, so the hole wanders through the crystal. Boron is called an acceptor, and it is left as a fixed negative ion.

- Majority carriers = holes; minority carriers = electrons.

- p ≈ NA (acceptor concentration), n = ni2/NA.

Left: a phosphorus atom in silicon donates its fifth electron (n-type). Right: a boron atom leaves one bond incomplete, creating a hole (p-type).

#### Example 1.1: carriers in n-type silicon

Question. Silicon at 300 K is doped with 1016 cm−3 phosphorus atoms. Taking ni = 1×1010 cm−3 and assuming every donor is ionised, calculate the electron and hole concentrations and state which carrier is the majority.

Given: ND = 1×1016 cm−3, ni = 1×1010 cm−3, T = 300 K, complete ionisation.

Find: n, p, and the majority carrier.

Formula:

n ≈ ND (complete ionisation, ND ≫ ni)
p = ni2 / n (mass-action law)

Solution.

Step 1. Each phosphorus atom gives one free electron, and ND ≫ ni, so

n ≈ ND = 1×1016 cm−3

Step 2. The mass-action law np = ni2 gives the holes:

p = ni2/n = (1×1010)2 / (1×1016) = 1020/1016 = 1×104 cm−3

Answer: n = 1×1016 cm−3, p = 1×104 cm−3. Electrons are the majority carriers; they outnumber the holes by 1012.

What this means: adding only one phosphorus atom for every 5 million silicon atoms makes electrons a million times more plentiful than in pure silicon, while the holes fall a million times below ni. Almost all the current in this material is carried by electrons.

## Elemental semiconductors

An elemental semiconductor is made primarily from a single chemical element.

- Silicon (Si): atomic number 14, four valence electrons. Widely used in integrated circuits, power electronics and solar cells.

- Germanium (Ge): atomic number 32, four valence electrons. Higher carrier mobility than silicon, lower band gap. Used in specialised high-speed and infrared applications.

## Compound semiconductors

Compound semiconductors consist of two or more different elements. Examples: GaAs, GaN, InP, GaP, CdTe. They can provide properties that are difficult to achieve with elemental semiconductors:

- GaAs has high electron mobility and is useful in high-frequency electronic systems.

- GaN has a wide band gap (3.4 eV) and is important in power electronics, LEDs, RF systems and high-temperature electronics.

They are named by the periodic-table groups of their elements: III–V (GaAs, GaN, InP, GaP), II–VI (CdTe, ZnSe), IV–IV (SiC, SiGe). By alloying (e.g. AlxGa1−xAs) the band gap can be tuned, which is called band-gap engineering.

## Silicon, germanium and gallium arsenide

### Silicon

Silicon is the most widely used semiconductor material in modern electronics.

- Atomic number 14; four valence electrons; diamond-cubic crystal structure.

- Band gap Eg ≈ 1.12 eV at room temperature.

- Used for microprocessors, memory chips, diodes, transistors, solar cells, power devices, sensors and integrated circuits.

Why it dominates: it is abundant (sand), cheap, grows an excellent native oxide (SiO2), has a band gap large enough for low leakage up to about 150 °C, and can be grown as huge, nearly perfect crystals.

### Germanium

Germanium was one of the earliest semiconductor materials, used extensively for early transistor technology (the first transistor, 1947, was germanium).

- Four valence electrons; diamond-cubic crystal structure.

- Band gap Eg ≈ 0.66 eV at room temperature.

- Advantages: high carrier mobility; useful for high-speed applications; useful in infrared technology.

- Disadvantages: smaller band gap; higher leakage current; less suitable than silicon for high-temperature applications (works only to about 75 °C).

### Gallium arsenide

Gallium arsenide is a compound semiconductor of gallium and arsenic (Ga + As), abbreviated GaAs.

- Band gap Eg ≈ 1.42 eV at room temperature (direct).

- High electron mobility (about 8500 cm2/V·s, six times silicon), so it is particularly useful for high-frequency and optoelectronic applications.

- Applications: microwave circuits, satellite communication, radar, high-frequency amplifiers, LEDs, laser diodes, photodetectors, solar cells.

### Comparison of Si, Ge and GaAs

| Property | Silicon | Germanium | GaAs |
| --- | --- | --- | --- |
| Symbol | Si | Ge | GaAs |
| Type | Elemental | Elemental | Compound |
| Valence electrons | 4 | 4 | III–V compound (average 4) |
| Band gap | ≈ 1.12 eV | ≈ 0.66 eV | ≈ 1.42 eV |
| Crystal structure | Diamond cubic | Diamond cubic | Zinc blende |
| Electron mobility | Moderate (1350) | High (3900) | Very high (8500) |
| Thermal stability | Good | Lower | Good |
| Cost | Relatively low | Higher | High |
| IC manufacturing | Excellent | Limited | Specialised |
| High-frequency use | Good | Good | Excellent |
| Optical applications | Limited | Good (infrared) | Excellent |

(Mobilities in cm2/V·s at 300 K, added for reference.)

## Energy band concept

The electrical behaviour of a semiconductor is explained using energy bands. When many atoms come together to form a solid, the discrete energy levels of the individual atoms spread into closely spaced energy states called energy bands. The two most important are:

- Valence band: contains electrons involved in bonding.

- Conduction band: contains electrons that can move through the material and contribute significantly to conduction.

Between them is the forbidden energy gap, or band gap Eg.

### Energy band gap

The band gap is the energy difference between the conduction band and the valence band:

Eg = EC − EV

Where:

- Eg = band-gap energy (eV); Si 1.12, Ge 0.66, GaAs 1.42 at 300 K

- EC = conduction-band energy: the bottom of the conduction band (eV)

- EV = valence-band energy: the top of the valence band (eV)

It is normally measured in electron-volts (1 eV = 1.6×10−19 J).

Why the band gap is important. It strongly affects semiconductor behaviour. A smaller band gap makes it easier for electrons to gain enough energy to enter the conduction band; a larger band gap makes it harder. The band gap influences:

- electrical conductivity (ni ∝ e−Eg/2kT);

- temperature dependence of conductivity;

- optical absorption (only photons with hν ≥ Eg are absorbed);

- light emission (emitted wavelength λ = 1.24/Eg μm);

- leakage current (smaller gap, more leakage);

- breakdown behaviour (wider gap, higher breakdown field);

- device operating temperature (wider gap, hotter operation).

## Direct and indirect band-gap semiconductors

Semiconductors are classified by the relationship between the valence-band maximum and the conduction-band minimum in momentum (k).

Direct band gap: electrons can transition between the conduction and valence bands without a significant change in momentum. Examples: GaAs, GaN, InP. These are suitable for light-emitting devices: LEDs, laser diodes, optical communication.

Indirect band gap: a momentum change is required during the transition, supplied by a lattice vibration (phonon). Examples: silicon, germanium. Silicon is therefore not an efficient light emitter.

E–k diagrams. In GaAs the band extrema line up at the same k, so an electron can drop straight down and emit a photon. In Si they are at different k, so a phonon must also take part.

### Direct versus indirect band gap at a glance

|  | Direct band gap | Indirect band gap |
| --- | --- | --- |
| Band edges in the E–k diagram | Conduction-band minimum directly above the valence-band maximum (same k) | Minimum and maximum at different k |
| What a transition needs | A photon only | A photon and a phonon (lattice vibration) to supply the momentum |
| Light emission | Efficient: energy leaves as light | Very inefficient: energy mostly leaves as heat |
| Light absorption near Eg | Strong; a few μm of material absorbs the light | Weaker; tens of μm needed (Si solar cells are thick) |
| Examples | GaAs (1.42 eV), GaN (3.4 eV), InP | Si (1.12 eV), Ge (0.66 eV), GaP |
| Typical applications | LEDs, laser diodes, optical-fibre transmitters | ICs, transistors, photodiodes and solar cells (absorb but do not emit) |

## Semiconductor crystal structure

A semiconductor is not simply a collection of independent atoms. The atoms are arranged in an ordered three-dimensional pattern called a crystal lattice, and this crystal structure determines many of its physical properties. The important concepts are: lattice, unit cell, crystal planes, crystal directions, Miller indices and atomic bonding.

### Crystal lattice and unit cell

- A crystal lattice is a regular, repeating arrangement of atoms or points in space.

- A semiconductor crystal can be described by repeating a basic structural unit known as the unit cell.

- The unit cell contains enough information to reproduce the entire crystal by translation.

## The cubic lattices

| Structure | Atoms per cell | Coordination no. | Nearest-neighbour distance | APF |
| --- | --- | --- | --- | --- |
| Simple cubic (SC) | 1 | 6 | a | 0.52 |
| Body-centred cubic (BCC) | 2 | 8 | (√3/2)a | 0.68 |
| Face-centred cubic (FCC) | 4 | 12 | (√2/2)a | 0.74 |
| Diamond cubic | 8 | 4 | (√3/4)a | 0.34 |

Counting atoms in a cubic cell: a corner atom is shared by 8 cells (counts 1/8), a face atom by 2 (counts 1/2), a body atom by 1.

- SC: 8 × 1/8 = 1

- BCC: 8 × 1/8 + 1 = 2

- FCC: 8 × 1/8 + 6 × 1/2 = 4

- Diamond: 8 × 1/8 + 6 × 1/2 + 4 inside = 8

### Silicon crystal structure

- Silicon has a diamond-cubic crystal structure.

- It can be regarded as two interpenetrating face-centred cubic (FCC) structures, displaced from each other by a quarter of the body diagonal.

- Each silicon atom has four nearest-neighbour silicon atoms, arranged at the corners of a tetrahedron (bond angle 109.5°).

- The bonding is predominantly covalent.

- This structure is responsible for many of silicon's useful semiconductor properties.

For Si (a = 5.43 Å): nearest-neighbour distance = (√3/4)a = 2.35 Å; atom density = 8/a3 = 5.0×1022 atoms/cm3.

### Germanium crystal structure

- Germanium also has the diamond-cubic structure; each Ge atom forms four covalent bonds with neighbouring Ge atoms.

- Silicon and germanium therefore have similar bonding arrangements, but their atomic sizes (a = 5.65 Å for Ge) and electronic properties differ.

### GaAs crystal structure

- GaAs forms the zinc-blende crystal structure under ordinary conditions.

- It consists of two interpenetrating FCC sublattices, one occupied by gallium and the other by arsenic. Each Ga has four As neighbours and vice versa.

- The bonding is mainly covalent with partial ionic character (As is more electronegative than Ga). This structure contributes to its important electronic and optical properties.

### Lattice constant

The lattice constant is a characteristic dimension of a crystal unit cell. For a cubic crystal it is written a and measured in metres, nanometres or angstroms (1 Å = 10−10 m = 0.1 nm). Si: 5.43 Å; Ge: 5.65 Å; GaAs: 5.65 Å.

The lattice constant determines: atomic spacing; crystal density; crystal matching between materials; epitaxial growth (a layer grows well only on a substrate with nearly the same a); and semiconductor heterostructures (e.g. AlGaAs on GaAs works because their lattice constants are almost identical).

## Miller indices

Miller indices provide a standard notation for crystallographic planes and directions:

| Notation | Meaning |
| --- | --- |
| (h k l) | A plane |
| {h k l} | A family of equivalent planes |
| [u v w] | A direction |
| ⟨u v w⟩ | A family of equivalent directions |

They are important in wafer orientation, crystal growth, etching, diffraction and device fabrication.

### Procedure

- Determine the plane's intercepts on the x, y and z axes in lattice units.

- Take the reciprocals of the intercepts.

- Multiply by a common factor to obtain the smallest integers.

- Write the result as (h k l).

- An intercept of ∞ gives an index of 0, because the plane is parallel to that axis.

- Negative indices are shown with a bar, e.g. (1̄10).

The three most important planes in a cubic crystal. MOS wafers are cut on (100); bipolar and some power wafers on (111).

### Examples (from the lecture)

#### Example 1.2: Miller indices of a plane

Question. A crystal plane cuts the x, y and z axes at a, 2b and 3c respectively. Determine its Miller indices.

Given: intercepts a, 2b, 3c, i.e. 1, 2, 3 in lattice units.

Find: (h k l).

Formula: for intercepts p, q, r (in lattice units),

(h k l) = smallest integers in the ratio 1/p : 1/q : 1/r

Solution.

| Step | x | y | z |
| --- | --- | --- | --- |
| Intercepts (lattice units) | 1 | 2 | 3 |
| Reciprocals | 1 | 1/2 | 1/3 |
| Multiply by the LCM, 6 | 6 | 3 | 2 |

Answer: (6 3 2). Remember: Miller indices come from the reciprocals of the intercepts, not the intercepts themselves.

What this means: the largest index (6) belongs to the axis the plane cuts closest to the origin; a large index means the plane is steeply inclined to that axis. Every plane parallel to this one has the same name, (6 3 2).

#### Example 1.3: a plane parallel to an axis

Question. A plane has intercepts x = a, y = 2b and is parallel to the z-axis (z = ∞). Determine its Miller indices.

Given: intercepts 1, 2, ∞ in lattice units.

Find: (h k l).

Formula:

(h k l) = smallest integers in the ratio 1/p : 1/q : 1/r, with 1/∞ = 0

Solution.

| Step | x | y | z |
| --- | --- | --- | --- |
| Intercepts | 1 | 2 | ∞ |
| Reciprocals | 1 | 1/2 | 0 |
| Multiply by 2 | 2 | 1 | 0 |

Answer: (2 1 0). The zero shows that the plane is parallel to the z-axis.

What this means: a plane that never meets an axis gets a zero for that axis, so any Miller index containing 0 describes a plane standing parallel to that axis, like the walls of a room are parallel to the vertical.

### Interplanar spacing (cubic crystals)

dhkl = a / √(h2 + k2 + l2)

Where:

- dhkl = perpendicular distance between neighbouring (h k l) planes (Å)

- a = lattice constant of the cubic cell (Å); Si 5.43

- h, k, l = Miller indices of the planes (integers)

For Si, d111 = 5.43/√3 = 3.135 Å and d100 = 5.43 Å. In cubic crystals the direction [h k l] is perpendicular to the plane (h k l).

## Why orientation matters in processing

- Surface atom density differs by plane: in Si, (100) has 6.8×1014 atoms/cm2, (111) has 7.8×1014 atoms/cm2.

- Oxidation rate: (111) oxidises faster than (100).

- Interface traps: (100) gives the lowest Si/SiO2 interface-state density, so MOS technology uses (100) wafers.

- Anisotropic etching: KOH etches (100) far faster than (111), giving V-grooves with 54.7° walls, used in MEMS.

- Cleavage: wafers break along {111} planes in Si and {110} in GaAs.

- Epitaxy: the substrate orientation and lattice constant set the orientation and quality of the grown layer.

- Ion implantation channelling: along low-index directions ions travel deep; wafers are tilted about 7° to avoid it.

## Bonding mechanisms (exam depth)

## The bonding mechanisms

Ionic bonding. One atom transfers electrons to another, producing positive and negative ions held together by electrostatic (Coulomb) attraction. Occurs between elements of very different electronegativity, e.g. Na+Cl−. The bond is strong but non-directional. Electrons are tightly bound to the ions, so ionic solids are insulators with large gaps; they are hard, brittle and have high melting points.

Covalent bonding. Neighbouring atoms share pairs of valence electrons, one electron from each, so each atom completes its outer shell (8 electrons). The bond is strong and directional, which fixes the crystal geometry (tetrahedral, 109.5°). Electrons are localised in bonds at low temperature but can be freed by modest energy, which gives semiconducting behaviour. Examples: Si, Ge, diamond.

Metallic bonding. Valence electrons leave their atoms and form a delocalised "sea" or gas of electrons shared by the whole crystal, holding a lattice of positive ion cores together. Non-directional. The free electron sea explains the high electrical and thermal conductivity, lustre and ductility of metals. Examples: Cu, Al, Na.

Van der Waals bonding. Weak attraction between fluctuating dipoles in neutral atoms or molecules. Important in layered materials (graphite, MoS2) and noble-gas solids, not in Si or GaAs.

Mixed ionic–covalent. Real compound semiconductors lie between the ideal limits.

|  | Ionic | Covalent | Metallic |
| --- | --- | --- | --- |
| Mechanism | Electron transfer, ion attraction | Electron-pair sharing | Shared electron sea |
| Directional? | No | Yes | No |
| Free electrons | None | Few (created thermally) | Very many |
| Electrical behaviour | Insulator | Semiconductor (or insulator) | Conductor |
| Example | NaCl | Si, Ge, C | Cu, Al |

## Defects in real crystals

| Type | Dimension | Examples | Effect |
| --- | --- | --- | --- |
| Point | 0-D | Vacancy, self-interstitial, substitutional or interstitial impurity, Frenkel pair (vacancy + interstitial) | Traps, recombination centres; vacancies assist diffusion |
| Line | 1-D | Edge and screw dislocations | Leakage paths, recombination along the line, enhanced diffusion |
| Planar | 2-D | Grain boundaries, stacking faults, twin boundaries, surfaces and interfaces | Scattering, interface traps, junction leakage |
| Volume | 3-D | Voids, precipitates (e.g. SiO2 clusters), inclusions | Gettering sites if controlled, device failure if not |

Defects act as scattering centres (lower mobility), recombination–generation centres (shorter lifetime, more leakage), traps (charge storage and noise) and diffusion paths. Not all impurities are unwanted: deliberate dopants are substitutional point defects.

## Key points of Week 1

- A semiconductor's conductivity lies between a conductor's and an insulator's and can be controlled, above all by doping.

- Conductors: bands overlap, conductivity falls when hot. Insulators: gap > 4 eV. Semiconductors: gap ≈ 1 eV, conductivity rises when hot.

- Si and Ge have 4 valence electrons and form 4 covalent bonds (diamond cubic). GaAs averages 4 per atom (zinc blende).

- Breaking a bond (energy ≥ Eg) makes an electron–hole pair; both carry current. Intrinsic: n = p = ni.

- Pentavalent donors (P, As, Sb) → n-type, electrons majority. Trivalent acceptors (B, Al, Ga, In) → p-type, holes majority. np = ni2.

- Eg = EC − EV sets conductivity, leakage, light emission (λ = 1.24/Eg μm) and maximum temperature. Direct gap (GaAs) emits light; indirect (Si) does not.

- Miller indices: intercepts → reciprocals → smallest integers → (h k l); ∞ gives 0. d = a/√(h2 + k2 + l2).

## Lecture revision questions solved

These are the lecturer's own Week 1 revision questions (Lecture 2, pages 41–43), in her order.

### R1. Define a semiconductor.

A semiconductor is a material whose electrical conductivity lies between that of a conductor and an insulator (ρ ≈ 10−3 to 108 Ω·cm), and whose conductivity can be significantly controlled by temperature, light, electric and magnetic fields, and especially by adding small amounts of impurities (doping). Examples: Si, Ge, GaAs.

### R2. Distinguish between a conductor, semiconductor and insulator.

A conductor has many free electrons and overlapping (or no) band gap, very high conductivity, and its conductivity falls as temperature rises (Cu, Ag, Al). An insulator has a large band gap (> 4 eV), very few free carriers, very high resistivity, and is used for isolation (glass, rubber, mica). A semiconductor has a small band gap (Si 1.12 eV), a moderate and controllable number of carriers (both electrons and holes), and its conductivity rises with temperature and with doping (Si, Ge, GaAs). See the comparison table above.

### R3. What are valence electrons?

Valence electrons are the electrons in the outermost energy level (shell) of an atom. They take part in chemical bonding and determine the electrical properties of a material. Silicon has 4, gallium 3, arsenic and phosphorus 5, boron 3.

### R4. Why does silicon have four valence electrons?

Silicon has atomic number Z = 14, so its 14 electrons fill the shells as 2, 8 and 4 (configuration 1s22s22p63s23p2). The first two shells (n = 1 and n = 2) are complete; the third shell (n = 3) holds only 3s23p2, i.e. 4 electrons. These four outer electrons are the valence electrons, which places silicon in Group IV (14) of the periodic table.

### R5. Explain covalent bonding in silicon.

Each silicon atom has four valence electrons. In the crystal it shares one electron with each of four neighbouring Si atoms, and each neighbour shares one back, so each pair of atoms is joined by a shared electron pair (a covalent bond). Each atom therefore forms four covalent bonds, arranged tetrahedrally at 109.5° (diamond-cubic structure), and is surrounded by eight shared electrons, a stable full shell. The shared electrons hold the crystal together. At low temperature all electrons are locked in bonds, so pure Si hardly conducts; when energy of at least 1.12 eV is supplied, a bond breaks and creates a free electron and a hole.

### R6. Define intrinsic semiconductor.

An intrinsic semiconductor is a pure semiconductor with no intentionally added impurities, in which carriers are produced only by thermal breaking of bonds. Electrons and holes are therefore equal in number: n = p = ni (Si: ni ≈ 1×1010 cm−3 at 300 K).

### R7. Define extrinsic semiconductor.

An extrinsic semiconductor is one whose electrical properties have been deliberately modified by adding controlled amounts of impurity atoms (doping). It is n-type if doped with donors (electrons are majority carriers) or p-type if doped with acceptors (holes are majority carriers). n ≠ p, but np = ni2 still holds.

### R8. What is doping?

Doping is the deliberate, controlled introduction of small amounts of specific impurity atoms (typically 1014–1020 cm−3) into a pure semiconductor to increase its conductivity and set its carrier type. Pentavalent dopants (P, As, Sb) give n-type material; trivalent dopants (B, Al, Ga, In) give p-type. Methods are covered in Week 3 (diffusion and ion implantation).

### R9. Differentiate between n-type and p-type semiconductors.

|  | n-type | p-type |
| --- | --- | --- |
| Impurity | Pentavalent (P, As, Sb) | Trivalent (B, Al, Ga, In) |
| Impurity name | Donor | Acceptor |
| Majority carriers | Electrons | Holes |
| Minority carriers | Holes | Electrons |
| Fixed ion left | Positive | Negative |
| Concentrations | n ≈ ND, p = ni2/ND | p ≈ NA, n = ni2/NA |
| Fermi level | Near the conduction band | Near the valence band |

### R10. What is a donor impurity?

A donor is a pentavalent impurity atom (P, As or Sb in silicon) with five valence electrons. Four form covalent bonds with neighbouring Si atoms; the fifth is weakly bound (≈ 0.045 eV) and is "donated" to the conduction band as a free electron. The donor becomes a fixed positive ion and makes the material n-type.

### R11. What is an acceptor impurity?

An acceptor is a trivalent impurity atom (B, Al, Ga or In in silicon) with three valence electrons. It completes only three bonds; the incomplete fourth bond "accepts" an electron from a neighbouring bond, creating a mobile hole in the valence band. The acceptor becomes a fixed negative ion and makes the material p-type.

### R12. Define energy band gap.

The energy band gap Eg is the energy difference between the bottom of the conduction band and the top of the valence band, Eg = EC − EV. It is the minimum energy needed to free an electron from a covalent bond and create an electron–hole pair. It is measured in eV: Si 1.12 eV, Ge 0.66 eV, GaAs 1.42 eV.

### R13. Differentiate between direct and indirect band-gap semiconductors.

In a direct band-gap semiconductor (GaAs, GaN, InP) the conduction-band minimum and valence-band maximum occur at the same momentum, so an electron can fall across the gap and emit a photon without any change in momentum. Light emission is efficient: LEDs, laser diodes, optical communication. In an indirect band-gap semiconductor (Si, Ge) they occur at different momenta, so a transition also needs a phonon (lattice vibration) to supply the momentum. This is unlikely, so light emission is very inefficient; the energy is mostly lost as heat. Silicon is therefore not used for LEDs or lasers.

### R14. State the crystal structure of silicon.

Silicon has the diamond-cubic crystal structure: two interpenetrating face-centred cubic lattices displaced by one quarter of the body diagonal. Each atom has four nearest neighbours at the corners of a tetrahedron, bonded covalently. Lattice constant a = 5.43 Å, 8 atoms per unit cell, nearest-neighbour distance 2.35 Å.

### R15. State the crystal structure of GaAs.

GaAs has the zinc-blende crystal structure: two interpenetrating FCC sublattices, one of gallium atoms and one of arsenic atoms, displaced by a quarter of the body diagonal. Each Ga atom has four As nearest neighbours and each As has four Ga neighbours, tetrahedrally arranged. Lattice constant a = 5.65 Å. The bonding is covalent with partial ionic character.

### R16. What are Miller indices?

Miller indices are a set of three integers (h k l), obtained from the reciprocals of a plane's intercepts on the crystal axes (in lattice units) reduced to the smallest whole numbers, that identify the orientation of a crystal plane. The same notation gives directions [u v w], families of planes {h k l} and families of directions ⟨u v w⟩. They are used to specify wafer orientation, etching and cleavage planes, epitaxial growth and X-ray diffraction.

### R17. Why is silicon widely used in integrated circuits?

- It is abundant and cheap (sand, quartz), with a mature refining industry.

- It grows a stable, high-quality native oxide, SiO2, used for masking, passivation, isolation and the MOSFET gate insulator.

- Its 1.12 eV band gap gives low leakage and operation up to about 150 °C.

- Large, nearly defect-free single crystals (300 mm wafers) can be grown.

- It is mechanically strong and conducts heat well.

- Its doping by diffusion and ion implantation is well understood and controllable.

### R18. State three applications of GaAs.

Any three of: microwave and RF amplifiers (mobile phones, radar); satellite communication circuits; high-frequency transistors (HEMTs, MESFETs); LEDs; laser diodes for optical-fibre communication; photodetectors; high-efficiency solar cells for satellites.

### R19. Define carrier mobility.

Carrier mobility μ is the average drift velocity acquired by a charge carrier per unit applied electric field: μ = vd/E, in cm2/V·s. It measures how easily electrons or holes move through the crystal. In silicon μn ≈ 1350 and μp ≈ 480 cm2/V·s. (Full treatment in Week 7.)

### R20. Explain why semiconductor conductivity increases with temperature.

Conductivity is σ = q(nμn + pμp). As temperature rises, more valence electrons gain enough thermal energy to cross the band gap, breaking covalent bonds and creating electron–hole pairs. The intrinsic carrier concentration rises exponentially, ni ∝ T3/2e−Eg/2kT: in Si it roughly doubles every 8 °C. Mobility does fall slightly with temperature because of increased lattice scattering (μ ∝ T−3/2), but this is a weak power law against an exponential increase in carriers, so the overall conductivity increases. This is the opposite of a metal, where the carrier number is fixed and only scattering increases.

## Lecture calculation questions solved

### C1. An n-type semiconductor has an electron concentration of 5 × 1016 cm−3. If the electron mobility is 1200 cm2/V·s, calculate its conductivity, assuming hole conduction is negligible.

Given: n = 5×1016 cm−3, μn = 1200 cm2/V·s, q = 1.6×10−19 C, hole conduction negligible.

Find: σ (and ρ).

Formula:

σ = q(nμn + pμp) ≈ q n μn (pμp neglected), ρ = 1/σ

Solution. With hole conduction neglected, σ = q n μn:

σ = (1.6×10−19 C)(5×1016 cm−3)(1200 cm2/V·s)
= 1.6×10−19 × 6×1019
= 9.6 S/cm (Ω−1cm−1)

Answer: σ = 9.6 S/cm (= 960 S/m), so the resistivity is ρ = 1/σ = 0.104 Ω·cm. (With q = 1.602×10−19 C, σ = 9.61 S/cm.)

What this means: a 1 cm cube of this silicon would have a resistance of only about 0.1 Ω, over three million times less than pure silicon (σi ≈ 2.9×10−6 S/cm); the doping, not the silicon itself, decides how well it conducts.

### C2. A semiconductor has n = 2 × 1016 cm−3, p = 5 × 1015 cm−3, μn = 1300 cm2/V·s, μp = 450 cm2/V·s. Calculate its conductivity using σ = q(nμn + pμp).

Given: n = 2×1016 cm−3, p = 5×1015 cm−3, μn = 1300 cm2/V·s, μp = 450 cm2/V·s, q = 1.6×10−19 C.

Find: σ (and ρ).

Formula:

σ = q(nμn + pμp), ρ = 1/σ

Solution.

nμn = 2×1016 × 1300 = 2.6×1019
pμp = 5×1015 × 450 = 2.25×1018
nμn + pμp = 2.825×1019 (cm·V·s)−1

σ = 1.6×10−19 × 2.825×1019 = 4.52 S/cm

Answer: σ ≈ 4.52 S/cm, ρ = 1/σ ≈ 0.221 Ω·cm. The electrons contribute 92 % of the conductivity (2.6 of 2.825), the holes 8 %.

What this means: electrons dominate for two reasons: there are four times as many of them, and each moves almost three times as easily (1300 against 450). Neglecting the holes here would underestimate σ by only 8 %.

### C3. Explain why GaAs is preferred to silicon for some high-frequency applications.

- Higher electron mobility: about 8500 cm2/V·s against 1350 for Si, because of its small electron effective mass (0.067m0). Electrons cross a transistor faster, giving higher transconductance and cut-off frequency (fT), and lower noise.

- Higher peak electron velocity (about 2×107 cm/s against 1×107 cm/s), so short transit times in small devices.

- Semi-insulating substrates (ρ ≈ 108 Ω·cm) reduce parasitic capacitance and substrate losses, ideal for microwave integrated circuits (MMICs) with on-chip transmission lines.

- It supports heterostructure devices (AlGaAs/GaAs HEMTs and HBTs) with very high mobility two-dimensional electron gases.

- Larger band gap (1.42 eV) gives better radiation hardness and higher-temperature operation than Si.

Silicon is still preferred where cost, integration density and hole mobility matter.

### C4. A crystal plane has intercepts 2a, 3b and ∞c. Determine its Miller indices.

Given: intercepts 2, 3, ∞ in lattice units.

Find: (h k l).

Formula:

(h k l) = smallest integers in the ratio 1/p : 1/q : 1/r, with 1/∞ = 0

Solution.

| Step | x | y | z |
| --- | --- | --- | --- |
| Intercepts | 2 | 3 | ∞ |
| Reciprocals | 1/2 | 1/3 | 0 |
| Multiply by 6 | 3 | 2 | 0 |

Answer: Miller indices (3 2 0). The zero shows that the plane is parallel to the z-axis. For a cubic crystal, d320 = a/√(9 + 4 + 0) = a/√13.

What this means: the plane stands parallel to the z-axis, and in silicon (a = 5.43 Å) neighbouring (3 2 0) planes are only 5.43/√13 = 1.51 Å apart; higher-index planes are always more closely spaced.

### C5. Explain the importance of semiconductor band gap in electronic and optoelectronic device design.

Electronic devices.

- Intrinsic carrier concentration and leakage: ni ∝ e−Eg/2kT. A wider gap gives far fewer thermally generated carriers, so lower reverse leakage and less noise (Si leaks less than Ge).

- Maximum operating temperature: a device stops working when ni approaches the doping level. Ge fails at about 75 °C, Si at about 150–200 °C, and SiC and GaN (3.3–3.4 eV) work above 300 °C.

- Breakdown field and power handling: wider gap means a higher critical field (Si 0.3 MV/cm, GaN 3.3 MV/cm), so thinner, lower-resistance high-voltage devices.

- Turn-on voltage: the diode forward voltage rises with Eg (Ge ≈ 0.3 V, Si ≈ 0.7 V, GaAs ≈ 1.1 V).

Optoelectronic devices.

- Emission wavelength: an LED or laser emits at λ = hc/Eg, i.e. λ(μm) = 1.24/Eg(eV). Designers choose or alloy materials for the colour: GaAs 0.87 μm (infrared), GaP green-yellow, GaN 365 nm (blue/UV with InGaN), InGaAsP 1.3–1.55 μm for optical fibres.

- Absorption and detection: only photons with hν ≥ Eg are absorbed. Si detects up to 1.1 μm; Ge and InGaAs are used for longer wavelengths.

- Solar cells: the band gap sets the trade-off between absorbing more of the spectrum and the voltage obtained; the optimum single-junction gap is about 1.1–1.4 eV (Si, GaAs).

- Direct or indirect: only direct-gap materials emit light efficiently.

## Examination questions solved (Q1–Q8)

### Q1. Define a semiconductor and explain how its electrical conductivity differs from that of a conductor and an insulator.

Definition. A semiconductor is a material whose conductivity lies between that of conductors and insulators (resistivity roughly 10−3 to 108 Ω·cm) and can be controlled by temperature, light, electric field and, above all, by adding small amounts of impurity (doping). Examples: Si, Ge, GaAs.

Difference, explained with energy bands.

- Conductor. The valence and conduction bands overlap, or the highest band is only partly filled. There is no gap, so a huge number of free electrons (about 1022 cm−3) is always present. Conductivity is very high (σ ≈ 106 S/cm) and almost independent of impurities. It decreases as temperature rises because lattice scattering increases.

- Insulator. The valence band is full and the conduction band is empty, separated by a wide gap (Eg > about 4 eV, e.g. SiO2 ≈ 9 eV). Thermal energy at room temperature (kT ≈ 0.026 eV) cannot lift electrons across, so there are practically no carriers. Conductivity is extremely small (σ < 10−10 S/cm).

- Semiconductor. Same full/empty arrangement but a small gap (Si 1.12 eV). At room temperature a small fraction of electrons is thermally excited into the conduction band, leaving holes behind, so both electrons and holes conduct. Conductivity is moderate and increases with temperature (negative temperature coefficient of resistance), and can be raised by many orders of magnitude by doping.

Summary. Conductors have no gap and fixed, abundant carriers; insulators have a wide gap and essentially no carriers; semiconductors have a small gap, two carrier types, and a carrier density that can be engineered.

### Q2. Distinguish between elemental semiconductors and compound semiconductors, giving two examples of each.

|  | Elemental | Compound |
| --- | --- | --- |
| Composition | One chemical element | Two or more elements |
| Periodic table | Group IV (14) | Combinations such as III–V, II–VI, IV–IV |
| Crystal structure | Diamond cubic | Zinc blende or wurtzite |
| Bonding | Purely covalent | Covalent with partial ionic character |
| Band gap | Fixed by the element; Si and Ge are indirect | Adjustable by choice of elements and alloying; many are direct |
| Processing | Mature, cheap (especially Si) | More difficult and costly; stoichiometry must be controlled |
| Typical use | ICs, power, detectors | Optoelectronics, RF, high power |
| Examples | Silicon (Si), Germanium (Ge) | Gallium arsenide (GaAs), Indium phosphide (InP); also GaN, SiC, CdTe |

### Q3. Explain why silicon is widely used in semiconductor device fabrication.

- Abundance and cost. Si makes up about 28 % of the Earth's crust as SiO2 (sand, quartz). Raw material is cheap and the refining industry is enormous.

- Excellent native oxide. Silicon oxidises to SiO2, which is stable, insoluble in water, an excellent insulator (Eg ≈ 9 eV, breakdown ≈ 10 MV/cm) and forms a very clean interface with Si (interface trap density about 1010 cm−2eV−1). SiO2 is used as a diffusion mask, surface passivation, field isolation and the MOSFET gate dielectric. No other semiconductor has a comparable oxide.

- Suitable band gap. At 1.12 eV it is large enough to give low intrinsic concentration and low leakage, so devices work up to about 150 °C (Ge fails above about 75 °C), yet small enough for good conduction when doped.

- Mature crystal growth. Very large (300 mm), nearly defect-free, highly pure single crystals are routinely grown by the Czochralski method.

- Mechanical and thermal strength. Si is hard, can be handled as thin wafers, and conducts heat well (about 3 times better than GaAs), which matters in power devices and dense ICs.

- Well-understood doping. B, P, As and Sb dope it predictably by diffusion and ion implantation.

- Elemental. No stoichiometry to control and no toxic constituents, unlike GaAs.

Its main limitation is the indirect gap, which makes it a poor light emitter; that is why lasers and LEDs use compound semiconductors.

### Q4. Compare the properties and applications of silicon (Si), germanium (Ge), and gallium arsenide (GaAs).

Use the comparison table of Si, Ge and GaAs above as the core of the answer, then comment:

- Structure and bonding. Si and Ge are elemental, diamond cubic, purely covalent. GaAs is a III–V compound, zinc blende, mainly covalent with partial ionic character (As is more electronegative than Ga).

- Band gap. Ge (0.66 eV) < Si (1.12 eV) < GaAs (1.42 eV). The larger the gap, the lower ni, the lower the leakage and the higher the maximum operating temperature. Si and Ge are indirect; GaAs is direct, so only GaAs emits light efficiently.

- Mobility. GaAs electrons are fastest (8500), then Ge (3900), then Si (1350) cm2/V·s. Hence GaAs and Ge suit high-speed work, though GaAs hole mobility is poor.

- Oxide. Only Si has an excellent native oxide, which is why MOS technology and VLSI are silicon.

- Cost and processing. Si cheapest and most mature; Ge more expensive; GaAs most expensive, brittle and toxic.

Applications.

- Si: microprocessors, memories, all digital and analogue ICs, MOSFETs and BJTs, power devices (IGBTs, thyristors), solar cells, sensors and MEMS.

- Ge: infrared detectors and lenses, high-speed SiGe heterojunction transistors, substrates for multi-junction space solar cells; historically the first transistors.

- GaAs: microwave and RF amplifiers in mobile phones and radar, satellite communication, HEMTs and MESFETs, LEDs, laser diodes for optical fibre links, high-efficiency solar cells for satellites.

### Q5. What is a crystal lattice? Explain the significance of crystal structure in semiconductor materials.

Crystal lattice. A crystal lattice is an infinite, periodic three-dimensional array of points in space such that every point has identical surroundings. It is generated by repeating a unit cell (edges a, b, c and angles α, β, γ) by translation. Attaching a basis of one or more atoms to each lattice point gives the real crystal: crystal = lattice + basis. Si, for example, is an FCC lattice with a two-atom basis, which produces the diamond structure.

Significance of crystal structure.

- It produces the energy bands. The periodic potential of the lattice splits the atomic levels into allowed bands and forbidden gaps (Bloch's theorem, Kronig–Penney model). The size and type (direct or indirect) of the band gap depend on the structure and the atomic spacing.

- Carrier mobility. In a perfect periodic lattice electrons move without scattering; departures from periodicity (vibrations, impurities, defects, grain boundaries) cause scattering. Single crystals therefore have much higher mobility than polycrystalline or amorphous material.

- Anisotropy. Properties such as surface atom density, oxidation rate, etch rate, interface trap density, piezoelectric response and mobility differ with crystal direction. Wafer orientation ((100) or (111)) is chosen accordingly.

- Doping and diffusion. Dopant atoms sit on substitutional lattice sites to become active. Open structures (diamond, APF 0.34) allow interstitial diffusion.

- Epitaxy and heterostructures. Layers can be grown defect-free only on substrates with matching structure and lattice constant (e.g. AlGaAs on GaAs).

- Mechanical behaviour. Cleavage planes, hardness and how wafers are diced all follow from the structure and bond directions.

- Defects. Departures from the ideal structure (vacancies, dislocations) create states in the gap that act as traps and recombination centres, shortening carrier lifetime.

### Q6. Define Miller indices and explain how they are used to identify crystal planes.

Definition. Miller indices are a set of three smallest integers (h k l), proportional to the reciprocals of the intercepts a plane makes on the crystal axes (measured in units of the lattice constants), that specify the orientation of that plane and all planes parallel to it.

How they identify a plane (procedure):

- Choose the origin at a lattice point not on the plane. Find the intercepts on x, y, z in units of a, b, c: say p, q, r.

- Take reciprocals 1/p, 1/q, 1/r. A plane parallel to an axis has an infinite intercept and so a zero index.

- Multiply by the lowest common multiple of the denominators to obtain integers.

- Reduce to the smallest integers and enclose in round brackets (h k l). Negative indices carry a bar.

Use and notation. (h k l) names a particular plane; {h k l} the family of symmetry-equivalent planes; [u v w] a direction and ⟨u v w⟩ a family of directions. In cubic crystals [h k l] is normal to (h k l), and the spacing between planes is d = a/√(h2 + k2 + l2). Miller indices are used to specify wafer orientation ((100) for MOS, (111) for bipolar), etch planes, cleavage planes and X-ray diffraction peaks.

Example. Intercepts a, 2b, 3c → reciprocals 1, 1/2, 1/3 → × 6 → (6 3 2).

### Q7. Determine the Miller indices of a crystal plane having intercepts of 2a, 3b, and 1c.

Given: intercepts 2, 3, 1 in lattice units.

Find: (h k l).

Formula:

(h k l) = smallest integers in the ratio 1/p : 1/q : 1/r

Solution.

| Step | x | y | z |
| --- | --- | --- | --- |
| Intercepts (in units of a, b, c) | 2 | 3 | 1 |
| Reciprocals | 1/2 | 1/3 | 1/1 |
| Multiply by the LCM of the denominators, 6 | 3 | 2 | 6 |

Answer: Miller indices = (3 2 6).

Check: the integers 3, 2, 6 have no common factor, so no further reduction is possible. If the crystal is cubic with lattice constant a, the spacing of these planes is d326 = a/√(9 + 4 + 36) = a/√49 = a/7.

What this means: the plane cuts the z-axis closest to the origin, so z gets the largest index (6). In silicon these planes would be only 5.43/7 = 0.78 Å apart, far closer than the main (100) and (111) planes used for wafers.

The (3 2 6) plane, cutting the axes at 2a, 3b and 1c.

### Q8. Explain the difference between covalent, ionic, and metallic bonding and identify the dominant bonding mechanism in silicon.

Covalent bonding. Adjacent atoms share pairs of valence electrons so that each completes a stable outer shell. The shared electrons are localised between the two atoms, making the bond strong and directional. Covalent solids are hard, have high melting points, and are semiconductors or insulators depending on how tightly the bonds hold their electrons.

Ionic bonding. An electropositive atom gives up valence electrons to an electronegative atom; the resulting positive and negative ions attract electrostatically. The bond is strong but non-directional, there are no free electrons, and ionic solids (NaCl, MgO) are brittle insulators that conduct only when molten or dissolved.

Metallic bonding. Each atom releases its valence electrons into a common delocalised electron gas that binds the positive ion cores. The bond is non-directional, and the mobile electron gas gives high electrical and thermal conductivity, ductility and metallic lustre.

Key differences: how the electrons are held (shared between pairs / transferred to ions / shared by all atoms), directionality (yes / no / no), and the resulting electrical behaviour (semiconductor or insulator / insulator / conductor).

Bonding in silicon: covalent. Si has four valence electrons. In the diamond-cubic lattice each Si atom forms four sp3 covalent bonds with four nearest neighbours at 109.5°, sharing one electron pair with each so that every atom has a full octet. Because Si–Si bonds are between identical atoms there is no ionic character. The modest bond strength (equivalent to Eg = 1.12 eV) is what lets thermal energy break a few bonds at room temperature, creating electron–hole pairs and giving silicon its semiconducting behaviour.

## Practice questions

These extra questions practise this week's ideas. Work each one on paper before reading the solution; the calculation questions follow the same Question, Given, Find, Solution, Answer layout as the worked examples.

#### Practice 1.1: why germanium leaks more than silicon

Question. Explain why a germanium diode has a much larger reverse leakage current than a silicon diode of the same doping.

Answer. Leakage is carried by minority carriers, whose concentration is ni2/N. Germanium's band gap (0.66 eV) is much smaller than silicon's (1.12 eV), so far more bonds are broken thermally: ni(Ge) ≈ 2.4×1013 cm−3 against 1×1010 cm−3 for Si. Since leakage ∝ ni2, the Ge diode has about (2.4×103)2 ≈ 6×106 times more minority carriers and a correspondingly larger leakage current.

#### Practice 1.2: Miller indices with a negative intercept

Question. A plane cuts the x-axis at −a, the y-axis at 2b and is parallel to the z-axis. Determine its Miller indices.

Given: intercepts −1, 2, ∞ (lattice units).

Find: (h k l).

Solution.

Reciprocals: −1, 1/2, 0
Multiply by 2: −2, 1, 0

Answer: (2̄ 1 0), written with a bar over the 2 (in plain text (−2 1 0)).

#### Practice 1.3: interplanar spacing in germanium

Question. Germanium has a lattice constant of 5.65 Å. Calculate the spacing of the (110) and (111) planes.

Given: a = 5.65 Å.

Find: d110 and d111.

Solution.

d110 = a/√(1 + 1 + 0) = 5.65/√2 = 3.995 Å
d111 = a/√(1 + 1 + 1) = 5.65/√3 = 3.262 Å

Answer: d110 = 4.00 Å, d111 = 3.26 Å.

What this means: spacings of a few ångströms are comparable to X-ray wavelengths (Cu Kα ≈ 1.54 Å), which is why X-ray diffraction can measure them and so identify the crystal and its orientation.

#### Practice 1.4: atom density and mass density of silicon

Question. Silicon has the diamond structure with a = 5.43 Å and atomic mass 28.085 g/mol. Calculate the number of atoms per cm3 and the density of silicon in g/cm3.

Given: a = 5.43×10−8 cm, 8 atoms per unit cell, M = 28.085 g/mol, NA(Avogadro) = 6.022×1023 mol−1.

Find: atoms per cm3 and density ρ.

Solution.

Cell volume a3 = (5.43×10−8)3 = 1.601×10−22 cm3
Atoms per cm3 = 8/a3 = 8/1.601×10−22 = 5.0×1022 cm−3
Mass of one cell = 8 × 28.085/6.022×1023 = 3.731×10−22 g
ρ = 3.731×10−22 / 1.601×10−22 = 2.33 g/cm3

Answer: 5.0×1022 atoms/cm3; ρ = 2.33 g/cm3.

#### Practice 1.5: atom density of GaAs

Question. GaAs has the zinc-blende structure with a = 5.65 Å. Each unit cell contains 4 Ga and 4 As atoms; the molar mass of GaAs is 144.64 g/mol. Find the total atom density and the density of GaAs.

Given: a = 5.65×10−8 cm, 8 atoms (4 GaAs pairs) per cell, M = 144.64 g/mol.

Find: atoms per cm3 and ρ.

Solution.

a3 = (5.65×10−8)3 = 1.804×10−22 cm3
Atoms per cm3 = 8/a3 = 4.44×1022 cm−3
ρ = 4 × 144.64 / (6.022×1023 × 1.804×10−22) = 578.6/108.6 = 5.33 g/cm3

Answer: 4.44×1022 atoms/cm3 (half Ga, half As); ρ = 5.33 g/cm3.

#### Practice 1.6: the effect of doping on conductivity

Question. Compare the conductivity of intrinsic silicon (ni = 1×1010 cm−3) with that of silicon doped with 1×1015 cm−3 donors. Use μn = 1350 and μp = 480 cm2/V·s.

Given: ni = 1010 cm−3, ND = 1015 cm−3, μn = 1350, μp = 480 cm2/V·s.

Find: σintrinsic, σdoped and their ratio.

Solution.

σi = qni(μn + μp) = 1.6×10−19 × 1010 × 1830 = 2.93×10−6 S/cm
σ = qNDμn = 1.6×10−19 × 1015 × 1350 = 0.216 S/cm
ratio = 0.216/2.93×10−6 = 7.4×104

Answer: doping with only one atom in 5×107 raises the conductivity about 74 000 times.

#### Practice 1.7: which light can silicon absorb?

Question. What is the longest wavelength of light that silicon (Eg = 1.12 eV) can absorb? Can a silicon photodiode detect the 1.55 μm light used in optical-fibre links?

Given: Eg = 1.12 eV.

Find: λmax, and whether 1.55 μm is absorbed.

Solution.

λmax = 1.24/Eg = 1.24/1.12 = 1.11 μm
A 1.55 μm photon has energy 1.24/1.55 = 0.80 eV < 1.12 eV

Answer: λmax = 1.11 μm; no, 1.55 μm photons do not have enough energy to create electron–hole pairs in silicon. Fibre receivers use Ge or InGaAs.

## Objectives check

Use this table to confirm you have met this week's objectives. Cover the Answer column and answer each check question from memory. If you cannot, go back to the section in the last column before moving on.

| # | Objective | Check yourself | Answer | Where it is taught |
| --- | --- | --- | --- | --- |
| 1 | Define a semiconductor and distinguish it from a conductor and an insulator. | Why does a semiconductor conduct better when it is heated, while a metal conducts worse? | Heat breaks bonds and creates many more electron–hole pairs (∝ e−Eg/2kT); in a metal the carrier number is fixed and only scattering increases. | Classification of materials |
| 2 | Describe the atomic structure of Si, Ge, Ga and As and identify their valence electrons. | How many valence electrons do Si, Ga and As have? | Si 4, Ga 3, As 5 (GaAs averages 4 per atom). | Atomic structure; valence electrons |
| 3 | Explain covalent bonding in silicon and electron–hole pair generation. | What two carriers are created when a covalent bond in Si breaks, and what minimum energy is needed? | A free electron and a hole; at least Eg = 1.12 eV. | Covalent bonding; electron–hole pairs |
| 4 | Distinguish intrinsic, n-type and p-type semiconductors, and donors from acceptors. | Si is doped with 1017 cm−3 boron. Is it n- or p-type, and what is the electron concentration (ni = 1010 cm−3)? | p-type; n = ni2/NA = 103 cm−3. | Intrinsic and extrinsic semiconductors |
| 5 | Compare elemental and compound semiconductors, and Si, Ge and GaAs. | Give one reason GaAs is preferred to Si for high-frequency work and one reason Si is preferred for ICs. | GaAs: electron mobility ≈ 8500 vs 1350 cm2/V·s. Si: excellent native SiO2 (also cheaper, larger wafers). | Elemental and compound; comparison table |
| 6 | Explain the energy-band picture, the band gap and direct versus indirect gaps. | Why is silicon not used for LEDs? | Its gap is indirect: a phonon is needed to conserve momentum, so radiative recombination is very inefficient. | Energy band concept; direct and indirect band gaps (comparison table) |
| 7 | Describe crystal lattices, unit cells and the diamond and zinc-blende structures. | How many atoms are in the diamond-cubic unit cell, and how many nearest neighbours does each atom have? | 8 atoms per cell; 4 nearest neighbours. | Semiconductor crystal structure |
| 8 | Determine Miller indices of planes and the spacing between planes. | Find the Miller indices of a plane with intercepts 3a, ∞, c. | Reciprocals 1/3, 0, 1 → × 3 → (1 0 3). | Miller indices; Examples 1.2–1.3; C4 and Q7 |

Week 2 · Module 1 · Material Physics & Semiconductor Growth

# Material Growth Techniques

Plan: purification of silicon (metallurgical to electronic grade); the Czochralski bulk crystal growth method; epitaxial growth techniques (VPE, LPE, MBE).

## Learning objectives

By the end of this week you should be able to:

- Describe the conversion of quartzite into metallurgical-grade silicon.

- Explain how MG-Si is purified into electronic-grade silicon.

- Explain the principle and steps of the Czochralski method.

- State the advantages and limitations of CZ growth and compare it with float-zone growth.

- Use the segregation coefficient to predict doping along an ingot.

- Explain the principles of VPE, LPE and MBE and compare them.

- Calculate the lattice mismatch between an epitaxial layer and its substrate and judge whether the layer can grow defect-free.

## Symbols and abbreviations used this week

Every symbol, constant and abbreviation on this page is listed here, even if an earlier week already defined it, so you can study this page on its own.

Constants and units

| Symbol | Meaning | Units / typical value |
| --- | --- | --- |
| q | Magnitude of the electronic charge | 1.6×10−19 C |
| k | Boltzmann constant | 8.617×10−5 eV/K = 1.381×10−23 J/K |
| h | Planck constant | 6.626×10−34 J·s |
| Å | Ångström, a unit of length | 1 Å = 10−10 m = 0.1 nm |
| μm | Micrometre (micron) | 1 μm = 10−4 cm = 10−6 m |

Symbols

| Symbol | Meaning | Units / typical value |
| --- | --- | --- |
| f(E) | Fermi–Dirac function: probability that a state at energy E is occupied | dimensionless, 0 to 1 |
| ND | Donor concentration | cm−3 |
| NA | Acceptor concentration | cm−3 |
| a | Lattice constant: edge length of the cubic unit cell | Å; Si 5.43, Ge and GaAs 5.65 |
| k0 | Segregation coefficient, Cs/Cl at the freezing interface | dimensionless; B 0.8, P 0.35 |
| Cs | Surface concentration of a diffusion (or solid concentration when freezing) | cm−3 |
| Cl, C0 | Concentration in the melt (liquid); C0 at the start | cm−3 |
| f (growth) | Fraction of the melt already solidified | 0 to 1 |
| μ, μn, μp | Mobility: drift velocity per unit field (electrons, holes) | cm2/(V·s); Si μn 1350, μp 480 |
| ρ | Resistivity, 1/σ | Ω·cm |
| alayer, asub | Lattice constants of the grown layer and of the substrate | Å |
| fm | Lattice mismatch, (alayer − asub)/asub | dimensionless, usually in % |
| vpull | Pull rate of a Czochralski crystal | mm/min |
| r (atom) | Atomic radius (hard-sphere model), half the nearest-neighbour distance | Å |
| t | Time (or a thickness, where the text says so) | s (or cm) |

Abbreviations

| Abbreviation | Meaning |
| --- | --- |
| Si | Silicon |
| Ge | Germanium |
| GaAs | Gallium arsenide |
| GaN | Gallium nitride |
| InP | Indium phosphide |
| SiO2 | Silicon dioxide (silica), the oxide insulator |
| III–V | Compound of Group III and Group V elements (e.g. GaAs) |
| MG-Si | Metallurgical-grade silicon (≈ 98 % pure) |
| EG-Si | Electronic-grade silicon (99.9999999 % or better) |
| CZ | Czochralski crystal growth |
| FZ | Float-zone crystal growth |
| CVD | Chemical vapour deposition |
| VPE | Vapour-phase epitaxy |
| LPE | Liquid-phase epitaxy |
| MBE | Molecular-beam epitaxy |
| MOCVD | Metal-organic chemical vapour deposition |
| UHV | Ultra-high vacuum (≈ 10−10 Torr) |
| RHEED | Reflection high-energy electron diffraction (counts atomic layers during MBE) |
| CMOS | Complementary MOS (n- and p-channel MOSFETs together) |
| HEMT | High-electron-mobility transistor |
| BJT | Bipolar junction transistor |
| HBT | Heterojunction bipolar transistor |
| IC | Integrated circuit |
| LED | Light-emitting diode |
| RF | Radio frequency |
| IGBT | Insulated-gate bipolar transistor |
| VCSEL | Vertical-cavity surface-emitting laser |

## Key terms

Every important word used this week is defined here, so you can read this week on its own.

Single crystal. A solid in which the atoms are arranged in one regular, repeating pattern with the same orientation throughout the whole piece. Devices are built in single-crystal silicon because carriers move through it freely and leak little.

Polycrystalline material (polysilicon). A solid made of many small single-crystal grains pointing in different directions. The boundaries between grains scatter carriers and provide leakage paths, so polysilicon is used as a raw material (and for some thin films), not as the wafer.

Lattice constant (a). The edge length of the cubic unit cell, the basic repeating block of the crystal, in ångströms (1 Å = 10−10 m). Si: 5.43 Å; Ge and GaAs: 5.65 Å (more precisely 5.658 and 5.653 Å).

Dislocation. A line defect in a crystal, where a row of atoms is out of place. Dislocations carry leakage current and kill carriers, so device wafers must be dislocation-free.

Doping and dopant. Doping is the deliberate addition of a small, controlled amount of an impurity element (the dopant) to set the conductivity type and resistivity. Boron gives p-type silicon (holes carry the current); phosphorus, arsenic and antimony give n-type silicon (electrons carry the current).

Resistivity (ρ). How strongly a material opposes current, the inverse of conductivity. In doped silicon it is set mainly by the dopant concentration.

ρ = 1 / (q NA μp) (p-type), ρ = 1 / (q ND μn) (n-type)

Where:

- ρ = resistivity (Ω·cm)

- q = electronic charge, 1.6×10−19 C

- NA, ND = acceptor and donor concentrations (cm−3)

- μp, μn = hole and electron mobilities (cm2/V·s); Si μp = 480, μn = 1350 when lightly doped

Why it matters: wafer buyers specify resistivity, so a change in doping along an ingot is a change in the product.

Metallurgical-grade silicon (MG-Si). Silicon about 98 % pure, made by reducing quartz with carbon in an arc furnace. Good enough for steel and aluminium alloys, far too impure for devices.

Electronic-grade silicon (EG-Si). Polycrystalline silicon with no more than about one impurity atom in a billion (99.9999999 %, "9N", or better), made by distilling trichlorosilane and depositing silicon from it in the Siemens process.

Chemical vapour deposition (CVD). Growing a solid film from gases that react or decompose on a hot surface, leaving the wanted atoms behind. The Siemens process and vapour-phase epitaxy are both CVD processes.

Czochralski (CZ) growth. Making a large single crystal by dipping a small seed crystal into molten silicon in a quartz crucible and pulling it up slowly while rotating it. The melt freezes onto the seed and copies its crystal orientation.

Seed, ingot and wafer. The seed is the small single crystal, cut to the wanted orientation, that starts the growth. The ingot (boule) is the large cylindrical single crystal that is pulled. Wafers are the thin discs, typically 0.5–0.8 mm thick, sliced from the ingot and polished.

Dash necking. Pulling a thin neck (about 3 mm across) quickly at the start of CZ growth so that dislocations created by the thermal shock of dipping grow out of the sides, leaving the rest of the crystal dislocation-free.

Segregation coefficient (k0). The ratio of the dopant concentration in the freezing solid to that in the liquid it is freezing from. When k0 < 1 the crystal rejects dopant into the melt.

k0 = Cs / Cl

Where:

- k0 = equilibrium segregation coefficient (dimensionless); B 0.8, P 0.35 in Si

- Cs = dopant concentration in the solid at the freezing interface (cm−3)

- Cl = dopant concentration in the liquid at the interface (cm−3)

Why it matters: because k0 < 1 for almost every dopant, the doping (and so the resistivity) changes from the seed end to the tail end of every CZ ingot.

Float-zone (FZ) growth. Making a single crystal by passing a narrow molten zone along a vertical polysilicon rod, without any crucible. It gives the purest, highest-resistivity silicon.

Epitaxy. Growing a thin single-crystal layer on top of a single-crystal wafer so that the layer continues the wafer's crystal structure and orientation. The wafer underneath is called the substrate. Growing the same material (Si on Si) is homoepitaxy; growing a different material (AlGaAs on GaAs) is heteroepitaxy.

Lattice mismatch (fm). The fractional difference between the lattice constants of a grown layer and its substrate.

fm = (alayer − asub) / asub

Where:

- fm = lattice mismatch (dimensionless, often quoted in %)

- alayer = lattice constant of the grown layer (Å)

- asub = lattice constant of the substrate (Å)

Why it matters: only layers with a very small mismatch (well under 1 %) grow thick without misfit dislocations; this decides which materials can be stacked.

## The big picture

To make a chip you need three things, in this order:

- Extremely pure silicon. A device stops working if more than about one atom in a billion is an unwanted impurity. Sand is nowhere near that pure.

- One single crystal. The atoms must be lined up perfectly across the whole wafer (Week 1). Polycrystalline silicon, with grains pointing in different directions, scatters carriers and leaks current.

- Thin layers on top, with different doping or even a different material, grown so that they continue the crystal perfectly.

This week covers each step: purification (sand → pure polysilicon), crystal growth (polysilicon → one big crystal, by the Czochralski method), and epitaxy (growing thin crystalline layers on top).

## Part A: Purification of silicon

The whole route, from sand to wafer:

quartzite (SiO2) → metallurgical-grade Si (98 %) → trichlorosilane SiHCl3 → purified SiHCl3 → electronic-grade polysilicon → single crystal → wafers

| Stage | Product | Purity |
| --- | --- | --- |
| Arc furnace (reduction with carbon) | Metallurgical-grade Si (MG-Si) | About 98–99 % |
| Chlorination, distillation, Siemens CVD | Electronic-grade polysilicon (EG-Si) | 99.9999999 % ("nine nines", 9N) or better |
| Czochralski or float-zone growth | Single-crystal ingot, doped as required | Dopant added deliberately |

### Step 1: making metallurgical-grade silicon (MG-Si)

Quartzite, a fairly pure form of SiO2 (sand, quartz), is mixed with carbon (coal, coke, wood chips) and heated to about 2000 °C in an electric arc furnace. Carbon pulls the oxygen off the silicon:

SiO2 + 2C → Si + 2CO

Molten silicon is drained from the furnace. This MG-Si is about 98 % pure. The 2 % of impurities (Fe, Al, Ca, C, B, P) is still about 1020 impurity atoms per cm3, a hundred million times too many for devices. MG-Si is good enough for making steel and aluminium alloys, but not chips.

### Step 2: turning silicon into a liquid that can be purified

Solids are hard to purify; liquids are easy to purify by distillation. So the next step is to convert silicon into a liquid compound. MG-Si powder is reacted with hydrogen chloride gas at about 300 °C:

Si + 3HCl → SiHCl3 + H2

The product, trichlorosilane (SiHCl3), is a liquid that boils at only 32 °C. The impurities also react with HCl and form their own chlorides (FeCl3, BCl3, PCl3 and so on), which boil at different temperatures.

### Step 3: fractional distillation

The trichlorosilane is purified by fractional distillation, the same process used to separate petrol from crude oil. Because SiHCl3 and each impurity chloride boil at different temperatures, repeated distillation leaves SiHCl3 with impurities at only a few parts per billion.

### Step 4: Siemens process (back to solid silicon)

The pure SiHCl3 is now turned back into silicon. It is mixed with pure hydrogen and passed over thin silicon rods heated electrically to about 1100 °C inside a reactor. Silicon deposits on the hot rods (chemical vapour deposition, CVD):

SiHCl3 + H2 → Si + 3HCl

Over many hours the rods grow into thick bars of electronic-grade polycrystalline silicon (EG-Si), 9N to 11N pure. The HCl is recycled.

EG-Si is pure but still polycrystalline (many small grains) and undoped. The next step turns it into a single crystal and adds the doping.

In plain words. Steps 2–4 are a round trip: solid silicon → liquid compound → solid silicon. The trip is worth it because the liquid can be distilled, and distillation removes almost all the impurities.

## Part B: Czochralski (CZ) crystal growth

### The principle

Dip a small seed crystal into molten silicon and pull it out very slowly. Silicon from the melt freezes onto the seed, and as each atom freezes it lines up with the atoms already there. So the growing piece continues the seed's crystal, and you end up with one large single crystal (an ingot) with the same orientation as the seed.

It is like pulling a candle out of hot wax, except that each new layer copies the arrangement of the layer before it.

The Czochralski puller. The seed is dipped into the melt and slowly withdrawn while seed and crucible rotate in opposite directions; the melt freezes onto the seed with the seed's orientation.

### The equipment

- A quartz (SiO2) crucible holding the molten silicon, inside a graphite holder.

- Heaters (RF induction or resistance) keeping the melt just above silicon's melting point, 1414 °C.

- A pull rod holding the seed, which rotates and rises slowly.

- A chamber filled with argon gas, so the hot silicon does not react with air.

- Sensors and control electronics to keep the diameter constant.

### The steps

- Load. Chunks of EG-Si and a carefully weighed amount of dopant (boron for p-type; phosphorus, arsenic or antimony for n-type) go into the crucible.

- Melt. The chamber is filled with argon and the charge is melted at about 1420 °C.

- Dip. The seed (cut to the wanted orientation, e.g. ⟨100⟩) is lowered until it just touches the melt.

- Neck (Dash technique). The seed is pulled up quickly, growing a thin neck about 3 mm across. Dipping a cold seed into hot liquid creates crystal defects (dislocations); in a thin neck they run out of the sides and disappear, so the crystal below is dislocation-free.

- Shoulder and body. The pull rate is reduced so the crystal widens to the full diameter (up to 300 mm). It is then pulled at about 1 mm per minute while the seed and crucible rotate in opposite directions (10–30 rpm) to stir the melt and keep temperature and doping even.

- Tail. At the end the pull rate is increased so the diameter narrows to a cone before the crystal leaves the melt. A sudden break would send defects back up the crystal.

- Cool slowly. A typical ingot is 300 mm wide and up to 2 m long.

Controlling the diameter: pulling faster, or making the melt hotter, gives a thinner crystal; pulling slower or cooler gives a thicker one.

After growth the ingot is ground to an exact diameter, marked with a flat or notch to show its orientation, sliced into wafers with a wire saw, then lapped, etched and polished to a mirror finish.

### Dopant segregation: why the doping changes along the ingot

When silicon freezes, impurity atoms "prefer" to stay in the liquid. The segregation coefficient measures this:

k0 = Cs / Cl

Where:

- k0 = equilibrium segregation coefficient (dimensionless)

- Cs = dopant concentration in the solid, where solid and liquid meet (cm−3)

- Cl = dopant concentration in the liquid, where solid and liquid meet (cm−3)

For most dopants k0 < 1: the crystal takes in less dopant than the melt contains.

| Impurity | B | P | As | Sb | Al | Ga | O | Fe |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| k0 in Si | 0.8 | 0.35 | 0.3 | 0.023 | 0.002 | 0.008 | 0.25 | 8×10−6 |

Consequence. The dopant left behind builds up in the shrinking pool of melt. So the end of the ingot that grows last is more heavily doped than the start. If C0 is the starting melt concentration and f the fraction already frozen,

Cs = k0 C0 (1 − f)k0 − 1

Where:

- Cs = dopant concentration in the crystal at the point being grown (cm−3)

- k0 = segregation coefficient of the dopant (dimensionless)

- C0 = dopant concentration in the melt at the start of growth (cm−3)

- f = fraction of the original melt that has already solidified (0 at the seed end, approaching 1 at the tail)

This is the normal-freezing (Scheil) equation; it assumes the melt is well stirred, so the dopant is evenly mixed through the liquid. At the seed end (f = 0) it gives Cs = k0C0.

#### Example 2.1: dopant segregation in a CZ crystal

Question. A boron-doped silicon crystal is to be grown by the Czochralski method with a boron concentration of 1×1016 cm−3 at the seed end. The segregation coefficient of boron in silicon is k0 = 0.8. (a) What boron concentration must the melt contain at the start? (b) What is the boron concentration in the crystal when half of the melt has solidified?

Given: Cs(start) = 1×1016 cm−3, k0 = 0.8, f = 0.5 for part (b).

Find: (a) C0, the initial melt concentration; (b) Cs at f = 0.5.

Formula:

Cs = k0 C0 (1 − f)k0 − 1 (at the seed end, f = 0, this is Cs = k0C0)

Solution.

(a) At the start, Cs = k0C0, so

C0 = Cs/k0 = 1×1016 / 0.8 = 1.25×1016 cm−3

(b) Use Cs = k0C0(1 − f)k0 − 1 with f = 0.5:

Cs = 0.8 × 1.25×1016 × (0.5)−0.2 = 1×1016 × 1.149 = 1.15×1016 cm−3

Answer: (a) C0 = 1.25×1016 cm−3; (b) Cs = 1.15×1016 cm−3, about 15 % higher than at the seed end, because rejected boron builds up in the melt.

What this means: the melt must be made 25 % richer in boron than the crystal you want, and even halfway along the ingot the doping has already drifted up by 15 %, so wafers cut from the middle have about 13 % lower resistivity than those from the seed end. Boron (k0 = 0.8, close to 1) is one of the gentlest cases.

The same effect also purifies: iron (k0 ≈ 10−5) is almost entirely rejected into the melt.

#### Example 2.2: how much of the ingot meets a resistivity specification?

Question. A p-type CZ silicon ingot is grown with NA = 1×1015 cm−3 boron at the seed end. (a) What is the resistivity at the seed end (μp = 480 cm2/V·s)? (b) The customer accepts wafers whose doping is at most 50 % above the seed-end value. What fraction of the melt can be grown into acceptable crystal? (c) Repeat (b) for an n-type ingot doped with phosphorus.

Given: NA(seed) = 1×1015 cm−3, μp = 480 cm2/V·s, q = 1.6×10−19 C, k0(B) = 0.8, k0(P) = 0.35, allowed ratio Cs/Cs(seed) = 1.5.

Find: (a) ρ at the seed end; (b) and (c) the solidified fraction f at which the doping reaches 1.5 times the seed value.

Formula:

ρ = 1 / (q NA μp)
Cs / Cs(seed) = (1 − f)k0 − 1 so 1 − f = (Cs / Cs(seed))1/(k0 − 1)

Solution.

(a) Seed-end resistivity:

ρ = 1 / (1.6×10−19 × 1×1015 × 480) = 1 / 0.0768 = 13.0 Ω·cm

(b) Boron, k0 − 1 = −0.2:

1 − f = 1.51/(−0.2) = 1.5−5 = 0.132
f = 0.868

At that point the resistivity has fallen to 13.0/1.5 = 8.7 Ω·cm.

(c) Phosphorus, k0 − 1 = −0.65:

1 − f = 1.51/(−0.65) = 1.5−1.54 = 0.536
f = 0.464

Answer: (a) ρ = 13.0 Ω·cm; (b) about 87 % of the melt (boron); (c) only about 46 % of the melt (phosphorus) grows into crystal within the specification.

What this means: the smaller k0 is, the faster the doping climbs along the ingot. A boron-doped ingot is usable almost to the tail, but more than half of a phosphorus-doped one falls outside a ±50 % window, which is one reason n-type wafers with tight resistivity limits are more expensive (or are made by FZ or neutron transmutation doping instead).

#### Example 2.3: growth time and mass of a CZ ingot

Question. A 200 mm diameter CZ silicon ingot is pulled at 1 mm/min from a crucible charged with 100 kg of boron-doped silicon. The cylindrical body is 1.2 m long. Ignoring the neck, shoulder and tail: (a) how long does it take to grow the body; (b) what is the mass of the body (density of Si = 2.33 g/cm3); (c) what fraction of the melt has frozen at the end of the body, and how much higher is the boron concentration there than at the seed end (k0 = 0.8)?

Given: diameter 20 cm (r = 10 cm), L = 120 cm, pull rate vpull = 1 mm/min = 0.1 cm/min, charge 100 kg, density 2.33 g/cm3, k0 = 0.8.

Find: growth time t, body mass m, solidified fraction f and Cs(end)/Cs(seed).

Formula:

t = L / vpull
m = density × π r2 L
f = m / (mass of charge)
Cs(end) / Cs(seed) = (1 − f)k0 − 1

Solution.

(a) t = 120 cm / 0.1 cm per min = 1200 min = 20 h
(b) m = 2.33 × π × 102 × 120 = 8.78×104 g = 87.8 kg
(c) f = 87.8/100 = 0.878
Cs(end)/Cs(seed) = (1 − 0.878)−0.2 = (0.122)−0.2 = 1.52

Answer: (a) 20 hours; (b) about 88 kg; (c) f ≈ 0.88, and the boron concentration at the end of the body is about 1.5 times (52 % higher than) the seed-end value.

What this means: one CZ run takes about a day of continuous, carefully controlled pulling, and nearly 90 % of the melt ends up in the crystal. Compared with Example 2.2, the last 1–2 cm of this body (grown between f = 0.868 and f = 0.878) would just exceed a 50 % doping limit, so that part would be cut off and recycled.

### Float-zone (FZ) growth, for comparison

A polysilicon rod is held vertically and a narrow molten zone, heated by an RF coil, is moved slowly along it, starting from a seed. No crucible touches the molten silicon, so there is almost no oxygen or carbon contamination, and very pure, high-resistivity silicon (up to 104 Ω·cm) can be made. FZ is used for power devices and radiation detectors, but wafers are smaller (≤ 200 mm) and more expensive.

### CZ versus FZ at a glance

|  | Czochralski (CZ) | Float-zone (FZ) |
| --- | --- | --- |
| Principle | Seed pulled from a melt held in a crucible | Narrow molten zone moved along a polysilicon rod; no crucible |
| Crucible contact | Yes (quartz, SiO2, in graphite) | None: the zone is held by surface tension |
| Oxygen content | High, ≈ 1018 cm−3 (from the crucible) | Very low, < 1016 cm−3 |
| Carbon content | Higher (graphite parts) | Very low |
| Maximum resistivity | ≈ 100 Ω·cm | Up to ≈ 104 Ω·cm |
| Wafer diameter | Up to 300 mm (450 mm demonstrated) | Up to 200 mm |
| Mechanical strength | Higher: oxygen pins dislocations, resists warping and slip | Lower: wafers warp more easily in hot processing |
| Gettering | Intrinsic gettering by oxygen precipitates possible | Not possible (no oxygen) |
| Axial doping uniformity | Varies by segregation, Cs = k0C0(1 − f)k0 − 1 | Better; can be improved further by neutron transmutation doping |
| Cost and throughput | Low cost, high throughput, ≈ 95 % of all silicon | Higher cost, lower throughput |
| Main applications | CMOS ICs, memories, microprocessors, most solar cells | High-voltage power devices (thyristors, IGBTs), radiation and infrared detectors, RF |

## Part C: Epitaxial growth

### What epitaxy is and why we need it

Epitaxy (Greek epi, "upon", and taxis, "arrangement") is the growth of a thin single-crystal layer on a single-crystal wafer (the substrate), so that the new layer continues the substrate's crystal structure and orientation.

Why not just make everything in the bulk crystal? Because devices need thin layers with different properties stacked on each other, with sharp boundaries:

- a lightly doped layer on a heavily doped substrate (bipolar transistors, power diodes);

- a layer of a different material, such as AlGaAs on GaAs or InGaAs on InP (lasers, LEDs, high-speed transistors);

- a layer cleaner than the CZ substrate (less oxygen, fewer defects).

Homoepitaxy: same material (Si on Si). Heteroepitaxy: different materials (GaAs on Si, AlGaAs on GaAs). In heteroepitaxy the two lattice constants must be nearly equal (Week 1); otherwise the mismatch creates defects. The mismatch is measured by

fm = (alayer − asub) / asub

Where:

- fm = lattice mismatch (dimensionless; usually quoted in %); positive when the layer's natural lattice is larger than the substrate's

- alayer = lattice constant of the material being grown (Å)

- asub = lattice constant of the substrate (Å)

A thin layer with a small mismatch simply stretches or squeezes to fit the substrate (it is strained). Above a certain critical thickness, which falls rapidly as fm grows, the strain is relieved by misfit dislocations at the interface, and these thread up through the layer and spoil devices. As a rule of thumb, mismatches of about 0.2 % or less allow layers micrometres thick with few defects, while several per cent allow only a few nanometres.

#### Example 2.4: lattice mismatch of GaAs on silicon and on germanium

Question. GaAs (a = 5.653 Å) is to be grown epitaxially. Calculate the lattice mismatch (a) on a silicon substrate (a = 5.431 Å) and (b) on a germanium substrate (a = 5.658 Å). Which substrate is suitable for a thick, defect-free GaAs layer, for example in a space solar cell?

Given: a(GaAs) = 5.653 Å = alayer; asub = 5.431 Å (Si) or 5.658 Å (Ge).

Find: fm for each substrate.

Formula:

fm = (alayer − asub) / asub

Solution.

(a) fm = (5.653 − 5.431) / 5.431 = 0.222 / 5.431 = +0.0409 = +4.1 %
(b) fm = (5.653 − 5.658) / 5.658 = −0.005 / 5.658 = −0.00088 = −0.09 %

Answer: (a) +4.1 % on Si; (b) −0.09 % on Ge. Germanium is the suitable substrate.

What this means: on germanium the GaAs lattice needs to stretch by less than one part in a thousand, so micrometre-thick layers grow essentially free of dislocations, which is why high-efficiency multi-junction space solar cells are built on Ge wafers. On silicon, a 4 % mismatch means that roughly every 25th atomic plane of GaAs has no partner in the substrate, so misfit dislocations form after only a few nanometres; GaAs-on-Si needs special buffer layers and still has far more defects.

The three methods side by side: gas reacting on a hot surface (VPE), a cooling saturated melt (LPE), and atomic beams in ultra-high vacuum (MBE).

### Vapour-phase epitaxy (VPE), also called CVD epitaxy

Principle. Gases containing silicon flow over a heated wafer. At the hot surface they react or break down, leaving silicon atoms behind. The atoms move about on the surface until they find the right place in the crystal, so the layer grows as a continuation of the wafer.

For silicon, the common reactions are:

SiCl4 + 2H2 → Si + 4HCl (≈ 1150–1250 °C)
SiH2Cl2 → Si + 2HCl (≈ 1000–1100 °C)
SiH4 → Si + 2H2 (≈ 600–1000 °C)

Doping is done by adding a little dopant gas: B2H6 (diborane) for p-type, PH3 (phosphine) or AsH3 (arsine) for n-type.

The growth rate is limited by one of two steps: how fast gas can reach the surface (mass-transport limited, at high temperature) or how fast the reaction happens on the surface (reaction-rate limited, at lower temperature).

For compound semiconductors the metal-organic version, MOCVD, is used: (CH3)3Ga + AsH3 → GaAs + 3CH4 at about 600–750 °C. Nearly all commercial LEDs are made this way.

- Growth rate 0.1–5 μm/min; good uniformity; many wafers at once: the industrial workhorse.

- Problems: dopant from the substrate can evaporate and re-enter the layer (autodoping), and at high temperature dopant diffuses up from the substrate (out-diffusion), blurring the boundary.

### Liquid-phase epitaxy (LPE)

Principle. Dissolve the semiconductor in a molten metal until no more will dissolve (a saturated solution), like sugar in hot water. Bring the wafer into contact with it and cool slowly. As the liquid cools it can hold less, so the extra semiconductor comes out of solution and crystallises onto the wafer, continuing its crystal.

Example: GaAs dissolved in molten gallium, at about 700–900 °C, cooled at 0.1–1 °C per minute. A sliding graphite boat with several wells of different melts moves the wafer from one melt to the next to build up layers.

- Growth happens close to equilibrium, so crystal quality is excellent and defects few; the equipment is simple and cheap.

- But thickness control is poor (about 0.1 μm at best), boundaries are not sharp, surfaces are rough, and the area is small.

- Used for LEDs and the first heterostructure lasers.

### Molecular-beam epitaxy (MBE)

Principle. In an ultra-high vacuum (about 10−10 Torr, roughly a ten-trillionth of atmospheric pressure), each element (Ga, As, Al, dopants) is heated in its own small oven (effusion cell). Atoms evaporate and travel in straight lines, as a beam, to the heated wafer, because there is no air to collide with. They land, move around, and join the crystal. Each oven has a shutter that can open or close in a fraction of a second, switching that element on or off.

Example: GaAs from Ga and As cells, wafer at about 550–650 °C.

- Growth is slow, about 1 μm per hour, which is about one atomic layer per second. So layers can be controlled to a single atomic layer.

- Boundaries are atomically sharp. Ideal for quantum wells, superlattices, high-electron-mobility transistors (HEMTs) and advanced lasers.

- Growth can be watched while it happens by RHEED (electron diffraction), which counts the atomic layers.

- Very expensive equipment, slow, low throughput.

### Comparing VPE, LPE, MBE and MOCVD at a glance

MOCVD is strictly a kind of VPE, but it is used so differently (compound semiconductors, lower temperature, very thin layers) that it is usually compared as a fourth method.

|  | VPE (CVD, silicon) | LPE | MBE | MOCVD |
| --- | --- | --- | --- | --- |
| Atoms arrive from | A gas, by chemical reaction | A liquid solution, by precipitation | A beam of atoms, in vacuum | Metal-organic and hydride gases, e.g. (CH3)3Ga + AsH3, cracked at the hot surface |
| Pressure | Atmospheric or reduced | Atmospheric (H2 or inert) | Ultra-high vacuum, ≈ 10−10 Torr | Reduced, ≈ 10–100 Torr, or atmospheric |
| Temperature | Highest (Si: 1000–1250 °C) | Medium (700–900 °C) | Lowest (500–650 °C) | Medium (GaAs 600–750 °C; GaN ≈ 1000 °C) |
| Growth rate | Fast, 0.1–5 μm/min | Fast, 0.1–1 μm/min | Slow, ≈ 1 μm/h | Moderate, ≈ 1–5 μm/h |
| Thickness control | Good (tens of nm) | Poor (~0.1 μm) | Excellent (one atomic layer) | Very good (about a nanometre, a few atomic layers) |
| Interfaces | Moderately sharp (autodoping, out-diffusion) | Graded | Atomically abrupt | Nearly abrupt |
| Throughput | High, many wafers per run | Low, small area | Low, one or a few wafers | High, many wafers per run |
| Cost | Moderate | Low | Very high | High (toxic gases need careful handling) |
| Best for | Silicon epitaxial layers for BJTs, CMOS and power devices | Simple, thick, high-quality III–V layers | Quantum wells, HEMTs, research | Mass production of LEDs, lasers, solar cells and HEMTs (GaAs, InP, GaN) |

## Key points of Week 2

- MG-Si (98 %) is made from quartz and carbon in an arc furnace: SiO2 + 2C → Si + 2CO.

- It is purified by converting it to liquid SiHCl3, distilling, then depositing EG-Si by the Siemens process: SiHCl3 + H2 → Si + 3HCl.

- CZ growth: a seed is pulled slowly from the melt, rotating; the crystal copies the seed. Dash necking removes dislocations.

- CZ gives large, cheap, dislocation-free crystals, but oxygen from the crucible and segregation (k0 < 1) are its limitations.

- Epitaxy grows thin crystalline layers on a wafer: VPE from gas (production), LPE from a cooling melt (simple), MBE from atomic beams in vacuum (atomic precision), MOCVD from metal-organic gases (mass production of III–V devices).

- Heteroepitaxy needs a small lattice mismatch, fm = (alayer − asub)/asub: GaAs on Ge (−0.09 %) works; GaAs on Si (4.1 %) forms misfit dislocations.

## Examination questions solved (Q9–Q13)

### Q9. Describe the major stages involved in converting metallurgical-grade silicon (MG-Si) into electronic-grade silicon (EG-Si).

Starting point: production of MG-Si. Quartzite is reduced with carbon in an electric arc furnace at about 2000 °C: SiO2 + 2C → Si + 2CO. The product is about 98 % pure, with Fe, Al, Ca, B, P and C as the main impurities.

Stage 1: Hydrochlorination (conversion to a volatile compound). Pulverised MG-Si is reacted with anhydrous HCl at about 300 °C, usually with a catalyst in a fluidised bed: Si + 3HCl → SiHCl3 + H2. Silicon becomes trichlorosilane, a liquid boiling at 32 °C. Impurities form their own chlorides.

Stage 2: Purification by fractional distillation. Because SiHCl3 and the impurity chlorides have different boiling points, repeated fractional distillation separates them, leaving SiHCl3 with electrically active impurities at parts-per-billion levels.

Stage 3: Reduction and deposition (Siemens process). The purified SiHCl3 is mixed with high-purity hydrogen and passed over electrically heated thin silicon filaments (about 1100 °C) in a CVD reactor: SiHCl3 + H2 → Si + 3HCl. Silicon deposits on the rods, which grow into thick polycrystalline bars of electronic-grade silicon (purity 9N–11N, i.e. 99.9999999 % or better). HCl and unreacted chlorosilanes are recovered and recycled.

Stage 4 (to make device material): single-crystal growth. The EG-Si polysilicon is broken into chunks, melted with the required dopant and grown into a single-crystal ingot by Czochralski or float-zone growth. Segregation during freezing purifies it further. The ingot is then shaped, sliced, lapped, etched and polished into wafers.

### Q10. Explain the principle and operation of the Czochralski (CZ) crystal growth method.

Principle. Crystal pulling from the melt. A small single-crystal seed of known orientation is brought into contact with molten silicon held slightly above its melting point (1414 °C). Heat is conducted away up the seed, so the melt at the seed–melt interface solidifies. The freezing atoms take up positions that continue the seed's lattice, so the growing ingot is a single crystal with the same orientation as the seed. Pull rate and temperature control the diameter.

Equipment. Furnace (quartz crucible in a graphite susceptor, RF or resistance heater); crystal-pulling mechanism (seed holder on a rotating, slowly rising shaft; crucible rotation and lift); ambient control (argon flow at reduced pressure); diameter and temperature control system.

Operation.

- Polysilicon EG-Si and a precise amount of dopant are loaded into the crucible. The chamber is purged with argon and the charge is melted.

- The seed is lowered to touch the melt surface.

- A thin neck is pulled quickly (Dash necking) to eliminate dislocations.

- The pull rate and temperature are lowered so the crystal widens (shoulder) to the target diameter.

- The body is grown at constant diameter with typical pull rate about 1 mm/min while seed and crucible counter-rotate to stir the melt and keep it thermally symmetric.

- At the end the diameter is tapered to a tail cone and the crystal is lifted clear and cooled slowly.

The finished ingot is then characterised for orientation, resistivity and defects before being sliced into wafers.

### Q11. State four advantages and two limitations of the Czochralski method.

Advantages:

- Large diameters: 200 mm and 300 mm ingots are routine, which lowers cost per chip.

- Dislocation-free crystals of controlled orientation ((100), (111)) from the seed, thanks to Dash necking.

- Controlled doping: dopant added to the melt gives the required type and resistivity.

- High throughput and low cost: mature, highly automated, relatively fast growth.

- Oxygen content strengthens the wafer against warping and slip, and allows intrinsic gettering (oxygen precipitates in the bulk trap metallic impurities away from the device surface).

Limitations:

- Contamination from the crucible: the quartz crucible dissolves slowly, introducing oxygen (≈ 1018 cm−3) and the graphite parts introduce carbon. Oxygen forms thermal donors and precipitates, and limits the attainable resistivity (CZ cannot easily exceed about 100 Ω·cm), so FZ is preferred for high-power and detector devices.

- Non-uniform axial doping because of segregation (k0 < 1): the dopant concentration rises from seed end to tail end, so resistivity varies along the ingot. Melt convection also causes radial non-uniformity and growth striations.

(Also acceptable: the crucible is consumed in each run; high energy consumption; batch process.)

### Q12. Explain the principles of vapour-phase epitaxy (VPE), liquid-phase epitaxy (LPE), and molecular-beam epitaxy (MBE).

Epitaxy is the growth of a thin single-crystal film on a single-crystal substrate such that the film adopts the substrate's crystal structure and orientation. The three methods differ in the phase from which atoms arrive.

Vapour-phase epitaxy (VPE). The semiconductor is supplied as a gas-phase chemical compound carried by hydrogen over a heated substrate inside a reactor. The compound decomposes or is reduced at the hot surface, and the released atoms move to lattice sites. For silicon the standard reaction is hydrogen reduction of silicon tetrachloride at about 1200 °C, SiCl4 + 2H2 → Si + 4HCl; silane SiH4 → Si + 2H2 is used at lower temperature. Doping is achieved by adding gases such as PH3, AsH3 or B2H6. The rate is set either by mass transport of reactants through the gas boundary layer or by the surface reaction. MOCVD is the metal-organic version used for III–V compounds.

Liquid-phase epitaxy (LPE). The substrate is placed in contact with a saturated solution of the semiconductor in a molten metal solvent (e.g. GaAs in liquid Ga). On slow, controlled cooling the solubility decreases, the solution becomes supersaturated and the semiconductor precipitates epitaxially on the substrate. Growth occurs near thermodynamic equilibrium. A sliding graphite boat moves the substrate under successive melts to grow multilayers.

Molecular-beam epitaxy (MBE). In ultra-high vacuum (≈ 10−10 Torr), elemental sources in heated effusion cells produce collision-free molecular beams aimed at a heated substrate. Atoms adsorb, migrate and incorporate in the lattice. Each beam has a shutter, so composition and doping can be switched abruptly. Growth is slow (≈ 1 monolayer/s) and is monitored in real time by RHEED, so thickness is controlled to atomic precision.

### Q13. Compare VPE, LPE, and MBE in terms of growth mechanism, temperature, precision, and applications.

| Feature | VPE (CVD) | LPE | MBE |
| --- | --- | --- | --- |
| Source phase | Gas (chlorosilanes, silane, metal-organics) | Liquid solution (melt) | Atomic or molecular beams from solid sources |
| Growth mechanism | Chemical reaction / decomposition at the hot surface | Precipitation from a supersaturated solution on cooling; near equilibrium | Physical deposition: adsorption and surface migration; far from equilibrium |
| Environment | Atmospheric or reduced pressure, H2 carrier | Inert or H2, graphite boat | Ultra-high vacuum, 10−10–10−11 Torr |
| Typical temperature | High: Si 1000–1250 °C; MOCVD 600–750 °C | Intermediate: 700–900 °C (GaAs) | Low: 400–650 °C (GaAs ≈ 600 °C) |
| Growth rate | 0.1–5 μm/min | 0.1–1 μm/min | ≈ 1 μm/h (≈ 1 monolayer/s) |
| Thickness precision | ≈ tens of nm; good uniformity | Poor, ≈ 0.1 μm; rough surface | Excellent, one atomic layer |
| Interface abruptness | Moderate (autodoping, out-diffusion) | Poor (graded) | Atomically abrupt |
| Crystal purity | Good | Very high, low deep-level defects | Very high (UHV) |
| In-situ monitoring | Limited | None | RHEED, mass spectrometry |
| Cost and throughput | Moderate cost, high throughput (batch) | Low cost, low throughput, small area | Very high cost, low throughput |
| Applications | Si epi layers for BJTs, CMOS, power devices; MOCVD for LEDs, lasers, solar cells | LEDs, early heterostructure lasers, thick layers, photodetectors | Quantum wells, superlattices, HEMTs, HBTs, quantum-cascade and VCSEL lasers, research |

Conclusion. VPE is the industrial choice for volume production, LPE is a simple low-cost method giving high-quality thick layers with poor control, and MBE gives the ultimate atomic-scale control for advanced heterostructure devices at high cost.

## Practice questions

These extra questions practise this week's ideas. Work each one on paper before reading the solution; the calculation questions follow the same Question, Given, Find, Solution, Answer layout as the worked examples.

#### Practice 2.1: the purification route

Question. List the stages from quartzite to electronic-grade silicon, giving the chemical reaction and approximate temperature of each.

Answer.

| Stage | Reaction | Temperature |
| --- | --- | --- |
| 1. Arc furnace → MG-Si (98 %) | SiO2 + 2C → Si + 2CO | ≈ 2000 °C |
| 2. Hydrochlorination | Si + 3HCl → SiHCl3 + H2 | ≈ 300 °C |
| 3. Fractional distillation of SiHCl3 | (physical separation by boiling point) | ≈ 32 °C boiling point |
| 4. Siemens CVD → EG-Si polysilicon | SiHCl3 + H2 → Si + 3HCl | ≈ 1100 °C |

#### Practice 2.2: phosphorus segregation along an ingot

Question. An n-type CZ crystal must have 5×1015 cm−3 phosphorus at the seed end. The segregation coefficient of P in Si is 0.35. Find the starting melt concentration and the phosphorus concentration in the crystal when 80 % of the melt has solidified.

Given: Cs(0) = 5×1015 cm−3, k0 = 0.35, f = 0.8.

Find: C0 and Cs at f = 0.8.

Solution.

C0 = Cs/k0 = 5×1015/0.35 = 1.43×1016 cm−3
Cs = k0C0(1 − f)k0 − 1 = 5×1015 × (0.2)−0.65 = 5×1015 × 2.85 = 1.42×1016 cm−3

Answer: C0 = 1.43×1016 cm−3; at f = 0.8, Cs = 1.42×1016 cm−3, almost three times the seed-end value. This is why P-doped CZ ingots vary so much in resistivity along their length.

#### Practice 2.3: how much silicon in an ingot?

Question. A CZ ingot is 300 mm in diameter and 1.5 m long. Find its mass (density 2.33 g/cm3) and how many wafers it gives if each wafer is 775 μm thick and the saw removes another 200 μm per cut.

Given: diameter 30 cm, length 150 cm, density 2.33 g/cm3, 775 + 200 = 975 μm per wafer.

Find: mass and number of wafers.

Solution.

Volume = π r2 L = π × 152 × 150 = 1.06×105 cm3
Mass = 1.06×105 × 2.33 = 2.47×105 g = 247 kg
Wafers = 150 cm / 0.0975 cm = 1538

Answer: about 247 kg and roughly 1500 wafers (fewer after the shoulder and tail are cut off).

#### Practice 2.4: MBE growth time

Question. A 0.5 μm GaAs layer is grown by MBE at 1 μm/h. How long does it take, and how many monolayers (each a/2 = 0.2825 nm thick) are deposited? What is the average monolayer rate?

Given: thickness 500 nm, rate 1 μm/h, monolayer 0.2825 nm.

Find: time, number of monolayers, rate.

Solution.

t = 0.5 μm / (1 μm/h) = 0.5 h = 1800 s
monolayers = 500 nm / 0.2825 nm = 1770
rate = 1770/1800 ≈ 1 monolayer per second

Answer: 30 minutes, about 1770 monolayers, at about one atomic layer per second, which is why MBE can control thickness to a single layer.

#### Practice 2.5: lattice mismatch

Question. Calculate the lattice mismatch for (a) Ge on Si (a = 5.65 and 5.43 Å) and (b) AlAs on GaAs (a = 5.661 and 5.653 Å). Which pair is suitable for defect-free heteroepitaxy?

Given: lattice constants above. fm = (alayer − asub)/asub.

Find: fm for each pair.

Solution.

(a) fm = (5.65 − 5.43)/5.43 = 0.041 = 4.1 %
(b) fm = (5.661 − 5.653)/5.653 = 0.0014 = 0.14 %

Answer: 4.1 % and 0.14 %. AlAs/GaAs is almost perfectly matched and grows defect-free, which is why AlGaAs/GaAs heterostructures are so widely used. Ge on Si quickly forms misfit dislocations unless the layer is very thin or graded.

#### Practice 2.6: CZ operating conditions

Question. Why is the CZ puller filled with argon, and why do the seed and crucible rotate in opposite directions?

Answer. Argon is inert: it stops the hot silicon reacting with oxygen and nitrogen, and the gas flow carries away SiO evaporating from the melt. Counter-rotation stirs the melt, so the temperature around the growing crystal is uniform (giving a round, constant-diameter crystal) and dopant is mixed evenly (giving uniform radial resistivity).

## Objectives check

Use this table to confirm you have met this week's objectives. Cover the Answer column and answer each check question from memory. If you cannot, go back to the section in the last column before moving on.

| # | Objective | Check yourself | Answer | Where it is taught |
| --- | --- | --- | --- | --- |
| 1 | Describe the conversion of quartzite into metallurgical-grade silicon. | Write the arc-furnace reaction and state the purity of MG-Si. | SiO2 + 2C → Si + 2CO; about 98 % pure. | Part A, Step 1 |
| 2 | Explain how MG-Si is purified into electronic-grade silicon. | Why is silicon converted into SiHCl3 before purification? | SiHCl3 is a liquid (boils at 32 °C) that can be purified by fractional distillation; solids cannot. | Part A, Steps 2–4 |
| 3 | Explain the principle and steps of the Czochralski method. | What is the purpose of the Dash neck? | Growing a thin neck lets dislocations from the thermal shock run out of the crystal, so the ingot is dislocation-free. | Part B; Example 2.3 |
| 4 | State the advantages and limitations of CZ growth and compare it with float-zone growth. | Why does FZ silicon reach higher resistivity than CZ silicon? | No crucible touches the melt, so there is almost no oxygen or carbon contamination. | Part B; Float-zone; CZ versus FZ table |
| 5 | Use the segregation coefficient to predict doping along an ingot. | For phosphorus (k0 = 0.35), is the tail end of a CZ ingot more or less heavily doped than the seed end? | More heavily doped: rejected phosphorus builds up in the melt. | Dopant segregation; Examples 2.1–2.3 |
| 6 | Explain the principles of VPE, LPE and MBE and compare them. | Which epitaxy method gives single-atomic-layer thickness control, and why? | MBE: slow growth (≈ one monolayer per second) and shuttered atomic beams in ultra-high vacuum. | Part C; comparison table of VPE, LPE, MBE and MOCVD |
| 7 | Calculate the lattice mismatch between an epitaxial layer and its substrate and judge whether the layer can grow defect-free. | Find the mismatch of GaAs (5.653 Å) on Ge (5.658 Å) and say whether a thick layer can be grown. | fm = (5.653 − 5.658)/5.658 = −0.09 %; small enough for thick, nearly dislocation-free layers. | What epitaxy is; Example 2.4 |

Week 3 · Module 1 · Material Physics & Semiconductor Growth

# Impurity Control and Doping

Plan: diffusion and ion implantation mechanisms; controlled doping profiles and evaluation of impurity distribution. This page follows your lecturer's handwritten notes on diffusion and ion implantation, including every calculation in them.

## Learning objectives

By the end of this week you should be able to:

- Explain why doping is needed and name the common dopants of silicon.

- Explain diffusion and state Fick's first law and the temperature dependence of D.

- Distinguish constant-source (erfc) and limited-source (Gaussian) diffusion and calculate their profiles.

- Describe the step-by-step diffusion process and the atomic diffusion mechanisms.

- Describe ion implantation, its equipment and the Gaussian implant profile.

- Calculate implant peak concentration, junction depth, dose and beam current.

- Compare diffusion with ion implantation, and explain channelling and annealing.

- Describe how a doping profile is evaluated.

## Symbols and abbreviations used this week

Every symbol, constant and abbreviation on this page is listed here, even if an earlier week already defined it, so you can study this page on its own.

Constants and units

| Symbol | Meaning | Units / typical value |
| --- | --- | --- |
| q | Magnitude of the electronic charge | 1.6×10−19 C |
| k | Boltzmann constant | 8.617×10−5 eV/K = 1.381×10−23 J/K |
| kT | Thermal energy | 0.0259 eV (often 0.02585 eV) at 300 K |
| T | Absolute temperature | kelvin (K); room temperature = 300 K |
| h | Planck constant | 6.626×10−34 J·s |
| eV | Electron-volt, a unit of energy | 1 eV = 1.6×10−19 J |
| μm | Micrometre (micron) | 1 μm = 10−4 cm = 10−6 m |

Symbols

| Symbol | Meaning | Units / typical value |
| --- | --- | --- |
| Ec (EC) | Energy of the bottom of the conduction band | eV |
| Ev (EV) | Energy of the top of the valence band | eV |
| EF | Fermi level: the energy at which a state has a 50 % chance of being occupied | eV |
| Ei | Intrinsic Fermi level, close to mid-gap | eV |
| ED | Donor energy level, just below Ec | eV; Ec − ED ≈ 0.045 eV for P in Si |
| EA | Acceptor energy level, just above Ev | eV; EA − Ev ≈ 0.045 eV for B in Si |
| Ea | Activation energy of dopant diffusion | eV; about 3–4 eV |
| n | Electron concentration (free electrons per cm3) | cm−3 |
| p | Hole concentration (holes per cm3) | cm−3 |
| ni | Intrinsic carrier concentration (n = p = ni in pure material) | cm−3; Si ≈ 1×1010 at 300 K |
| ND | Donor concentration | cm−3 |
| NA | Acceptor concentration | cm−3 |
| ND+, NA− | Concentrations of ionised donors and acceptors | cm−3 |
| Cs | Surface concentration of a diffusion (or solid concentration when freezing) | cm−3 |
| C(x, t) | Dopant concentration at depth x and time t | cm−3 |
| D | Diffusion coefficient (dopants in a furnace, or carriers) | cm2/s |
| D0 | Diffusion constant in D = D0e−Ea/kT | cm2/s |
| J (Fick) | Dopant flux: atoms crossing 1 cm2 per second | atoms/(cm2·s) |
| F | Particle flux in Fick's law | particles/(cm2·s) |
| Q | Dose: dopant atoms per unit area (in Weeks 13–14, Q also means charge) | atoms/cm2 (C or C/cm2 for charge) |
| Φ (dose) | Implanted dose (ions per cm2) | cm−2 |
| erfc | Complementary error function, erfc(u) = 1 − erf(u); read from a table | dimensionless |
| xj | Junction depth: where the dopant concentration equals the background | μm |
| NB (CB) | Background doping of the wafer (in Week 13, NB is the base doping) | cm−3 |
| Rp | Projected range: average depth at which implanted ions stop | μm |
| ΔRp | Straggle: spread of the implanted ions' stopping depths | μm |
| Np | Peak concentration of an implanted profile | cm−3 |
| Sn, Se | Nuclear and electronic stopping power of an implanted ion | eV·cm2 |
| NSi | Atom density of silicon | 5×1022 cm−3 |
| Rs | Sheet resistance (or diode series resistance in Week 12) | Ω/□ (ohms per square); Ω |
| xmask | Thickness of an implant mask | μm |
| μ, μn, μp | Mobility: drift velocity per unit field (electrons, holes) | cm2/(V·s); Si μn 1350, μp 480 |
| σ | Conductivity, q(nμn + pμp) (in Week 8, σ is also a capture cross-section) | S/cm (siemens per cm) |
| ρ | Resistivity, 1/σ | Ω·cm |
| R | Recombination rate | cm−3s−1 |
| L, Ln, Lp | Diffusion length √(Dτ): distance a minority carrier travels before recombining | μm or cm |
| V, Va | Applied voltage (positive for forward bias) | V |
| W | Depletion-region width (in Week 13 WB, WE are base and emitter widths; in Week 14 W is channel width) | μm or cm |
| I | Current | A |
| A (area) | Device or contact area | cm2 |
| Ntotal | Total number of dopant atoms in a region | atoms |
| Bz, Ix, VH | Hall effect: magnetic field (z), current (x) and Hall voltage | T (tesla); A; V |
| Gn, Gp, Rn, Rp | Generation and recombination rates of electrons and holes | cm−3s−1 |
| Qcharge | Total charge delivered by the ion beam, I × t | C |
| erfc(u), erfc−1 | Complementary error function, 1 − erf(u), and its inverse (read from a table) | dimensionless |
| N(x), N(W) | Doping concentration at depth x (or at the depletion edge W), from C-V profiling | cm−3 |
| r (atom) | Atomic radius (hard-sphere model), half the nearest-neighbour distance | Å |
| t | Time (or a thickness, where the text says so) | s (or cm) |

Abbreviations

| Abbreviation | Meaning |
| --- | --- |
| Si | Silicon |
| GaAs | Gallium arsenide |
| SiO2 | Silicon dioxide (silica), the oxide insulator |
| RTA | Rapid thermal annealing |
| SIMS | Secondary-ion mass spectrometry |
| LDD | Lightly doped drain |
| C-V | Capacitance–voltage (measurement or characteristic) |
| MOSFET | Metal–oxide–semiconductor field-effect transistor |
| CMOS | Complementary MOS (n- and p-channel MOSFETs together) |
| BJT | Bipolar junction transistor |
| IC | Integrated circuit |
| VLSI | Very-large-scale integration |
| n+ | Very heavily doped n-type (similarly p+) |

## Key terms

Every important word used this week is defined here, so you can read this week on its own.

Doping. The deliberate addition of small, controlled amounts of chosen impurity atoms (called dopants) to a pure semiconductor in order to change how well it conducts and whether its current is carried mainly by electrons or by holes. Typical dopant levels in silicon are 1014 to 1020 atoms per cm3.

Why it matters: pure silicon conducts far too little to be useful; every diode, transistor and integrated circuit is built from doped regions.

Donor. A dopant atom with one more outer (valence) electron than the silicon atom it replaces, such as phosphorus, arsenic or antimony (Group V). The spare electron is easily set free to carry current, leaving behind a fixed positive ion.

Acceptor. A dopant atom with one fewer valence electron than silicon, such as boron or gallium (Group III). It takes an electron from a neighbouring bond, leaving behind a fixed negative ion and a mobile empty bond called a hole, which behaves like a positive charge carrier.

n-type and p-type semiconductor. Silicon doped mainly with donors is n-type: most of its free carriers are electrons. Silicon doped mainly with acceptors is p-type: most of its free carriers are holes.

p-n junction. The boundary inside one crystal between a p-type region and an n-type region. It is the basic building block of diodes and transistors.

Diffusion. The net movement of atoms from where they are crowded (high concentration) to where they are sparse (low concentration), caused only by their random thermal jumping. In processing, dopants diffuse into a silicon wafer heated to about 900–1200 °C.

Concentration gradient (dC/dx). How fast the dopant concentration changes with depth. A steep gradient means a large change over a short distance. It is measured in atoms/cm4 (atoms per cm3, per cm).

Fick's first law. The rule that the flow of diffusing atoms is proportional to the concentration gradient, and runs from high to low concentration.

J = −D dC/dx

Where:

- J = dopant flux: number of dopant atoms crossing 1 cm2 each second (atoms/cm2·s)

- D = diffusion coefficient (cm2/s), defined next

- C = dopant concentration (atoms/cm3)

- x = depth into the wafer (cm)

Diffusion coefficient (D). A number that says how easily a dopant moves through the crystal. It rises steeply with temperature because each atomic jump needs a certain minimum energy, the activation energy Ea.

D = D0 e−Ea/kT

Where:

- D = diffusion coefficient (cm2/s)

- D0 = diffusion constant for that dopant in silicon (cm2/s)

- Ea = activation energy, about 3–4 eV for common dopants in silicon (eV)

- k = Boltzmann constant, 8.617×10−5 eV/K

- T = absolute temperature (K)

Why it matters: a furnace only 100 °C hotter makes dopants diffuse about ten times faster, so temperature must be controlled tightly.

Dose (Q). The total number of dopant atoms put into the wafer under each square centimetre of surface, in atoms/cm2. It is the area under the concentration-against-depth curve.

Predeposition (constant-source diffusion). A diffusion in which a dopant source is present at the surface the whole time, so the surface concentration Cs stays fixed while dopant creeps deeper. It gives a complementary-error-function (erfc) profile and is used as the first doping step.

Drive-in (limited-source diffusion). A second heating with the source removed, so the fixed dose already in the wafer spreads deeper and the surface concentration falls. It gives a Gaussian (bell-curve) profile and is used to reach the wanted depth.

Background doping (NB). The doping the wafer already had before the new dopant was added, usually of the opposite type (cm−3).

Junction depth (xj). The depth below the surface at which the added dopant concentration has fallen to equal the background doping, so that a p-n junction forms there (μm).

C(xj) = NB

Why it matters: the junction depth sets the size of a device; modern transistors need junctions only a few tens of nanometres deep.

Ion implantation. A doping method in which dopant atoms are turned into ions, accelerated by a high voltage and fired into the wafer, where they stop at a depth set by their energy. The dose is counted exactly from the beam current.

Projected range (Rp) and straggle (ΔRp). The average depth at which implanted ions stop (Rp), and the spread of stopping depths about that average (ΔRp, a standard deviation). Both are in μm and both increase with ion energy.

Channelling. The unwanted travel of implanted ions far deeper than Rp along open "channels" between rows of atoms in the crystal. It is avoided by tilting the wafer about 7° or covering it with a thin non-crystalline layer.

Annealing. Heating a wafer after implantation to repair the crystal damage caused by the ions and to move dopant atoms onto proper lattice sites, where they become electrically active.

Sheet resistance (Rs). The resistance of a thin doped layer measured between opposite edges of any square of it, in ohms per square (Ω/□). It shows how much dopant has been put in: more dopant, lower Rs.

Rs = ρ / xj

Where:

- Rs = sheet resistance (Ω/□)

- ρ = average resistivity of the layer (Ω·cm)

- xj = thickness of the layer, the junction depth (cm)

## The big picture

A pure silicon wafer is almost useless. To make a diode, a transistor or a chip, we must put dopant atoms (boron, phosphorus, arsenic) into chosen parts of the wafer, in chosen amounts, down to a chosen depth. There are two ways to do this:

- Diffusion: heat the wafer in an atmosphere rich in dopant. The dopant atoms creep in by themselves, the way a drop of ink spreads through water.

- Ion implantation: turn the dopant atoms into ions, accelerate them with a high voltage, and fire them into the wafer like tiny bullets.

The purpose of both is the same: to change the electrical properties of the material and form the n-type and p-type regions needed for diodes, transistors, MOSFETs and integrated circuits.

Common dopants for silicon:

| Dopant | Symbol | Makes silicon |
| --- | --- | --- |
| Phosphorus | P | n-type |
| Arsenic | As | n-type |
| Antimony | Sb | n-type |
| Boron | B | p-type |
| Gallium | Ga | p-type |

## Part A: Diffusion

### What diffusion is

Diffusion is the movement of dopant atoms from a region of high concentration to a region of low concentration, driven by thermal energy.

In processing, the silicon wafer is heated to a high temperature (about 900–1200 °C) and exposed to a dopant source. Dopant atoms enter the silicon surface and gradually move into the crystal.

### Why atoms move "downhill"

Your notes illustrate this with gas molecules in a box. Suppose 21 of 32 oxygen molecules start on the left side of a box. Every molecule moves randomly, left or right with equal chance. Nothing pushes them in any particular direction. But because there are more molecules on the left, more of them happen to cross from left to right than from right to left. The result is a net flow towards the emptier side.

- Concentration difference: more particles on one side (21 of 32 on the left) creates a concentration gradient.

- Net diffusion: random motion carries particles both ways, but more move from the crowded side to the less crowded side.

- Dynamic equilibrium: eventually both sides have similar concentrations. Particles still move randomly in both directions, but the two flows now cancel, so there is no net change.

In plain words. Diffusion is not a force. It is just statistics: if you have more atoms here than there, random jumping will, on average, carry atoms from here to there. The steeper the difference, the faster the flow.

The basic process is:

Dopant source → silicon surface → dopant penetration → desired dopant profile

### Fick's first law: how fast atoms flow

J = −D dC/dx

| Symbol | Meaning | Unit |
| --- | --- | --- |
| J | dopant flux: number of dopant atoms crossing 1 cm2 each second | atoms/cm2·s |
| D | diffusion coefficient: how easily the dopant moves in silicon | cm2/s |
| C | dopant concentration | atoms/cm3 |
| x | distance into the semiconductor | cm |
| dC/dx | the concentration gradient: how fast C changes with depth | atoms/cm4 |

Reading the equation. The flow is proportional to how steeply the concentration changes. No gradient, no flow. The minus sign says the flow goes from high concentration towards low concentration: if C falls as x increases (dC/dx negative), J is positive, meaning atoms flow in the +x direction, deeper into the wafer.

(The J here is a flow of atoms, not an electric current. Later weeks use J for current density.)

### The diffusion coefficient depends strongly on temperature

D = D0 e−Ea/kT

| Symbol | Meaning |
| --- | --- |
| D | diffusion coefficient at temperature T (cm2/s) |
| D0 | diffusion constant (cm2/s), a property of the dopant–silicon pair |
| Ea | activation energy (eV): the energy barrier an atom must jump over to move one lattice site |
| k | Boltzmann constant, 8.617×10−5 eV/K |
| T | absolute temperature (K) |

Because T sits inside an exponential, increasing temperature greatly increases the diffusion rate. Typical Ea is 3–4 eV, so D rises about tenfold for every 50–100 °C. This is why diffusion only happens in a furnace: at room temperature D is so small that dopants do not move at all in a lifetime.

### How far do atoms travel? The diffusion length

The depth to which dopants spread grows with the square root of time:

diffusion length ≈ √(Dt)

Where:

- D = diffusion coefficient of the dopant at the furnace temperature (cm2/s)

- t = diffusion time (s)

- √(Dt) = characteristic diffusion length (cm; multiply by 104 for μm)

Your notes use the form L = √(2Dt). Other books write 2√(Dt), which is what appears inside the erfc formula below. They are the same idea with a different constant in front. The key fact is that depth ∝ √(Dt): diffusing four times as long only doubles the depth. In a calculation, use whichever form the question gives.

### Two types of diffusion

#### A. Constant-source diffusion (predeposition)

The surface of the semiconductor is kept at an approximately constant dopant concentration Cs, because the source (dopant gas or glass) is present all the time. The profile is:

C(x, t) = Cs erfc( x / 2√(Dt) )

| Symbol | Meaning |
| --- | --- |
| C(x, t) | dopant concentration at depth x after time t (atoms/cm3) |
| Cs | surface concentration (atoms/cm3), fixed |
| x | depth |
| D | diffusion coefficient |
| t | diffusion time |
| erfc | the complementary error function, erfc(u) = 1 − erf(u). You read it from a table. |

Characteristics:

- The dopant source remains available throughout the process.

- The surface concentration stays approximately constant.

- It produces an erfc concentration profile.

- It is often used for the initial doping step.

The dose put in by predeposition. Integrating the erfc profile over all depths gives the dose introduced after time t:

Q = 2Cs √(Dt/π) = (2/√π) Cs √(Dt)

Where:

- Q = dose: dopant atoms introduced per cm2 of surface (atoms/cm2)

- Cs = fixed surface concentration (atoms/cm3)

- D = diffusion coefficient (cm2/s)

- t = predeposition time (s)

The dose grows as √t: the longer the source is left on, the more dopant enters, but ever more slowly.

What erfc looks like. erfc(0) = 1, so at the surface C = Cs. As the argument u = x/2√(Dt) grows, erfc falls: erfc(0.5) = 0.48, erfc(1) = 0.16, erfc(2) = 0.005, erfc(3) ≈ 2×10−5. So the concentration is highest at the surface and falls off steeply with depth. As time goes on, 2√(Dt) gets bigger, so the same depth corresponds to a smaller u, and the profile pushes deeper.

| u | erfc(u) | u | erfc(u) |
| --- | --- | --- | --- |
| 0 | 1.000 | 1.0 | 0.157 |
| 0.25 | 0.724 | 1.5 | 0.034 |
| 0.5 | 0.480 | 2.0 | 4.7×10−3 |
| 0.527 | 0.456 | 2.5 | 4.1×10−4 |
| 0.75 | 0.289 | 3.0 | 2.2×10−5 |

#### B. Limited-source diffusion (drive-in)

After a dopant has been introduced into the surface, the wafer is heated without supplying any more dopant. The fixed amount already there spreads deeper. The profile is approximately Gaussian:

C(x, t) = ( Q / √(πDt) ) e−x2/4Dt

| Symbol | Meaning |
| --- | --- |
| C(x, t) | dopant concentration at depth x after drive-in time t (atoms/cm3) |
| Q | total dopant dose per unit area (atoms/cm2), fixed |
| D | diffusion coefficient at the drive-in temperature (cm2/s) |
| t | drive-in time (s) |
| x | depth below the surface (cm) |

Characteristics:

- The dopant penetrates deeper.

- The surface concentration decreases (the same atoms are spread over a greater depth).

- The total dopant quantity is approximately conserved.

- It is used to obtain a desired junction depth.

The surface concentration is the value at x = 0, where e0 = 1:

C(0, t) = Q / √(πDt)

Where:

- C(0, t) = surface concentration after drive-in time t (atoms/cm3)

- Q = dose (atoms/cm2)

- D = diffusion coefficient (cm2/s)

- t = drive-in time (s)

Left: constant-source (erfc) profiles at three times; the surface value stays fixed while the profile deepens. Right: limited-source (Gaussian) profiles; the area under each curve (the dose) is the same, so the surface value falls as the profile spreads.

In plain words. Constant source: keep pouring ink on the surface, and the colour soaks deeper while the surface stays dark. Limited source: put one drop on, stop, and wait; the colour spreads deeper but gets paler everywhere.

### Junction depth

If the wafer was already doped with the opposite type, at background concentration NB (for example n-type 1016 cm−3 and we diffuse boron in), a p-n junction forms at the depth xj where the diffused concentration has fallen to equal the background:

C(xj) = NB

erfc profile: xj = 2√(Dt) · erfc−1(NB/Cs)
Gaussian profile: xj = 2√(Dt) · √( ln(Cs/NB) )

Where:

- xj = junction depth (cm; multiply by 104 for μm)

- D = diffusion coefficient (cm2/s); t = diffusion time (s)

- NB = background doping of the wafer (cm−3)

- Cs = surface concentration (cm−3); for the Gaussian profile this is the surface value after drive-in, Q/√(πDt)

- erfc−1 = inverse complementary error function: the value u for which erfc(u) equals the number in brackets, read backwards from the erfc table

#### Example 3.1: predeposition dose and junction depth

Question. Boron is predeposited into n-type silicon with background doping NB = 1×1016 cm−3. The surface concentration is held at Cs = 1×1020 cm−3, D = 4×10−14 cm2/s and the time is 20 minutes. Find the dose introduced and the junction depth.

Given: Cs = 1×1020 cm−3, NB = 1×1016 cm−3, D = 4×10−14 cm2/s, t = 20 min = 1200 s.

Find: Q and xj.

Formula:

Q = 2Cs √(Dt/π), xj = 2√(Dt) · erfc−1(NB/Cs)

Solution.

Step 1. The diffusion length:

Dt = 4×10−14 × 1200 = 4.8×10−11 cm2, √(Dt) = 6.93×10−6 cm, 2√(Dt) = 1.386×10−5 cm

Step 2. The dose:

√(Dt/π) = √(4.8×10−11/3.142) = 3.91×10−6 cm
Q = 2 × 1×1020 × 3.91×10−6 = 7.8×1014 atoms/cm2

Step 3. The junction is where erfc(u) = NB/Cs = 1016/1020 = 10−4. A fuller erfc table gives u = 2.75.

xj = 2.75 × 1.386×10−5 = 3.81×10−5 cm = 0.381 μm

Answer: Q = 7.8×1014 atoms/cm2, xj = 0.38 μm.

What this means: a 20-minute predeposition puts in a dose typical of a transistor base or a resistor, but only about 0.4 μm deep. To push the junction deeper without adding more dopant, the wafer is given a drive-in (Example 3.2).

#### Example 3.2: junction depth after a Gaussian drive-in

Question. The dose of Example 3.1 (Q = 7.8×1014 atoms/cm2) is driven in, with the boron source removed, at a higher temperature where D = 3×10−13 cm2/s, for 2 hours. The background is still NB = 1×1016 cm−3. Find the new surface concentration and the junction depth.

Given: Q = 7.8×1014 cm−2, D = 3×10−13 cm2/s, t = 2 h = 7200 s, NB = 1×1016 cm−3.

Find: C(0, t) and xj.

Formula:

C(0, t) = Q / √(πDt), xj = 2√(Dt) · √( ln(C(0, t)/NB) )

Solution.

Step 1. The Dt product:

Dt = 3×10−13 × 7200 = 2.16×10−9 cm2

Step 2. The surface concentration:

√(πDt) = √(6.79×10−9) = 8.24×10−5 cm
C(0, t) = 7.8×1014 / 8.24×10−5 = 9.5×1018 cm−3

Step 3. The junction depth:

2√(Dt) = 2 × 4.65×10−5 = 9.30×10−5 cm
ln(C(0, t)/NB) = ln(947) = 6.85, √6.85 = 2.62
xj = 9.30×10−5 × 2.62 = 2.43×10−4 cm = 2.43 μm

Answer: C(0) ≈ 9.5×1018 cm−3, xj ≈ 2.4 μm.

What this means: the same atoms now occupy a layer about six times deeper, so the surface concentration has dropped about tenfold (from 1020 to under 1019 cm−3). This is the two-step recipe: predeposition fixes how much dopant goes in, drive-in fixes how deep it goes.

### Step-by-step diffusion process

- Wafer preparation. A high-purity silicon wafer is cleaned to remove (a) dust, (b) organic contamination, (c) metallic impurities and (d) native surface oxide and contamination.

- Dopant source preparation. A suitable dopant source is selected: boron for p-type, phosphorus or arsenic for n-type.

- Heating. The wafer is placed in a diffusion furnace and heated to a high temperature.

- Dopant introduction. The dopant is supplied to the surface of the silicon.

- Dopant penetration. Thermal energy allows dopant atoms to move from the surface into the silicon lattice.

- Drive-in. Additional heating may be used to drive the dopant deeper into the wafer.

- Cooling. The wafer is cooled under controlled conditions.

- Characterisation. The resulting dopant profile is measured to determine (1) junction depth, (2) sheet resistance, (3) dopant concentration and (4) electrical properties.

### Diffusion at the atomic level

Dopant atoms move through the silicon crystal mainly by two mechanisms:

A. Vacancy mechanism. A dopant atom sitting on a lattice site can only move when a neighbouring site is empty (a vacancy). It jumps into the vacancy:

atom → vacancy → new lattice position

This is how the main dopants (B, P, As, Sb) move. It is slow, because it needs a vacancy to be next to the atom at the right moment.

B. Interstitial mechanism. A small atom moves through the spaces between the normal lattice positions without needing a vacancy. This is much faster. Metals such as gold, copper and iron move this way.

Some dopants use both: they move through interstitial sites, or by interactions involving both interstitials and vacancies. Which mechanism a dopant uses determines how quickly it diffuses.

### Advantages and disadvantages of diffusion

| Advantages | Disadvantages |
| --- | --- |
| Relatively simple process | Requires high temperature |
| Can process many wafers simultaneously | Dopants spread laterally (sideways) as well as vertically |
| Suitable for high-temperature processing | Less precise depth control |
| Good for introducing large dopant concentrations | Difficult to form extremely shallow junctions |
| Historically important in semiconductor fabrication | High-temperature exposure can affect previously fabricated structures |

## Diffusion calculations (from the lecture notes)

### Q1. Phosphorus is diffused into silicon with D = 2×10−13 cm2/s for t = 500 s. Find the approximate diffusion distance using L = √(2Dt).

Given: D = 2×10−13 cm2/s, t = 500 s. Find: L = √(2Dt).

Formula: L = √(2Dt).

Solution.

L = √(2 × 2×10−13 × 500) = √(2×10−10) = 1.414×10−5 cm

Convert to micrometres (1 cm = 104 μm):

L = 1.414×10−5 × 104 = 0.141 μm

Answer: L ≈ 0.141 μm.

What this means: dopants move only a fraction of a micrometre in about eight minutes, so diffusion depths are controlled on the scale of tenths of a micrometre by choosing the time and temperature.

### Q2. A dopant concentration gradient in silicon is 4×1018 cm−4 and D = 3×10−14 cm2/s. Find the diffusion flux using Fick's first law.

Given: dC/dx = 4×1018 cm−4, D = 3×10−14 cm2/s. Find: the flux J = −D dC/dx.

Formula: Fick's first law, J = −D dC/dx.

Solution.

J = −D dC/dx = −(3×10−14)(4×1018) = −1.2×105 atoms/cm2·s

Answer: |J| = 1.2×105 atoms/cm2·s. The minus sign means the dopant moves from the region of higher concentration towards lower concentration (against the direction in which C increases).

What this means: about a hundred thousand atoms cross each cm2 every second. That sounds a lot, but a typical dose is 1014–1015 atoms/cm2, so at this rate building up a doped layer would take a very long time; real diffusions use far steeper gradients and hotter furnaces.

### Q4. Find D at T = 1273 K for a dopant with D0 = 0.5 cm2/s and Ea = 3.5 eV.

Given: D0 = 0.5 cm2/s, Ea = 3.5 eV, T = 1273 K, k = 8.617×10−5 eV/K. Find: D = D0e−Ea/kT.

Formula: D = D0 e−Ea/kT.

Solution.

kT = 8.617×10−5 × 1273 = 0.1097 eV
Ea/kT = 3.5/0.1097 = 31.90
D = 0.5 × e−31.90 = 0.5 × 1.39×10−14 = 6.9×10−15 cm2/s

Answer: D ≈ 6.9×10−15 cm2/s. Try T = 1373 K (100 °C hotter): kT = 0.1183 eV, Ea/kT = 29.58, D = 7.1×10−14 cm2/s, ten times larger.

What this means: a 100 °C change in furnace temperature changes the diffusion rate tenfold, so a small temperature error gives a large error in junction depth. Furnace temperatures are therefore held to within about ±1 °C.

### Q5. Constant-source diffusion: Cs = 1×1020 cm−3, D = 1×10−13 cm2/s, t = 3600 s. Find C at x = 0.2 μm.

Given: Cs = 1×1020 cm−3, D = 1×10−13 cm2/s, t = 3600 s, x = 0.2 μm. Find: C(x, t) = Cs erfc(x/2√(Dt)).

Formula: C(x, t) = Cs erfc( x / 2√(Dt) ).

Solution.

Step 1, convert the depth: x = 0.2 μm = 2×10−5 cm.

Step 2, the diffusion length: √(Dt) = √(1×10−13 × 3600) = √(3.6×10−10) = 1.897×10−5 cm.

Step 3, the erfc argument:

u = x / 2√(Dt) = 2×10−5 / (2 × 1.897×10−5) = 0.527

Step 4, from the table: erf(0.527) = 0.544, so erfc(0.527) = 1 − 0.544 = 0.456.

Step 5:

C = Cs × erfc(u) = 1×1020 × 0.456 = 4.56×1019 atoms/cm3

Answer: C(0.2 μm) = 4.56×1019 cm−3, a little under half the surface value.

What this means: after one hour the boron-rich layer is still very shallow: only 0.2 μm down, the concentration has already halved, and it keeps falling ever faster with depth.

### Q6. Drive-in: dose Q = 2×1015 atoms/cm2, D = 5×10−14 cm2/s, t = 1000 s. Find the concentration at x = 0.

Given: Q = 2×1015 cm−2, D = 5×10−14 cm2/s, t = 1000 s, x = 0. Find: C(0, t) = Q/√(πDt).

Formula: C(x, t) = ( Q/√(πDt) ) e−x2/4Dt, which at x = 0 becomes C(0, t) = Q/√(πDt).

Solution.

At x = 0, e−0 = 1, so

C(0, t) = Q / √(πDt)
Dt = 5×10−14 × 1000 = 5×10−11 cm2
πDt = 1.571×10−10, √(πDt) = 1.253×10−5 cm
C(0, t) = 2×1015 / 1.253×10−5 = 1.60×1020 atoms/cm3

Answer: Surface concentration = 1.60×1020 cm−3.

What this means: a short drive-in leaves the dose packed close to the surface, so the surface is still very heavily doped. Longer drive-in times would lower this value as √t grows.

Why x = 0? x is the distance from the silicon surface: x = 0 is exactly at the surface; x = 0.1 μm is 0.1 μm below it; any x > 0 means below the surface. The question asks for the surface concentration, so we set x = 0 and the exponential becomes 1. (The dose is atoms per cm2 because it is the total number of atoms under each square centimetre of surface.)

## Part B: Ion implantation

### What ion implantation is

Ion implantation is a doping technique in which dopant atoms are converted into ions, accelerated to high energy, and physically injected into the semiconductor wafer.

Unlike thermal diffusion, ion implantation allows the dopant dose and implantation depth to be controlled very precisely.

Basic flowchart:

Dopant source → ioniser → mass analyser → accelerator → beam → wafer

Main components: ion source, mass analyser, acceleration system, beam focusing system, scanning system, the semiconductor wafer, and a vacuum chamber (the ions must not hit air molecules on the way).

### Step-by-step ion implantation

- Dopant ion generation. A dopant-containing material (boron, phosphorus, arsenic) is introduced into an ion source, where its atoms are converted into positively charged ions.

- Ion extraction. An electric field pulls the ions out of the source.

- Mass analysis. The ion beam passes through a magnetic mass analyser. A magnet bends the path of each ion by an amount that depends on its mass-to-charge ratio, so only the wanted ion goes through the exit slit. This prevents unwanted species being implanted.

- Acceleration. The selected ions are accelerated through a high electric potential. Their kinetic energy is E = qV, where E is the ion energy, q the ion charge and V the accelerating voltage. For a singly charged ion E = eV, so an ion accelerated through 100 kV has 100 keV.

- Beam focusing and scanning. The ion beam is focused and scanned across the wafer so that the dopant is distributed uniformly.

- Implantation. The energetic ions enter the silicon. As they travel through it, they collide with silicon nuclei and electrons and lose energy. Eventually they stop at a particular average depth.

- Annealing. Implantation damages the crystal, because energetic ions knock silicon atoms out of place. The wafer is therefore heated (thermal annealing), which repairs crystal damage and moves the dopant atoms into proper lattice positions where they become electrically active.

- The implantation profile. The implanted dopant normally produces an approximately Gaussian distribution.

### The implanted profile

C(x) = ( Q / (√(2π) ΔRp) ) exp[ −(x − Rp)2 / (2ΔRp2) ]

| Symbol | Meaning |
| --- | --- |
| C(x) | implanted dopant concentration at depth x (atoms/cm3) |
| Q | implanted dose (ions/cm2) |
| Rp | projected range: the average depth at which ions stop |
| ΔRp | straggle: the spread of stopping depths about Rp (standard deviation) |
| x | depth |

The peak is at x = Rp, below the surface, and its height is

Np = Q / (√(2π) ΔRp) ≈ 0.4 Q/ΔRp

Where:

- Np = peak concentration, at depth x = Rp (atoms/cm3)

- Q = implanted dose (ions/cm2)

- ΔRp = straggle (cm: convert from μm by multiplying by 10−4)

- √(2π) = 2.507, a number from the shape of the bell curve

An implanted profile is a bell curve centred at Rp below the surface, with width set by ΔRp. The junction forms where it falls to the background doping NB.

In plain words. Fire a million identical bullets into sand at the same speed. They do not all stop at exactly the same depth, but most stop near an average depth (Rp), with a spread (ΔRp). That is the bell curve.

### Implantation parameters

- Implantation dose Q = number of implanted ions per unit area, usually expressed in ions/cm2.

- Implantation energy, usually expressed in keV or MeV. A higher implant energy generally produces a deeper implant.

The dose comes from the beam current I, the time t and the area A:

Q = (I t)/(q A) (singly charged ions)

Where:

- Q = dose (ions/cm2)

- I = ion beam current (A)

- t = implant time (s)

- q = charge on each ion, 1.6×10−19 C for a singly charged ion

- A = implanted area (cm2)

#### Example 3.3: peak concentration and junction depth of a phosphorus implant

Question. Phosphorus is implanted into p-type silicon (NB = 1×1016 cm−3) with dose Q = 5×1013 cm−2. At the chosen energy Rp = 0.12 μm and ΔRp = 0.045 μm. Find the peak concentration, the surface concentration and the junction depth.

Given: Q = 5×1013 cm−2, Rp = 0.12 μm, ΔRp = 0.045 μm = 4.5×10−6 cm, NB = 1×1016 cm−3.

Find: Np, C(0) and xj.

Formula:

Np = Q / (√(2π) ΔRp), C(x) = Np exp[ −(x − Rp)2/(2ΔRp2) ]
xj = Rp ± ΔRp √( 2 ln(Np/NB) )

(The junction formula comes from setting C(xj) = NB, as in P2 below. The + sign gives the junction below the peak, the − sign a possible junction above it.)

Solution.

Step 1. Peak concentration:

√(2π) ΔRp = 2.507 × 4.5×10−6 = 1.128×10−5 cm
Np = 5×1013 / 1.128×10−5 = 4.43×1018 cm−3

Step 2. Surface concentration (x = 0):

Rp/ΔRp = 0.12/0.045 = 2.667, (Rp/ΔRp)2/2 = 3.556
C(0) = 4.43×1018 × e−3.556 = 4.43×1018 × 0.0286 = 1.27×1017 cm−3

Step 3. Junction depth:

Np/NB = 443, ln 443 = 6.094, √(2 × 6.094) = 3.491
ΔRp × 3.491 = 0.045 × 3.491 = 0.157 μm
deep side: xj = 0.12 + 0.157 = 0.277 μm
shallow side: 0.12 − 0.157 < 0, so there is no junction above the peak

Answer: Np = 4.4×1018 cm−3, C(0) = 1.3×1017 cm−3, xj = 0.28 μm.

What this means: because the surface concentration (1.3×1017 cm−3) is still above the background, the n-type layer runs all the way from the surface down to 0.28 μm, giving a single shallow junction. The whole layer is formed at room temperature, and only a short anneal is then needed.

### How ion implantation works inside silicon

ion enters → collisions with atoms → loses energy → changes direction → eventually stops

There are two major energy-loss mechanisms:

Nuclear stopping. The implanted ion collides with silicon nuclei. This causes (i) deflection of the ion and (ii) displacement of silicon atoms, which is lattice damage. The nuclear stopping power is

Sn = −(1/NSi) (dE/dx)nuclear

Electronic stopping. The ion interacts with the electrons in the silicon, losing energy through excitation and ionisation. At high energies electronic stopping is particularly important. It causes little damage.

Se = −(1/NSi) (dE/dx)electronic

Where:

- Sn, Se = nuclear and electronic stopping power (eV·cm2)

- NSi = atom density of silicon, 5×1022 cm−3

- (dE/dx) = rate of change of the ion's energy with distance travelled, due to collisions with nuclei or with electrons (eV/cm); it is negative because the ion slows down, so the minus sign makes S positive

Here NSi is the number of silicon atoms per cm3 (5×1022 cm−3) and dE/dx the energy lost per unit distance. Heavy ions (As) lose energy mainly to nuclei and stop shallow; light ions (B) lose it mainly to electrons and go deeper.

### Channelling

Channelling occurs when ions enter the crystal along certain crystallographic directions and travel relatively deeply through open channels between rows of atoms. This produces an unexpectedly deep dopant distribution.

To reduce channelling, manufacturers may:

- tilt the wafer relative to the ion beam (typically 7°);

- rotate the wafer;

- use suitable implantation conditions;

- sometimes introduce a thin amorphous layer (a screen oxide, or a pre-amorphising implant) so the crystal channels are hidden.

### Advantages and limitations of ion implantation

| Advantages | Limitations |
| --- | --- |
| Dose known very accurately (about ±1 %) from the measured beam charge | Expensive, complex equipment that needs a high vacuum |
| Depth set by ion energy, independently of dose | Ions damage the crystal, so annealing is always needed |
| Done near room temperature, so earlier profiles are not disturbed | Channelling can give unwanted deep tails unless the wafer is tilted |
| Photoresist can be used as a mask | Wafers are processed one (or a few) at a time, so throughput is lower |
| Peak can be buried below the surface; very shallow junctions possible | Very deep junctions need very high energies (MeV), or a diffusion drive-in afterwards |

### Example: forming an n-type region both ways

Suppose we want to convert part of a silicon wafer into an n-type region.

Using diffusion: silicon wafer → phosphorus source → high temperature → P atoms diffuse into Si → n-type region
Using ion implantation: phosphorus source → P+ ions → mass analysis → acceleration → implantation into Si → annealing → n-type region

### Diffusion versus ion implantation

| Feature | Diffusion | Ion implantation |
| --- | --- | --- |
| Dopant introduction | Thermal movement | Accelerated ions |
| Main driving force | Concentration gradient | Ion kinetic energy |
| Temperature | High | Relatively low (implant near room temperature) |
| Depth control | Less precise | Highly precise |
| Dose control | Moderate | Excellent |
| Crystal damage | Low | Significant |
| Annealing | Sometimes required | Normally required |
| Profile | erfc or Gaussian, maximum at the surface | Approximately Gaussian, peak below the surface |
| Modern IC use | Less dominant for shallow junctions | Widely used |
| Equipment | Diffusion furnace | Ion implanter |

## Ion implantation calculations (from the lecture notes)

### P1. A silicon wafer is implanted with boron, Q = 1.0×1013 cm−2, Rp = 0.5 μm, ΔRp = 0.05 μm. (a) Find the peak concentration Np. (b) Find the boron concentration at the surface (x = 0).

Given: Q = 1.0×1013 cm−2, Rp = 0.5 μm, ΔRp = 0.05 μm. Find: (a) Np; (b) N(0).

Formula: Np = Q/(√(2π)ΔRp) and N(x) = Np exp[ −(x − Rp)2/(2ΔRp2) ].

Solution.

(a) Convert ΔRp = 0.05 μm = 5.0×10−6 cm.

Np = Q / (√(2π) ΔRp) = 1.0×1013 / (2.5066 × 5.0×10−6) = 1.0×1013 / 1.253×10−5
= 7.98×1017 cm−3

(b) At x = 0:

N(0) = Np exp( −Rp2/2ΔRp2 ), Rp/ΔRp = 0.5/0.05 = 10
N(0) = Np exp(−102/2) = Np e−50 = 7.98×1017 × 1.93×10−22 = 1.54×10−4 cm−3

Answer: (a) Np = 7.98×1017 cm−3; (b) N(0) ≈ 1.5×10−4 cm−3, effectively zero boron at the surface.

What this means: the whole dose is buried in a layer around 0.5 μm deep, with undoped silicon above it. A buried profile like this is impossible with diffusion, which always peaks at the surface.

### P2. An n-type substrate with CB = 1.0×1015 cm−3 is implanted with boron to form a p-type region. Peak Np = 1.0×1017 cm−3 at Rp = 0.4 μm, ΔRp = 0.05 μm. Find the junction depth xj (where the boron concentration equals CB).

Given: CB = 1.0×1015 cm−3, Np = 1.0×1017 cm−3, Rp = 0.4 μm, ΔRp = 0.05 μm. Find: xj where N(xj) = CB.

Formula: N(x) = Np exp[ −(x − Rp)2/(2ΔRp2) ], with N(xj) = CB.

Solution.

At the junction N(xj) = CB:

CB = Np exp( −(xj − Rp)2/2ΔRp2 )
ln(Np/CB) = (xj − Rp)2/2ΔRp2
xj = Rp + ΔRp √( 2 ln(Np/CB) )

Numbers: Np/CB = 1017/1015 = 100; ln(100) = 4.605; × 2 = 9.21; √9.21 = 3.035.

xj = 0.4 μm + 0.05 μm × 3.035 = 0.4 + 0.152 = 0.552 μm

Answer: The p-n junction is formed 0.552 μm below the silicon surface. (There is also a second junction on the shallow side, at Rp − 0.152 = 0.248 μm, because the buried p-region has n-type silicon above it as well as below it.)

What this means: the implant creates a buried p-type layer only about 0.3 μm thick (0.248 to 0.552 μm), sandwiched between n-type silicon. Its position is set by the ion energy (through Rp) and its thickness by the straggle.

### P3. A 300 mm diameter wafer needs a boron dose Q = 2.0×1014 ions/cm2. (a) Find the total number of ions. (b) If the implanter uses singly charged ions (q = 1.6×10−19 C) and processes the wafer in 60 s, what beam current is needed?

Given: diameter 300 mm, Q = 2.0×1014 cm−2, q = 1.6×10−19 C, t = 60 s. Find: (a) total ions N; (b) beam current I.

Formula: Ntotal = Q × A with A = πr2, and I = Qcharge/t = Ntotal q/t (the same as Q = It/qA rearranged).

Solution.

(a) Radius r = 300/2 = 150 mm = 15 cm. Area A = πr2 = 3.142 × 225 = 706.9 cm2.

Ntotal = Q × A = 2.0×1014 × 706.9 = 1.414×1017 ions

(b) Total charge delivered = Ntotal × q = 1.414×1017 × 1.6×10−19 = 0.0226 C.

I = Qcharge / t = 0.0226 / 60 = 3.77×10−4 A = 0.377 mA

Answer: (a) Ntotal = 1.41×1017 ions; (b) I = 0.377 mA.

What this means: a beam current of under half a milliampere is enough to dope a whole 300 mm wafer in a minute. Because the charge is measured directly, the dose is known very accurately, which is the main advantage of implantation.

### P4. A photoresist mask must protect part of a wafer during a boron implant. In photoresist Rp = 0.8 μm and ΔRp = 0.08 μm. The substrate under the mask must receive no more than 0.1 % of the peak concentration. Find the minimum mask thickness xmask.

Given: Rp = 0.8 μm, ΔRp = 0.08 μm in resist, N(xmask)/Np ≤ 10−3. Find: minimum xmask.

Formula: N(x)/Np = exp[ −(x − Rp)2/(2ΔRp2) ], set equal to 10−3 at x = xmask.

Solution.

At the bottom of the mask the concentration must be 10−3 of the peak:

N(xmask)/Np = exp( −(xmask − Rp)2/2ΔRp2 ) = 10−3

Take logarithms. ln(10−3) = −3 ln 10 = −6.908. The minus signs cancel:

(xmask − Rp)2/2ΔRp2 = 6.908
xmask − Rp = ΔRp √(2 × 6.908) = ΔRp √13.816 = 3.717 ΔRp
xmask = 0.8 + 0.08 × 3.717 = 0.8 + 0.297 = 1.097 μm

Answer: To keep transmission below 0.1 % the photoresist must be at least 1.10 μm thick.

What this means: the mask must be thicker than the projected range plus nearly four straggles to stop almost every ion. In real manufacturing engineers add a safety margin and use about 1.3–1.4 μm.

## Part C: Evaluating the impurity distribution

After doping, the engineer must check that the dose, the profile and the junction depth are what was intended (step 8 of the diffusion process). The main methods:

| Method | What it measures | How it works |
| --- | --- | --- |
| Four-point probe | Sheet resistance Rs (Ω/□) | Pass current through the outer two of four probes in a line; measure voltage across the inner two |
| Groove-and-stain | Junction depth xj | Grind a shallow groove, stain it (p and n regions take different colours), measure under a microscope |
| Spreading resistance profiling | Carrier concentration against depth | Step two probes down a shallow bevel, measuring resistance at each point |
| C-V profiling | Doping against depth | Capacitance of a junction against reverse bias (Week 12) |
| SIMS | All dopant atoms against depth | Sputter the surface with an ion beam and count ejected dopant ions in a mass spectrometer |
| Hall measurement | Carrier type, concentration, mobility | Hall voltage in a magnetic field (Week 7) |

### Sheet resistance, explained

A diffused layer is a thin conducting skin of thickness xj. Its resistance is described by the sheet resistance:

Rs = ρ / xj [ohms per square, Ω/□]

Where:

- Rs = sheet resistance (Ω/□)

- ρ = average resistivity of the doped layer (Ω·cm)

- xj = thickness of the layer, taken as the junction depth (cm)

"Per square" means: any square piece of the layer, whatever its size, has resistance Rs between two opposite edges. (A bigger square is longer, which raises R, but also wider by the same factor, which lowers R; the two cancel.) So a resistor L long and W wide made from the layer has

R = Rs × (L/W) = Rs × (number of squares)

Where:

- R = resistance of the resistor (Ω)

- L = length of the resistor in the direction of current flow (μm or cm)

- W = width of the resistor (same unit as L, so L/W is a pure number: the number of squares)

Measured with a four-point probe on a large thin sample:

Rs = 4.532 × (V/I)

Where:

- V = voltage measured between the two inner probes (V)

- I = current passed through the two outer probes (A)

- 4.532 = π/ln 2, a geometry factor for equally spaced probes on a large, thin sheet

#### Example 3.4: sheet resistance from a four-point probe

Question. A four-point probe on a boron-diffused wafer reads V = 2.0 mV when I = 1.0 mA is passed. The junction depth is 1.0 μm. Calculate the sheet resistance of the layer and its average resistivity.

Given: V = 2.0 mV, I = 1.0 mA, xj = 1.0 μm = 1.0×10−4 cm, Rs = 4.532 V/I.

Find: Rs and the average resistivity ρ.

Formula:

Rs = 4.532 × V/I, ρ = Rs × xj

Solution.

Step 1. Sheet resistance:

Rs = 4.532 × V/I = 4.532 × (2.0×10−3 / 1.0×10−3) = 4.532 × 2.0 = 9.06 Ω/□

Step 2. Average resistivity, from Rs = ρ/xj:

ρ = Rs × xj = 9.06 × 1.0×10−4 = 9.1×10−4 Ω·cm

Answer: Rs = 9.06 Ω/□, ρ ≈ 9×10−4 Ω·cm.

What this means: a resistivity this low corresponds to an average boron concentration of a few times 1019 cm−3, a heavily doped p+ layer. A resistor 10 squares long made from it would have only about 91 Ω.

### Junction depth by groove and stain

A cylindrical groove of radius R is ground into the surface and stained. If the stained chord is a wide at the surface and b wide at the junction:

xj ≈ (a2 − b2) / (8R)

Where:

- xj = junction depth (same unit as a, b and R, usually μm)

- a = width of the groove where it cuts the wafer surface

- b = width of the groove where it cuts the junction (the edge of the stained region)

- R = radius of the grinding cylinder

## Key points of Week 3

- Doping puts controlled amounts of B (p-type) or P, As, Sb (n-type) into chosen regions.

- Diffusion: random thermal motion carries dopant from high to low concentration. Fick: J = −D dC/dx.

- D = D0e−Ea/kT: hotter means much faster. Depth grows as √(Dt).

- Constant source → erfc profile, fixed surface concentration. Limited source → Gaussian, fixed dose, surface concentration falls.

- Ion implantation: ions accelerated to E = qV, Gaussian profile peaked at Rp with spread ΔRp, dose Q = It/qA, annealing required, channelling avoided by tilting.

- Junction depth is where the dopant concentration equals the background doping.

- Profiles are checked by sheet resistance, junction depth, SIMS, spreading resistance and C-V.

## Examination questions solved (Q14–Q21)

### Q14. What is semiconductor doping? Explain why doping is necessary in semiconductor device fabrication.

Doping is the intentional introduction of controlled, small quantities of specific impurity atoms into a pure (intrinsic) semiconductor to change its electrical properties. Group V donors (P, As, Sb) make silicon n-type; Group III acceptors (B, Al, Ga) make it p-type. Typical levels are 1014 to 1020 cm−3.

Why it is necessary:

- Intrinsic conductivity is too low and uncontrolled. Pure Si has only ni ≈ 1010 cm−3 carriers, giving ρ = 1/(qni(μn + μp)) ≈ 3×105 Ω·cm. Doping with 1016 cm−3 P raises n a million times, to ρ ≈ 0.5 Ω·cm.

- It sets the carrier type. Devices depend on regions where electrons or holes dominate. Without n- and p-type regions there can be no p-n junction, no diode, no BJT and no MOSFET.

- Temperature stability. In an extrinsic semiconductor the carrier density is fixed by ND or NA over a wide temperature range (the extrinsic region) instead of varying exponentially with T as ni does.

- Device design. Doping profiles set the built-in potential, depletion width, breakdown voltage, threshold voltage of MOSFETs, current gain of BJTs, sheet resistance of resistors and the quality of Ohmic contacts (heavily doped n+, p+ regions).

- Selective, local control. Using masks, different areas of one chip can be given different doping, which is what makes integrated circuits possible.

### Q15. Differentiate between n-type and p-type semiconductors.

| Feature | n-type | p-type |
| --- | --- | --- |
| Dopant added | Pentavalent (Group V): P, As, Sb | Trivalent (Group III): B, Al, Ga, In |
| Name of dopant | Donor | Acceptor |
| Effect of dopant | Donates a free electron to the conduction band | Accepts an electron, creating a hole in the valence band |
| Fixed ion left behind | Positive donor ion ND+ | Negative acceptor ion NA− |
| Majority carriers | Electrons | Holes |
| Minority carriers | Holes | Electrons |
| Carrier densities | n ≈ ND, p = ni2/ND | p ≈ NA, n = ni2/NA |
| Impurity level | ED just below Ec | EA just above Ev |
| Fermi level | Above Ei, towards Ec | Below Ei, towards Ev |
| Conductivity | σ ≈ qNDμn | σ ≈ qNAμp |
| Hall coefficient | Negative | Positive |

Both remain electrically neutral overall: every free electron (or hole) is balanced by a fixed ion.

### Q16. Explain the difference between donor impurities and acceptor impurities, giving suitable examples.

Donor impurities have one more valence electron than the host atom they replace. In Si, Group V atoms such as phosphorus, arsenic and antimony have five valence electrons; four form covalent bonds with neighbouring Si atoms, and the fifth is bound only by about 0.04–0.05 eV. It is easily thermally released into the conduction band, leaving a positively charged, immobile donor ion. Donors introduce an energy level ED just below the conduction band and make the material n-type.

Acceptor impurities have one fewer valence electron than the host. In Si, Group III atoms such as boron, aluminium, gallium and indium have three valence electrons and leave one bond incomplete. A nearby valence electron moves in with very little energy (≈ 0.045 eV for B), so the acceptor becomes a negative ion and a mobile hole is created in the valence band. Acceptors introduce a level EA just above the valence band and make the material p-type.

|  | Donor | Acceptor |
| --- | --- | --- |
| Valence electrons (in Si) | 5 | 3 |
| Gives / takes | Gives an electron | Takes an electron (gives a hole) |
| Ionised charge | + | − |
| Level | Near Ec | Near Ev |
| Examples in Si | P, As, Sb | B, Al, Ga, In |
| Examples in GaAs | S, Se, Te (on As site); Si on Ga site | Zn, Be, Mg (on Ga site); C on As site |

### Q17. Describe the mechanism of dopant diffusion in a semiconductor.

Diffusion is the net movement of dopant atoms from a region of high concentration to one of low concentration, driven by random thermal jumps of the atoms in the lattice. At room temperature it is negligible; at 900–1200 °C (silicon) it is significant.

Atomic mechanisms:

- Vacancy (substitutional) diffusion. Substitutional dopants (B, P, As, Sb) occupy lattice sites. A dopant can jump only when an adjacent lattice site is vacant. The rate depends on the vacancy concentration (which rises steeply with temperature) and the jump probability. High activation energy (≈ 3–4 eV), so D is small (10−15 to 10−12 cm2/s).

- Interstitial diffusion. Small atoms or those that do not bond into the lattice (Au, Cu, Fe, Na, Li, H) move between lattice sites through the open spaces of the diamond structure. Low activation energy (0.5–1.5 eV), so they diffuse many orders of magnitude faster. These are usually unwanted contaminants.

- Interstitialcy (kick-out) and dissociative mechanisms. A dopant is pushed off its site by a silicon self-interstitial, travels interstitially, then returns to a substitutional site. This explains enhanced diffusion of B and P during oxidation (oxidation-enhanced diffusion).

Temperature dependence. D = D0 exp(−Ea/kT), so D roughly doubles every 20–30 °C.

Macroscopic description. The flux obeys Fick's first law F = −D ∂C/∂x, and the profile evolves by Fick's second law ∂C/∂t = D ∂2C/∂x2. In practice a two-step process is used: predeposition from a constant surface source (erfc profile) followed by drive-in of the fixed dose (Gaussian profile). Diffusion is masked by SiO2 windows, and the dopant spreads sideways under the mask edge by about 0.8 of its depth (lateral diffusion).

### Q18. State and explain Fick's first and second laws of diffusion.

Fick's first law. The diffusion flux is proportional to the negative of the concentration gradient:

F = −D ∂C/∂x

- F: number of atoms crossing unit area per unit time (cm−2s−1).

- C(x, t): impurity concentration (cm−3).

- D: diffusion coefficient (cm2/s), D = D0exp(−Ea/kT).

- The minus sign: atoms move from high to low concentration. If there is no gradient, there is no net flux.

It describes the flux at one instant but not how the profile changes.

Fick's second law. Consider a thin slice of thickness dx. Atoms entering minus atoms leaving equals the increase stored (continuity, no generation or loss):

∂C/∂t = −∂F/∂x

Substituting the first law (with D constant):

∂C/∂t = D ∂2C/∂x2

This is the diffusion equation. It says the concentration rises where the profile is curved upward (concave) and falls where it is curved downward, so diffusion always smooths the profile. Its solutions, set by the boundary conditions, are the complementary-error-function profile (constant surface source) and the Gaussian profile (fixed dose) described in Part A above.

### Q19. A semiconductor is doped by diffusion with a constant surface concentration of 1 × 1020 cm−3. Explain how the impurity concentration varies with depth.

A constant surface concentration is the predeposition (unlimited source) case. Solve Fick's second law with:

- C(0, t) = Cs = 1×1020 cm−3 (held fixed for all t)

- C(∞, t) = 0 (deep in the wafer)

- C(x, 0) = 0 (no dopant at the start)

The solution is the complementary error function:

C(x, t) = Cs erfc( x / 2√(Dt) ) = 1×1020 · erfc( x / 2√(Dt) ) cm−3

How it varies with depth:

- At the surface (x = 0), erfc(0) = 1, so C = 1×1020 cm−3, independent of time.

- The concentration decreases monotonically with depth. Near the surface it falls almost linearly; deeper it falls faster than exponentially, because erfc(u) ≈ e−u2/(u√π) for large u.

- The depth scale is the diffusion length 2√(Dt). At x = 2√(Dt), erfc(1) = 0.157, so C = 1.57×1019 cm−3. At x = 4√(Dt), erfc(2) = 4.7×10−3, so C = 4.7×1017 cm−3.

- As time increases, the profile penetrates deeper (as √t) while the surface stays at 1020 cm−3, so the total dose grows: Q = (2/√π)Cs√(Dt).

- If the wafer has background doping NB of the opposite type, a junction forms where C(xj) = NB.

Worked illustration (assume boron into n-Si with NB = 1×1016 cm−3, D = 1×10−13 cm2/s at about 1100 °C, t = 1 h = 3600 s):

√(Dt) = √(1×10−13 × 3600) = 1.90×10−5 cm = 0.190 μm
2√(Dt) = 0.379 μm

Junction: erfc(u) = NB/Cs = 1016/1020 = 10−4 ⇒ u ≈ 2.75
xj = 2.75 × 0.379 μm ≈ 1.04 μm

Dose: Q = (2/√π)(1×1020)(1.90×10−5) = 2.14×1015 atoms/cm2

| Depth x (μm) | u = x/2√(Dt) | erfc(u) | C (cm−3) |
| --- | --- | --- | --- |
| 0 | 0 | 1 | 1.0×1020 |
| 0.19 | 0.5 | 0.480 | 4.8×1019 |
| 0.38 | 1.0 | 0.157 | 1.6×1019 |
| 0.57 | 1.5 | 0.034 | 3.4×1018 |
| 0.76 | 2.0 | 4.7×10−3 | 4.7×1017 |
| 1.04 | 2.75 | 1.0×10−4 | 1.0×1016 (junction) |

So the impurity concentration is highest at the surface and falls off as an erfc curve, reaching the background doping about 1 μm below the surface for these conditions.

### Q20. Explain the principle of ion implantation and identify its major advantages over thermal diffusion.

Principle. Ion implantation introduces dopant atoms into a semiconductor by bombarding it with a beam of energetic dopant ions. The dopant is ionised in an ion source, the ions are extracted, selected by mass in a magnetic analyser, accelerated to an energy of a few keV to MeV and scanned uniformly across the wafer. Each ion penetrates the crystal, losing energy by nuclear and electronic collisions, and stops at a depth that depends on its energy and mass. The resulting distribution is approximately Gaussian, peaking at the projected range Rp with straggle ΔRp. The dose is measured exactly by integrating the beam current in a Faraday cup (Φ = It/qA). Because the impact damages the lattice and leaves dopants on non-lattice sites, the wafer is then annealed (furnace or RTA) to repair the damage and electrically activate the dopants.

Advantages over thermal diffusion:

- Precise, reproducible dose control (±1 % or better) over a very wide range, 1011 to 1016 cm−2, by measuring charge. Diffusion dose depends on solid solubility, time and temperature and is much less accurate.

- Independent control of depth and dose. Depth is set by energy, dose by charge. In diffusion both depend on the same Dt product.

- Low-temperature process. Implantation is done near room temperature; only a short anneal is needed. Existing profiles are not disturbed and the thermal budget is small, which is vital for shallow junctions.

- Wide choice of masks, including photoresist, which diffusion cannot use.

- Buried and retrograde profiles. The peak can be placed below the surface (e.g. retrograde wells, buried layers); diffusion always peaks at the surface.

- Very shallow junctions with low-energy implants.

- Less lateral spread under the mask edge, allowing smaller devices and self-aligned structures.

- Purity. Mass separation guarantees only the chosen species is implanted.

- Not limited by solid solubility: concentrations above solubility can be obtained (though not all are activated).

- Uniformity across large wafers, and the process is clean (vacuum, dry).

### Q21. Compare diffusion and ion implantation as semiconductor doping techniques.

| Feature | Thermal diffusion | Ion implantation |
| --- | --- | --- |
| Principle | Dopant moves in from a surface source by random thermal jumps (Fick's laws) | Energetic ions are driven into the crystal and stop by collisions |
| Process temperature | High, 900–1200 °C | Room temperature, plus anneal (RTA ≈ 1000 °C for seconds) |
| Profile shape | erfc or Gaussian, always maximum at the surface | Gaussian peaking at Rp below the surface; buried and retrograde profiles possible |
| Dose control | Limited (± 5–10 %), set by solubility, T and t | Excellent (± 1 %), set by measured charge |
| Depth control | Coupled to dose through Dt | Independent: set by energy |
| Junction depth | Relatively deep; hard to make very shallow junctions | Very shallow junctions possible |
| Lateral spread | Large (≈ 0.8 × depth) | Small (≈ straggle) |
| Masking | SiO2, Si3N4 (must survive high T) | Photoresist, oxide, nitride, polysilicon |
| Lattice damage | None | Significant; needs annealing; amorphisation at high dose |
| Channelling | Not applicable | Must be avoided (7° tilt, screen oxide) |
| Throughput and cost | Batch of 100+ wafers, cheap equipment | Single wafer or small batch, expensive equipment |
| Purity | Depends on source and furnace cleanliness | Mass-analysed, very pure |
| Concentration limit | Limited by solid solubility | Can exceed solubility |
| Typical use today | Drive-in, deep wells, solar cells, emitter diffusion in older processes | Source/drain, threshold-adjust, wells, LDD, channel stops in all modern CMOS |

Summary: diffusion is simple, cheap and damage-free but gives coarse, coupled control of dose and depth and needs high temperature. Ion implantation gives precise, independent, low-temperature control of dose and depth and is the standard technique for modern VLSI, at the cost of expensive equipment and lattice damage that must be annealed. In practice the two are often combined: implant to set the dose, then a thermal drive-in to set the depth.

## Practice questions

These extra questions practise this week's ideas. Work each one on paper before reading the solution; the calculation questions follow the same Question, Given, Find, Solution, Answer layout as the worked examples.

#### Practice 3.1: how far does boron move?

Question. Boron diffuses in silicon with D = 1×10−14 cm2/s. Find the characteristic diffusion length √(Dt) after 2 hours, and the scale length 2√(Dt) used in the erfc profile.

Given: D = 1×10−14 cm2/s, t = 2 h = 7200 s.

Find: √(Dt) and 2√(Dt).

Solution.

√(Dt) = √(1×10−14 × 7200) = √(7.2×10−11) = 8.49×10−6 cm = 0.085 μm
2√(Dt) = 0.17 μm

Answer: √(Dt) = 0.085 μm, 2√(Dt) = 0.17 μm.

#### Practice 3.2: predeposition junction depth and dose

Question. Boron is predeposited into n-type silicon (NB = 1×1017 cm−3) from a constant source with Cs = 1×1020 cm−3, D = 5×10−14 cm2/s, for 30 minutes. Find the junction depth and the dose introduced.

Given: Cs = 1020 cm−3, NB = 1017 cm−3, D = 5×10−14 cm2/s, t = 1800 s.

Find: xj and Q.

Solution.

√(Dt) = √(5×10−14 × 1800) = 9.49×10−6 cm, 2√(Dt) = 1.90×10−5 cm
erfc(u) = NB/Cs = 10−3 ⇒ u = 2.33 (from erfc tables)
xj = u × 2√(Dt) = 2.33 × 1.90×10−5 = 4.4×10−5 cm = 0.44 μm
Q = (2/√π) Cs √(Dt) = 1.128 × 1020 × 9.49×10−6 = 1.07×1015 cm−2

Answer: xj = 0.44 μm, Q = 1.07×1015 cm−2.

#### Practice 3.3: driving in the dose

Question. The dose of Practice 3.2 is driven in, with no further source, at D = 1×10−13 cm2/s for 1 hour. Find the new surface concentration and junction depth (NB = 1×1017 cm−3).

Given: Q = 1.07×1015 cm−2, D = 10−13 cm2/s, t = 3600 s, NB = 1017 cm−3.

Find: C(0) and xj.

Solution.

√(πDt) = √(π × 3.6×10−10) = 3.36×10−5 cm
C(0) = Q/√(πDt) = 1.07×1015 / 3.36×10−5 = 3.2×1019 cm−3
2√(Dt) = 2√(3.6×10−10) = 3.79×10−5 cm
xj = 2√(Dt) √(ln(C(0)/NB)) = 3.79×10−5 × √(ln 318) = 3.79×10−5 × 2.40 = 9.1×10−5 cm

Answer: C(0) = 3.2×1019 cm−3 (down from 1020), xj = 0.91 μm (up from 0.44 μm). Drive-in trades surface concentration for depth.

#### Practice 3.4: dose from beam current

Question. An implanter delivers a singly charged boron beam of 50 μA for 200 s, uniformly over a 150 mm wafer. What dose is implanted?

Given: I = 50×10−6 A, t = 200 s, r = 7.5 cm, q = 1.6×10−19 C.

Find: Q (ions/cm2).

Solution.

A = π × 7.52 = 176.7 cm2
Q = It/(qA) = (50×10−6 × 200)/(1.6×10−19 × 176.7) = 10−2/2.83×10−17 = 3.5×1014 cm−2

Answer: Q = 3.5×1014 ions/cm2.

#### Practice 3.5: shallow implanted junction

Question. Arsenic is implanted into p-type silicon (NB = 1×1016 cm−3) with Q = 5×1014 cm−2, Rp = 0.10 μm and ΔRp = 0.03 μm. Find the peak concentration and the depth of the junction below the peak.

Given: Q = 5×1014 cm−2, Rp = 0.10 μm, ΔRp = 0.03 μm = 3×10−6 cm, NB = 1016 cm−3.

Find: Np and xj.

Solution.

Np = Q/(√(2π)ΔRp) = 5×1014 / (2.507 × 3×10−6) = 6.6×1019 cm−3
xj = Rp + ΔRp √(2 ln(Np/NB)) = 0.10 + 0.03 × √(2 ln 6650) = 0.10 + 0.03 × 4.20 = 0.226 μm

Answer: Np = 6.6×1019 cm−3, xj = 0.23 μm. (Here the surface concentration is high enough that the n+ region reaches the surface, so there is only the one junction.)

#### Practice 3.6: diffusion coefficient of phosphorus

Question. For phosphorus in silicon D0 = 3.85 cm2/s and Ea = 3.66 eV. Find D at 1100 °C.

Given: D0 = 3.85 cm2/s, Ea = 3.66 eV, T = 1373 K, k = 8.617×10−5 eV/K.

Find: D.

Solution.

kT = 8.617×10−5 × 1373 = 0.1183 eV
Ea/kT = 3.66/0.1183 = 30.93
D = 3.85 × e−30.93 = 3.85 × 3.7×10−14 = 1.4×10−13 cm2/s

Answer: D ≈ 1.4×10−13 cm2/s.

#### Practice 3.7: annealing and tilt

Question. Give two reasons an implanted wafer must be annealed, and explain why implants are usually done with the wafer tilted by about 7°.

Answer. Annealing (1) repairs the lattice damage caused by the ions knocking silicon atoms out of place (heavy implants even make the surface amorphous), and (2) moves the dopant atoms onto substitutional lattice sites where they become electrically active donors or acceptors. Tilting by about 7° stops the beam lining up with the open channels between rows of atoms along low-index directions; ions entering a channel travel much deeper than Rp predicts (channelling), giving an unwanted deep tail.

## Objectives check

Use this table to confirm you have met this week's objectives. Cover the Answer column and answer each check question from memory. If you cannot, go back to the section in the last column before moving on.

| # | Objective | Check yourself | Answer | Where it is taught |
| --- | --- | --- | --- | --- |
| 1 | Explain why doping is needed and name the common dopants of silicon. | Which of P, B, As, Ga make silicon n-type? | P and As (Group V); B and Ga make it p-type. | The big picture |
| 2 | Explain diffusion and state Fick's first law and the temperature dependence of D. | By roughly what factor does D change when the furnace is 100 °C hotter (Ea ≈ 3.5 eV, ~1000 °C)? | About tenfold (Q4: 6.9×10−15 → 7.1×10−14 cm2/s). | Part A; Q4 |
| 3 | Distinguish constant-source (erfc) and limited-source (Gaussian) diffusion and calculate their profiles. | In which type of diffusion does the surface concentration fall with time? | Limited-source (drive-in): the fixed dose spreads deeper, so C(0) = Q/√(πDt) falls. | Two types of diffusion; Examples 3.1–3.2; Q5–Q6 |
| 4 | Describe the step-by-step diffusion process and the atomic diffusion mechanisms. | Which mechanism, vacancy or interstitial, is faster, and which do B and P use? | Interstitial is faster; B and P move mainly by the vacancy mechanism. | Step-by-step process; atomic level |
| 5 | Describe ion implantation, its equipment and the Gaussian implant profile. | What does the mass analyser do? | Bends the ion beam with a magnet so only ions of the chosen mass-to-charge ratio reach the wafer. | Part B |
| 6 | Calculate implant peak concentration, junction depth, dose and beam current. | Q = 1014 cm−2 with ΔRp = 0.04 μm: find Np. | Np = Q/(√(2π)ΔRp) = 1014/(2.507 × 4×10−6) = 1.0×1019 cm−3. | Example 3.3; implantation calculations P1–P4 |
| 7 | Compare diffusion with ion implantation, and explain channelling and annealing. | Why is the wafer tilted about 7° during implantation? | To stop ions travelling deep along open crystal channels (channelling). | Channelling; comparison table |
| 8 | Describe how a doping profile is evaluated. | What does a four-point probe measure, and how is it calculated? | Sheet resistance, Rs = 4.532 V/I (Ω/□). | Part C; Example 3.4 |

Week 4 · Module 2 · Energy Bands & Carrier Statistics

# Energy Bands and Carrier Concentrations

Plan: quantum-mechanics foundations (Schrödinger equation overview, Kronig–Penney model); energy band gaps, allowed and forbidden states; intrinsic and extrinsic carrier concentrations.

## Learning objectives

By the end of this week you should be able to:

- State the basic ideas of quantum mechanics needed for solids.

- State the time-independent Schrödinger equation and explain its terms.

- Explain how discrete atomic levels become energy bands.

- Explain the Kronig–Penney model and how it produces allowed and forbidden bands.

- Explain E–k diagrams, effective mass and holes.

- Distinguish direct and indirect band gaps and calculate emission wavelengths.

- Derive ni and calculate intrinsic and extrinsic carrier concentrations.

## Symbols and abbreviations used this week

Every symbol, constant and abbreviation on this page is listed here, even if an earlier week already defined it, so you can study this page on its own.

Constants and units

| Symbol | Meaning | Units / typical value |
| --- | --- | --- |
| q | Magnitude of the electronic charge | 1.6×10−19 C |
| k | Boltzmann constant | 8.617×10−5 eV/K = 1.381×10−23 J/K |
| kT | Thermal energy | 0.0259 eV (often 0.02585 eV) at 300 K |
| T | Absolute temperature | kelvin (K); room temperature = 300 K |
| h | Planck constant | 6.626×10−34 J·s |
| ħ | Reduced Planck constant, h/2π | 1.055×10−34 J·s |
| m0 | Free-electron mass | 9.11×10−31 kg |
| eV | Electron-volt, a unit of energy | 1 eV = 1.6×10−19 J |
| Å | Ångström, a unit of length | 1 Å = 10−10 m = 0.1 nm |
| μm | Micrometre (micron) | 1 μm = 10−4 cm = 10−6 m |

Symbols

| Symbol | Meaning | Units / typical value |
| --- | --- | --- |
| Ec (EC) | Energy of the bottom of the conduction band | eV |
| Ev (EV) | Energy of the top of the valence band | eV |
| Eg | Band-gap energy, Ec − Ev | eV; Si 1.12, Ge 0.66, GaAs 1.42 at 300 K |
| EF | Fermi level: the energy at which a state has a 50 % chance of being occupied | eV |
| Ei | Intrinsic Fermi level, close to mid-gap | eV |
| En | Allowed energy of level n of a particle in a box | J or eV |
| f(E) | Fermi–Dirac function: probability that a state at energy E is occupied | dimensionless, 0 to 1 |
| g(E), gc, gv | Density of states: allowed states per unit energy per unit volume | states/(eV·cm3) |
| Nc | Effective density of states in the conduction band | cm−3; Si 2.8×1019 at 300 K |
| Nv | Effective density of states in the valence band | cm−3; Si 1.04×1019 at 300 K |
| n | Electron concentration (free electrons per cm3) | cm−3 |
| p | Hole concentration (holes per cm3) | cm−3 |
| ni | Intrinsic carrier concentration (n = p = ni in pure material) | cm−3; Si ≈ 1×1010 at 300 K |
| n0, p0 | Equilibrium electron and hole concentrations | cm−3 |
| ND | Donor concentration | cm−3 |
| NA | Acceptor concentration | cm−3 |
| m∗, mn∗, mp∗ | Effective mass of electrons or holes | kg, or as a multiple of m0 |
| ψ | Wave function (¦ψ¦2 is the probability density) | — |
| V(x) | Potential energy in the Schrödinger equation | J or eV |
| k (wave vector) | Wave vector, 2π/λ; measures the electron's momentum, p = ħk | m−1 or cm−1 |
| α (Kronig–Penney) | √(2mE)/ħ, set by the electron energy | m−1 |
| P (Kronig–Penney) | Barrier strength mV0ba/ħ2 | dimensionless |
| V0 | Height of a potential barrier | J or eV |
| λ | Wavelength | μm or nm; λ(μm) = 1.24/E(eV) |
| ν, hν | Frequency of light, and photon energy | Hz; eV |
| a | Lattice constant: edge length of the cubic unit cell | Å; Si 5.43, Ge and GaAs 5.65 |
| μ, μn, μp | Mobility: drift velocity per unit field (electrons, holes) | cm2/(V·s); Si μn 1350, μp 480 |
| σ | Conductivity, q(nμn + pμp) (in Week 8, σ is also a capture cross-section) | S/cm (siemens per cm) |
| ρ | Resistivity, 1/σ | Ω·cm |
| V, Va | Applied voltage (positive for forward bias) | V |
| α | Common-base current gain, IC/IE | dimensionless; 0.98–0.999 |
| β | Common-emitter current gain, IC/IB (also hFE) | dimensionless; 50–500 |
| ψk(x), uk(x) | Bloch wavefunction of an electron, and its part that repeats with the lattice | — |
| λc | Cut-off wavelength of a detector, 1.24/Eg (μm, Eg in eV) | μm |
| c | Speed of light in vacuum | 3×108 m/s |

Abbreviations

| Abbreviation | Meaning |
| --- | --- |
| Si | Silicon |
| Ge | Germanium |
| GaAs | Gallium arsenide |
| GaN | Gallium nitride |
| SiC | Silicon carbide |
| InP | Indium phosphide |
| GaP | Gallium phosphide |
| SiO2 | Silicon dioxide (silica), the oxide insulator |
| CB | Conduction band |
| VB | Valence band |
| IC | Integrated circuit |
| LED | Light-emitting diode |

## Key terms

Every important word used this week is defined here, so you can read this week on its own.

Electron-volt (eV). The energy an electron gains when it moves through a potential difference of one volt: 1 eV = 1.6×10−19 J. Energies of electrons in solids are almost always quoted in eV.

Wave function (ψ). The mathematical wave that describes an electron in quantum mechanics. It cannot be measured directly, but its square, |ψ|2, gives the probability of finding the electron at each point.

Wave vector (k). A number that says how many wave cycles fit into each unit of length, k = 2π/λ. It measures the electron's momentum, p = ħk.

Energy band. A range of energies that electrons in a crystal are allowed to have. It forms because each sharp energy level of a single atom splits into a huge number of very closely spaced levels when billions of atoms are packed together.

Valence band. The highest energy band that is completely filled with electrons at absolute zero (0 K). Its electrons are the ones that hold the atoms together in chemical bonds. Its top edge is at energy Ev.

Conduction band. The energy band just above the valence band, empty at 0 K. Electrons that reach it are free to move through the crystal and carry current. Its bottom edge is at energy Ec.

Band gap (Eg). The range of energies between the top of the valence band and the bottom of the conduction band, in which a perfect crystal has no allowed electron states (also called the forbidden gap). An electron needs at least this much energy to break free of a bond and become a conduction electron.

Eg = Ec − Ev

Where:

- Eg = band-gap energy (eV); Si 1.12, Ge 0.66, GaAs 1.42 at 300 K

- Ec = energy of the bottom of the conduction band (eV)

- Ev = energy of the top of the valence band (eV)

Why it matters: the band gap decides whether a material is a metal, a semiconductor or an insulator, how many carriers it has at a given temperature, and what colour of light it can emit or absorb.

Hole. An empty electron state (a missing electron) in the valence band. Neighbouring electrons can move into it, so the empty state moves around and behaves like a positively charged particle that carries current.

E–k diagram (band structure). A graph of the allowed electron energies E against the wave vector k. Its shape near the band edges sets how carriers move and whether the material emits light well.

Effective mass (m∗). The mass an electron or hole appears to have when it is pushed by a force inside a crystal. It differs from the free-electron mass because the crystal's atoms also act on the carrier; a smaller m∗ means a lighter, faster carrier.

Phonon. A quantum (packet) of vibration of the crystal lattice. It carries very little energy but can carry a large momentum, so it can supply the momentum change an electron needs in an indirect-gap material.

Direct and indirect band gap. In a direct-gap material (e.g. GaAs) the lowest point of the conduction band sits at the same k as the highest point of the valence band, so an electron can drop across the gap and emit light directly. In an indirect-gap material (e.g. Si) they are at different k, so a phonon must also take part, and light emission is very weak.

Why it matters: LEDs and lasers are made from direct-gap materials; silicon is used for chips but not for light sources.

Fermi level (EF). The energy at which an electron state has exactly a 50 % chance of being occupied. Its position in the gap tells you which carrier dominates: near Ec there are many electrons, near Ev many holes.

Intrinsic semiconductor and intrinsic carrier concentration (ni). A pure, undoped semiconductor, in which every free electron comes from a broken bond that also leaves a hole, so the electron and hole concentrations are equal. Their common value is ni (cm−3), about 1×1010 cm−3 for Si at 300 K. Its Fermi level, the intrinsic level Ei, lies very close to the middle of the gap.

Dopant: donor and acceptor. A donor is an impurity atom (e.g. phosphorus in Si) that gives a free electron to the conduction band; its concentration is ND. An acceptor (e.g. boron in Si) takes an electron from the valence band and so creates a hole; its concentration is NA. Both are in cm−3.

Extrinsic semiconductor (n-type, p-type). A doped semiconductor whose carrier concentrations are set mainly by its dopants rather than by ni. n-type material has more electrons than holes; p-type has more holes than electrons.

Majority and minority carriers. The carrier type present in larger numbers is the majority carrier (electrons in n-type, holes in p-type); the other type is the minority carrier.

Mass-action law. In thermal equilibrium the product of the electron and hole concentrations equals ni2, whatever the doping. Raising one carrier type therefore lowers the other.

n p = ni2

Where:

- n = electron concentration (cm−3)

- p = hole concentration (cm−3)

- ni = intrinsic carrier concentration (cm−3); 1×1010 for Si at 300 K

Why it matters: it lets you find the minority-carrier concentration, which controls diode and transistor currents, from the doping alone.

Compensated semiconductor. A semiconductor containing both donors and acceptors. They partly cancel, so the carriers are set by the difference ND − NA (or NA − ND), called the net doping.

## The big picture

In Week 1 we simply stated that a solid has a valence band, a conduction band and a gap between them. This week explains why. The answer needs one idea from quantum mechanics: an electron behaves like a wave, and a wave trapped in a region can only vibrate in certain ways. In a single atom that gives sharp energy levels. In a crystal, where the electron wave runs through a regular row of atoms, it gives broad bands of allowed energies separated by forbidden gaps.

You do not need to solve hard equations for this course. You need to understand three steps:

- Electrons are waves, described by the Schrödinger equation.

- Trapped waves have only certain allowed energies.

- A periodic crystal turns those allowed energies into bands with gaps (the Kronig–Penney model shows this).

Then Part C uses the bands to count the carriers.

## Part A: Quantum-mechanics foundations

### Why classical physics is not enough

Classical physics treats an electron as a tiny ball. That picture cannot explain why copper conducts and glass does not, or why an atom emits light only at certain colours. Three ideas from early quantum theory fix this:

- Energy comes in packets (quanta). Light of frequency ν comes in photons of energy E = hν. Electrons in atoms can only have certain energies.

- Particles behave as waves. An electron with momentum p behaves as a wave of wavelength λ = h/p (de Broglie). We often write p = ħk, where k = 2π/λ is the wave vector: k is just "how many waves per unit length", and it measures the electron's momentum.

- Uncertainty. We cannot know an electron's position and momentum exactly at the same time. So instead of a definite position we describe it by a wave function ψ, and |ψ|2 tells us where it is likely to be found.

Constants: h = 6.626×10−34 J·s, ħ = h/2π = 1.055×10−34 J·s, electron mass m0 = 9.11×10−31 kg.

### The Schrödinger equation

The time-independent Schrödinger equation (in one dimension) is

−(ħ2/2m) d2ψ/dx2 + V(x) ψ = E ψ

Read it as an energy balance: kinetic energy + potential energy = total energy.

| Term | Meaning |
| --- | --- |
| ψ(x) | the wave function. ψ itself is not measurable, but ¦ψ(x)¦2 dx is the probability of finding the electron between x and x + dx |
| −(ħ2/2m) d2ψ/dx2 | the kinetic energy term. d2ψ/dx2 measures how sharply the wave curves: a more tightly wiggling wave means more kinetic energy |
| V(x) ψ | the potential energy term. V(x) is the potential energy at each point (for example the pull of the atomic nuclei) |
| E | the total energy, a constant. The equation only has sensible solutions for certain values of E: that is how quantisation appears |
| ħ | reduced Planck constant, h/2π = 1.055×10−34 J·s |
| m | mass of the electron, 9.11×10−31 kg (in a crystal, the effective mass m∗) |
| x | position (m) |

The wave function must be finite, single-valued and smooth (continuous, with a continuous slope), and the total probability must be 1.

### Two simple cases that explain everything

A free electron (no forces, V = 0). The solution is a travelling wave, ψ = Aeikx, with energy

E = ħ2k2/2m

Where:

- E = kinetic energy of the free electron (J; divide by 1.6×10−19 for eV)

- ħ = reduced Planck constant, 1.055×10−34 J·s

- k = wave vector of the electron wave (m−1)

- m = electron mass, 9.11×10−31 kg

Any energy is allowed. The graph of E against k is a smooth parabola. This is the starting point for electrons in a solid.

An electron in a box of width L with walls it cannot pass. The wave must be zero at both walls, just as a guitar string is fixed at both ends. So only whole numbers of half-waves fit, and only certain energies are allowed:

En = n2π2ħ2/2mL2, n = 1, 2, 3, …

Where:

- En = energy of the nth allowed level (J)

- n = quantum number: the number of half-waves that fit in the box (1, 2, 3, …)

- ħ = reduced Planck constant, 1.055×10−34 J·s

- m = electron mass, 9.11×10−31 kg

- L = width of the box (m)

In plain words. A guitar string can only play certain notes, because only certain wavelengths fit between its fixed ends. An electron trapped in a region is the same: only certain wavelengths fit, so only certain energies are allowed. That is what "quantised energy levels" means.

### From atoms to bands

One isolated silicon atom has sharp energy levels (1s, 2s, 2p, 3s, 3p). Now bring two atoms close together. Their outer wave functions overlap, and each level splits into two slightly different levels. (Two identical pendulums joined by a spring do the same: instead of one frequency they now have two, swinging together and swinging opposite.)

Bring N atoms together and each level splits into N levels. A crystal has about 5×1022 atoms per cm3, so each level splits into so many closely spaced levels that they form a practically continuous band. Between bands are ranges of energy where there are no levels at all: the forbidden gaps.

In silicon, the outer 3s and 3p levels (4 electrons per atom) mix and split into two bands:

- a lower band with room for 4 electrons per atom: the valence band. Silicon has exactly 4 outer electrons per atom, so this band is completely full at 0 K;

- an upper band, also with room for 4 per atom: the conduction band, empty at 0 K;

- separated by the band gap Eg = 1.12 eV.

### Bloch's theorem

In a perfect crystal the potential energy repeats with the spacing of the atoms a: V(x + a) = V(x). Bloch showed that the electron wave in such a crystal is

ψk(x) = uk(x) eikx, with uk(x + a) = uk(x)

Where:

- ψk(x) = wave function of an electron with wave vector k (the Bloch wave)

- uk(x) = a function that repeats exactly from one atom to the next

- eikx = a plane (travelling) wave with wave vector k (m−1)

- a = spacing of the atoms, the period of the crystal potential (m or Å)

A travelling wave (eikx) multiplied by a pattern that repeats from atom to atom (uk). The important consequence: an electron in a perfect crystal travels without being scattered by the atoms. The atoms are not obstacles; they just shape the wave. Only imperfections (vibrations, impurities, defects) scatter electrons. This is why carriers in a crystal can move so freely (Week 7).

### The Kronig–Penney model: how a periodic crystal makes bands and gaps

The real potential inside a crystal is complicated. Kronig and Penney (1931) replaced it with the simplest repeating potential that can be solved exactly: a row of rectangular wells and barriers.

- Each well (width a, V = 0) represents the region near an atom, where the electron is attracted.

- Each barrier (height V0, width b) represents the region between atoms.

- The pattern repeats forever with period a + b.

What they did:

- Solved the Schrödinger equation inside a well (where the solution oscillates) and inside a barrier (where it decays).

- Joined the pieces smoothly at every edge (ψ and dψ/dx continuous).

- Applied Bloch's theorem (the solution must repeat, up to a phase factor, from one period to the next).

- Simplified by making the barriers very thin and very high.

The result is one condition that the energy must satisfy:

P · sin(αa)/(αa) + cos(αa) = cos(ka)

α = √(2mE)/ħ, P = m V0 b a / ħ2

| Symbol | Meaning |
| --- | --- |
| α | depends on the electron energy E: larger E, larger α |
| a | well width (the atomic spacing) |
| k | the electron's wave vector (momentum) |
| P | barrier strength: how strongly the electron is held by each atom (dimensionless) |
| E | electron energy (J) |
| m | electron mass (kg) |
| V0 | barrier height (J) |
| b | barrier width (m) |
| ħ | reduced Planck constant, 1.055×10−34 J·s |

How to read it: the key step. The right-hand side, cos(ka), is a cosine. A cosine can only be between −1 and +1. The left-hand side depends on the energy through α. So:

- for energies where the left-hand side is between −1 and +1, there is a k that satisfies the equation: these energies are allowed;

- for energies where the left-hand side is greater than +1 or less than −1, no real k works: these energies are forbidden.

Plot the left-hand side against αa (i.e. against energy). It wiggles like a fading cosine, starting above +1 and repeatedly overshooting the ±1 lines. Every time it is inside the ±1 strip you have a band; every time it pokes outside you have a gap.

The Kronig–Penney condition plotted against αa for P = 3π/2. Shaded strips are the energies where the curve stays between −1 and +1: the allowed bands. Where the curve goes outside ±1 there are no solutions: the forbidden gaps.

What the model teaches:

- The energy spectrum is a series of allowed bands separated by forbidden gaps.

- The band edges occur at ka = nπ, i.e. k = ±nπ/a, the Brillouin-zone boundaries. Physically, at these wavelengths the electron wave reflects off the rows of atoms (Bragg reflection), forming standing waves, which split the energies and open a gap.

- Bands get wider at higher energy (the curve's wiggles fade, so it spends longer inside ±1).

- If the atoms hold their electrons very tightly (P → ∞), the bands shrink to the sharp levels of single atoms.

- If the barriers vanish (P → 0), the gaps close and the electron is free: E = ħ2k2/2m.

In plain words. A wave running through a regular row of obstacles is fine at most wavelengths, but at certain wavelengths the reflections from every row add up and the wave cannot travel. Those wavelengths correspond to the forbidden energies: the band gaps.

## Part B: Band gaps, allowed and forbidden states

### E–k diagrams and effective mass

The band structure of a material is a graph of the allowed energies E against the wave vector k. Near the bottom of the conduction band (and the top of the valence band) the curve looks like a parabola, just like a free electron's E = ħ2k2/2m, but with a different curvature. We describe that curvature by an effective mass m∗:

1/m∗ = (1/ħ2) d2E/dk2

Where:

- m∗ = effective mass of the carrier (kg, or quoted as a multiple of m0 = 9.11×10−31 kg)

- ħ = reduced Planck constant, 1.055×10−34 J·s

- d2E/dk2 = curvature of the E–k curve at the band edge (J·m2)

The electron then responds to forces as if it were a free particle of mass m∗. The effect of all the crystal's atoms is packed into this one number.

- A sharply curved band means small m∗: a light, fast, high-mobility carrier (GaAs electrons, m∗ = 0.067m0).

- A flatter band means large m∗: a heavy, slow carrier (Si holes, about 0.56m0).

Near the top of the valence band the curve bends downward. An electron there would have negative mass. It is simpler to describe the missing electron instead: it behaves as a positive particle with positive mass, the hole.

### Valence band, conduction band and forbidden gap

- Valence band: the highest band that is completely full at 0 K. Its top is Ev. Its electrons are the bonding electrons. A full band cannot carry current (for every electron moving one way there is one moving the other), but a band with a few holes can.

- Conduction band: the next band up, empty at 0 K. Its bottom is Ec. Electrons here move freely and carry current.

- Forbidden gap: Eg = Ec − Ev. In a perfect crystal there are no states here at all. Impurities and defects can add a few states inside it (donor, acceptor and trap levels).

The gap shrinks slightly with temperature: for Si, 1.17 eV at 0 K and 1.12 eV at 300 K.

### Metals, semiconductors and insulators

The band picture explains at once why materials conduct so differently. What matters is whether the highest occupied band is full, and how big the gap above it is.

|  | Metal | Semiconductor | Insulator |
| --- | --- | --- | --- |
| Band picture | Highest band only partly full, or bands overlap: no gap | Full valence band, small gap, empty conduction band | Full valence band, wide gap, empty conduction band |
| Band gap Eg | None | About 0.1–3 eV (Ge 0.66, Si 1.12, GaAs 1.42 eV) | Above about 4 eV (diamond 5.5, SiO2 ≈ 9 eV) |
| Free carriers at 300 K | About 1022 cm−3, fixed | ni = 106–1013 cm−3 when pure; set by doping when doped | Practically none |
| Resistivity at 300 K | About 10−6 Ω·cm (Cu 1.7×10−6) | About 10−3 to 106 Ω·cm (pure Si ≈ 3×105) | Above about 1012 Ω·cm (SiO2 ≈ 1014–1016) |
| Effect of heating | Resistance rises (more lattice vibration scatters the electrons) | Resistance falls steeply (more electrons cross the gap) | Stays extremely high |
| Effect of doping | Little | Huge: conductivity can be set over many orders of magnitude | Little (cannot be usefully doped) |
| Uses | Wires, contacts, interconnects | Diodes, transistors, ICs, LEDs, solar cells | Gate oxides, insulation between layers, capacitor dielectrics |

### Direct and indirect band gaps

In a direct-gap material (GaAs) the bottom of the conduction band sits directly above the top of the valence band in k. In an indirect-gap material (Si) they are at different k, so an electron dropping across the gap must also change its momentum.

When an electron falls from the conduction band to the valence band it must lose energy and keep momentum balanced. A photon carries plenty of energy but almost no momentum. So on an E–k diagram, a photon can only make vertical jumps.

- Direct gap (GaAs, InP, GaN): the conduction-band minimum is directly above the valence-band maximum. The electron can drop straight down and give out a photon. Light emission is fast and efficient: LEDs and lasers.

- Indirect gap (Si, Ge): the minimum is at a different k. To drop across, the electron must also get rid of momentum, which needs a phonon (a lattice vibration) at the same instant. That is unlikely, so the electron usually loses its energy as heat instead. Silicon is a poor light emitter.

The wavelength of light from a band-to-band transition is

λ (μm) = 1.24 / Eg (eV)

Where:

- λ = wavelength of the emitted (or just-absorbed) light (μm)

- Eg = band-gap energy (eV)

- 1.24 = hc expressed in eV·μm (h = 6.626×10−34 J·s, c = 3×108 m/s, 1 eV = 1.6×10−19 J)

GaAs: 1.24/1.42 = 0.87 μm (near infrared). Si: 1.24/1.12 = 1.11 μm, which is also the longest wavelength a silicon photodetector can absorb.

The same formula works the other way round for absorption. A photon can only lift an electron across the gap if its energy hν is at least Eg. Longer wavelengths carry less energy, so light with λ greater than 1.24/Eg passes straight through. This longest absorbed wavelength is the cut-off wavelength λc.

#### Example 4.1: cut-off wavelength of silicon and germanium photodetectors

Question. Optical-fibre links use light of wavelength 1.55 μm. Find the cut-off wavelengths of silicon (Eg = 1.12 eV) and germanium (Eg = 0.66 eV) photodetectors, and decide which of them can detect 1.55 μm light.

Given: Eg(Si) = 1.12 eV, Eg(Ge) = 0.66 eV, λ = 1.55 μm.

Find: λc for Si and Ge; the photon energy at 1.55 μm.

Formula:

λc (μm) = 1.24 / Eg (eV), photon energy E (eV) = 1.24 / λ (μm)

Solution.

Si: λc = 1.24/1.12 = 1.11 μm
Ge: λc = 1.24/0.66 = 1.88 μm
Photon energy at 1.55 μm: E = 1.24/1.55 = 0.80 eV

Compare: 0.80 eV is less than 1.12 eV (Si) but more than 0.66 eV (Ge).

Answer: λc = 1.11 μm for Si and 1.88 μm for Ge. Only germanium can detect 1.55 μm light.

What this means: a 1.55 μm photon does not have enough energy to break a bond in silicon, so silicon is transparent to it and gives no signal. That is why fibre-optic receivers use Ge or InGaAs, while cheap silicon photodiodes are used for visible and near-infrared light below 1.1 μm.

## Part C: Intrinsic and extrinsic carrier concentrations

Now that we have bands, we can count carriers. The full method (Fermi–Dirac statistics, density of states) is Week 5. Here are the results you need this week.

### The two key equations

The number of electrons in the conduction band and holes in the valence band depend on how far the Fermi level EF is from each band edge:

n = Nc e−(Ec − EF)/kT, p = Nv e−(EF − Ev)/kT

Where:

- n, p = electron and hole concentrations (cm−3)

- Nc, Nv = effective densities of states in the conduction and valence bands (cm−3)

- Ec, Ev = conduction-band bottom and valence-band top (eV)

- EF = Fermi level (eV)

- kT = thermal energy, 0.0259 eV at 300 K

Nc and Nv are the effective densities of states (Si at 300 K: 2.8×1019 and 1.04×1019 cm−3). The closer EF is to Ec, the more electrons; the closer to Ev, the more holes.

### Intrinsic semiconductor

In pure silicon every free electron came from a broken bond, which also left a hole, so n = p = ni. Multiply the two equations above; EF cancels:

n p = Nc Nv e−(Ec − Ev)/kT = Nc Nv e−Eg/kT

With n = p = ni:

ni = √(Nc Nv) e−Eg/2kT

Where:

- ni = intrinsic carrier concentration (cm−3)

- Nc, Nv = effective densities of states (cm−3); Si 2.8×1019 and 1.04×1019 at 300 K

- Eg = band gap (eV); 1.12 eV for Si

- kT = thermal energy, 0.0259 eV at 300 K

For Si at 300 K, ni ≈ 1×1010 cm−3. The Fermi level of an intrinsic semiconductor, Ei, is almost exactly at mid-gap.

What controls ni: the band gap (exponentially: wider gap, far fewer carriers) and temperature (exponentially: hotter, far more carriers). Ge (0.66 eV) has ni = 2.4×1013; GaAs (1.42 eV) has only about 2×106 cm−3.

### The mass-action law

Because EF cancelled, the product is the same whether or not the material is doped:

n p = ni2

Where:

- n, p = equilibrium electron and hole concentrations (cm−3)

- ni = intrinsic carrier concentration (cm−3); 1×1010 for Si at 300 K

### Extrinsic (doped) semiconductor

With full ionisation and doping well above ni:

- n-type: n ≈ ND, p = ni2/ND.

- p-type: p ≈ NA, n = ni2/NA.

- Both present (compensation): use the net doping. The exact result from charge neutrality is

n = (ND − NA)/2 + √( ((ND − NA)/2)2 + ni2 )

Where:

- n = electron concentration (cm−3)

- ND, NA = donor and acceptor concentrations (cm−3)

- ni = intrinsic carrier concentration (cm−3)

When NA > ND the material is p-type and the same formula is used for holes, with ND and NA swapped: p = (NA − ND)/2 + √( ((NA − ND)/2)2 + ni2 ). In both cases the minority carrier then follows from np = ni2.

#### Example 4.2: how doping shifts both carrier concentrations

Question. Silicon at 300 K (ni = 1×1010 cm−3) is doped with ND = 1×1016 cm−3. Calculate n and p, and compare each with its intrinsic value.

Given: ND = 1×1016 cm−3, ni = 1×1010 cm−3.

Find: n, p, and the factors n/ni and ni/p.

Formula:

n ≈ ND, p = ni2/n

Solution.

n ≈ ND = 1×1016 cm−3

p = ni2/n = 1020/1016 = 1×104 cm−3

n/ni = 1016/1010 = 106, ni/p = 1010/104 = 106

Answer: n = 1016 cm−3, p = 104 cm−3.

What this means: doping with only about one phosphorus atom per five million silicon atoms raised the electrons a million times above ni and lowered the holes by the same factor, so np = ni2 still holds. The electrons are now the majority carriers and the holes a tiny minority.

#### Example 4.3: carrier concentrations in compensated silicon

Question. A silicon wafer at 300 K contains NA = 5×1016 cm−3 boron atoms and ND = 2×1016 cm−3 phosphorus atoms. Find the majority and minority carrier concentrations and the resistivity (take μp = 480 cm2/V·s).

Given: NA = 5×1016 cm−3, ND = 2×1016 cm−3, ni = 1×1010 cm−3, μp = 480 cm2/V·s, q = 1.6×10−19 C.

Find: p, n and ρ.

Formula:

p = (NA − ND)/2 + √( ((NA − ND)/2)2 + ni2 ), n = ni2/p, ρ ≈ 1/(q p μp)

Solution.

Step 1. NA > ND, so the material is p-type. The net doping is

NA − ND = 5×1016 − 2×1016 = 3×1016 cm−3

Step 2. Because (NA − ND)/2 = 1.5×1016 is vastly larger than ni = 1010, the square root is simply 1.5×1016, so

p = 1.5×1016 + 1.5×1016 = 3×1016 cm−3

Step 3. Minority electrons:

n = ni2/p = 1020 / 3×1016 = 3.3×103 cm−3

Step 4. Resistivity (the electrons are far too few to matter):

σ = q p μp = 1.6×10−19 × 3×1016 × 480 = 2.30 S/cm, ρ = 1/σ = 0.43 Ω·cm

Answer: p = 3×1016 cm−3, n ≈ 3.3×103 cm−3, ρ ≈ 0.43 Ω·cm.

What this means: the 2×1016 donors cancel 2×1016 of the acceptors, so the wafer behaves exactly like p-type silicon doped with 3×1016 cm−3 boron. (In practice the extra ionised impurities scatter carriers and lower the mobility a little, so the real resistivity is slightly higher.)

#### Example 4.4: where is the Fermi level in doped silicon?

Question. Silicon at 300 K is doped with ND = 1×1016 cm−3 donors. Find how far the Fermi level lies below the conduction-band edge and how far it lies above the intrinsic level Ei.

Given: ND = 1×1016 cm−3 (so n ≈ 1×1016 cm−3), Nc = 2.8×1019 cm−3, ni = 1×1010 cm−3, kT = 0.0259 eV.

Find: Ec − EF and EF − Ei.

Formula: Rearranging n = Nc e−(Ec − EF)/kT, and its intrinsic form n = ni e(EF − Ei)/kT:

Ec − EF = kT ln(Nc/n), EF − Ei = kT ln(n/ni)

Solution.

Ec − EF = 0.0259 × ln(2.8×1019 / 1×1016) = 0.0259 × ln(2800) = 0.0259 × 7.94 = 0.206 eV
EF − Ei = 0.0259 × ln(1×1016 / 1×1010) = 0.0259 × ln(106) = 0.0259 × 13.8 = 0.358 eV

Check: 0.206 + 0.358 = 0.56 eV, which is half of the 1.12 eV gap, as it should be since Ei is close to mid-gap.

Answer: EF is 0.21 eV below Ec and 0.36 eV above Ei.

What this means: moderate n-type doping lifts the Fermi level about two-thirds of the way from mid-gap towards the conduction band. Every tenfold increase in ND raises EF by a further kT ln 10 = 0.060 eV, so EF is a sensitive "meter" of the doping.

Temperature regions (n-type): at very low temperature the donors are not all ionised (freeze-out, n < ND); over the normal range n ≈ ND (extrinsic); at high temperature ni overtakes ND and the material behaves as intrinsic (intrinsic region). Week 5 works through these in detail.

## Key points of Week 4

- Electrons are waves; the Schrödinger equation is kinetic + potential = total energy, and only certain energies give acceptable waves.

- Bringing N atoms together splits each level into N levels, forming bands; between them are forbidden gaps.

- Kronig–Penney: P sin(αa)/(αa) + cos(αa) = cos(ka). Energies where the left side is between ±1 are allowed (bands); elsewhere forbidden (gaps).

- Effective mass m∗ describes the band curvature. A missing electron near the top of the valence band acts as a positive hole.

- Direct gap: photon emission is efficient (GaAs). Indirect gap: a phonon is needed, so emission is poor (Si). λ = 1.24/Eg μm.

- ni = √(NcNv)e−Eg/2kT; np = ni2; n ≈ ND in n-type, p ≈ NA in p-type.

## Examination questions solved (Q22–Q29, Q34)

### Q22. Explain the basic assumptions of the quantum mechanical model of electrons in a semiconductor.

- Wave nature of electrons. Each electron is described by a wave function ψ obeying the Schrödinger equation; |ψ|2 gives the probability of finding it at a point. Energy and momentum (p = ħk) are related through the band structure E(k).

- Adiabatic (Born–Oppenheimer) approximation. The nuclei are much heavier than electrons and are treated as fixed at their lattice sites. Their vibrations (phonons) are added later as a perturbation that causes scattering.

- Perfect periodic crystal. The ion cores form an infinite, perfectly periodic lattice, so the potential energy is periodic, V(r + R) = V(r) for every lattice vector R. Surfaces, impurities and defects are treated separately.

- One-electron (independent-electron) approximation. Each electron moves independently in an average periodic potential produced by the ion cores and all the other electrons (mean-field or Hartree approximation), so a many-body problem becomes a single-particle one.

- Bloch's theorem follows: wave functions are modulated plane waves ψ = uk(r)eik·r.

- Pauli exclusion principle. Each quantum state (k and spin) holds at most one electron, so the states fill from the bottom up. This, with the Fermi–Dirac distribution, gives the occupation of the bands.

- Effective-mass approximation. Near the band edges, electrons and holes respond to external forces as free particles with an effective mass m∗ that contains the effect of the crystal potential.

- Thermal equilibrium statistics. In equilibrium, electrons are distributed among the available states according to the Fermi–Dirac function.

### Q23. State the time-independent Schrödinger equation and explain the physical meaning of its terms.

In one dimension:

−(ħ2/2m) d2ψ(x)/dx2 + V(x) ψ(x) = E ψ(x)

In three dimensions: −(ħ2/2m)∇2ψ(r) + V(r)ψ(r) = Eψ(r), compactly Ĥψ = Eψ.

Meaning of each term:

- ψ(x), the wave function: the amplitude of the electron's probability wave. It has no direct physical meaning, but |ψ(x)|2 dx is the probability of finding the electron between x and x + dx. ψ must be finite, single-valued, continuous and normalised.

- ħ = h/2π, the reduced Planck constant (1.055×10−34 J·s); m, the electron mass (or the effective mass m∗ in a crystal).

- −(ħ2/2m) d2ψ/dx2: the kinetic-energy term. It comes from p2/2m with the momentum operator p = −iħ d/dx. The more sharply ψ curves, the higher the kinetic energy.

- V(x)ψ: the potential-energy term. V(x) is the potential energy of the electron at x, e.g. the periodic potential of the crystal ions, a barrier, or a well.

- E: the total energy of the electron, a constant (the equation is valid for stationary states whose energy does not change with time). Acceptable solutions exist only for particular values of E (eigenvalues), which is how quantisation arises.

- The left-hand side as a whole is the Hamiltonian operator Ĥ acting on ψ.

The full time-dependent wave function is Ψ(x, t) = ψ(x)e−iEt/ħ; the time-independent equation is obtained when V does not depend on time.

### Q24. Explain the basic principle of the Kronig-Penney model and how it leads to the formation of energy bands.

Principle. The real periodic potential of a crystal is complicated. Kronig and Penney (1931) replaced it with the simplest periodic potential that can be solved exactly: a one-dimensional infinite array of rectangular potential wells and barriers. Each well (V = 0, width a) represents the region near an ion; each barrier (height V0, width b) represents the region between ions. The period is a + b.

Method.

- Solve Schrödinger's equation separately in a well (oscillating solutions, α2 = 2mE/ħ2) and in a barrier (exponential solutions, β2 = 2m(V0 − E)/ħ2).

- Apply continuity of ψ and dψ/dx at each boundary.

- Apply Bloch's theorem, ψ(x + (a + b)) = eik(a+b)ψ(x), because the potential is periodic.

- A non-trivial solution exists only if a determinant vanishes. Taking the limit of narrow, high barriers (b → 0, V0 → ∞, with V0b finite) gives:

P · sin(αa)/(αa) + cos(αa) = cos(ka), P = mV0ba/ħ2

How bands form. The right-hand side, cos(ka), must lie between −1 and +1 for real k. Plot the left-hand side f(αa) against αa (i.e. against energy). It starts at 1 + P, oscillates like a damped cosine, and repeatedly rises above +1 and falls below −1. Only the energy ranges where −1 ≤ f(αa) ≤ +1 are solutions: these are the allowed energy bands. The ranges where |f| > 1 have no real k and therefore no electron states: these are the forbidden energy gaps.

Results:

- The spectrum consists of alternating allowed bands and forbidden gaps.

- Discontinuities in E(k) occur at k = nπ/a (Brillouin-zone boundaries), where Bragg reflection of the electron wave occurs.

- The width of allowed bands increases with energy (because the 1/αa factor damps the oscillation).

- As P → ∞ (electrons tightly bound), bands shrink to discrete atomic levels. As P → 0 (free electrons), the gaps vanish and E = ħ2k2/2m.

The model explains in a simple way why solids have bands and gaps, which is the basis of the classification into metals, semiconductors and insulators.

### Q25. Distinguish between valence band, conduction band, and forbidden energy gap.

|  | Valence band | Conduction band | Forbidden energy gap |
| --- | --- | --- | --- |
| What it is | The highest band that is completely filled with electrons at 0 K | The lowest band above the valence band, empty at 0 K | The energy range between Ev and Ec in which no electron states exist (in a perfect crystal) |
| Edge | Top at Ev | Bottom at Ec | Width Eg = Ec − Ev |
| Electrons | Bound in covalent bonds; cannot conduct while the band is full | Free; move through the crystal and conduct | None (only impurity or defect levels) |
| Carriers | Holes (empty states) conduct here | Electrons conduct here | — |
| Origin | Bonding combinations of the atomic sp3 orbitals | Antibonding combinations | Splitting of bonding and antibonding states |
| Values | — | — | Si 1.12 eV, Ge 0.66 eV, GaAs 1.42 eV, SiO2 ≈ 9 eV |

An electron needs at least Eg to jump from the valence to the conduction band; it then leaves a hole behind. The width of the gap decides whether a material is a metal (no gap), a semiconductor (small gap) or an insulator (large gap).

### Q26. Explain the difference between a direct band-gap and an indirect band-gap semiconductor.

On the E–k diagram, look at where the conduction-band minimum and the valence-band maximum occur.

|  | Direct band gap | Indirect band gap |
| --- | --- | --- |
| Band-edge positions | CB minimum and VB maximum at the same k (usually k = 0, the Γ point) | CB minimum at a different k from the VB maximum |
| Transition across the gap | Vertical: an electron can drop and emit a photon directly, conserving momentum | Needs a change of momentum, which a photon cannot supply; a phonon must take part |
| Process | Two-particle (electron + photon) | Three-particle (electron + photon + phonon), much less probable |
| Radiative recombination | Fast, efficient; lifetime ≈ ns | Slow, inefficient; recombination is mostly non-radiative via traps; lifetime μs–ms |
| Absorption near Eg | Sharp, strong (α ≈ 104 cm−1 just above Eg) | Weak, gradual; thicker material needed to absorb light |
| Examples | GaAs (1.42 eV), InP, GaN, InGaAs, CdTe | Si (1.12 eV), Ge (0.66 eV), GaP, AlAs, SiC |
| Applications | LEDs, laser diodes, efficient thin-film solar cells, fast photodetectors | ICs, transistors, power devices, Si solar cells and photodiodes (absorb but do not emit well) |

The emitted wavelength is λ = hc/Eg, i.e. λ(μm) = 1.24/Eg(eV). GaAs emits at 0.87 μm. Silicon's indirect gap is why there is no practical silicon laser.

### Q27. What is meant by an intrinsic semiconductor? Derive the expression for intrinsic carrier concentration.

Intrinsic semiconductor. A pure semiconductor crystal with no significant impurities or defects, in which free carriers are produced only by thermal excitation of electrons from the valence band to the conduction band. Each excited electron leaves a hole, so

n = p = ni

and the Fermi level lies at the intrinsic level Ei, very near the middle of the gap.

Derivation.

Step 1: electrons. The electron concentration is the density of states times the occupation probability, integrated over the conduction band:

n = ∫Ec∞ gc(E) f(E) dE, gc(E) = (4π(2mn∗)3/2/h3) √(E − Ec)

Step 2: Boltzmann approximation. For Ec − EF ≫ kT, f(E) ≈ exp(−(E − EF)/kT). Then

n = (4π(2mn∗)3/2/h3) exp(−(Ec − EF)/kT) ∫0∞ √x · e−x/kT dx, x = E − Ec

Step 3: the integral. ∫0∞ x1/2 e−x/kT dx = (kT)3/2 Γ(3/2) = (kT)3/2 (√π/2). Hence

n = Nc exp( −(Ec − EF)/kT ), Nc = 2(2πmn∗kT/h2)3/2

Step 4: holes. Similarly, with 1 − f(E) ≈ exp(−(EF − E)/kT) in the valence band,

p = Nv exp( −(EF − Ev)/kT ), Nv = 2(2πmp∗kT/h2)3/2

Step 5: the intrinsic condition. Multiply n and p. EF cancels:

n p = Nc Nv exp( −(Ec − Ev)/kT ) = Nc Nv exp( −Eg/kT )

In an intrinsic semiconductor n = p = ni, so n·p = ni2, and

ni = √(Nc Nv) · exp( −Eg / 2kT )

Substituting Nc and Nv gives the explicit temperature dependence:

ni = 2 (2πkT/h2)3/2 (mn∗ mp∗)3/4 exp( −Eg / 2kT ) ∝ T3/2 e−Eg/2kT

Step 6: the intrinsic Fermi level. Setting n = p and solving:

Ei = (Ec + Ev)/2 + (kT/2) ln(Nv/Nc) = (Ec + Ev)/2 + (3kT/4) ln(mp∗/mn∗)

Numerical check for Si at 300 K: √(2.8×1019 × 1.04×1019) = 1.71×1019; exp(−1.12/(2 × 0.0259)) = exp(−21.6) = 4.1×10−10; ni ≈ 7×109 cm−3, the same order as the accepted 1×1010 cm−3 (the difference comes from the exact values of Eg and the effective masses).

### Q28. Explain the difference between intrinsic and extrinsic carrier concentrations.

|  | Intrinsic carrier concentration | Extrinsic carrier concentration |
| --- | --- | --- |
| Material | Pure (undoped) semiconductor | Doped semiconductor |
| Source of carriers | Thermal breaking of covalent bonds only (band-to-band excitation) | Mainly ionised dopants (donors or acceptors), plus a small thermal contribution |
| Electron vs hole | n = p = ni | Unequal: n ≫ p (n-type) or p ≫ n (p-type); majority and minority carriers |
| Formula | ni = √(NcNv) exp(−Eg/2kT) | n ≈ ND, p = ni2/ND (n-type); p ≈ NA, n = ni2/NA (p-type) |
| Typical value (Si, 300 K) | 1×1010 cm−3 | 1014–1020 cm−3 majority |
| Temperature dependence | Very strong, exponential | Nearly constant over the extrinsic range; becomes intrinsic at high T |
| Controlled by | Material (Eg) and temperature | Doping level, chosen by the designer |
| Fermi level | At Ei, near mid-gap | Shifted toward Ec (n-type) or Ev (p-type) |
| Conductivity | Low (σ ≈ 3×10−6 S/cm for Si) | Much higher, set by doping |

The two are linked by the mass-action law np = ni2: doping increases one carrier type and decreases the other so that their product equals the intrinsic value squared.

### Q29. Silicon has an intrinsic carrier concentration of approximately 1.0 × 1010 cm−3 at a specified temperature. If the electron and hole concentrations are equal, determine the electron and hole concentrations.

Given: ni = 1.0×1010 cm−3, n = p.

Find: n and p.

Formula: the mass-action law, n p = ni2.

Solution. If n = p, the semiconductor is intrinsic (undoped, or exactly compensated). From the mass-action law:

n · p = ni2 and n = p ⇒ n2 = ni2 ⇒ n = ni

Check: n·p = (1.0×1010)2 = 1.0×1020 cm−6 = ni2. ✓

Answer: n = p = ni = 1.0×1010 cm−3

What this means: only about one silicon atom in 5×1012 has given up an electron, so pure silicon is a very poor conductor. Using μn = 1350 and μp = 480 cm2/V·s, the intrinsic conductivity would be σ = qni(μn + μp) = 1.6×10−19 × 1010 × 1830 = 2.9×10−6 S/cm, i.e. ρ ≈ 3.4×105 Ω·cm.

### Q34. An n-type semiconductor has a donor concentration of 5 × 1016 cm−3. Assuming complete ionization, determine the approximate majority-carrier concentration.

Given: ND = 5×1016 cm−3, complete ionisation; for the extra results, silicon at 300 K with ni = 1×1010 cm−3.

Find: the majority-carrier concentration n0 (and, as extras, p0, EF and σ).

Formula: n0 ≈ ND (for ND ≫ ni); p0 = ni2/n0; EF − Ei = kT ln(n0/ni); σ ≈ qn0μn.

Solution. With complete ionisation and ND ≫ ni (5×1016 ≫ 1010), every donor contributes one electron:

n0 ≈ ND = 5 × 1016 cm−3

Answer: Majority-carrier (electron) concentration ≈ 5×1016 cm−3.

Additional results (assuming silicon at 300 K, ni = 1×1010 cm−3):

Minority holes: p0 = ni2/n0 = (1010)2 / (5×1016) = 2×103 cm−3

Fermi level: EF − Ei = kT ln(n0/ni) = 0.0259 × ln(5×106) = 0.0259 × 15.42 = 0.40 eV above Ei

Conductivity: σ ≈ q n0 μn = 1.6×10−19 × 5×1016 × 1350 ≈ 10.8 S/cm (ρ ≈ 0.093 Ω·cm)

What this means: the thermal contribution ni is negligible, which is why the majority-carrier density is simply the donor density, and the material conducts millions of times better than pure silicon. (Mobility falls at this doping to about 1000 cm2/V·s, so the real σ is nearer 8 S/cm.)

## Practice questions

These extra questions practise this week's ideas. Work each one on paper before reading the solution; the calculation questions follow the same Question, Given, Find, Solution, Answer layout as the worked examples.

#### Practice 4.1: energy levels in a quantum well

Question. An electron is confined in a 1 nm wide well with infinitely high walls. Calculate the energies of the first two levels in eV.

Given: L = 1×10−9 m, m = 9.11×10−31 kg, h = 6.626×10−34 J·s.

Find: E1 and E2.

Solution. En = n2h2/(8mL2) (the same as n2π2ħ2/2mL2).

E1 = (6.626×10−34)2 / (8 × 9.11×10−31 × 10−18) = 6.02×10−20 J = 0.376 eV
E2 = 4E1 = 1.50 eV

Answer: E1 = 0.38 eV, E2 = 1.50 eV. Confinement on the nanometre scale gives level spacings comparable to band gaps, the basis of quantum-well lasers.

#### Practice 4.2: wavelength of a thermal electron

Question. An electron in a semiconductor at 300 K has a kinetic energy of about (3/2)kT = 0.0388 eV. Find its de Broglie wavelength and compare it with the silicon lattice constant.

Given: E = 0.0388 eV = 6.21×10−21 J, m = 9.11×10−31 kg.

Find: λ = h/p.

Solution.

p = √(2mE) = √(2 × 9.11×10−31 × 6.21×10−21) = 1.06×10−25 kg·m/s
λ = h/p = 6.626×10−34 / 1.06×10−25 = 6.2×10−9 m = 6.2 nm

Answer: λ ≈ 6 nm, about 11 times the lattice constant (0.543 nm). The electron is a wave spread over many atoms, which is why a wave description is needed.

#### Practice 4.3: emission wavelengths

Question. Find the band-to-band emission wavelength of GaN (3.4 eV), GaP (2.26 eV) and InP (1.35 eV), and say where each lies in the spectrum.

Given: Eg values above; λ(μm) = 1.24/Eg(eV).

Find: λ for each.

Solution.

GaN: 1.24/3.4 = 0.365 μm
GaP: 1.24/2.26 = 0.549 μm
InP: 1.24/1.35 = 0.919 μm

Answer: GaN 365 nm (near ultraviolet), GaP 549 nm (green), InP 919 nm (near infrared). (GaP is indirect, so its LEDs need special doping; GaN and InP are direct.)

#### Practice 4.4: intrinsic concentration of GaAs

Question. For GaAs at 300 K, Nc = 4.7×1017 cm−3, Nv = 7.0×1018 cm−3 and Eg = 1.42 eV. Calculate ni.

Given: Nc, Nv, Eg above; 2kT = 0.0518 eV.

Find: ni.

Solution.

√(NcNv) = √(4.7×1017 × 7.0×1018) = 1.81×1018 cm−3
e−Eg/2kT = e−1.42/0.0518 = e−27.4 = 1.25×10−12
ni = 1.81×1018 × 1.25×10−12 = 2.3×106 cm−3

Answer: ni ≈ 2×106 cm−3, about 4000 times smaller than in silicon, which is why GaAs can be made semi-insulating.

#### Practice 4.5: how fast ni rises with temperature

Question. Ignoring the small change of band gap with temperature, by what factor does ni of silicon (Eg = 1.12 eV) increase between 300 K and 350 K?

Given: ni ∝ T3/2 e−Eg/2kT, Eg = 1.12 eV, k = 8.617×10−5 eV/K.

Find: ni(350)/ni(300).

Solution.

(350/300)3/2 = 1.26
exp[ (Eg/2k)(1/300 − 1/350) ] = exp[ 6499 × 4.76×10−4 ] = e3.09 = 22.1
ratio = 1.26 × 22.1 = 27.8

Answer: about 28 times. A 50 K rise gives a 28-fold increase, almost all from the exponential.

#### Practice 4.6: compensated silicon

Question. Silicon contains ND = 1×1016 cm−3 and NA = 4×1015 cm−3. Find n and p at 300 K (ni = 1×1010 cm−3).

Given: ND = 1016, NA = 4×1015, ni = 1010 cm−3.

Find: n and p.

Solution.

ND > NA, so the material is n-type with net doping ND − NA = 6×1015 cm−3 ≫ ni
n ≈ 6×1015 cm−3
p = ni2/n = 1020/6×1015 = 1.7×104 cm−3

Answer: n = 6×1015 cm−3, p = 1.7×104 cm−3.

#### Practice 4.7: why bands widen

Question. Using the Kronig–Penney model, explain why allowed bands become wider at higher energies.

Answer. The left-hand side of P sin(αa)/(αa) + cos(αa) = cos(ka) is a cosine plus a term whose amplitude falls as 1/(αa). At low energy (small αa) the P sin(αa)/(αa) term is large, so the curve swings far beyond ±1 and spends only short stretches inside the allowed strip: narrow bands, wide gaps. As energy increases, αa increases, that term shrinks, and the curve is mostly the plain cosine, which stays between ±1 almost everywhere: wide bands, narrow gaps. Physically, high-energy electrons are less affected by the atomic barriers and behave more like free electrons.

## Objectives check

Use this table to confirm you have met this week's objectives. Cover the Answer column and answer each check question from memory. If you cannot, go back to the section in the last column before moving on.

| # | Objective | Check yourself | Answer | Where it is taught |  |  |
| --- | --- | --- | --- | --- | --- | --- |
| 1 | State the basic ideas of quantum mechanics needed for solids. | What is the meaning of | ψ | 2? | The probability density of finding the electron at a point. | Why classical physics is not enough |
| 2 | State the time-independent Schrödinger equation and explain its terms. | Which term of −(ħ2/2m)d2ψ/dx2 + Vψ = Eψ is the kinetic energy? | −(ħ2/2m) d2ψ/dx2. | The Schrödinger equation |  |  |
| 3 | Explain how discrete atomic levels become energy bands. | Into how many levels does one atomic level split when N atoms form a crystal? | N levels, so close together that they form a band. | From atoms to bands |  |  |
| 4 | Explain the Kronig–Penney model and how it produces allowed and forbidden bands. | In P sin(αa)/(αa) + cos(αa) = cos(ka), which energies are forbidden? | Those for which the left-hand side is greater than +1 or less than −1. | The Kronig–Penney model |  |  |
| 5 | Explain E–k diagrams, effective mass and holes. | Does a strongly curved band give a heavy or a light effective mass? | Light: 1/m∗ = (1/ħ2) d2E/dk2 is large. | E–k diagrams and effective mass |  |  |
| 6 | Distinguish direct and indirect band gaps and calculate emission wavelengths. | What wavelength does GaAs (Eg = 1.42 eV) emit? | λ = 1.24/1.42 = 0.87 μm. | Direct and indirect band gaps; Example 4.1 |  |  |
| 7 | Derive ni and calculate intrinsic and extrinsic carrier concentrations. | Write ni in terms of Nc, Nv and Eg. | ni = √(NcNv) e−Eg/2kT. | Part C; Examples 4.2–4.4; Q27 |  |  |

Week 5 · Module 2 · Energy Bands & Carrier Statistics

# Carrier Statistics

Plan: the Fermi–Dirac distribution function; density of states; Fermi energy level calculation as a function of temperature and doping. This page follows the order of your lecturer's carrier-statistics note (sections 7–26) and adds the background those sections assume.

## Learning objectives

By the end of this week you should be able to:

- Define and use the Fermi–Dirac distribution function.

- Explain the physical meaning of the Fermi level and the shape of f(E) at 0 K.

- Explain the density of states and the effective density of states.

- Calculate electron and hole concentrations and apply the mass action law.

- Determine the position of the Fermi level for given doping.

- Apply the charge-neutrality condition, including compensated material.

- Explain the effect of temperature on carrier concentration and the Fermi level.

- Distinguish degenerate and non-degenerate semiconductors.

## Symbols and abbreviations used this week

Every symbol, constant and abbreviation on this page is listed here, even if an earlier week already defined it, so you can study this page on its own.

Constants and units

| Symbol | Meaning | Units / typical value |
| --- | --- | --- |
| q | Magnitude of the electronic charge | 1.6×10−19 C |
| k | Boltzmann constant | 8.617×10−5 eV/K = 1.381×10−23 J/K |
| kT | Thermal energy | 0.0259 eV (often 0.02585 eV) at 300 K |
| T | Absolute temperature | kelvin (K); room temperature = 300 K |
| h | Planck constant | 6.626×10−34 J·s |
| ħ | Reduced Planck constant, h/2π | 1.055×10−34 J·s |
| m0 | Free-electron mass | 9.11×10−31 kg |
| eV | Electron-volt, a unit of energy | 1 eV = 1.6×10−19 J |

Symbols

| Symbol | Meaning | Units / typical value |
| --- | --- | --- |
| Ec (EC) | Energy of the bottom of the conduction band | eV |
| Ev (EV) | Energy of the top of the valence band | eV |
| Eg | Band-gap energy, Ec − Ev | eV; Si 1.12, Ge 0.66, GaAs 1.42 at 300 K |
| EF | Fermi level: the energy at which a state has a 50 % chance of being occupied | eV |
| Ei | Intrinsic Fermi level, close to mid-gap | eV |
| EFn, EFp | Quasi-Fermi levels for electrons and holes, used out of equilibrium | eV |
| ED | Donor energy level, just below Ec | eV; Ec − ED ≈ 0.045 eV for P in Si |
| f(E) | Fermi–Dirac function: probability that a state at energy E is occupied | dimensionless, 0 to 1 |
| g(E), gc, gv | Density of states: allowed states per unit energy per unit volume | states/(eV·cm3) |
| Nc | Effective density of states in the conduction band | cm−3; Si 2.8×1019 at 300 K |
| Nv | Effective density of states in the valence band | cm−3; Si 1.04×1019 at 300 K |
| n | Electron concentration (free electrons per cm3) | cm−3 |
| p | Hole concentration (holes per cm3) | cm−3 |
| ni | Intrinsic carrier concentration (n = p = ni in pure material) | cm−3; Si ≈ 1×1010 at 300 K |
| ND | Donor concentration | cm−3 |
| NA | Acceptor concentration | cm−3 |
| ND+, NA− | Concentrations of ionised donors and acceptors | cm−3 |
| m∗, mn∗, mp∗ | Effective mass of electrons or holes | kg, or as a multiple of m0 |
| k (wave vector) | Wave vector, 2π/λ; measures the electron's momentum, p = ħk | m−1 or cm−1 |

Abbreviations

| Abbreviation | Meaning |
| --- | --- |
| Si | Silicon |
| GaAs | Gallium arsenide |
| MOS | Metal–oxide–semiconductor |
| n+ | Very heavily doped n-type (similarly p+) |
| FD | Fermi–Dirac (distribution) |

## Key terms

Every important word used this week is defined here, so you can read this week on its own.

Thermal equilibrium. The steady condition of a material left alone at a fixed temperature, with no applied voltage, light or current. Carriers are still being created and lost, but at equal rates, so their numbers do not change.

Valence band and conduction band (Ev, Ec). The valence band is the highest range of electron energies that is normally full, holding the electrons that form the covalent bonds; its top edge is Ev. The conduction band is the next range of energies above it, normally almost empty; its bottom edge is Ec. Electrons in the conduction band are free to move and carry current.

Band gap (Eg). The range of energies between the top of the valence band and the bottom of the conduction band, in which an electron cannot exist in a perfect crystal. Its width is the energy needed to free an electron from a bond.

Eg = Ec − Ev

Where:

- Eg = band-gap energy (eV); 1.12 eV for Si at 300 K

- Ec = energy of the bottom of the conduction band (eV)

- Ev = energy of the top of the valence band (eV)

Why it matters: the wider the gap, the fewer electrons are thermally freed, so ni falls exponentially as Eg rises.

Hole. An empty state in the valence band, left behind when an electron leaves a bond. It behaves like a positive charge carrier of charge +q that can move through the crystal.

Intrinsic semiconductor (ni). A pure semiconductor with no deliberate impurities. Its free electrons and holes come only from broken bonds, so they are equal in number; that common number per cm3 is the intrinsic carrier concentration ni (1×1010 cm−3 for Si at 300 K).

Doping (donor, acceptor). Adding a small, controlled amount of impurity atoms to a semiconductor. A donor (P, As, Sb in Si) gives up an extra electron to the conduction band; an acceptor (B, Al, Ga in Si) takes an electron from the valence band and so creates a hole. A dopant that has given up or taken its electron is said to be ionised.

n-type and p-type; majority and minority carriers. Donor-doped material has many more electrons than holes and is n-type; acceptor-doped material has many more holes and is p-type. The more numerous carrier is the majority carrier and the less numerous one is the minority carrier.

Why it matters: minority carriers are few, but they control how p-n junctions and transistors work.

Fermi level (EF). The energy at which an electron state has exactly a 50 % chance of being occupied. Its position between Ev and Ec sets how many electrons and holes there are.

Why it matters: once you know where EF lies, you can calculate n and p; most of this week is about finding it.

Fermi–Dirac distribution function (f(E)). The probability that an allowed electron state at energy E is occupied in thermal equilibrium.

f(E) = 1 / ( 1 + e(E − EF)/kT )

Where:

- f(E) = occupation probability, between 0 and 1 (dimensionless)

- E = energy of the state (eV)

- EF = Fermi level (eV)

- kT = thermal energy, 0.0259 eV at 300 K (k = 8.617×10−5 eV/K, T in K)

Why it matters: it supplies the "probability occupied" half of every carrier-concentration calculation.

Boltzmann (Maxwell–Boltzmann) approximation. The simpler form f(E) ≈ e−(E − EF)/kT, accurate to about 5 % or better when the state is more than about 3kT above EF.

Density of states (g(E)). The number of allowed electron states per unit energy per unit volume at energy E, in states/(eV·cm3). It is zero inside the band gap and grows as the square root of the distance into each band.

Effective density of states (Nc, Nv). The number of states which, if all placed exactly at the band edge (Ec or Ev), would give the same carrier concentration as the real, spread-out band. For Si at 300 K, Nc = 2.8×1019 cm−3 and Nv = 1.04×1019 cm−3.

Intrinsic Fermi level (Ei). The position of the Fermi level in an intrinsic semiconductor, where n = p. It lies very close to the middle of the band gap (13 meV below it in Si).

Mass action law. In thermal equilibrium the product of the electron and hole concentrations is fixed at a given temperature, whatever the doping (for non-degenerate material).

n p = ni2

Where:

- n = electron concentration (cm−3)

- p = hole concentration (cm−3)

- ni = intrinsic carrier concentration (cm−3); 1×1010 cm−3 for Si at 300 K

Why it matters: it gives the minority-carrier concentration as soon as the majority concentration is known.

Charge neutrality and compensation. Charge neutrality is the rule that a uniform piece of semiconductor has no net charge, so positive charges (holes, ionised donors) equal negative charges (electrons, ionised acceptors). Compensation is the partial cancelling of donors and acceptors when both are present; the material behaves as if doped with the difference, ND − NA or NA − ND.

Degenerate semiconductor. A very heavily doped semiconductor (above about 1018–1019 cm−3 in Si) whose Fermi level is within about 3kT of a band edge, or inside a band. The Boltzmann approximation fails and full Fermi–Dirac statistics must be used. A semiconductor with EF more than 3kT from both edges is non-degenerate.

## The big picture

Carrier statistics is the method for answering one question: how many free electrons and holes does a piece of semiconductor contain? Everything else in the course (conductivity, diodes, transistors) depends on that number.

Think of the conduction band as a large theatre:

- The seats are the allowed energy states. How many seats there are at each energy is the density of states.

- Whether a seat is occupied is a matter of probability. The probability is given by the Fermi–Dirac function.

- The number of electrons = (number of seats) × (probability each is filled), added up over all energies.

number of electrons = Σ (states available) × (probability occupied)

The Fermi level EF is the single number that sets those probabilities. Once you know where EF sits in the band gap, you know n and p. That is why most of this week is about finding EF.

## 1. The Fermi–Dirac distribution function

Electrons obey the Pauli exclusion principle: no two can occupy the same state. In thermal equilibrium, the probability that a state at energy E is occupied by an electron is:

f(E) = 1 / ( 1 + e(E − EF)/kT )

| Symbol | Meaning |
| --- | --- |
| f(E) | probability (between 0 and 1) that a state at energy E holds an electron |
| E | energy of the state (eV) |
| EF | the Fermi energy or Fermi level (eV) |
| k | Boltzmann constant, 8.617×10−5 eV/K |
| T | absolute temperature (K); kT = 0.02585 eV at 300 K |

### Three things to remember about f(E)

- At E = EF, the exponent is zero, e0 = 1, and f = 1/(1 + 1) = ½. The Fermi level is the energy where a state has a 50 % chance of being occupied, at any temperature.

- Below EF (E < EF), the exponent is negative, so f is close to 1: states are almost certainly full.

- Above EF (E > EF), the exponent is positive, so f is close to 0: states are almost certainly empty.

The change from "full" to "empty" happens over a few kT (about ±0.1 eV at room temperature).

At absolute zero (T = 0 K), kT → 0 and the change becomes instantaneous: f = 1 for every state below EF and f = 0 for every state above. f(E) is a sharp step. A pure semiconductor at 0 K therefore has a full valence band, an empty conduction band, and no free carriers.

The Fermi–Dirac function. At 0 K it is a step at EF. At 300 K and 900 K the step is smoothed over a few kT. It always passes through ½ at EF.

Probability that a state is empty. A state is either full or empty, so

probability empty = 1 − f(E)

An empty state in the valence band is a hole, so 1 − f(E) is the probability of finding a hole.

### Calculating an occupation probability

At 300 K (kT = 0.02585 eV), a state 0.10 eV above EF:

(E − EF)/kT = 0.10/0.02585 = 3.868
f = 1/(1 + e3.868) = 1/(1 + 47.85) = 0.0205

About a 2 % chance of being occupied. A state 0.10 eV below EF has f = 1/(1 + e−3.868) = 0.980, a 98 % chance; its probability of being empty is 2 %. The function is symmetric about EF.

### The Boltzmann approximation

If E − EF is more than about 3kT (0.08 eV at 300 K), e(E−EF)/kT is much larger than 1, and we can drop the "1 +":

f(E) ≈ e−(E − EF)/kT (Maxwell–Boltzmann approximation)

Where:

- f(E) = probability that a state at energy E is occupied (dimensionless)

- E − EF = height of the state above the Fermi level (eV); must be more than about 3kT

- kT = thermal energy, 0.02585 eV at 300 K

This is accurate to better than 5 %. For the 0.10 eV example: e−3.868 = 0.0209, against the exact 0.0205. Almost every calculation in this course uses this approximation, because the conduction band is usually well above EF.

## 2. Density of states

The density of states g(E) is the number of allowed electron states per unit energy, per unit volume, at energy E (units: states per eV per cm3).

Conduction band: gc(E) ∝ (mn∗)3/2 √(E − Ec) for E above Ec
Valence band: gv(E) ∝ (mp∗)3/2 √(Ev − E) for E below Ev
In the gap: g(E) = 0

Where:

- gc(E), gv(E) = density of states in the conduction and valence bands (states/(eV·cm3))

- mn∗, mp∗ = effective masses of electrons and holes (kg, or as a multiple of m0)

- E = energy of the state (eV)

- Ec, Ev = conduction-band bottom and valence-band top (eV)

In words: there are no states in the gap; just above Ec the number of states starts at zero and grows as the square root of how far you go into the band. The effective masses mn∗ and mp∗ describe the shape of each band; a heavier mass means more states.

### Effective density of states

Adding up "states × probability" over the whole conduction band (with the Boltzmann approximation) gives a very simple result. It is as if all the conduction-band states were squeezed into one level at Ec, with a total number Nc of them. Nc is the effective density of states:

Nc = 2 (2π mn∗ kT / h2)3/2, Nv = 2 (2π mp∗ kT / h2)3/2

Where:

- Nc, Nv = effective densities of states in the conduction and valence bands (cm−3 once converted from m−3)

- mn∗, mp∗ = density-of-states effective masses of electrons and holes (kg)

- kT = thermal energy (J in this formula; 1.381×10−23 J/K × T)

- h = Planck constant, 6.626×10−34 J·s

For silicon at 300 K: Nc = 2.8×1019 cm−3, Nv = 1.04×1019 cm−3. Both grow with temperature as T3/2.

## 7. Electron concentration

The electron concentration in the conduction band is obtained by adding up available states × occupation probability:

n = ∫ gc(E) f(E) dE (from Ec to the top of the band)

For a non-degenerate semiconductor, f(E) is replaced by the Maxwell–Boltzmann form, and the integral gives:

n = Nc e−(Ec − EF)/kT

or, measuring from the intrinsic level Ei,

n = ni e(EF − Ei)/kT

Where:

- n = electron concentration in the conduction band (cm−3)

- Nc = effective density of states in the conduction band, 2.8×1019 cm−3 for Si at 300 K

- Ec − EF = distance from the Fermi level up to the conduction-band edge (eV)

- ni = intrinsic carrier concentration, 1×1010 cm−3 for Si at 300 K

- EF − Ei = height of the Fermi level above the intrinsic level (eV)

- kT = thermal energy, 0.02585 eV at 300 K

Reading it. Ec − EF is the distance from the Fermi level up to the conduction-band edge. The smaller that distance, the larger n, and the dependence is exponential: every 60 mV that EF moves towards Ec multiplies n by 10.

## 8. Hole concentration

The probability that a valence-band state is empty is 1 − f(E). The hole concentration is

p = ∫ gv(E) [1 − f(E)] dE (over the valence band)

For a non-degenerate semiconductor this gives:

p = Nv e−(EF − Ev)/kT

and

p = ni e(Ei − EF)/kT

Where:

- p = hole concentration in the valence band (cm−3)

- Nv = effective density of states in the valence band, 1.04×1019 cm−3 for Si at 300 K

- EF − Ev = height of the Fermi level above the valence-band edge (eV)

- Ei − EF = depth of the Fermi level below the intrinsic level (eV)

- ni = intrinsic carrier concentration (cm−3); kT = 0.02585 eV at 300 K

These four equations (two for n, two for p) are the fundamental equations of semiconductor carrier statistics.

## 9. Position of the Fermi level

Turn the electron equation round to find EF when n is known. From n = Nc e−(Ec − EF)/kT, divide by Nc and take the natural logarithm:

ln(n/Nc) = −(Ec − EF)/kT

Therefore:

Ec − EF = kT ln(Nc/n)

Similarly, from the hole concentration:

EF − Ev = kT ln(Nv/p)

And, using the intrinsic level:

EF − Ei = kT ln(n/ni), Ei − EF = kT ln(p/ni)

Where:

- Ec − EF, EF − Ev = distances from the Fermi level to the conduction- and valence-band edges (eV)

- EF − Ei, Ei − EF = distance of the Fermi level above or below the intrinsic level (eV)

- n, p = electron and hole concentrations (cm−3)

- Nc, Nv = effective densities of states, 2.8×1019 and 1.04×1019 cm−3 for Si at 300 K

- ni = intrinsic carrier concentration, 1×1010 cm−3 for Si at 300 K

- kT = thermal energy, 0.02585 eV at 300 K; ln = natural logarithm

These equations let the Fermi level be calculated when the carrier concentration is known.

#### Example 5.1: Fermi level from the electron concentration

Question. An n-type silicon sample at 300 K has an electron concentration of 1×1016 cm−3. Taking Nc = 2.8×1019 cm−3 and kT = 0.02585 eV, find how far the Fermi level lies below the conduction-band edge.

Given: n = 1×1016 cm−3, Nc = 2.8×1019 cm−3, kT = 0.02585 eV.

Find: Ec − EF.

Formula:

Ec − EF = kT ln(Nc/n)

Solution.

Nc/n = 2.8×1019 / 1×1016 = 2800, ln(2800) = 7.94

Ec − EF = 0.02585 × 7.94 = 0.205 eV

Answer: Ec − EF = 0.205 eV: the Fermi level is 0.205 eV below the conduction band.

What this means: 0.205 eV is about 8kT, well over 3kT, so the sample is non-degenerate and the simple Boltzmann formulas are valid. The Fermi level sits in the upper part of the 1.12 eV gap, as expected for n-type material.

## 10. Intrinsic semiconductor

A semiconductor with no intentional donor or acceptor doping is called intrinsic. Every free electron came from a broken bond that also left a hole, so

n = p = ni

where ni is the intrinsic carrier concentration. Multiplying the n and p equations, EF cancels out:

n · p = Nc Nv e−(Ec − Ev)/kT = Nc Nv e−Eg/kT

and since n = p = ni,

ni = √(Nc Nv) · e−Eg/2kT

Where:

- ni = intrinsic carrier concentration (cm−3)

- Nc, Nv = effective densities of states, 2.8×1019 and 1.04×1019 cm−3 for Si at 300 K

- Eg = Ec − Ev = band-gap energy (eV); 1.12 eV for Si

- kT = thermal energy, 0.0259 eV at 300 K

This equation shows that the intrinsic carrier concentration depends strongly on temperature and on the band gap. For Si at 300 K, ni ≈ 1×1010 cm−3 (many textbooks use 1.5×1010; the accurate modern value is 9.65×109).

## 11. Intrinsic Fermi level

For an intrinsic semiconductor, n = p. Set the two expressions equal:

Nc e−(Ec − Ei)/kT = Nv e−(Ei − Ev)/kT

Solving for Ei gives

Ei = (Ec + Ev)/2 + (kT/2) ln(Nv/Nc)

Where:

- Ei = intrinsic Fermi level (eV)

- (Ec + Ev)/2 = mid-gap energy (eV)

- Nc, Nv = effective densities of states in the conduction and valence bands (cm−3)

- kT = thermal energy, 0.02585 eV at 300 K

If Nc and Nv were equal, the logarithm would be zero, and then

Ei = (Ec + Ev)/2

Thus the intrinsic Fermi level is approximately at the middle of the forbidden gap. For Si the correction is (0.02585/2) ln(1.04/2.8) = −0.013 eV, only 13 meV below mid-gap.

## 12. Mass action law

For a semiconductor in thermal equilibrium:

n · p = ni2

Where:

- n = electron concentration (cm−3)

- p = hole concentration (cm−3)

- ni = intrinsic carrier concentration, 1×1010 cm−3 for Si at 300 K (so ni2 = 1×1020 cm−6)

This is the mass action law. It holds for intrinsic and doped (non-degenerate) material alike, because when we multiplied n by p above, EF cancelled.

- For an intrinsic semiconductor n = p, therefore n = p = ni.

- For an n-type semiconductor where n ≫ p: n ≈ ND, and therefore p = ni2/ND.

- For a p-type semiconductor where p ≫ n: p ≈ NA, and therefore n = ni2/NA.

In plain words. n × p is fixed. Add donors, and the extra electrons fill in holes, so the hole count drops by exactly the same factor the electron count rises. Doping one carrier up pushes the other down.

## 13. Effect of doping on the Fermi level

Doping changes the concentration of carriers, and therefore shifts the Fermi level.

N-type. Donor atoms introduce additional electrons, so the Fermi level moves towards the conduction band:

Ec − EF = kT ln(Nc/n), EF − Ei = kT ln(n/ni)

If donors are fully ionised and ND ≫ ni, then n ≈ ND, and

Ec − EF = kT ln(Nc/ND), EF − Ei = kT ln(ND/ni)

P-type. Acceptor atoms create holes, so the Fermi level moves towards the valence band:

EF − Ev = kT ln(Nv/p), Ei − EF = kT ln(p/ni)

If acceptors are fully ionised, p ≈ NA, so

EF − Ev = kT ln(Nv/NA), Ei − EF = kT ln(NA/ni)

Where the Fermi level sits: at mid-gap (Ei) when intrinsic, near Ec for n-type, near Ev for p-type.

How big are the shifts? Each factor of 10 in doping moves EF by kT ln 10 = 0.0595 eV ≈ 60 mV at 300 K.

| Doping (Si, 300 K) | EF − Ei | Ec − EF |
| --- | --- | --- |
| Intrinsic | 0 | 0.56 eV |
| ND = 1014 cm−3 | 0.238 eV | 0.324 eV |
| ND = 1016 cm−3 | 0.357 eV | 0.205 eV |
| ND = 1018 cm−3 | 0.476 eV | 0.086 eV |

## 14. Charge neutrality in a doped semiconductor

A piece of semiconductor is electrically neutral overall. The positive charges (holes and ionised donors) must equal the negative charges (electrons and ionised acceptors):

p + ND+ = n + NA−

Where:

- p, n = hole and electron concentrations (cm−3)

- ND+ = concentration of ionised (positively charged) donors (cm−3)

- NA− = concentration of ionised (negatively charged) acceptors (cm−3)

If donors and acceptors are completely ionised (ND+ = ND, NA− = NA):

p + ND = n + NA

This is the charge-neutrality condition. Combined with np = ni2 it gives n exactly:

n = (ND − NA)/2 + √( ((ND − NA)/2)2 + ni2 )

Where:

- n = electron concentration (cm−3)

- ND, NA = donor and acceptor concentrations, all assumed ionised (cm−3)

- ni = intrinsic carrier concentration (cm−3)

(For p-type material, NA > ND, the same formula with n and p swapped and NA − ND in place of ND − NA gives p.)

When ND − NA ≫ ni, this reduces to n ≈ ND − NA. When both dopants are present they partly cancel, which is called compensation.

## 15. N-type semiconductor

When silicon is doped with a donor impurity (phosphorus P, arsenic As, antimony Sb), it becomes n-type. A donor contributes an extra electron. If ND ≫ ni and all donors are ionised:

n ≈ ND

Using the mass action law np = ni2, we obtain:

p ≈ ni2 / ND

## 16. P-type semiconductor

When silicon is doped with an acceptor impurity (boron B, aluminium Al, gallium Ga), it becomes p-type. An acceptor creates a hole. If NA ≫ ni, then:

p ≈ NA

and:

n ≈ ni2 / NA

### Intrinsic, n-type and p-type compared

| Feature | Intrinsic | n-type | p-type |
| --- | --- | --- | --- |
| Dopant | None | Donors (P, As, Sb) | Acceptors (B, Al, Ga) |
| Carrier concentrations | n = p = ni | n ≈ ND, p = ni2/ND | p ≈ NA, n = ni2/NA |
| Majority / minority carrier | Neither (equal) | Electrons / holes | Holes / electrons |
| Fermi level | EF = Ei, near mid-gap | Above Ei: EF − Ei = kT ln(ND/ni) | Below Ei: Ei − EF = kT ln(NA/ni) |
| Example (Si, 300 K) | n = p = 1010 cm−3 | ND = 1016: p = 104 cm−3, EF = Ei + 0.357 eV | NA = 1017: n = 103 cm−3, EF = Ei − 0.417 eV |

## 17. Fermi level as a function of temperature

Temperature has a major effect on carrier concentration and Fermi level. There are generally three regions:

Region 1: Freeze-out region. At very low temperature (below about 100 K in Si), donor and acceptor atoms are not fully ionised: there is not enough thermal energy to free the extra electron from each donor. Consequently there are relatively few free carriers, and n < ND.

Region 2: Extrinsic region. At moderate temperature (roughly 150–450 K for Si), the dopants are fully ionised:

n-type: n ≈ ND p-type: p ≈ NA

The carrier concentration is set by the doping and hardly changes with temperature. This is the region used in most basic semiconductor calculations, and the region where devices operate.

Region 3: Intrinsic region. At sufficiently high temperature, thermally generated electron–hole pairs become dominant. Eventually

ni ≫ ND so n ≈ p ≈ ni

The semiconductor behaves more and more like an intrinsic semiconductor, and EF returns to Ei. The doping no longer controls the material, which is why every device has a maximum operating temperature.

#### Example 5.2: Fermi level against temperature

Question. Silicon is doped with ND = 1×1015 cm−3. Using the intrinsic concentrations in the table (ni = 1×1010 cm−3 at 300 K, rising with temperature), calculate the electron concentration and the position of the Fermi level relative to Ei at 300, 400, 500 and 600 K. At what temperature does the material become effectively intrinsic?

Given: ND = 1×1015 cm−3, complete ionisation; ni(T) from ni ∝ T3/2e−Eg(T)/2kT, scaled to 1×1010 cm−3 at 300 K.

Find: n and EF − Ei at each temperature.

Formula:

n = ND/2 + √( (ND/2)2 + ni2 ), EF − Ei = kT ln(n/ni)

Solution. At each temperature work out kT = 8.617×10−5 × T, use the exact charge-neutrality result for n, then find EF − Ei.

| T (K) | kT (eV) | ni (cm−3) | n (cm−3) | EF − Ei = kT ln(n/ni) (eV) |
| --- | --- | --- | --- | --- |
| 300 | 0.0259 | 1.0×1010 | 1.00×1015 | 0.0259 × ln(1.0×105) = 0.298 |
| 400 | 0.0345 | 5.3×1012 | 1.00×1015 | 0.0345 × ln(189) = 0.181 |
| 500 | 0.0431 | 2.6×1014 | 1.06×1015 | 0.0431 × ln(4.16) = 0.061 |
| 600 | 0.0517 | 3.7×1015 | 4.18×1015 | 0.0517 × ln(1.15) = 0.007 |

Answer: EF − Ei falls from 0.298 eV at 300 K to 0.007 eV at 600 K. ni passes ND at about 550 K; above that the material is effectively intrinsic and the doping no longer controls it.

What this means: up to about 400 K the electron concentration is fixed by the doping, which is what a device designer relies on. By 600 K thermally generated pairs outnumber the donor electrons more than three to one (p ≈ 3.2×1015 against ND = 1×1015 cm−3), EF has fallen back to Ei, and a device made from this silicon would no longer work as designed.

Fermi level relative to Ei against temperature for silicon at four donor concentrations (cm⁻³). Heavier doping keeps the Fermi level away from mid-gap up to a higher temperature.

## 18. Worked example: n-type silicon

#### Example 5.3: majority and minority carriers

Question. Silicon at 300 K is doped with ND = 1×1016 cm−3. Assuming ni = 1×1010 cm−3 and complete donor ionisation, calculate the electron and hole concentrations and identify the majority and minority carriers.

Given: ND = 1×1016 cm−3, ni = 1×1010 cm−3, T = 300 K.

Find: n, p; majority and minority carriers.

Formula:

n ≈ ND, p = ni2/n

Solution.

Step 1: electron concentration. Since ND ≫ ni (1016 ≫ 1010), every donor contributes one electron:

n ≈ ND = 1×1016 cm−3

Step 2: hole concentration, from the mass-action law:

p = ni2/n = (1×1010)2 / (1×1016) = 1020/1016 = 1×104 cm−3

Answer: n = 1×1016 cm−3, p = 1×104 cm−3. Electrons are the majority carriers, holes the minority carriers. (With ni = 1.5×1010 cm−3, p = 2.25×104 cm−3; the method is identical.)

What this means: raising the electrons a million times above ni has pushed the holes a million times below it. There is only one hole for every 1012 electrons, yet, as later weeks show, these few minority holes are what control current in a p-n junction.

## 19. Worked example: Fermi level of n-type silicon

#### Example 5.4: Fermi level of n-type silicon

Question. For the silicon of Example 5.3 (n = ND = 1×1016 cm−3, ni = 1×1010 cm−3) at 300 K, calculate the position of the Fermi level relative to the intrinsic level, and estimate how far it lies below the conduction band.

Given: n = 1×1016 cm−3, ni = 1×1010 cm−3, kT = 0.02585 eV, Eg = 1.12 eV.

Find: EF − Ei, and Ec − EF.

Formula:

EF − Ei = kT ln(n/ni), Ec − EF ≈ Eg/2 − (EF − Ei)

Solution.

EF − Ei = kT ln(n/ni) = 0.02585 × ln(1016/1010) = 0.02585 × ln(106)

Since ln(106) = 6 × 2.303 = 13.82,

EF − Ei = 0.02585 × 13.82 = 0.357 eV

Ei is close to mid-gap, 0.56 eV below Ec, so

Ec − EF ≈ 0.56 − 0.357 = 0.20 eV

Answer: EF = Ei + 0.357 eV, about 0.20 eV below Ec: the Fermi level has moved up towards the conduction band. (With ni = 1.5×1010 cm−3: EF − Ei = 0.02585 ln(6.67×105) = 0.347 eV.)

What this means: a millionfold increase in electrons moves the Fermi level only 0.357 eV, because the dependence is logarithmic. The answer agrees with Example 5.1 (0.205 eV), which found the same quantity directly from Nc.

## 20. Worked example: p-type silicon

#### Example 5.5: carriers and Fermi level in p-type silicon

Question. Silicon at 300 K is doped with NA = 1×1017 cm−3 boron atoms. Taking ni = 1×1010 cm−3, calculate the hole and electron concentrations and the position of the Fermi level.

Given: NA = 1×1017 cm−3, ni = 1×1010 cm−3, kT = 0.02585 eV.

Find: p, n and Ei − EF.

Formula:

p ≈ NA, n = ni2/p, Ei − EF = kT ln(p/ni)

Solution.

p ≈ NA = 1×1017 cm−3
n = ni2/p = 1020/1017 = 1×103 cm−3
Ei − EF = kT ln(p/ni) = 0.02585 × ln(107) = 0.02585 × 16.12 = 0.417 eV

Answer: p = 1×1017 cm−3, n = 1×103 cm−3, EF = Ei − 0.417 eV: the Fermi level moves down towards the valence band, about 0.56 − 0.417 = 0.14 eV above Ev.

What this means: the more exact value EF − Ev = kT ln(Nv/NA) = 0.02585 ln(104) = 0.120 eV is still about 4.6kT, more than 3kT, so even at this fairly heavy doping the silicon is still non-degenerate. Only about 1000 free electrons remain in each cm3, so electron current in this material is negligible unless electrons are injected from outside.

## 21. Degenerate and non-degenerate semiconductors

The Maxwell–Boltzmann approximation is valid only when the Fermi level is far enough from the band edges. For a non-degenerate semiconductor:

Ec − EF ≫ kT (n-type), EF − Ev ≫ kT (p-type)

In practice "≫" means more than about 3kT.

In a degenerate semiconductor the doping is very high (in Si, above about 1018–1019 cm−3) and the Fermi level approaches, or even enters, the conduction or valence band. Then the full Fermi–Dirac statistics must be used, and the material behaves almost like a metal. Degenerate n+ and p+ layers are used for Ohmic contacts (Week 11) and tunnel diodes.

| Feature | Non-degenerate | Degenerate |
| --- | --- | --- |
| Doping | Relatively low or moderate | Very high |
| Statistics | Maxwell–Boltzmann approximation | Fermi–Dirac |
| Fermi level | Inside the band gap, more than 3kT from the edges | Near or inside a band |
| Carrier concentration | Simple exponential equations | More complex |

Check. For Si with ND = 1018 cm−3, Ec − EF = 0.02585 ln(2.8×1019/1018) = 0.086 eV = 3.3kT, just non-degenerate. At 1019 cm−3, Ec − EF = 0.027 eV ≈ 1kT: degenerate.

## 22. Relationship between carrier concentration and Fermi level

The electron concentration increases exponentially as the Fermi level approaches the conduction band, n = Nc e−(Ec − EF)/kT. Similarly, the hole concentration increases as the Fermi level approaches the valence band, p = Nv e−(EF − Ev)/kT. Therefore:

- Fermi level closer to Ec → more electrons (n-type).

- Fermi level closer to Ev → more holes (p-type).

- Fermi level at Ei → n = p = ni (intrinsic).

## 23. Temperature dependence of intrinsic carrier concentration

Recall ni = √(NcNv) e−Eg/2kT. Since Nc and Nv are each proportional to T3/2, their product's square root is proportional to T3/2, so approximately

ni ∝ T3/2 e−Eg/2kT

Where:

- ni = intrinsic carrier concentration (cm−3)

- T = absolute temperature (K)

- Eg = band-gap energy (eV); it decreases slightly as T rises

- kT = thermal energy (eV), with k = 8.617×10−5 eV/K

The exponential term is especially important. As temperature increases, kT increases, the negative exponent −Eg/2kT gets smaller in magnitude, and e−Eg/2kT increases rapidly. The T3/2 factor adds a smaller increase. For silicon, ni roughly doubles every 8 °C near room temperature, and rises about 25,000 times between 300 K and 500 K.

Therefore semiconductor conductivity generally increases with temperature, because more electron–hole pairs are thermally generated.

## 24. Formula sheet for carrier statistics

| Quantity | Formula |
| --- | --- |
| Fermi–Dirac function | f(E) = 1/(1 + e(E − EF)/kT) |
| Electron concentration | n = Nc e−(Ec − EF)/kT = ni e(EF − Ei)/kT |
| Hole concentration | p = Nv e−(EF − Ev)/kT = ni e(Ei − EF)/kT |
| Effective density of states | Nc = 2(2πmn∗kT/h2)3/2, Nv = 2(2πmp∗kT/h2)3/2 |
| Intrinsic carrier concentration | ni = √(NcNv) e−Eg/2kT |
| Mass action law | np = ni2 |
| Intrinsic Fermi level | Ei = (Ec + Ev)/2 + (kT/2) ln(Nv/Nc) ≈ mid-gap |
| N-type Fermi level | EF − Ei = kT ln(ND/ni) |
| P-type Fermi level | Ei − EF = kT ln(NA/ni) |
| Charge neutrality | p + ND+ = n + NA− |

## 25. Summary: what you should be able to do

- Explain the concept of carrier statistics in semiconductors.

- Define and use the Fermi–Dirac distribution function.

- Explain the physical meaning of the Fermi energy level.

- Calculate the probability of electron occupation of an energy state.

- Explain the density of states in the conduction and valence bands.

- Calculate electron and hole concentrations.

- Calculate the intrinsic carrier concentration.

- Apply the mass action law.

- Determine the position of the Fermi level.

- Explain the effect of donor and acceptor doping on the Fermi level.

- Distinguish between intrinsic, n-type and p-type semiconductors.

- Explain the effect of temperature on carrier concentration.

- Distinguish between degenerate and non-degenerate semiconductors.

- Apply the charge-neutrality equation to doped semiconductors.

## 26. Mid-module evaluation, solved

These are the lecturer's mid-module evaluation questions. The numerical values in the printed note did not come through in the copy provided, so the calculations below use the standard silicon values stated in each question. If your copy gives different numbers, follow the same steps.

### Part A: short-answer questions

A1. Define carrier statistics. Carrier statistics is the study of how electrons and holes are distributed among the allowed energy states of a semiconductor in thermal equilibrium. It combines the density of states with the Fermi–Dirac probability to calculate the electron and hole concentrations and the position of the Fermi level.

A2. What is the Fermi energy level? The Fermi level EF is the energy at which the probability of a state being occupied by an electron is exactly one half. At 0 K it is the boundary between filled and empty states. Its position relative to Ec and Ev determines the electron and hole concentrations, and in equilibrium it is constant throughout a material or device.

A3. State the Fermi–Dirac distribution function. f(E) = 1/(1 + e(E − EF)/kT), where f(E) is the probability that a state of energy E is occupied, EF the Fermi level, k Boltzmann's constant and T the absolute temperature.

A4. What is the probability that a state at E = EF is occupied? Exactly ½ (50 %), because the exponent is zero: f = 1/(1 + e0) = 1/2. This is true at any temperature.

A5. Define density of states. The density of states g(E) is the number of allowed electron energy states per unit energy per unit volume at energy E (states/eV·cm3). In a parabolic band, gc(E) ∝ √(E − Ec) in the conduction band and gv(E) ∝ √(Ev − E) in the valence band; it is zero in the band gap.

A6. What is meant by effective density of states? The effective density of states (Nc for the conduction band, Nv for the valence band) is the number of states that, if all placed at the band edge, would give the same carrier concentration as the real distributed band. It lets the carrier concentration be written simply as n = Nce−(Ec − EF)/kT. For Si at 300 K, Nc = 2.8×1019 and Nv = 1.04×1019 cm−3.

A7. Distinguish between intrinsic and extrinsic semiconductors. An intrinsic semiconductor is pure: its carriers come only from thermal breaking of bonds, so n = p = ni and EF ≈ Ei (mid-gap). An extrinsic semiconductor is doped with donors or acceptors: one carrier type dominates (n ≈ ND or p ≈ NA), EF moves towards Ec or Ev, and the carrier concentration is set by the doping rather than by temperature.

A8. Define majority and minority carriers. Majority carriers are the more numerous carrier type in a doped semiconductor (electrons in n-type, holes in p-type). Minority carriers are the less numerous type (holes in n-type, electrons in p-type). In n-type Si with ND = 1016 cm−3, there are 1016 majority electrons and only 104 minority holes per cm3.

A9. State the mass action law. In thermal equilibrium the product of the electron and hole concentrations is constant at a given temperature: np = ni2, regardless of doping (for a non-degenerate semiconductor).

A10. Explain why doping changes the Fermi level. The Fermi level is tied to the carrier concentrations by n = nie(EF − Ei)/kT. Donors add electrons, so n rises above ni; for the equation to hold, EF must rise above Ei (towards Ec), by kT ln(ND/ni). Acceptors add holes, so p rises and EF must fall towards Ev by kT ln(NA/ni). The heavier the doping, the larger the shift.

### Part B: calculation questions

B1. At 300 K, find the probability that a state 0.10 eV above the Fermi level is occupied (kT = 0.02585 eV).

Given: E − EF = 0.10 eV, kT = 0.02585 eV.

Find: f(E).

Formula:

f(E) = 1/(1 + e(E − EF)/kT)

Solution.

f = 1/(1 + e0.10/0.02585) = 1/(1 + e3.868) = 1/(1 + 47.85) = 0.0205

Answer: the probability is 0.0205, about 2 %.

What this means: only 0.1 eV (about 4kT) above EF, a state is already almost certainly empty; this is why the conduction band, several tenths of an eV above EF, holds so few electrons.

B2. Silicon has ND = 1×1016 cm−3 and ni = 1×1010 cm−3. Assuming complete ionisation, find (a) n, (b) p, (c) the majority carrier.

Given: ND = 1×1016 cm−3, ni = 1×1010 cm−3, complete ionisation.

Find: n, p and the majority carrier.

Formula:

n ≈ ND, p = ni2/n

Solution.

(a) n ≈ ND = 1×1016 cm−3
(b) p = ni2/n = 1020/1016 = 1×104 cm−3

Answer: (a) n = 1×1016 cm−3, (b) p = 1×104 cm−3, (c) electrons are the majority carriers (n-type).

What this means: the donors have raised n a millionfold above ni, and the mass action law has lowered p by the same factor.

B3. P-type silicon has NA = 5×1016 cm−3 and ni = 1×1010 cm−3. Find (a) p, (b) n, (c) the minority carrier.

Given: NA = 5×1016 cm−3, ni = 1×1010 cm−3, complete ionisation.

Find: p, n and the minority carrier.

Formula:

p ≈ NA, n = ni2/p

Solution.

(a) p ≈ NA = 5×1016 cm−3
(b) n = ni2/p = 1020/(5×1016) = 2×103 cm−3

Answer: (a) p = 5×1016 cm−3, (b) n = 2×103 cm−3, (c) electrons are the minority carriers.

What this means: there are only 2000 free electrons in each cm3 against 5×1016 holes, so almost all the current in this material is carried by holes.

B4. At 300 K an n-type semiconductor has ND = 1×1017 cm−3 and ni = 1×1010 cm−3. Find the Fermi level relative to the intrinsic level.

Given: ND = 1×1017 cm−3, ni = 1×1010 cm−3, kT = 0.02585 eV.

Find: EF − Ei.

Formula:

EF − Ei = kT ln(ND/ni)

Solution.

EF − Ei = 0.02585 × ln(107) = 0.02585 × 16.12 = 0.417 eV

Answer: the Fermi level is 0.417 eV above Ei.

What this means: with Ei about 0.56 eV below Ec, the Fermi level is now only about 0.14 eV below the conduction band, which is why this sample has so many free electrons.

B5. Explain, using equations, why increasing temperature increases the intrinsic carrier concentration.

ni = √(NcNv) e−Eg/2kT, with Nc, Nv ∝ T3/2 ⇒ ni ∝ T3/2 e−Eg/2kT

Two factors increase with T. The T3/2 factor grows slowly: more states become effectively available as the electrons' thermal energy spreads. The exponential grows very fast: Eg/2kT becomes smaller as T increases, so e−Eg/2kT increases steeply. Physically, a higher temperature gives more electrons enough thermal energy to cross the band gap, breaking more covalent bonds and creating more electron–hole pairs. For Si, ni is about 1010 cm−3 at 300 K, 5×1012 at 400 K and 2.6×1014 at 500 K.

## Examination questions solved (Q30–Q33)

### Q30. Explain the Fermi-Dirac distribution function and its significance in semiconductor physics.

The function. Electrons are indistinguishable particles of half-integer spin that obey the Pauli exclusion principle (fermions). In thermal equilibrium at temperature T, the probability that an available state of energy E is occupied by an electron is given by Fermi–Dirac statistics:

f(E) = 1 / ( 1 + exp((E − EF)/kT) )

where EF is the Fermi level and k is Boltzmann's constant.

Properties:

- 0 ≤ f(E) ≤ 1 (at most one electron per state).

- f(EF) = ½ at any temperature: EF is the energy with a 50 % chance of occupation.

- f is symmetric about EF: the probability that a state ΔE above EF is occupied equals the probability that a state ΔE below EF is empty, so 1 − f(EF + ΔE) = f(EF − ΔE).

- The transition from 1 to 0 happens over a few kT (about 0.1 eV at 300 K).

- For E − EF > 3kT it reduces to the Boltzmann factor exp(−(E − EF)/kT).

Significance:

- Gives the carrier concentrations. n = ∫gc f dE and p = ∫gv(1 − f)dE. Without f(E) we could not calculate n, p or ni.

- Defines the Fermi level, the single most useful quantity in device physics. Its position relative to Ec and Ev tells immediately whether the material is n-type, p-type or intrinsic and how heavily doped.

- Constant Fermi level in equilibrium. EF is flat across any system in equilibrium; this determines band bending and built-in potential in p-n junctions, Schottky contacts and MOS structures.

- Explains temperature dependence of carrier concentration, intrinsic behaviour, freeze-out and degeneracy.

- Out of equilibrium, the concept is extended to quasi-Fermi levels EFn and EFp, which are used to describe biased devices.

### Q31. Write the Fermi-Dirac distribution equation and explain what happens to the distribution at absolute zero.

f(E) = 1 / ( 1 + e(E − EF)/kT )

At T = 0 K, kT → 0, so the exponent (E − EF)/kT → ±∞:

- For E < EF: (E − EF)/kT → −∞, e−∞ = 0, so f(E) = 1/(1 + 0) = 1. Every state below EF is certainly filled.

- For E > EF: (E − EF)/kT → +∞, e+∞ → ∞, so f(E) = 0. Every state above EF is certainly empty.

The distribution becomes a sharp rectangular step at E = EF. The Fermi level is then the boundary between completely filled and completely empty states: the highest occupied energy at 0 K.

For a semiconductor this means the valence band is completely full and the conduction band completely empty at 0 K. There are no free carriers, and a pure semiconductor is a perfect insulator at absolute zero.

As T increases, the step softens over a range of about ±3kT: some states just below EF become empty and some just above become filled. This tail reaching into the conduction band is what produces free electrons at room temperature. At E = EF, f = ½ always. (See the Fermi–Dirac figure above.)

| E − EF | f at 0 K | f at 300 K (kT = 0.0259 eV) |
| --- | --- | --- |
| −0.1 eV | 1 | 0.979 |
| 0 | ½ (undefined step) | 0.500 |
| +0.1 eV | 0 | 0.021 |
| +0.3 eV | 0 | 9.3×10−6 |

### Q32. Define the density of states in a semiconductor and explain its importance in determining carrier concentration.

Definition. The density of states g(E) is the number of allowed electron energy states (including both spins) per unit energy interval per unit volume of the crystal, at energy E. Unit: cm−3eV−1 (or m−3J−1).

For the conduction and valence bands (parabolic band approximation):

gc(E) = (4π (2mn∗)3/2 / h3) √(E − Ec), E ≥ Ec
gv(E) = (4π (2mp∗)3/2 / h3) √(Ev − E), E ≤ Ev
g(E) = 0 inside the gap

Physical origin. In a crystal of volume V, the allowed wave vectors k are quantised, each occupying (2π)3/V of k-space. The number of states with energy up to E is the volume of the sphere of radius k divided by that, times 2 for spin. Differentiating with respect to E, using E − Ec = ħ2k2/2m∗, gives the square-root law. The effective mass enters because it describes the band's curvature: heavier mass means more states per unit energy.

Importance in determining carrier concentration:

- The carrier concentration is the product of available states and probability of occupation: n = ∫gc(E)f(E)dE, p = ∫gv(E)[1 − f(E)]dE. The Fermi function alone says nothing about how many electrons there are; g(E) supplies the number of places they can go.

- It produces the effective densities of states Nc and Nv, which appear in every carrier-concentration formula (n = Nc e−(Ec−EF)/kT).

- Because g(E) is zero in the gap, no carriers exist there even though f(E) is non-zero, which explains why the gap is "forbidden".

- It explains differences between materials. GaAs has a small mn∗ (0.067m0), so its Nc (4.7×1017 cm−3) is 60 times smaller than Si's; for the same doping its Fermi level sits much closer to Ec and it becomes degenerate at lower doping.

- It sets the T3/2 factor in Nc, Nv and ni, and determines where the Fermi level lies relative to mid-gap (Ei shifts by (3/4)kT ln(mp∗/mn∗)).

- It also governs optical absorption and the density of electrons available for tunnelling and contact behaviour.

### Q33. Explain how the Fermi energy level changes with doping in n-type and p-type semiconductors.

In an intrinsic semiconductor EF = Ei, near mid-gap. Doping shifts it so that the carrier concentrations satisfy n = ni e(EF − Ei)/kT and p = ni e(Ei − EF)/kT.

n-type (donor doping ND). n ≈ ND > ni, so EF moves up, towards Ec:

EF − Ei = kT ln(ND/ni), Ec − EF = kT ln(Nc/ND)

p-type (acceptor doping NA). p ≈ NA > ni, so EF moves down, towards Ev:

Ei − EF = kT ln(NA/ni), EF − Ev = kT ln(Nv/NA)

Behaviour:

- The shift is logarithmic: each tenfold increase in doping moves EF by kT ln10 ≈ 0.06 eV at 300 K.

- Heavier doping → closer to the band edge. At very high doping (≈ Nc or Nv) EF reaches or enters the band and the semiconductor becomes degenerate (n+, p+).

- Compensation (both ND and NA) shifts EF according to the net doping ND − NA.

- Temperature: as T rises, ni increases and EF moves back toward Ei; at high enough T every semiconductor becomes intrinsic. At very low T (freeze-out) EF rises above ED in n-type material.

- In equilibrium the Fermi level must be the same everywhere; when n and p regions meet, bands bend to keep EF flat.

Example (Si, 300 K, ni = 1010 cm−3):

| Doping | EF position |
| --- | --- |
| Intrinsic | EF = Ei |
| ND = 1015 cm−3 | EF − Ei = 0.0259 ln(105) = 0.298 eV |
| ND = 1017 cm−3 | EF − Ei = 0.0259 ln(107) = 0.417 eV |
| NA = 1016 cm−3 | Ei − EF = 0.0259 ln(106) = 0.358 eV |

(See the Fermi-level figure above.)

## Practice questions

These extra questions practise this week's ideas. Work each one on paper before reading the solution; the calculation questions follow the same Question, Given, Find, Solution, Answer layout as the worked examples.

#### Practice 5.1: accuracy of the Boltzmann approximation

Question. Calculate the occupation probability of a state 3kT above the Fermi level using (a) the Fermi–Dirac function and (b) the Boltzmann approximation. What is the error?

Given: E − EF = 3kT.

Find: f(FD), f(Boltzmann) and the percentage error.

Solution.

(a) f = 1/(1 + e3) = 1/21.09 = 0.0474
(b) f ≈ e−3 = 0.0498
error = (0.0498 − 0.0474)/0.0474 = 5 %

Answer: 0.0474 against 0.0498, a 5 % error: this is why "more than 3kT from EF" is the rule for using the Boltzmann approximation.

#### Practice 5.2: carriers from the Fermi-level position

Question. In silicon at 300 K the Fermi level is 0.30 eV below the conduction band. Find the probability that a state at Ec is occupied, and the electron concentration.

Given: Ec − EF = 0.30 eV, kT = 0.0259 eV, Nc = 2.8×1019 cm−3.

Find: f(Ec) and n.

Solution.

f(Ec) ≈ e−0.30/0.0259 = e−11.58 = 9.3×10−6
n = Nc e−(Ec − EF)/kT = 2.8×1019 × 9.3×10−6 = 2.6×1014 cm−3

Answer: f = 9.3×10−6, n = 2.6×1014 cm−3.

What this means: although each state at Ec has less than a one-in-100,000 chance of holding an electron, there are so many states (Nc) that the material still has about 2.6×1014 free electrons per cm3: a lightly doped n-type sample.

#### Practice 5.3: doping for a chosen Fermi level

Question. What donor concentration places the Fermi level of silicon 0.20 eV above the intrinsic level at 300 K?

Given: EF − Ei = 0.20 eV, ni = 1010 cm−3, kT = 0.02585 eV.

Find: ND.

Solution.

ND = ni e(EF − Ei)/kT = 1010 × e0.20/0.02585 = 1010 × e7.74 = 2.3×1013 cm−3

Answer: ND ≈ 2.3×1013 cm−3, a very light doping.

#### Practice 5.4: compensated p-type silicon

Question. Silicon is doped with NA = 3×1016 cm−3 and ND = 1×1016 cm−3. Find p, n and the Fermi-level position at 300 K.

Given: NA = 3×1016, ND = 1016, ni = 1010 cm−3, kT = 0.02585 eV.

Find: p, n and Ei − EF.

Solution.

p ≈ NA − ND = 2×1016 cm−3
n = ni2/p = 1020/2×1016 = 5×103 cm−3
Ei − EF = kT ln(p/ni) = 0.02585 × ln(2×106) = 0.375 eV

Answer: p = 2×1016 cm−3, n = 5×103 cm−3, EF = Ei − 0.375 eV.

#### Practice 5.5: lightly doped germanium

Question. Germanium (ni = 2.4×1013 cm−3) is doped with ND = 1×1014 cm−3. Find n and p using the full charge-neutrality equation.

Given: ND = 1014 cm−3, NA = 0, ni = 2.4×1013 cm−3.

Find: n and p.

Solution.

n = ND/2 + √((ND/2)2 + ni2) = 5×1013 + √(2.5×1027 + 5.76×1026)
= 5×1013 + 5.55×1013 = 1.05×1014 cm−3
p = ni2/n = 5.76×1026 / 1.05×1014 = 5.5×1012 cm−3

Answer: n = 1.05×1014 cm−3, p = 5.5×1012 cm−3. Thermal generation adds 5 % to the electron count, so n ≈ ND is only approximate here.

#### Practice 5.6: is it degenerate?

Question. Silicon is doped with ND = 5×1018 cm−3. Find Ec − EF and decide whether the Boltzmann approximation is valid.

Given: ND = 5×1018 cm−3, Nc = 2.8×1019 cm−3, kT = 0.02585 eV.

Find: Ec − EF in eV and in units of kT.

Solution.

Ec − EF = kT ln(Nc/ND) = 0.02585 × ln(5.6) = 0.02585 × 1.72 = 0.045 eV = 1.7kT

Answer: 0.045 eV, only 1.7kT: less than 3kT, so the material is (nearly) degenerate and full Fermi–Dirac statistics should be used.

#### Practice 5.7: where exactly is Ei?

Question. Show that the intrinsic level of silicon lies slightly below mid-gap, and by how much.

Given: Ei = (Ec + Ev)/2 + (kT/2) ln(Nv/Nc), Nc = 2.8×1019, Nv = 1.04×1019 cm−3.

Find: Ei − mid-gap.

Solution.

(kT/2) ln(Nv/Nc) = (0.02585/2) × ln(1.04/2.8) = 0.0129 × (−0.990) = −0.0128 eV

Answer: Ei is 13 meV below mid-gap, because the valence band has fewer effective states (Nv < Nc), so EF must sit a little closer to it to make p equal n.

## Objectives check

Use this table to confirm you have met this week's objectives. Cover the Answer column and answer each check question from memory. If you cannot, go back to the section in the last column before moving on.

| # | Objective | Check yourself | Answer | Where it is taught |
| --- | --- | --- | --- | --- |
| 1 | Define and use the Fermi–Dirac distribution function. | Find the probability that a state 0.2 eV above EF is occupied at 300 K. | f = 1/(1 + e0.2/0.02585) = 1/(1 + 2290) = 4.4×10−4. | Section 1 |
| 2 | Explain the physical meaning of the Fermi level and the shape of f(E) at 0 K. | What is f(E) below and above EF at 0 K? | 1 below EF, 0 above: a sharp step. | Section 1 |
| 3 | Explain the density of states and the effective density of states. | Why are there no carriers in the band gap even though f(E) is not zero there? | The density of states is zero in the gap: there are no states to occupy. | Section 2 |
| 4 | Calculate electron and hole concentrations and apply the mass action law. | Si with NA = 1015 cm−3: find p and n (ni = 1010 cm−3). | p = 1015, n = 105 cm−3. | Sections 7–8, 12, 15–16 (comparison table); Examples 5.3, 5.5 |
| 5 | Determine the position of the Fermi level for given doping. | Find EF − Ei for ND = 1014 cm−3. | 0.02585 ln(104) = 0.238 eV. | Sections 9, 13; Examples 5.1, 5.4 |
| 6 | Apply the charge-neutrality condition, including compensated material. | Si has ND = 5×1016 and NA = 2×1016 cm−3. Find n. | n ≈ ND − NA = 3×1016 cm−3. | Section 14 |
| 7 | Explain the effect of temperature on carrier concentration and the Fermi level. | Name the three temperature regions and what n equals in the middle one. | Freeze-out, extrinsic (n ≈ ND), intrinsic. | Sections 17, 23; Example 5.2 |
| 8 | Distinguish degenerate and non-degenerate semiconductors. | When must full Fermi–Dirac statistics be used instead of the Boltzmann approximation? | When EF is within about 3kT of a band edge (very heavy doping). | Section 21 |

Week 6 · Module 2 · Energy Bands & Carrier Statistics

# Continuous Assessment Test 1 and Review

Plan: mid-module evaluation of crystal structures and carrier statistics (Weeks 1–5).

## Learning objectives

By the end of this week you should be able to:

- Revise crystal structures, Miller indices and bonding (Week 1).

- Revise energy bands and direct/indirect gaps (Week 4).

- Calculate occupation probabilities with the Fermi–Dirac function (Week 5).

- Calculate n, p and EF for doped and compensated silicon and germanium (Weeks 4–5).

This page has a one-screen review of what CAT 1 covers, followed by a practice test with full solutions. The questions are written in the style of the lecturer's revision questions and the PGD exam paper. They are practice questions, not the actual CAT.

## Symbols and abbreviations used this week

Every symbol, constant and abbreviation on this page is listed here, even if an earlier week already defined it, so you can study this page on its own.

Constants and units

| Symbol | Meaning | Units / typical value |
| --- | --- | --- |
| q | Magnitude of the electronic charge | 1.6×10−19 C |
| k | Boltzmann constant | 8.617×10−5 eV/K = 1.381×10−23 J/K |
| kT | Thermal energy | 0.0259 eV (often 0.02585 eV) at 300 K |
| T | Absolute temperature | kelvin (K); room temperature = 300 K |
| h | Planck constant | 6.626×10−34 J·s |
| eV | Electron-volt, a unit of energy | 1 eV = 1.6×10−19 J |
| Å | Ångström, a unit of length | 1 Å = 10−10 m = 0.1 nm |
| μm | Micrometre (micron) | 1 μm = 10−4 cm = 10−6 m |

Symbols

| Symbol | Meaning | Units / typical value |
| --- | --- | --- |
| Ec (EC) | Energy of the bottom of the conduction band | eV |
| Ev (EV) | Energy of the top of the valence band | eV |
| Eg | Band-gap energy, Ec − Ev | eV; Si 1.12, Ge 0.66, GaAs 1.42 at 300 K |
| EF | Fermi level: the energy at which a state has a 50 % chance of being occupied | eV |
| Ei | Intrinsic Fermi level, close to mid-gap | eV |
| f(E) | Fermi–Dirac function: probability that a state at energy E is occupied | dimensionless, 0 to 1 |
| Nc | Effective density of states in the conduction band | cm−3; Si 2.8×1019 at 300 K |
| Nv | Effective density of states in the valence band | cm−3; Si 1.04×1019 at 300 K |
| n | Electron concentration (free electrons per cm3) | cm−3 |
| p | Hole concentration (holes per cm3) | cm−3 |
| ni | Intrinsic carrier concentration (n = p = ni in pure material) | cm−3; Si ≈ 1×1010 at 300 K |
| ND | Donor concentration | cm−3 |
| NA | Acceptor concentration | cm−3 |
| k (wave vector) | Wave vector, 2π/λ; measures the electron's momentum, p = ħk | m−1 or cm−1 |
| α (Kronig–Penney) | √(2mE)/ħ, set by the electron energy | m−1 |
| P (Kronig–Penney) | Barrier strength mV0ba/ħ2 | dimensionless |
| λ | Wavelength | μm or nm; λ(μm) = 1.24/E(eV) |
| a | Lattice constant: edge length of the cubic unit cell | Å; Si 5.43, Ge and GaAs 5.65 |
| (h k l), {h k l} | Miller indices of a plane; family of equivalent planes | integers |
| dhkl | Spacing between neighbouring (h k l) planes, a/√(h2 + k2 + l2) | Å |
| rnn | Nearest-neighbour distance | Å; Si 2.35 |
| f (growth) | Fraction of the melt already solidified | 0 to 1 |
| μ, μn, μp | Mobility: drift velocity per unit field (electrons, holes) | cm2/(V·s); Si μn 1350, μp 480 |
| σ | Conductivity, q(nμn + pμp) (in Week 8, σ is also a capture cross-section) | S/cm (siemens per cm) |
| ρ | Resistivity, 1/σ | Ω·cm |
| λmax | Longest wavelength a material absorbs, 1.24/Eg (μm, Eg in eV) | μm |
| σi, ρi | Conductivity and resistivity of intrinsic (undoped) material; σdoped after doping | S/cm; Ω·cm |
| r (atom) | Atomic radius (hard-sphere model), half the nearest-neighbour distance | Å |

Abbreviations

| Abbreviation | Meaning |
| --- | --- |
| Si | Silicon |
| Ge | Germanium |
| GaAs | Gallium arsenide |
| GaN | Gallium nitride |
| InP | Indium phosphide |
| CB | Conduction band |
| VB | Valence band |
| APF | Atomic packing factor |
| LED | Light-emitting diode |
| CAT | Continuous Assessment Test |
| PGD | Postgraduate Diploma |

## Key terms

Every important word used this week is defined here, so you can read this week on its own.

Crystal lattice. A regular, endlessly repeating pattern of points in space; placing the same group of atoms (the basis) at every point builds the crystal.

Unit cell. The smallest block of the lattice that, repeated in all three directions, rebuilds the whole crystal. Atoms on its corners and faces are shared with neighbouring cells (a corner atom counts ⅛, a face atom ½).

Lattice constant (a). The edge length of the cubic unit cell, measured in ångströms (Å). For Si a = 5.43 Å; for Ge and GaAs a = 5.65 Å.

Diamond cubic structure. The crystal structure of Si and Ge: a cubic cell holding 8 atoms, each bonded covalently to 4 nearest neighbours (coordination number 4) at distance rnn = (√3/4)a. Zinc blende, the structure of GaAs, is the same arrangement with two kinds of atom alternating.

Miller indices (h k l). Three whole numbers that name a crystal plane: take the plane's intercepts on the axes in units of a, take reciprocals, and clear fractions. An intercept at infinity gives 0; a negative intercept is written with a bar, e.g. 1̄.

dhkl = a / √(h2 + k2 + l2)

Where:

- dhkl = spacing between neighbouring (h k l) planes (Å)

- a = lattice constant (Å)

- h, k, l = Miller indices (integers)

Atomic packing factor (APF). The fraction of the unit-cell volume filled by atoms, treated as hard spheres that touch their nearest neighbours.

APF = (atoms per cell × (4/3)πr3) / a3

Where:

- r = atomic radius, half the nearest-neighbour distance (Å)

- a = lattice constant (Å)

Valence band and conduction band (Ev, Ec). The valence band is the highest range of electron energies that is normally full, holding the bonding electrons; its top edge is Ev. The conduction band is the next range above it, normally almost empty; its bottom edge is Ec. Electrons in the conduction band move freely and carry current.

Band gap (Eg). The range of energies between Ev and Ec in which no electron states exist in a perfect crystal; its width Eg = Ec − Ev is the energy needed to free an electron from a bond (1.12 eV for Si, 0.66 eV for Ge, 1.42 eV for GaAs).

Why it matters: a wider gap means far fewer thermally freed carriers, which is why intrinsic Si is about 104 times more resistive than intrinsic Ge.

Direct and indirect band gap. In a direct-gap semiconductor (GaAs, GaN, InP) the conduction-band minimum and valence-band maximum occur at the same electron momentum (wave vector k), so an electron can fall across the gap and emit a photon on its own. In an indirect-gap semiconductor (Si, Ge) they occur at different k, so a lattice vibration (phonon) must also take part, and light emission is weak. The photon energy at the gap fixes the wavelength:

λ = 1.24 / Eg

Where:

- λ = wavelength of light emitted or absorbed at the band edge (μm)

- Eg = band-gap energy (eV)

Hole. An empty state in the valence band, left when an electron leaves a bond. It behaves as a positive carrier of charge +q.

Fermi level (EF). The energy at which an electron state has exactly a 50 % chance of being occupied. Its position between Ev and Ec sets how many electrons and holes there are.

Fermi–Dirac function (f(E)). The probability that an allowed state at energy E holds an electron in thermal equilibrium. When E − EF is more than about 3kT it can be replaced by the Boltzmann approximation f ≈ e−(E − EF)/kT.

f(E) = 1 / ( 1 + e(E − EF)/kT )

Where:

- f(E) = occupation probability, 0 to 1 (dimensionless)

- E = energy of the state (eV)

- EF = Fermi level (eV)

- kT = thermal energy, 0.0259 eV at 300 K (k = 8.617×10−5 eV/K)

Why it matters: 1 − f(E) is the probability of a hole, and f combined with the number of states gives n and p.

Intrinsic semiconductor (ni). A pure semiconductor whose free electrons and holes come only from broken bonds, so n = p = ni, the intrinsic carrier concentration (1×1010 cm−3 for Si and 2.4×1013 cm−3 for Ge at 300 K). Its Fermi level, the intrinsic level Ei, lies close to mid-gap.

Doping and compensation. Doping is adding a small, controlled amount of impurity: donors (e.g. P) give electrons and make the material n-type; acceptors (e.g. B) create holes and make it p-type. When both are present they partly cancel (compensation), and the material behaves as if doped with the difference, ND − NA or NA − ND.

Majority and minority carriers. The majority carrier is the more numerous carrier type (electrons in n-type, holes in p-type); the minority carrier is the less numerous one.

Mass action law. In thermal equilibrium the product of electron and hole concentrations is fixed at a given temperature, whatever the doping.

n p = ni2

Where:

- n, p = electron and hole concentrations (cm−3)

- ni = intrinsic carrier concentration (cm−3)

Why it matters: it gives the minority concentration as soon as the majority concentration is known.

Mobility and conductivity (μ, σ). Mobility is the drift speed a carrier reaches per unit electric field, in cm2/(V·s). Conductivity measures how easily the material carries current; resistivity ρ = 1/σ is its inverse.

σ = q (n μn + p μp)

Where:

- σ = conductivity (S/cm); ρ = 1/σ (Ω·cm)

- q = electronic charge, 1.6×10−19 C

- n, p = electron and hole concentrations (cm−3)

- μn, μp = electron and hole mobilities (cm2/(V·s)); Si 1350 and 480, Ge 3900 and 1900

## Review: what you must be able to do

Crystals (Week 1)

- Define lattice, basis, unit cell, lattice constant, coordination number, APF.

- State the structures: Si and Ge diamond cubic, GaAs zinc blende; 8 atoms per cell; 4 nearest neighbours.

- Find Miller indices from intercepts (intercepts → reciprocals → clear fractions); handle ∞ (index 0) and negative intercepts (bar).

- Use dhkl = a/√(h2 + k2 + l2).

Materials and bonding (Week 1)

- Compare conductors, semiconductors and insulators; Si, Ge and GaAs.

- Explain covalent bonding, electron–hole pairs, n-type and p-type doping.

Bands and statistics (Weeks 4–5)

- Schrödinger equation terms; Kronig–Penney: allowed bands where |P sin(αa)/αa + cos αa| ≤ 1.

- Direct and indirect gaps; λ(μm) = 1.24/Eg(eV).

- f(E) = 1/(1 + e(E−EF)/kT); at 0 K a step; Boltzmann approximation for E − EF > 3kT.

- n = Nc e−(Ec−EF)/kT, p = Nv e−(EF−Ev)/kT, ni = √(NcNv)e−Eg/2kT, np = ni2.

- Charge neutrality and compensation; EF − Ei = kT ln(n/ni).

Also revise: the lecturer's own mid-module evaluation (ten short-answer and five calculation questions on carrier statistics) is solved at the end of Week 5, section 26.

## Practice test (60 minutes)

Use q = 1.6×10−19 C, kT = 0.0259 eV at 300 K, Si: ni = 1×1010 cm−3, Nc = 2.8×1019 cm−3, μn = 1350, μp = 480 cm2/V·s; Ge: ni = 2.4×1013 cm−3, μn = 3900, μp = 1900 cm2/V·s.

- Silicon has lattice constant 5.43 Å. Calculate (a) the number of atoms per cm3 and (b) the nearest-neighbour distance.

- Find the Miller indices of planes with intercepts (a) 3a, 2b, c and (b) a, −b, ∞. For (a), find the interplanar spacing in Si.

- Show that the atomic packing factor of the diamond structure is 0.34.

- State three differences between direct and indirect band-gap semiconductors and give the emission wavelength of GaAs.

- Find the probability that a state (a) 0.1 eV above EF and (b) kT above EF is occupied at 300 K.

- At what temperature is there a 10−4 probability that a state 0.30 eV above EF is occupied?

- In a Si sample at 300 K the Fermi level is 0.25 eV below Ec. Find n and p. Is it n- or p-type?

- Si is doped with NA = 1×1016 cm−3 and ND = 3×1015 cm−3. Find n, p and the Fermi level position at 300 K.

- Germanium is doped with ND = 1×1015 cm−3. Find n and p at 300 K, without assuming ni is negligible.

- Calculate the conductivity and resistivity of intrinsic germanium at 300 K.

## Solutions

### 1. Atom density and nearest neighbours in Si

Question. Silicon has lattice constant 5.43 Å. Calculate (a) the number of atoms per cm3 and (b) the nearest-neighbour distance.

Given: a = 5.43 Å = 5.43×10−8 cm; diamond cubic structure, 8 atoms per unit cell.

Find: (a) atom density N, (b) nearest-neighbour distance rnn.

Formula:

N = (atoms per cell)/a3, rnn = (√3/4)a

Solution.

The diamond unit cell holds 8 atoms (8 corners × ⅛ + 6 faces × ½ + 4 inside).

(a) N = 8/a3 = 8/(5.43×10−8 cm)3 = 8/(1.601×10−22 cm3) = 5.0×1022 atoms/cm3

(b) rnn = (√3/4)a = 0.433 × 5.43 Å = 2.35 Å

Answer: (a) N = 5.0×1022 atoms/cm3; (b) rnn = 2.35 Å.

What this means: a typical doping of 1016 cm−3 replaces only one silicon atom in every 5 million, yet it changes the conductivity enormously. The 2.35 Å spacing is the length of each covalent Si–Si bond.

### 2. Miller indices

Question. Find the Miller indices of planes with intercepts (a) 3a, 2b, c and (b) a, −b, ∞. For (a), find the interplanar spacing in Si.

Given: intercepts (a) 3, 2, 1 and (b) 1, −1, ∞ (in units of a); a = 5.43 Å.

Find: the Miller indices of each plane, and d for plane (a).

Formula: take reciprocals of the intercepts and clear fractions; then

dhkl = a/√(h2 + k2 + l2)

Solution.

|  | x | y | z |
| --- | --- | --- | --- |
| (a) Intercepts | 3 | 2 | 1 |
| Reciprocals | 1/3 | 1/2 | 1 |
| × 6 | 2 | 3 | 6 |

(a) (2 3 6). d236 = 5.43/√(4 + 9 + 36) = 5.43/7 = 0.776 Å.

(b) Intercepts 1, −1, ∞ → reciprocals 1, −1, 0 → (1 1̄ 0), a plane parallel to z.

Answer: (a) (2 3 6), d236 = 0.776 Å; (b) (1 1̄ 0).

What this means: high-index planes such as (2 3 6) lie very close together (less than 1 Å apart, about a third of the bond length) but each holds few atoms, whereas low-index planes such as (1 1̄ 0) are widely spaced (5.43/√2 = 3.84 Å) and densely packed with atoms.

### 3. Packing factor of diamond

Question. Show that the atomic packing factor of the diamond structure is 0.34.

Given: diamond cubic cell with 8 atoms; nearest neighbours touch at distance (√3/4)a.

Find: APF.

Formula:

APF = (atoms per cell × (4/3)πr3) / a3, r = rnn/2 = (√3/8)a

Solution.

Nearest neighbours touch along the body diagonal at distance (√3/4)a, so the atomic radius is r = (√3/8)a. With 8 atoms per cell:

APF = 8 × (4/3)πr3 / a3 = 8 × (4/3)π (√3/8)3 = (32π/3)(3√3/512) = π√3/16 = 0.34

Answer: APF = π√3/16 = 0.34.

What this means: only 34 % of the volume is filled (compared with 74 % for close-packed metals), an open structure that allows interstitial impurities to fit between the atoms.

### 4. Direct and indirect gaps

Question. State three differences between direct and indirect band-gap semiconductors and give the emission wavelength of GaAs.

Given: Eg(GaAs) = 1.42 eV (direct gap).

Find: three differences; the emission wavelength λ of GaAs.

Formula:

λ (μm) = 1.24 / Eg (eV)

Solution.

(1) In a direct gap the conduction-band minimum and valence-band maximum are at the same k; in an indirect gap they are at different k. (2) Direct transitions need only a photon; indirect transitions also need a phonon. (3) Direct-gap materials emit light efficiently (GaAs, GaN, InP: LEDs, lasers); indirect ones do not (Si, Ge). Also: absorption near Eg is strong in direct-gap and weak in indirect-gap material; radiative lifetime is ns in direct and much longer in indirect.

| Feature | Direct gap | Indirect gap |
| --- | --- | --- |
| CB minimum and VB maximum | Same k | Different k |
| What a band-to-band transition needs | A photon only | A photon and a phonon |
| Light emission | Efficient | Very weak |
| Absorption near Eg | Strong | Weak |
| Radiative lifetime | Nanoseconds | Much longer |
| Examples | GaAs, GaN, InP | Si, Ge |

GaAs: λ = 1.24/1.42 = 0.873 μm (near infrared)

Answer: see the table; GaAs emits at λ = 0.873 μm.

What this means: 0.873 μm is just beyond the red end of visible light (about 0.7 μm), which is why GaAs LEDs are used for infrared remote controls and optical links rather than for visible displays.

### 5. Occupation probabilities

Question. Find the probability that a state (a) 0.1 eV above EF and (b) kT above EF is occupied at 300 K.

Given: (a) E − EF = 0.1 eV, (b) E − EF = kT; kT = 0.0259 eV.

Find: f(E) in each case.

Formula:

f(E) = 1/(1 + e(E − EF)/kT)

Solution.

(a) f = 1/(1 + e0.1/0.0259) = 1/(1 + e3.861) = 1/(1 + 47.5) = 0.0206
(b) f = 1/(1 + e1) = 1/3.718 = 0.269

Answer: (a) f = 0.0206 (about 2 %); (b) f = 0.269 (about 27 %).

What this means: moving from 1kT to about 4kT above EF cuts the occupation probability more than tenfold; occupation falls off steeply within a tenth of an eV of the Fermi level.

### 6. Temperature for a given probability

Question. At what temperature is there a 10−4 probability that a state 0.30 eV above EF is occupied?

Given: f = 10−4, E − EF = 0.30 eV, k = 8.617×10−5 eV/K.

Find: T.

Formula:

f ≈ e−(E − EF)/kT ⇒ kT = (E − EF)/ln(1/f)

Solution.

Since f is small, use the Boltzmann form: f ≈ e−(E − EF)/kT = 10−4.

0.30/kT = ln(104) = 9.21 ⇒ kT = 0.0326 eV
T = 0.0326/8.617×10−5 = 378 K

(The exact form 1/(1 + ex) = 10−4 gives x = 9.21 as well, to three figures.)

Answer: T ≈ 378 K (about 105 °C).

What this means: a modest rise above room temperature (300 K) is enough to make a state 0.3 eV above EF noticeably occupied, showing how sensitive carrier numbers are to temperature.

### 7. Carrier densities from EF

Question. In a Si sample at 300 K the Fermi level is 0.25 eV below Ec. Find n and p. Is it n- or p-type?

Given: Ec − EF = 0.25 eV, Nc = 2.8×1019 cm−3, ni = 1×1010 cm−3, kT = 0.0259 eV.

Find: n, p and the type.

Formula:

n = Nc e−(Ec − EF)/kT, p = ni2/n

Solution.

n = Nc e−(Ec−EF)/kT = 2.8×1019 × e−0.25/0.0259 = 2.8×1019 × e−9.65
= 2.8×1019 × 6.4×10−5 = 1.8×1015 cm−3
p = ni2/n = 1020/1.8×1015 = 5.6×104 cm−3

Answer: n = 1.8×1015 cm−3, p = 5.6×104 cm−3. n ≫ p, so the sample is n-type (doped with about 1.8×1015 cm−3 donors).

What this means: the Fermi level sits about 0.31 eV above mid-gap, which corresponds to light n-type doping; the electrons outnumber the holes by about 3×1010 to one.

### 8. Compensated silicon

Question. Si is doped with NA = 1×1016 cm−3 and ND = 3×1015 cm−3. Find n, p and the Fermi level position at 300 K.

Given: NA = 1×1016 cm−3, ND = 3×1015 cm−3, ni = 1×1010 cm−3, kT = 0.0259 eV.

Find: n, p and Ei − EF.

Formula:

p ≈ NA − ND, n = ni2/p, Ei − EF = kT ln(p/ni)

Solution.

NA > ND, so the material is p-type with net doping NA − ND = 7×1015 cm−3 ≫ ni.

p ≈ 7×1015 cm−3
n = ni2/p = 1020/7×1015 = 1.4×104 cm−3
Ei − EF = kT ln(p/ni) = 0.0259 × ln(7×105) = 0.0259 × 13.46 = 0.349 eV

Answer: p = 7×1015 cm−3, n = 1.4×104 cm−3; the Fermi level is 0.349 eV below Ei.

What this means: the donors cancel 30 % of the acceptors, so the sample behaves as p-type silicon with 7×1015 cm−3 acceptors. Both dopants still scatter carriers, however, so the mobility is that for 1.3×1016 cm−3 total impurities.

### 9. Lightly doped germanium

Question. Germanium is doped with ND = 1×1015 cm−3. Find n and p at 300 K, without assuming ni is negligible.

Given: ND = 1×1015 cm−3, NA = 0, ni(Ge) = 2.4×1013 cm−3.

Find: n and p.

Formula:

n = ND/2 + √( (ND/2)2 + ni2 ), p = ni2/n

Solution.

ni = 2.4×1013 is not negligible compared with ND = 1015, so use the exact neutrality solution:

n = ND/2 + √((ND/2)2 + ni2) = 5×1014 + √(2.5×1029 + 5.76×1026)
= 5×1014 + 5.006×1014 = 1.0006×1015 cm−3
p = ni2/n = 5.76×1026/1.0006×1015 = 5.76×1011 cm−3

Answer: n = 1.0006×1015 cm−3 ≈ ND, p = 5.76×1011 cm−3.

What this means: n is still essentially ND, but the minority concentration (5.8×1011 cm−3) is about 6×106 times larger than in silicon with the same doping (105 cm−3): this is why Ge diodes leak so much.

### 10. Intrinsic germanium

Question. Calculate the conductivity and resistivity of intrinsic germanium at 300 K.

Given: n = p = ni = 2.4×1013 cm−3, μn = 3900, μp = 1900 cm2/V·s, q = 1.6×10−19 C.

Find: σi and ρi.

Formula:

σi = q ni (μn + μp), ρi = 1/σi

Solution.

σi = q ni (μn + μp) = 1.6×10−19 × 2.4×1013 × (3900 + 1900)
= 1.6×10−19 × 1.392×1017 = 0.0223 S/cm
ρi = 1/σi = 44.9 Ω·cm

Answer: σi = 0.0223 S/cm, ρi = 44.9 Ω·cm.

What this means: for comparison, intrinsic Si is about 3×105 Ω·cm, nearly 104 times higher, because its band gap is larger (1.12 eV against 0.66 eV) and so far fewer carriers are thermally freed.

## Practice questions

These extra questions practise this week's ideas. Work each one on paper before reading the solution; the calculation questions follow the same Question, Given, Find, Solution, Answer layout as the worked examples.

#### Practice 6.1: intercepts from Miller indices

Question. A plane has Miller indices (1 2 3). Find a set of intercepts it makes on the axes.

Given: (h k l) = (1 2 3).

Find: intercepts.

Solution. Intercepts are the reciprocals of the indices: 1, 1/2, 1/3. Multiplying by 6 to clear fractions gives an equivalent parallel plane.

Answer: a, b/2, c/3 (or, equivalently, 6a, 3b, 2c).

#### Practice 6.2: band gap from an absorption edge

Question. A semiconductor stops absorbing light at wavelengths longer than 1.1 μm. Estimate its band gap.

Given: λmax = 1.1 μm.

Find: Eg.

Solution.

Eg = 1.24/λ = 1.24/1.1 = 1.13 eV

Answer: Eg ≈ 1.13 eV (silicon).

#### Practice 6.3: hole concentration from the Fermi level

Question. In p-type silicon at 300 K the Fermi level is 0.10 eV above the valence band. Find the hole concentration.

Given: EF − Ev = 0.10 eV, Nv = 1.04×1019 cm−3, kT = 0.0259 eV.

Find: p.

Solution.

p = Nv e−(EF − Ev)/kT = 1.04×1019 × e−3.86 = 1.04×1019 × 0.0211 = 2.2×1017 cm−3

Answer: p = 2.2×1017 cm−3.

#### Practice 6.4: probability of a hole

Question. What is the probability that a state 0.05 eV below the Fermi level is empty (holds a hole) at 300 K?

Given: E = EF − 0.05 eV, kT = 0.0259 eV.

Find: 1 − f(E).

Solution.

1 − f = 1 − 1/(1 + e−0.05/0.0259) = 1/(1 + e0.05/0.0259) = 1/(1 + 6.89) = 0.127

Answer: 12.7 %.

#### Practice 6.5: short-answer revision

Question. (a) State the mass-action law. (b) What is the coordination number of the diamond structure? (c) Name the structure of GaAs. (d) Which carrier is the minority carrier in boron-doped silicon?

Answer. (a) np = ni2 in thermal equilibrium. (b) 4. (c) Zinc blende. (d) Electrons.

## Objectives check

Use this table to confirm you have met this week's objectives. Cover the Answer column and answer each check question from memory. If you cannot, go back to the section in the last column before moving on.

| # | Objective | Check yourself | Answer | Where it is taught |
| --- | --- | --- | --- | --- |
| 1 | Revise crystal structures, Miller indices and bonding (Week 1). | Find the Miller indices for intercepts 2a, 2b, 4c. | 1/2, 1/2, 1/4 → × 4 → (2 2 1). | Review; practice Q1–Q3 |
| 2 | Revise energy bands and direct/indirect gaps (Week 4). | State one property that distinguishes a direct-gap semiconductor. | Efficient light emission (also: CB minimum and VB maximum at the same k). | Practice Q4 |
| 3 | Calculate occupation probabilities with the Fermi–Dirac function (Week 5). | What is f at E = EF + kT? | 1/(1 + e) = 0.269. | Practice Q5–Q6 |
| 4 | Calculate n, p and EF for doped and compensated silicon and germanium (Weeks 4–5). | Si with EF 0.25 eV below Ec: n-type or p-type? | n-type (n = 1.8×1015 cm−3). | Practice Q7–Q10 |

Week 7 · Module 3 · Carrier Transport & Injection Phenomena

# Drift and Diffusion Currents

Plan: carrier mobility, scattering mechanisms and conductivity; diffusion of carriers, Fick's law and the Einstein relation.

## Learning objectives

By the end of this week you should be able to:

- Explain thermal motion, drift velocity and mobility.

- Explain the scattering mechanisms and the factors that affect mobility.

- Derive and use the drift current density and conductivity.

- Explain carrier diffusion and calculate diffusion current with Fick's law.

- State, explain and use the Einstein relation.

## Symbols and abbreviations used this week

Every symbol, constant and abbreviation on this page is listed here, even if an earlier week already defined it, so you can study this page on its own.

Constants and units

| Symbol | Meaning | Units / typical value |
| --- | --- | --- |
| q | Magnitude of the electronic charge | 1.6×10−19 C |
| k | Boltzmann constant | 8.617×10−5 eV/K = 1.381×10−23 J/K |
| kT | Thermal energy | 0.0259 eV (often 0.02585 eV) at 300 K |
| kT/q | Thermal voltage | 0.0259 V (about 26 mV) at 300 K |
| T | Absolute temperature | kelvin (K); room temperature = 300 K |
| m0 | Free-electron mass | 9.11×10−31 kg |
| eV | Electron-volt, a unit of energy | 1 eV = 1.6×10−19 J |
| μm | Micrometre (micron) | 1 μm = 10−4 cm = 10−6 m |

Symbols

| Symbol | Meaning | Units / typical value |
| --- | --- | --- |
| Ec (EC) | Energy of the bottom of the conduction band | eV |
| Eg | Band-gap energy, Ec − Ev | eV; Si 1.12, Ge 0.66, GaAs 1.42 at 300 K |
| EF | Fermi level: the energy at which a state has a 50 % chance of being occupied | eV |
| Ei | Intrinsic Fermi level, close to mid-gap | eV |
| Nc | Effective density of states in the conduction band | cm−3; Si 2.8×1019 at 300 K |
| n | Electron concentration (free electrons per cm3) | cm−3 |
| p | Hole concentration (holes per cm3) | cm−3 |
| ni | Intrinsic carrier concentration (n = p = ni in pure material) | cm−3; Si ≈ 1×1010 at 300 K |
| ND | Donor concentration | cm−3 |
| NA | Acceptor concentration | cm−3 |
| Δn, Δp | Excess electron and hole concentrations above equilibrium | cm−3 |
| m∗, mn∗, mp∗ | Effective mass of electrons or holes | kg, or as a multiple of m0 |
| C(x, t) | Dopant concentration at depth x and time t | cm−3 |
| D | Diffusion coefficient (dopants in a furnace, or carriers) | cm2/s |
| F | Particle flux in Fick's law | particles/(cm2·s) |
| Rs | Sheet resistance (or diode series resistance in Week 12) | Ω/□ (ohms per square); Ω |
| E (field) | Electric field (on band diagrams, E is energy instead) | V/cm |
| μ, μn, μp | Mobility: drift velocity per unit field (electrons, holes) | cm2/(V·s); Si μn 1350, μp 480 |
| μL, μI | Mobility limited by lattice scattering, by ionised-impurity scattering | cm2/(V·s) |
| vd | Drift velocity | cm/s |
| vth | Thermal velocity of carriers | ≈ 107 cm/s at 300 K |
| vsat | Saturation velocity at high field | ≈ 107 cm/s in Si |
| τm | Mean free time between collisions | s; about 0.1–1 ps |
| σ | Conductivity, q(nμn + pμp) (in Week 8, σ is also a capture cross-section) | S/cm (siemens per cm) |
| ρ | Resistivity, 1/σ | Ω·cm |
| J, Jn, Jp | Current density (total, electrons, holes) | A/cm2 |
| Dn, Dp | Diffusion coefficients of electrons and holes | cm2/s; Si 35 and 12.4 |
| RH, VH, B | Hall coefficient, Hall voltage, magnetic flux density | cm3/C; V; T (Wb/m2) |
| R | Recombination rate | cm−3s−1 |
| τ, τn, τp | Minority-carrier lifetime (τeff: effective, including surfaces) | s; Si 1 ns – 1 ms |
| L, Ln, Lp | Diffusion length √(Dτ): distance a minority carrier travels before recombining | μm or cm |
| I | Current | A |
| A (area) | Device or contact area | cm2 |
| σi, ρi | Conductivity and resistivity of intrinsic (undoped) material; σdoped after doping | S/cm; Ω·cm |
| Fn, Fp | Particle flux of electrons and holes (carriers crossing 1 cm2 per second) | cm−2s−1 |
| Bz, Ix, VH | Hall effect: magnetic field (z), current (x) and Hall voltage | T (tesla); A; V |
| RH | Hall coefficient, 1/qp (p-type) or −1/qn (n-type) | cm3/C |
| vdn, vdp | Drift velocity of electrons and holes | cm/s |
| μi, τi (μL, μI, NI) | Mobility and scattering time for one scattering mechanism (L: lattice, I: ionised impurity); NI = ionised-impurity density | cm2/(V·s); s; cm−3 |
| Jdrift, Jdiff | Drift and diffusion parts of the current density | A/cm2 |
| B (recombination) | Radiative recombination coefficient, R = B np | cm3/s; GaAs ≈ 10−10, Si ≈ 10−14 |
| t | Time (or a thickness, where the text says so) | s (or cm) |

Abbreviations

| Abbreviation | Meaning |
| --- | --- |
| Si | Silicon |
| Ge | Germanium |
| GaAs | Gallium arsenide |
| SiO2 | Silicon dioxide (silica), the oxide insulator |
| MOSFET | Metal–oxide–semiconductor field-effect transistor |
| BJT | Bipolar junction transistor |

## Key terms

Every important word used this week is defined here, so you can read this week on its own.

Band gap (Eg). The range of energies that an electron in a crystal cannot have. It lies between the valence band (the band of energies occupied by the electrons that form the bonds between atoms) and the conduction band (the next band up, where electrons are free to move through the crystal). For silicon Eg = 1.12 eV at 300 K.

Electron and hole (carriers). A free electron is an electron in the conduction band; a hole is an empty place left in the valence band, which behaves like a positive charge +q that can move. Together they are called carriers because they carry the current.

Why it matters: every current this week is a flow of electrons, of holes, or of both.

Doping (ND, NA). Adding small, controlled amounts of impurity atoms to a semiconductor. Donor atoms (concentration ND, e.g. phosphorus in Si) give free electrons and make the material n-type; acceptor atoms (concentration NA, e.g. boron) give holes and make it p-type.

Majority and minority carriers. The majority carriers are the more numerous type (electrons in n-type, holes in p-type); the minority carriers are the less numerous type.

Fermi level (EF). The energy at which an electron state has a 50 % chance of being occupied. In thermal equilibrium (no battery, no light) it is the same everywhere in the material: it is "flat".

Thermal velocity (vth). The average speed of the random motion that carriers have because of heat, about 107 cm/s in silicon at 300 K. Because the directions are random, it gives no current on its own.

Scattering and mean free time (τm). Scattering is a collision of a carrier with a vibrating atom, an impurity ion or a defect, which randomises its direction. The mean free time τm is the average time between collisions, about 0.1–1 ps.

Effective mass (m∗). The mass a carrier appears to have when it is pushed by a force inside the crystal. It is usually written as a multiple of the free-electron mass m0 (e.g. 0.067m0 for GaAs electrons). A small effective mass means the carrier is easy to accelerate.

Drift and drift velocity (vd). Drift is the movement of carriers caused by an electric field. The drift velocity vd is the small, steady average velocity in the field direction that is added on top of the random thermal motion.

Mobility (μ). The drift velocity a carrier gains per unit electric field: it measures how easily the carrier moves through the crystal.

μ = vd / E = qτm / m∗

Where:

- μ = mobility (cm2/V·s); Si: μn = 1350, μp = 480

- vd = drift velocity (cm/s)

- E = electric field (V/cm)

- q = electronic charge, 1.6×10−19 C

- τm = mean free time between collisions (s)

- m∗ = effective mass (kg)

Why it matters: mobility sets both the conductivity of a material and the speed of the devices made from it.

Current density (J). The electric current flowing through each square centimetre of cross-section, in A/cm2. The current is I = JA, where A is the cross-sectional area.

Conductivity and resistivity (σ, ρ). Conductivity σ measures how well a material conducts; resistivity ρ = 1/σ measures how strongly it opposes current. Both depend on how many carriers there are and on their mobilities.

σ = q(nμn + pμp), ρ = 1/σ

Where:

- σ = conductivity (S/cm)

- ρ = resistivity (Ω·cm)

- q = electronic charge, 1.6×10−19 C

- n, p = electron and hole concentrations (cm−3)

- μn, μp = electron and hole mobilities (cm2/V·s)

Diffusion (Fick's law). The net flow of particles from where there are more of them to where there are fewer, caused only by their random motion. Fick's law says the flow is proportional to the concentration gradient.

F = −D dC/dx

Where:

- F = particle flux: particles crossing 1 cm2 per second (cm−2s−1)

- D = diffusion coefficient (cm2/s)

- C = concentration of the particles (cm−3); for carriers, C is n or p

- x = position (cm)

Why it matters: diffusion carries the current in the neutral regions of a diode and across the base of a bipolar transistor.

Diffusion coefficient (D). The constant in Fick's law that measures how quickly particles spread out by random motion, in cm2/s. For carriers in Si at 300 K, Dn ≈ 35 cm2/s and Dp ≈ 12.4 cm2/s.

Thermal voltage (kT/q). The thermal energy kT expressed as a voltage: 0.0259 V (about 26 mV) at 300 K. It sets the voltage scale of almost every semiconductor equation.

Einstein relation. The rule that the diffusion coefficient and the mobility of a carrier are always in the same ratio, fixed only by temperature, because both are limited by the same collisions.

Dn / μn = Dp / μp = kT/q

Where:

- Dn, Dp = electron and hole diffusion coefficients (cm2/s)

- μn, μp = electron and hole mobilities (cm2/V·s)

- kT/q = thermal voltage, 0.0259 V at 300 K

Why it matters: measuring the mobility (which is easy) immediately gives the diffusion coefficient.

## The big picture

Weeks 4–5 told us how many carriers there are. This week asks how they move, because moving charge is current. There are exactly two reasons a carrier moves in a particular direction:

- Drift: an electric field pushes it. Like water flowing downhill because of gravity.

- Diffusion: there are more carriers in one place than another, and random motion spreads them out. Like a drop of ink spreading in still water (the same idea as dopant diffusion in Week 3, but for electrons and holes, and much faster).

Every current in every device in this course is drift, diffusion, or a mixture. At the end of the week we will see that the two are tied together by a surprisingly simple rule, the Einstein relation.

## Part A: Drift, mobility and conductivity

### Random thermal motion

Even with no voltage applied, electrons in a semiconductor are not still. At room temperature they rush about at the thermal velocity, about 107 cm/s (100 km/s), bouncing off vibrating atoms and impurities roughly every 0.1–1 picosecond (the mean free time τm). Their directions are random, so on average they go nowhere: no current.

### Drift in an electric field

Now apply an electric field E. Between collisions each electron is pushed by the field and gains a little extra speed in one direction. At each collision that extra speed is lost (the direction is randomised again). So on top of the random motion there is a small, steady average drift velocity:

vd = μE

Where:

- vd = drift velocity (cm/s)

- μ = mobility (cm2/V·s)

- E = electric field (V/cm)

For electrons the drift is against the field (they are negative); for holes it is along the field.

In plain words. Picture a crowd milling about randomly in a square. Tilt the square slightly. People still wander randomly, but on average the crowd now slides slowly downhill. The slow average slide is the drift velocity; the random wandering is much faster but cancels out.

### Mobility

The constant μ is the mobility: how much drift velocity you get per unit field.

μ = vd / E = qτm / m∗ [cm2/V·s]

Where:

- μ = mobility (cm2/V·s)

- vd = drift velocity (cm/s)

- E = electric field (V/cm)

- q = electronic charge, 1.6×10−19 C

- τm = mean free time between collisions (s)

- m∗ = effective mass of the carrier (kg)

From the formula, mobility is high when:

- collisions are rare (long τm): fewer things to bump into;

- the effective mass is small (m∗ small): the carrier is easy to accelerate.

| Material | μn (cm2/V·s) | μp (cm2/V·s) |
| --- | --- | --- |
| Si | 1350 | 480 |
| Ge | 3900 | 1900 |
| GaAs | 8500 | 400 |

Electrons are faster than holes in all three, mainly because of their smaller effective mass.

#### Example 7.1: drift velocity

Question. An electric field of 1000 V/cm is applied to a silicon sample. Calculate the drift velocity of the electrons and of the holes.

Given: E = 1000 V/cm, μn = 1350 cm2/V·s, μp = 480 cm2/V·s.

Find: vdn and vdp.

Formula:

vd = μE

Solution.

vdn = μnE = 1350 × 1000 = 1.35×106 cm/s
vdp = μpE = 480 × 1000 = 4.8×105 cm/s

Answer: electrons 1.35×106 cm/s, holes 4.8×105 cm/s, both far below the random thermal velocity of about 107 cm/s.

What this means: even in a fairly strong field the electrons' average drift is only about one-seventh of their random thermal speed, so the field only gently biases the random motion; this is why vd = μE (a constant mobility) still holds here. Holes drift almost three times more slowly than electrons in the same field.

### What scatters carriers

A perfectly regular, perfectly still crystal would not scatter electrons at all (Bloch's theorem, Week 4). Anything that breaks the perfect regularity causes scattering:

- Lattice (phonon) scattering. The atoms vibrate with heat. The hotter, the more they vibrate, and the more they scatter. Mobility falls as μL ∝ T−3/2.

- Ionised-impurity scattering. The charged donor and acceptor ions deflect passing carriers, like a magnet deflecting a passing steel ball. Slow carriers are deflected more, so this is worst at low temperature and high doping: μI ∝ T3/2/NI.

- Neutral-impurity scattering, important only at very low temperature.

- Carrier–carrier scattering, at very high carrier densities.

- Defect scattering from dislocations, grain boundaries and vacancies.

- Surface scattering. In a MOSFET channel, carriers are pressed against the rough Si/SiO2 surface; channel mobility is only about half the bulk value.

- Polar and alloy scattering in compound semiconductors and alloys.

When several mechanisms act, their scattering rates add, so the reciprocals of the mobilities add (Matthiessen's rule):

1/μ = 1/μL + 1/μI + …

Where:

- μ = total mobility (cm2/V·s)

- μL = mobility if only lattice scattering acted (cm2/V·s)

- μI = mobility if only ionised-impurity scattering acted (cm2/V·s)

- … = one more term for each further scattering mechanism

The lowest mobility dominates, just as the narrowest section of a pipe limits the flow.

Mobility against temperature. At low temperature impurity scattering limits mobility; at high temperature lattice scattering does. Heavier doping lowers the curve and moves its peak to higher temperature.

### What affects mobility (summary)

- Temperature: near room temperature, higher T → more lattice vibration → lower μ.

- Doping: more impurities → more scattering → lower μ (Si electrons: 1350 at light doping, about 800 at 1017, about 100 at 1020 cm−3).

- Effective mass: smaller m∗ → higher μ.

- Electric field: at very high fields μ falls (velocity saturation, Week 8).

- Crystal quality, surfaces, orientation and strain.

### Drift current density

Current density J is the charge crossing 1 cm2 per second. It equals (charge per carrier) × (number of carriers per cm3) × (their average speed). For electrons, the charge is −q and the velocity is −μnE; the two minus signs cancel:

Jn = (−q)(n)(−μnE) = qnμnE

For holes:

Jp = (+q)(p)(+μpE) = qpμpE

Electrons move against the field but carry negative charge, so their current is in the same direction as the hole current. The total drift current is

J = q(nμn + pμp) E = σE

Where:

- J = total drift current density (A/cm2)

- q = electronic charge, 1.6×10−19 C

- n, p = electron and hole concentrations (cm−3)

- μn, μp = electron and hole mobilities (cm2/V·s)

- E = electric field (V/cm)

- σ = conductivity (S/cm)

This is just Ohm's law, with conductivity and resistivity

σ = q(nμn + pμp), ρ = 1/σ

Where:

- σ = conductivity (S/cm)

- ρ = resistivity (Ω·cm)

- q, n, p, μn, μp as above

For n-type material n ≫ p, so σ ≈ qNDμn. For p-type, σ ≈ qNAμp.

#### Example 7.2: conductivity and resistance of a silicon bar

Question. A bar of n-type silicon doped with ND = 1×1016 cm−3 is 1 cm long and has a cross-section of 1 mm2. Calculate its conductivity, resistivity and resistance.

Given: ND = 1×1016 cm−3, μn = 1350 cm2/V·s, L = 1 cm, A = 1 mm2 = 0.01 cm2, q = 1.6×10−19 C.

Find: σ, ρ and R.

Formula:

σ ≈ qNDμn, ρ = 1/σ, R = ρL/A

Solution.

Step 1. n-type, so σ ≈ qNDμn:

σ = 1.6×10−19 × 1016 × 1350 = 2.16 S/cm

Step 2. ρ = 1/σ = 1/2.16 = 0.46 Ω·cm

Step 3. R = ρL/A:

R = 0.46 × 1 / 0.01 = 46 Ω

Answer: σ = 2.16 S/cm, ρ = 0.46 Ω·cm, R = 46 Ω.

What this means: only one atom in about five million is a donor (silicon has 5×1022 atoms per cm3), yet the bar's resistance drops from about 34 MΩ (undoped, σi = qni(μn + μp) = 2.9×10−6 S/cm) to 46 Ω. Doping is how we set the resistance of a semiconductor, and the 0.46 Ω·cm value is typical of the wafers used to make chips.

Sheet resistance. For a thin layer of thickness t, Rs = ρ/t in ohms per square (Ω/□), measured with a four-point probe (Week 3).

### Hall effect

Put a sample carrying current Ix in a magnetic field Bz. The magnetic force pushes the moving carriers sideways, so charge piles up on one side and a small Hall voltage VH appears across the sample. Its sign shows whether the carriers are electrons or holes, and its size gives their concentration:

RH = 1/qp (p-type, positive), RH = −1/qn (n-type, negative)

Where:

- RH = Hall coefficient (cm3/C), found from the measurement as RH = VH t/(IxBz)

- VH = Hall voltage (V)

- t = sample thickness along the magnetic field (cm)

- Ix = current through the sample (A)

- Bz = magnetic flux density (Wb/cm2; 1 T = 10−4 Wb/cm2)

- q = electronic charge, 1.6×10−19 C

- p, n = hole and electron concentrations (cm−3)

Combined with a resistivity measurement it gives the mobility, μ = |RH|σ. This is the standard way to measure carrier type, concentration and mobility.

## Part B: Diffusion, Fick's law and the Einstein relation

### Diffusion of carriers

Suppose there are more electrons on the left of a sample than on the right, for example because light shines on the left. Each electron moves randomly. With more of them on the left, more cross any plane from left to right than from right to left. There is a net flow towards the right, with no field at all. This is carrier diffusion.

The flow obeys Fick's law (the same law as in Week 3, now for carriers):

flux of electrons = −Dn dn/dx, flux of holes = −Dp dp/dx

Where:

- flux = number of carriers crossing 1 cm2 per second (cm−2s−1)

- Dn, Dp = electron and hole diffusion coefficients (cm2/s)

- dn/dx, dp/dx = gradients of the electron and hole concentrations (cm−4)

- the minus sign = the flow is from high concentration to low

Dn and Dp are the carrier diffusion coefficients (Si at 300 K: Dn ≈ 35 cm2/s, Dp ≈ 12 cm2/s). These are about 1014 times larger than dopant diffusion coefficients: carriers diffuse across a device in nanoseconds, while dopant atoms need hours in a furnace.

### Diffusion current density

Multiply each particle flux by the charge of the carrier:

Jn(diff) = (−q)(−Dn dn/dx) = +qDn dn/dx
Jp(diff) = (+q)(−Dp dp/dx) = −qDp dp/dx

Where:

- Jn(diff), Jp(diff) = electron and hole diffusion current densities (A/cm2)

- q = electronic charge, 1.6×10−19 C

- Dn, Dp = electron and hole diffusion coefficients (cm2/s)

- dn/dx, dp/dx = concentration gradients (cm−4)

Watch the signs. Both electrons and holes flow from high concentration to low. But because the electron charge is negative, the electron current points opposite to the electron flow, while the hole current points the same way as the hole flow.

Both carriers diffuse down their concentration gradient. Because electrons are negative, the electron diffusion current points against their flow, while the hole current points with it.

#### Example 7.3: electron diffusion current

Question. In a silicon sample the electron concentration falls linearly from 1×1017 cm−3 to zero over a distance of 1 μm. Taking Dn = 35 cm2/s, calculate the electron diffusion current density.

Given: Δn = 1×1017 cm−3 over Δx = 1 μm = 1×10−4 cm, Dn = 35 cm2/s, q = 1.6×10−19 C.

Find: Jn(diff).

Formula:

Jn(diff) = qDn dn/dx

Solution.

Step 1. The concentration gradient:

dn/dx = −1017 / 10−4 = −1021 cm−4

Step 2. Jn = qDn dn/dx:

Jn = 1.6×10−19 × 35 × (−1021) = −5.6×103 A/cm2

Answer: |Jn| = 5.6×103 A/cm2, flowing in the −x direction (opposite to the electron flow, because electrons are negative).

What this means: a large current, from a modest gradient: through a device area of 100 μm × 100 μm (10−4 cm2) it would be 0.56 A. Diffusion is not a small effect: it carries the whole current in a diode's neutral regions and in a transistor's base.

### The total current equations

When a field and a gradient are both present, simply add drift and diffusion:

Jn = qnμnE + qDn dn/dx
Jp = qpμpE − qDp dp/dx
J = Jn + Jp

Where:

- Jn, Jp, J = electron, hole and total current densities (A/cm2)

- q = electronic charge, 1.6×10−19 C

- n, p = electron and hole concentrations (cm−3)

- μn, μp = electron and hole mobilities (cm2/V·s)

- E = electric field (V/cm)

- Dn, Dp = electron and hole diffusion coefficients (cm2/s)

- dn/dx, dp/dx = concentration gradients (cm−4)

These two equations, together with the continuity equation (Week 9) and Poisson's equation, describe every semiconductor device.

### Drift and diffusion compared

|  | Drift | Diffusion |
| --- | --- | --- |
| Cause | An electric field E pushes the carriers | A difference in concentration (a gradient dn/dx or dp/dx); random motion spreads the carriers out |
| Needs a field? | Yes | No; it happens even with no field |
| Electron current | Jn = qnμnE | Jn = +qDn dn/dx |
| Hole current | Jp = qpμpE | Jp = −qDp dp/dx |
| Depends on | How many carriers there are (n, p) | How fast their number changes with position (dn/dx, dp/dx) |
| Material constant | Mobility μ (cm2/V·s) | Diffusion coefficient D (cm2/s) |
| Direction of carrier flow | Holes along E, electrons against E | Both from high to low concentration |
| Direction of current | Electron and hole currents both along E (they add) | Hole current along the hole flow; electron current opposite to the electron flow |
| Which carriers it usually matters for | Majority carriers (there are many of them) | Minority carriers (small numbers, but steep gradients) |
| Where it dominates | Resistors, the channel of a MOSFET, carriers swept across a reverse-biased junction | Neutral regions of a forward-biased diode, the base of a BJT, solar cells |
| Everyday picture | Water flowing downhill | Ink spreading in still water |

The two are tied together by the Einstein relation, D/μ = kT/q, because the same collisions limit both.

### The Einstein relation

Drift and diffusion are two responses of the same carriers to two different pushes, and both are limited by the same collisions. So it is no surprise that μ and D are related:

Dn / μn = Dp / μp = kT/q

Where:

- Dn, Dp = electron and hole diffusion coefficients (cm2/s)

- μn, μp = electron and hole mobilities (cm2/V·s)

- k = Boltzmann constant, 8.617×10−5 eV/K

- T = absolute temperature (K)

- q = electronic charge, 1.6×10−19 C

kT/q is the thermal voltage, 0.0259 V (about 26 mV) at 300 K.

Why it is true (the equilibrium argument). Take an n-type sample whose doping is higher on the left than on the right, and leave it alone (no battery).

- Electrons diffuse from the heavily doped left side towards the right.

- As they leave, they uncover positive donor ions on the left. Positive charge on the left and extra electrons on the right create an internal electric field.

- The field pulls electrons back to the left: a drift current opposite to the diffusion current.

- With no battery, no net current can flow, so in equilibrium drift exactly cancels diffusion: 0 = qnμnE + qDn dn/dx.

- In equilibrium the Fermi level is flat (Week 5). Using n = Nc e−(Ec − EF)/kT, the gradient dn/dx can be written in terms of the field: dn/dx = −(qn/kT)E.

- Substituting: 0 = qnμnE − qDn(qn/kT)E, which gives Dn/μn = kT/q.

Using it. Mobility is easy to measure (Hall effect, conductivity), so D follows immediately:

|  | μ (cm2/V·s) | D = μ × 0.0259 (cm2/s) |
| --- | --- | --- |
| Si electrons | 1350 | 35.0 |
| Si holes | 480 | 12.4 |
| GaAs electrons | 8500 | 220 |
| Ge electrons | 3900 | 101 |

In plain words. A carrier that rarely collides both drifts easily in a field (high μ) and spreads quickly by itself (high D). The ratio between the two depends only on temperature.

## Key points of Week 7

- Drift: vd = μE, with μ = qτ/m∗. Electrons are faster than holes; GaAs electrons are fastest.

- Mobility is limited by lattice scattering (worse when hot) and impurity scattering (worse when heavily doped); 1/μ = Σ1/μi.

- Drift current J = q(nμn + pμp)E = σE; σ ≈ qNDμn for n-type.

- Diffusion: carriers flow down their concentration gradient. Jn = qDn dn/dx, Jp = −qDp dp/dx.

- Total current = drift + diffusion.

- Einstein relation: D/μ = kT/q = 0.0259 V at 300 K.

## Examination questions solved (Q35–Q40)

### Q35. Define carrier mobility and explain the factors that affect electron and hole mobility in semiconductors.

Definition. Carrier mobility μ is the drift velocity acquired per unit applied electric field:

μ = |vd| / E = qτm / m∗ [cm2/V·s]

where τm is the mean free time between collisions and m∗ the effective mass. It measures how easily carriers move through the crystal under a field. Electron mobility μn and hole mobility μp are different (Si: 1350 and 480 cm2/V·s).

Factors affecting mobility:

- Effective mass. μ ∝ 1/m∗. Electrons generally have lighter effective mass than holes, so μn > μp. GaAs electrons (m∗ = 0.067m0) have μn ≈ 8500 cm2/V·s.

- Temperature. Two opposing effects: (a) Lattice scattering increases with T, μL ∝ T−3/2. (b) Ionised-impurity scattering decreases with T, μI ∝ T3/2/NI, since faster carriers are deflected less. Mobility therefore rises at low T, peaks, and falls at high T. Near room temperature lattice scattering usually dominates and μ falls as T rises.

- Doping (impurity) concentration. More ionised impurities mean more Coulomb scattering: μ falls as ND + NA increases (Si μn ≈ 1350 at 1014 cm−3 but about 100 at 1020 cm−3). Compensated material has low mobility even though net doping is small.

- Electric field. At low field μ is constant. At high field carriers heat up, emit optical phonons, and drift velocity saturates, so the effective mobility vd/E falls.

- Crystal defects (dislocations, grain boundaries, vacancies) add scattering; polycrystalline and amorphous material have much lower mobility.

- Surface and interface scattering. In MOSFET channels, roughness and interface charge reduce mobility to roughly half the bulk value, and it falls further with higher gate field.

- Crystal orientation and strain. Mobility depends on direction in anisotropic bands; strain alters effective masses (strained-Si technology).

- Carrier concentration at high injection (carrier–carrier scattering).

These are combined using Matthiessen's rule, 1/μ = 1/μL + 1/μI + …

### Q36. Explain the mechanisms responsible for carrier scattering in semiconductor materials.

In a perfectly periodic, motionless lattice an electron would move without scattering (Bloch's theorem). Scattering happens whenever something breaks that perfect periodicity. The main mechanisms:

- Lattice (phonon) scattering. Above 0 K the atoms vibrate about their positions, distorting the periodic potential. Carriers exchange energy and momentum with these lattice vibrations (phonons). Acoustic-phonon scattering is low-energy and nearly elastic, dominant at room temperature in Si; its rate increases with T, giving μL ∝ T−3/2. Optical-phonon scattering involves high-energy phonons (63 meV in Si); it matters at high temperatures and high fields and causes velocity saturation. Polar-optical and piezoelectric scattering occur in compound semiconductors (GaAs), where the vibrating ionic bonds create electric fields that scatter carriers strongly.

- Ionised-impurity scattering. Ionised donors (+) and acceptors (−) have Coulomb fields that deflect passing carriers (Rutherford-like scattering). Slower carriers spend more time near the ion and are deflected more, so it is strongest at low temperature and high doping: μI ∝ T3/2/NI.

- Neutral-impurity scattering. Non-ionised impurity atoms scatter weakly by their distorted potential. Matters only at low temperatures when dopants are frozen out.

- Carrier–carrier scattering. Coulomb interactions between carriers. Important at very high carrier densities (heavily doped or highly injected regions, e.g. in power devices and solar cells).

- Defect scattering. Dislocations (charged lines in n-type material), grain boundaries, stacking faults, vacancies and clusters disturb the lattice and scatter carriers.

- Surface and interface scattering. At surfaces and at the Si/SiO2 interface, surface roughness, interface traps and oxide charges scatter carriers confined near the interface (MOSFET channels).

- Alloy scattering. In alloys such as AlxGa1−xAs or SiGe, the random distribution of different atoms makes the potential non-periodic.

- Intervalley scattering. Carriers move between equivalent or non-equivalent conduction-band minima by absorbing or emitting phonons (basis of the Gunn effect).

The total rate is the sum of the individual rates, 1/τ = Σ 1/τi, giving Matthiessen's rule 1/μ = Σ 1/μi. Near room temperature in lightly doped Si, lattice scattering dominates; in heavily doped Si or at low temperature, ionised-impurity scattering dominates.

### Q37. Derive the expression for drift current density due to electrons and holes.

Assumptions: uniform semiconductor, steady state, uniform field E in the +x direction, low enough field that vd ∝ E.

Step 1: drift velocity. An electron experiences force F = −qE. Between collisions (mean free time τm), it accelerates by a = −qE/mn∗. Averaging over all electrons, momentum gained from the field equals momentum lost in collisions:

mn∗ vdn / τm = −qE ⇒ vdn = −(qτm/mn∗) E = −μn E

Similarly, holes (charge +q) drift with the field:

vdp = +(qτmp/mp∗) E = +μp E

Step 2: current density from charge flow. Current density is charge density × velocity. Consider a bar of cross-section A. In time dt, all carriers within distance vd·dt of a cross-section pass through it; that is (vd dt A) × concentration carriers.

For electrons, charge density −qn and velocity vdn:

Jn = (−qn)(vdn) = (−qn)(−μn E) = qnμn E

For holes, charge density +qp and velocity vdp:

Jp = (+qp)(+μp E) = qpμp E

Electrons move against the field but carry negative charge, so their current is in the same direction as the hole current: both are along E.

Step 3: total drift current density.

Jdrift = Jn + Jp = q( nμn + pμp ) E

Comparing with Ohm's law J = σE:

σ = q( nμn + pμp ), ρ = 1/σ = 1 / [ q(nμn + pμp) ]

For an n-type sample (n ≫ p), σ ≈ qnμn ≈ qNDμn; for p-type, σ ≈ qNAμp. For an intrinsic sample, σi = qni(μn + μp).

### Q38. A semiconductor has an electron concentration of 2 × 1016 cm−3, electron mobility of 1350 cm2/V·s, and an electric field of 10 V/cm. Calculate the electron drift current density.

Question. Calculate the electron drift current density for n = 2×1016 cm−3, μn = 1350 cm2/V·s and E = 10 V/cm.

Given: n = 2×1016 cm−3, μn = 1350 cm2/V·s, E = 10 V/cm, q = 1.602×10−19 C.

Find: Jn (drift).

Formula:

Jn = qnμnE

Solution.

Jn = q n μn E
= (1.602×10−19 C)(2×1016 cm−3)(1350 cm2/V·s)(10 V/cm)
= (1.602×10−19)(2.7×1020) A/cm2
= 43.3 A/cm2

Answer: Jn ≈ 43.3 A/cm2 (= 4.33×105 A/m2). (With the rounded q = 1.6×10−19 C the result is 43.2 A/cm2.)

Units check: C · cm−3 · cm2/(V·s) · V/cm = C/(s·cm2) = A/cm2. ✓

Supporting quantities:

- Drift velocity vd = μnE = 1350 × 10 = 1.35×104 cm/s (well below vsat = 107 cm/s, so the linear model is valid).

- Conductivity σ = qnμn = 4.33 S/cm, resistivity ρ = 0.231 Ω·cm, and J = σE = 4.33 × 10 = 43.3 A/cm2. ✓

What this means: a modest field of only 10 V/cm (1 V across 1 mm) already drives about 43 A through every square centimetre, because there are so many electrons; the electrons themselves creep along at only 1.35×104 cm/s, almost a thousand times slower than their thermal speed.

### Q39. Explain diffusion current in a semiconductor and state Fick's law.

Diffusion current is the current produced by the net movement of carriers from a region of higher concentration to one of lower concentration, caused by their random thermal motion. No electric field is needed. If the concentration varies with position, more carriers cross any plane from the high-concentration side than from the low side simply because there are more of them, so a net flux results. Because the carriers are charged, this flux is a current.

Diffusion current is important wherever carrier gradients exist: in the neutral regions of a forward-biased p-n junction (injected minority carriers diffusing away from the junction), in the base of a bipolar transistor, under non-uniform illumination, and in non-uniformly doped material.

Fick's (first) law. The particle flux is proportional to the negative of the concentration gradient:

F = −D dC/dx

where D is the diffusion coefficient (cm2/s). Applied to electrons and holes:

Electron flux: Fn = −Dn dn/dx Hole flux: Fp = −Dp dp/dx

Diffusion current densities (multiply by the charge, −q for electrons, +q for holes):

Jn,diff = +q Dn dn/dx
Jp,diff = −q Dp dp/dx

In three dimensions, Jn = qDn∇n and Jp = −qDp∇p.

Example. If the electron concentration falls linearly from 1017 cm−3 to 0 over 1 μm in Si (Dn = 35 cm2/s):

dn/dx = −1017/10−4 = −1021 cm−4
Jn = q Dn dn/dx = (1.602×10−19)(35)(−1021) = −5.6×103 A/cm2

The negative sign means the current flows in the −x direction, while the electrons themselves flow in +x (down their gradient).

Total current when a field is present: Jn = qnμnE + qDn dn/dx and Jp = qpμpE − qDp dp/dx.

### Q40. State and explain the Einstein relation between carrier mobility and diffusion coefficient.

Statement.

Dn/μn = kT/q, Dp/μp = kT/q

The ratio of diffusion coefficient to mobility equals the thermal voltage kT/q (0.0259 V at 300 K), for both electrons and holes, in a non-degenerate semiconductor.

Explanation. Drift and diffusion are two responses of the same carriers, both limited by the same random scattering events. Mobility describes the response to an electric field (μ = qτm/m∗); diffusion describes the response to a concentration gradient (D = vth2τm/3 ≈ kTτm/m∗). Dividing gives D/μ = kT/q: the scattering time and mass cancel, leaving only temperature.

Derivation (equilibrium argument). In a non-uniformly doped sample in thermal equilibrium, an internal field E develops such that the drift and diffusion currents cancel exactly:

Jn = qnμnE + qDn dn/dx = 0

In equilibrium EF is constant and n = ni exp((EF − Ei)/kT). Since Ei varies with the electrostatic potential, dEi/dx = qE, so

dn/dx = −(n/kT) dEi/dx = −(qn/kT) E

Substituting:

qnμnE − qDn(qn/kT)E = 0 ⇒ Dn = (kT/q)μn

Uses.

- One measurement gives the other: mobility is easy to measure (Hall effect, conductivity), so D follows. Si electrons: Dn = 0.0259 × 1350 = 35 cm2/s; holes: Dp = 0.0259 × 480 = 12.4 cm2/s.

- It links the drift and diffusion terms in the current equations and is needed to calculate diffusion lengths L = √(Dτ) and diode saturation currents.

- It shows why the built-in voltage of a junction is set by kT/q times a logarithm of a concentration ratio.

For degenerate semiconductors the relation is modified (D/μ > kT/q), because carriers then obey Fermi–Dirac rather than Boltzmann statistics.

## Practice questions

These extra questions practise this week's ideas. Work each one on paper before reading the solution; the calculation questions follow the same Question, Given, Find, Solution, Answer layout as the worked examples.

#### Practice 7.1: resistivity of p-type silicon

Question. Find the resistivity of silicon doped with 5×1015 cm−3 boron, taking μp = 470 cm2/V·s.

Given: NA = 5×1015 cm−3, μp = 470 cm2/V·s.

Find: ρ.

Solution.

σ = qNAμp = 1.6×10−19 × 5×1015 × 470 = 0.376 S/cm
ρ = 1/σ = 2.66 Ω·cm

Answer: ρ = 2.7 Ω·cm.

#### Practice 7.2: doping for a target resistivity

Question. What phosphorus concentration gives n-type silicon a resistivity of 1 Ω·cm? Take μn = 1300 cm2/V·s.

Given: ρ = 1 Ω·cm, μn = 1300 cm2/V·s.

Find: ND.

Solution.

ND = 1/(qμnρ) = 1/(1.6×10−19 × 1300 × 1) = 4.8×1015 cm−3

Answer: ND ≈ 4.8×1015 cm−3.

#### Practice 7.3: Hall measurement

Question. A semiconductor sample 0.01 cm thick carries I = 1 mA in a magnetic field of 0.1 T (10−5 Wb/cm2). A Hall voltage of +2 mV is measured, and the resistivity is 4 Ω·cm. Find the carrier type, concentration and mobility.

Given: t = 0.01 cm, I = 10−3 A, B = 10−5 Wb/cm2, VH = +2×10−3 V, ρ = 4 Ω·cm.

Find: type, p, μ.

Solution.

RH = VH t/(IB) = (2×10−3 × 0.01)/(10−3 × 10−5) = 2000 cm3/C (positive → holes)
p = 1/(qRH) = 1/(1.6×10−19 × 2000) = 3.1×1015 cm−3
μp = RH/ρ = 2000/4 = 500 cm2/V·s

Answer: p-type, p = 3.1×1015 cm−3, μp = 500 cm2/V·s.

#### Practice 7.4: combining scattering mechanisms

Question. In a silicon sample the lattice-limited mobility is 1400 cm2/V·s and the impurity-limited mobility is 2500 cm2/V·s. Find the total mobility.

Given: μL = 1400, μI = 2500 cm2/V·s.

Find: μ.

Solution.

1/μ = 1/1400 + 1/2500 = 7.14×10−4 + 4.0×10−4 = 1.114×10−3
μ = 897 cm2/V·s

Answer: μ ≈ 900 cm2/V·s, lower than either mechanism alone.

#### Practice 7.5: drift plus diffusion

Question. In a region of silicon the hole concentration is 1×1015 cm−3 and falls with a gradient of −1×1018 cm−4, while a field of 50 V/cm acts in the +x direction. Find the hole drift, diffusion and total current densities (μp = 480 cm2/V·s, Dp = 12.4 cm2/s).

Given: p = 1015 cm−3, dp/dx = −1018 cm−4, E = 50 V/cm, μp = 480, Dp = 12.4 cm2/s.

Find: Jp(drift), Jp(diff), Jp.

Solution.

Jp(drift) = qpμpE = 1.6×10−19 × 1015 × 480 × 50 = 3.84 A/cm2
Jp(diff) = −qDp dp/dx = −1.6×10−19 × 12.4 × (−1018) = +1.98 A/cm2
Jp = 3.84 + 1.98 = 5.82 A/cm2

Answer: 3.84 + 1.98 = 5.8 A/cm2, both in the +x direction.

#### Practice 7.6: Einstein relation at a higher temperature

Question. Holes in a sample have μp = 400 cm2/V·s at 400 K. Find Dp.

Given: μp = 400 cm2/V·s, T = 400 K.

Find: Dp.

Solution.

kT/q = 8.617×10−5 × 400 = 0.0345 V
Dp = (kT/q)μp = 0.0345 × 400 = 13.8 cm2/s

Answer: Dp = 13.8 cm2/s.

#### Practice 7.7: why doping lowers mobility

Question. Explain why electron mobility in silicon falls from about 1350 to about 100 cm2/V·s as the doping rises from 1014 to 1020 cm−3.

Answer. Each dopant is an ionised impurity with a Coulomb field that deflects passing carriers. Mobility is μ = qτm/m∗; more ionised impurities mean more frequent scattering, a shorter mean free time τm, and so a lower μ. At 1014 cm−3 lattice scattering dominates and impurities hardly matter; at 1020 cm−3 impurity scattering dominates completely (Matthiessen: 1/μ = 1/μL + 1/μI, with μI ∝ 1/NI).

## Objectives check

Use this table to confirm you have met this week's objectives. Cover the Answer column and answer each check question from memory. If you cannot, go back to the section in the last column before moving on.

| # | Objective | Check yourself | Answer | Where it is taught |
| --- | --- | --- | --- | --- |
| 1 | Explain thermal motion, drift velocity and mobility. | Si electrons in a 500 V/cm field: find vd. | vd = 1350 × 500 = 6.75×105 cm/s. | Part A; Example 7.1 |
| 2 | Explain the scattering mechanisms and the factors that affect mobility. | Which scattering mechanism dominates at low temperature in heavily doped Si? | Ionised-impurity scattering. | Scattering; factors affecting mobility |
| 3 | Derive and use the drift current density and conductivity. | Find σ for p-type Si with NA = 1016 cm−3 and μp = 480 cm2/V·s. | σ = 1.6×10−19 × 1016 × 480 = 0.77 S/cm. | Drift current density; Example 7.2 |
| 4 | Explain carrier diffusion and calculate diffusion current with Fick's law. | Why does electron diffusion current point opposite to the electron flow? | Because the electron charge is negative. | Part B; Example 7.3; Drift and diffusion compared |
| 5 | State, explain and use the Einstein relation. | Find Dn for GaAs (μn = 8500 cm2/V·s) at 300 K. | D = 0.0259 × 8500 = 220 cm2/s. | The Einstein relation |

Week 8 · Module 3 · Carrier Transport & Injection Phenomena

# High-Field Effects and Excess Carriers

Plan: velocity saturation and hot-carrier effects; generation and recombination mechanisms (Shockley–Read–Hall theory); carrier lifetime and steady-state excess carrier injection.

## Learning objectives

By the end of this week you should be able to:

- Explain velocity saturation and its effect on devices.

- Explain hot-carrier effects and how they are reduced.

- Explain excess carriers and low-level injection.

- Describe the generation and recombination mechanisms.

- Explain SRH recombination and calculate lifetime from trap data.

- Calculate decay of excess carriers and steady-state injection levels.

## Symbols and abbreviations used this week

Every symbol, constant and abbreviation on this page is listed here, even if an earlier week already defined it, so you can study this page on its own.

Constants and units

| Symbol | Meaning | Units / typical value |
| --- | --- | --- |
| q | Magnitude of the electronic charge | 1.6×10−19 C |
| k | Boltzmann constant | 8.617×10−5 eV/K = 1.381×10−23 J/K |
| kT | Thermal energy | 0.0259 eV (often 0.02585 eV) at 300 K |
| T | Absolute temperature | kelvin (K); room temperature = 300 K |
| h | Planck constant | 6.626×10−34 J·s |
| eV | Electron-volt, a unit of energy | 1 eV = 1.6×10−19 J |
| μm | Micrometre (micron) | 1 μm = 10−4 cm = 10−6 m |

Symbols

| Symbol | Meaning | Units / typical value |
| --- | --- | --- |
| Eg | Band-gap energy, Ec − Ev | eV; Si 1.12, Ge 0.66, GaAs 1.42 at 300 K |
| EF | Fermi level: the energy at which a state has a 50 % chance of being occupied | eV |
| Ei | Intrinsic Fermi level, close to mid-gap | eV |
| EFn, EFp | Quasi-Fermi levels for electrons and holes, used out of equilibrium | eV |
| Et | Energy level of a trap (recombination centre) in the gap | eV |
| n | Electron concentration (free electrons per cm3) | cm−3 |
| p | Hole concentration (holes per cm3) | cm−3 |
| ni | Intrinsic carrier concentration (n = p = ni in pure material) | cm−3; Si ≈ 1×1010 at 300 K |
| n0, p0 | Equilibrium electron and hole concentrations | cm−3 |
| ND | Donor concentration | cm−3 |
| NA | Acceptor concentration | cm−3 |
| Δn, Δp | Excess electron and hole concentrations above equilibrium | cm−3 |
| ν, hν | Frequency of light, and photon energy | Hz; eV |
| Q | Dose: dopant atoms per unit area (in Weeks 13–14, Q also means charge) | atoms/cm2 (C or C/cm2 for charge) |
| μ, μn, μp | Mobility: drift velocity per unit field (electrons, holes) | cm2/(V·s); Si μn 1350, μp 480 |
| vd | Drift velocity | cm/s |
| vth | Thermal velocity of carriers | ≈ 107 cm/s at 300 K |
| vsat | Saturation velocity at high field | ≈ 107 cm/s in Si |
| σ | Conductivity, q(nμn + pμp) (in Week 8, σ is also a capture cross-section) | S/cm (siemens per cm) |
| Dn, Dp | Diffusion coefficients of electrons and holes | cm2/s; Si 35 and 12.4 |
| Te | Electron temperature of hot carriers | K |
| G, GL | Generation rate of electron–hole pairs (GL: by light) | cm−3s−1 |
| R | Recombination rate | cm−3s−1 |
| U | Net recombination rate, R − G | cm−3s−1 |
| τ, τn, τp | Minority-carrier lifetime (τeff: effective, including surfaces) | s; Si 1 ns – 1 ms |
| Nt | Density of traps (recombination centres) | cm−3 |
| σn, σp | Capture cross-section of a trap for electrons, holes | cm2 |
| n1, p1 | SRH parameters nie(Et − Ei)/kT and nie(Ei − Et)/kT | cm−3 |
| L, Ln, Lp | Diffusion length √(Dτ): distance a minority carrier travels before recombining | μm or cm |
| V, Va | Applied voltage (positive for forward bias) | V |
| W | Depletion-region width (in Week 13 WB, WE are base and emitter widths; in Week 14 W is channel width) | μm or cm |
| Is, Js (IS) | Saturation current (density) of a diode or transistor | A; A/cm2 |
| A (area) | Device or contact area | cm2 |
| β | Common-emitter current gain, IC/IB (also hFE) | dimensionless; 50–500 |
| NE, WE, DE; NB, WB, DB | Doping, width and minority diffusion coefficient of the emitter; of the base | cm−3; μm; cm2/s |
| fT | Transition (cut-off) frequency | Hz |
| VT (Vth) | Threshold voltage of a MOSFET | V |
| VGS, VDS, VSB, VG | Gate–source, drain–source, source–body and gate voltages | V |
| Esat | Field at which the drift velocity saturates, vsat/μ | V/cm |
| Gth, Rth | Thermal generation and recombination rates (equal in equilibrium) | cm−3s−1 |
| ft, en, ep | Probability a trap is occupied by an electron; emission rates of electrons and holes from traps | dimensionless; s−1 |
| ra, rb, rc, rd | SRH rates: electron capture, electron emission, hole capture, hole emission | cm−3s−1 |
| τSRH, τradiative, τAuger | Lifetimes set by trap (SRH), radiative and Auger recombination | s |
| Igen, Jgen | Generation current (density) from carriers generated in the depletion region | A; A/cm2 |
| B (recombination) | Radiative recombination coefficient, R = B np | cm3/s; GaAs ≈ 10−10, Si ≈ 10−14 |
| Cn, Cp (Auger) | Auger recombination coefficients | cm6/s; Si ≈ 10−31 |
| τ0 (τg) | Effective generation lifetime in a depletion region | s |
| t | Time (or a thickness, where the text says so) | s (or cm) |

Abbreviations

| Abbreviation | Meaning |
| --- | --- |
| Si | Silicon |
| Ge | Germanium |
| GaAs | Gallium arsenide |
| GaN | Gallium nitride |
| InP | Indium phosphide |
| SiO2 | Silicon dioxide (silica), the oxide insulator |
| CB | Conduction band |
| VB | Valence band |
| SRH | Shockley–Read–Hall (trap-assisted) recombination |
| LDD | Lightly doped drain |
| MOSFET | Metal–oxide–semiconductor field-effect transistor |
| CMOS | Complementary MOS (n- and p-channel MOSFETs together) |
| BJT | Bipolar junction transistor |
| LED | Light-emitting diode |
| IGBT | Insulated-gate bipolar transistor |
| PCD | Photoconductive decay (lifetime measurement) |

## Key terms

Every important word used this week is defined here, so you can read this week on its own.

Band gap (Eg). The range of energies that an electron in a crystal cannot have. It lies between the valence band (the band of energies occupied by the electrons that form the bonds between atoms) and the conduction band (the next band up, where electrons are free to move). For silicon Eg = 1.12 eV at 300 K.

Electron and hole (carriers). A free electron is an electron in the conduction band; a hole is an empty place left in the valence band, which behaves like a positive charge that can move. Together they are called carriers because they carry the current.

Doping (ND, NA). Adding small, controlled amounts of impurity atoms to a semiconductor. Donors (concentration ND) give free electrons and make the material n-type; acceptors (concentration NA) give holes and make it p-type.

Majority and minority carriers. The majority carriers are the more numerous type (electrons in n-type, holes in p-type); the minority carriers are the less numerous type.

Why it matters: this week shows that it is the minority carriers whose numbers change, and so they control how devices behave.

Intrinsic carrier concentration (ni). The number of electrons (equal to the number of holes) per cm3 in pure, undoped material; about 1×1010 cm−3 in Si at 300 K. In thermal equilibrium (no light, no applied voltage, steady temperature) the electron and hole concentrations of any sample obey the mass-action law:

n0p0 = ni2

Where:

- n0, p0 = equilibrium electron and hole concentrations (cm−3)

- ni = intrinsic carrier concentration (cm−3)

Fermi level (EF). The energy at which an electron state has a 50 % chance of being occupied. In thermal equilibrium one Fermi level describes both electrons and holes, and it is the same everywhere in the material.

Drift velocity and saturation velocity (vd, vsat). The drift velocity is the average velocity carriers gain in an electric field; at low field it is vd = μE, where μ is the mobility (cm2/V·s). At high field it stops rising and levels off at the saturation velocity vsat, about 1×107 cm/s in silicon.

Why it matters: the carriers in a modern short-channel transistor travel at vsat, which limits its current and speed.

Hot carriers. Carriers whose average energy, gained from a strong electric field, is far above the normal thermal energy of the crystal. Their energy is described by an electron temperature Te much higher than the lattice temperature T.

Impact ionisation. The process in which a hot carrier collides with the lattice hard enough to break a bond and create a new electron–hole pair. Repeated, it becomes an avalanche, which causes avalanche breakdown.

Excess carriers (Δn, Δp). Electrons and holes present in addition to the equilibrium numbers, for example created by light or injected by a forward-biased junction: n = n0 + Δn and p = p0 + Δp.

Low-level injection. The condition in which the excess carrier concentration is much smaller than the equilibrium majority concentration (Δp ≪ n0 in n-type). The majority concentration is then almost unchanged.

Generation and recombination (G, R, U). Generation is the creation of an electron–hole pair; recombination is the loss of one, when a conduction-band electron falls back into a hole. G and R are rates in pairs per cm3 per second; U = R − G is the net recombination rate.

Trap (recombination centre, Nt, Et). A localised energy level Et inside the band gap, created by a crystal defect or an impurity atom such as gold or iron. It can capture an electron and then a hole, helping them recombine in two small steps. Nt is the density of traps (cm−3).

Shockley–Read–Hall (SRH) recombination. Recombination through traps. The energy is released as lattice vibrations (heat). It is the main recombination mechanism in silicon.

Minority-carrier lifetime (τ). The average time an excess minority carrier survives before it recombines. After the source of excess carriers is removed, the excess falls to 1/e (37 %) of its starting value in one lifetime.

Δp(t) = Δp(0) e−t/τp

Where:

- Δp(t) = excess hole concentration at time t (cm−3)

- Δp(0) = excess hole concentration when the light is switched off (cm−3)

- t = time since switch-off (s)

- τp = hole (minority-carrier) lifetime in n-type material (s)

Why it matters: lifetime decides how far minority carriers can travel, how fast a diode switches off and how efficient a solar cell is.

Quasi-Fermi levels (EFn, EFp). When the material is out of equilibrium (np ≠ ni2), one Fermi level can no longer describe both carriers, so two are used: EFn gives the electron concentration and EFp the hole concentration. Their separation measures how far the material is from equilibrium.

## The big picture

This week covers two separate stories.

Story 1: what happens at very high fields. Week 7 said vd = μE: double the field, double the speed. That stops being true at high fields. Carriers hit a speed limit, and the fastest ones become "hot" and start damaging things. This matters in modern transistors, which are so small that even a volt across them gives enormous fields.

Story 2: what happens when we disturb the balance of carriers. Light, or a forward-biased junction, can add extra electrons and holes beyond the equilibrium numbers. These extras do not last: they recombine and disappear. How long they last, the lifetime, controls how diodes switch, how transistors amplify and how well solar cells work.

## Part A: High-field effects

### Velocity saturation

At low fields carriers lose the energy they pick up from the field to small lattice vibrations, so they stay "cool" and vd = μE.

At high fields (above about 104 V/cm in Si) they pick up energy faster than they can lose it that way. Once a carrier has about 0.06 eV of extra energy (in Si), it can shake the lattice much harder by emitting an optical phonon, which takes that energy away in one go. So every time a carrier speeds up, it is quickly slowed down again. The drift velocity stops increasing and levels off at the saturation velocity:

vsat ≈ 1×107 cm/s (Si electrons and holes, at 300 K)

In plain words. Pushing harder on a cyclist on a flat road makes them go faster, until air resistance grows so quickly that extra effort gives almost no extra speed. Optical phonons are the "air resistance" for carriers.

An empirical formula that joins the two regimes smoothly (Caughey–Thomas):

vd = μE / [ 1 + (μE/vsat)β ]1/β (β ≈ 2 for Si electrons, about 1 for holes)

Where:

- vd = drift velocity (cm/s)

- μ = low-field mobility (cm2/V·s); Si μn = 1350, μp = 480

- E = electric field (V/cm)

- vsat = saturation velocity, about 1×107 cm/s in Si

- β = fitting exponent that sets how sharply the curve bends (dimensionless; not the transistor gain β)

At low field it reduces to μE; at high field to vsat.

GaAs is different. Its electrons speed up to about 2×107 cm/s near 3.5 kV/cm, and then actually slow down at higher fields, because they jump into a different part of the conduction band where they are heavier. A region where more field gives less current is called negative differential mobility; it is used in Gunn diodes to make microwave oscillators.

Drift velocity against field. Silicon carriers level off near 10⁷ cm/s. GaAs electrons overshoot to about 2×10⁷ cm/s, then fall as they transfer to a heavier valley.

Why it matters: in a short-channel MOSFET the carriers are at vsat across most of the channel, so the current depends on (VGS − VT) rather than (VGS − VT)2 (Week 14), and the transistor speed is limited to about vsat/(2πL).

### Hot-carrier effects

When carriers gain energy much faster than they lose it, their average energy rises far above the normal thermal energy. They are called hot carriers (their energy is described by an "electron temperature" Te much higher than the crystal's temperature). Hot carriers cause:

- Velocity saturation and reduced mobility (above).

- Impact ionisation. A carrier with energy above about 1.5Eg can knock an electron out of a covalent bond when it collides, creating a new electron–hole pair. The new carriers are accelerated too and do the same: an avalanche. This causes avalanche breakdown of junctions (Week 10) and is used deliberately in avalanche photodiodes.

- Hot-carrier injection into the gate oxide of MOSFETs. Near the drain, some electrons gain enough energy (over 3.1 eV) to jump over the Si/SiO2 barrier into the oxide, where they get trapped or create defects. The threshold voltage slowly shifts and the transistor degrades over months or years: a key reliability problem.

- Substrate current from holes created by impact ionisation, which can trigger unwanted bipolar action or latch-up in CMOS.

- Velocity overshoot in very short devices, where carriers cross before they have time to reach vsat, briefly going faster.

Cures: the lightly doped drain (LDD) structure, which spreads the voltage drop and lowers the peak field; lower supply voltages; better oxides.

## Part B: Generation and recombination

### Equilibrium and excess carriers

In thermal equilibrium, electron–hole pairs are being created (generated) by heat and destroyed (recombined) all the time, at exactly equal rates. That balance is what keeps n0p0 = ni2.

Now shine light on the sample, or inject carriers through a junction. We get excess carriers:

n = n0 + Δn, p = p0 + Δp

Where:

- n, p = actual electron and hole concentrations (cm−3)

- n0, p0 = equilibrium concentrations, with n0p0 = ni2 (cm−3)

- Δn, Δp = excess electron and hole concentrations (cm−3)

Light creates electrons and holes in pairs, so usually Δn = Δp. Now np > ni2, recombination is faster than generation, and the extras start disappearing.

Low-level injection means the excess is much smaller than the majority concentration (Δp ≪ n0 in n-type). Then:

- the majority concentration hardly changes;

- the minority concentration may change enormously.

#### Example 8.1: what low-level injection does to each carrier

Question. n-type silicon with ND = 1×1016 cm−3 (so p0 = 1×104 cm−3) is illuminated, creating Δn = Δp = 1×1014 cm−3 excess carriers. Calculate the new electron and hole concentrations and the factor by which each has changed.

Given: n0 = 1×1016 cm−3, p0 = 1×104 cm−3, Δn = Δp = 1×1014 cm−3.

Find: n, p and their change factors.

Formula:

n = n0 + Δn, p = p0 + Δp

Solution.

n = n0 + Δn = 1×1016 + 1×1014 = 1.01×1016 cm−3 (n/n0 = 1.01)

p = p0 + Δp = 1×104 + 1×1014 ≈ 1×1014 cm−3 (p/p0 = 1010)

Answer: The electrons change by only 1 %; the holes increase ten-billion-fold.

What this means: the conductivity (set mainly by the electrons) barely changes, but the hole population, and so the hole recombination and hole diffusion, changes enormously. This is why minority carriers control device behaviour: they are the ones that change. Since Δp = 1014 is only 1 % of n0, this is low-level injection.

### How carriers are generated

- Thermal generation: heat breaks a bond. Usually it happens in two small steps through a defect level in the gap, which is easier than one big jump.

- Optical generation: a photon with energy hν ≥ Eg is absorbed and creates a pair. This is how photodiodes and solar cells work.

- Impact ionisation: a hot carrier creates a pair (above).

- Tunnelling across the gap at extremely high fields (Zener effect).

### How carriers recombine

The three recombination paths. Band-to-band: the electron drops straight across and emits a photon. Shockley–Read–Hall: it drops in two steps via a trap in the gap, giving heat. Auger: the energy is handed to a third carrier.

- Direct (band-to-band, radiative). An electron drops straight from the conduction band into a hole and emits a photon of energy ≈ Eg. Rate = B·np, where B is the radiative recombination coefficient (cm3/s). Strong in direct-gap GaAs (LEDs, lasers); very weak in indirect-gap Si (Week 4).

- Indirect (trap-assisted, Shockley–Read–Hall, SRH). The electron drops in two steps through a trap, a localised energy level in the gap created by a defect or an impurity atom such as gold, iron or copper. The energy goes into lattice vibrations (heat). This is the dominant mechanism in silicon.

- Auger. The energy released is given to a third carrier, which is kicked high into its band and then cools down. Important at very high carrier densities.

- Surface recombination: SRH through the many traps at a surface (Week 9).

### The three recombination mechanisms compared

|  | Shockley–Read–Hall (trap-assisted) | Radiative (band-to-band) | Auger |
| --- | --- | --- | --- |
| How it happens | Electron drops in two steps via a trap level Et in the gap | Electron drops straight across the gap into a hole | Electron and hole recombine and hand the energy to a third carrier |
| Where the energy goes | Heat (lattice vibrations, phonons) | A photon of energy ≈ Eg (light) | Kinetic energy of the third carrier, then heat |
| Net rate | U = (np − ni2)/[τp(n + n1) + τn(p + p1)]; ≈ Δp/τp at low level in n-type | R = B(np − ni2) | R = (Cnn + Cpp)(np − ni2) |
| What it depends on | Trap density Nt: τ = 1/(σvthNt) | Material: B ≈ 10−10 cm3/s (GaAs), ≈ 10−14 cm3/s (Si) | Carrier density squared: C ≈ 10−31 cm6/s in Si |
| Lifetime (low-level, majority density N) | τ = 1/(σvthNt): 1 ns – 1 ms in Si, set by purity | τ = 1/(BN): about 10 ns in GaAs at N = 1018 cm−3; about 10 ms in Si at 1016 cm−3 | τ ≈ 1/(CN2): about 0.1 μs at 1019 cm−3, about 1 ns at 1020 cm−3 in Si |
| Where it dominates | Indirect-gap Si and Ge at normal doping; depletion regions | Direct-gap GaAs, InP, GaN | Very heavy doping or very high injection (emitters, lasers, power devices) |
| Where it matters in practice | Leakage current; gold or platinum doping for fast-switching diodes; solar-cell efficiency | LEDs and lasers (the light output) | Limits lifetime in heavily doped emitters; efficiency "droop" of LEDs at high current |

So in silicon the lifetime is almost always set by SRH (traps), except in very heavily doped regions, where Auger takes over; radiative recombination is too slow to matter.

### Shockley–Read–Hall recombination: how it works

Picture a trap level Et in the middle of the gap. It can be empty or hold one electron. Four things can happen to it:

| Step | What happens | Result |
| --- | --- | --- |
| 1. Electron capture | A conduction-band electron falls into the empty trap | Trap now full |
| 2. Electron emission | The trapped electron is shaken back up into the conduction band | Trap empty again |
| 3. Hole capture | The trapped electron drops down into the valence band, filling a hole | A hole disappears; trap empty |
| 4. Hole emission | A valence-band electron jumps up into the empty trap | A hole appears; trap full |

Recombination = step 1 then step 3: an electron and a hole have both disappeared, via the trap. Generation = step 4 then step 2: an electron and a hole have both been created.

In plain words. It is much easier to go down a staircase two steps at a time than to jump the whole flight. A trap in the middle of the gap is a landing half-way down. That is why a few impurity atoms can make recombination enormously faster.

Working out the balance of the four steps gives the SRH recombination rate:

U = (np − ni2) / [ τp(n + n1) + τn(p + p1) ]

τn = 1/(σn vth Nt), τp = 1/(σp vth Nt)
n1 = ni e(Et − Ei)/kT, p1 = ni e(Ei − Et)/kT

| Symbol | Meaning |
| --- | --- |
| U | net recombination rate (pairs per cm3 per second) |
| Nt | trap density (cm−3) |
| σn, σp | capture cross-sections: how "big a target" the trap is for electrons, holes (cm2) |
| vth | thermal velocity, about 107 cm/s |
| Et | trap energy level (eV) |
| n, p | electron and hole concentrations (cm−3) |
| ni | intrinsic carrier concentration, 1×1010 cm−3 in Si at 300 K |
| τn, τp | electron and hole lifetimes set by the traps (s) |
| n1, p1 | the electron and hole concentrations there would be if EF were at Et (cm−3) |
| Ei | intrinsic Fermi level, close to mid-gap (eV) |
| kT | thermal energy, 0.0259 eV at 300 K |

What the formula tells you:

- The top line, np − ni2, is the driving force. If np > ni2 (extra carriers), U is positive: net recombination. If np < ni2 (carriers removed, as in a reverse-biased depletion region), U is negative: net generation, which is the source of diode leakage current. In equilibrium, np = ni2 and U = 0.

- U is largest when Et is near mid-gap. Traps near a band edge just catch and re-release carriers. Mid-gap traps are the effective recombination centres. Gold sits close to mid-gap, which is why it is used deliberately to make fast-switching diodes.

- More traps, faster recombination: τ ∝ 1/Nt.

- Low-level injection in n-type (n ≫ p): the formula simplifies to the short form below. The recombination rate is set by how fast the minority carriers (holes) get captured.

U ≈ Δp / τp

Where:

- U = net recombination rate (cm−3s−1)

- Δp = excess hole (minority-carrier) concentration (cm−3)

- τp = hole lifetime, 1/(σp vth Nt) (s)

#### Example 8.2: lifetime from the trap density

Question. An n-type silicon wafer contains 1×1013 cm−3 mid-gap recombination centres with a hole capture cross-section of 1×10−15 cm2. The thermal velocity is 1×107 cm/s. Calculate the minority-carrier (hole) lifetime.

Given: Nt = 1×1013 cm−3, σp = 1×10−15 cm2, vth = 1×107 cm/s.

Find: τp.

Formula:

τp = 1/(σp vth Nt)

Solution.

τp = 1/(σp vth Nt) = 1 / (10−15 × 107 × 1013) = 1/105 = 1×10−5 s

Answer: τp = 10 μs. Doubling the trap density would halve the lifetime.

What this means: a trap density of 1013 cm−3 is less than one atom in a billion of silicon (5×1022 atoms per cm3), yet it fixes the lifetime at 10 μs. A hole in this wafer survives about 10 μs before a trap catches it, which is why chip and solar-cell makers keep metal contamination so low.

## Part C: Lifetime and steady-state injection

### Minority-carrier lifetime

Switch off the light at t = 0. With U = Δp/τp, the excess holes decay as

dΔp/dt = −Δp/τp ⇒ Δp(t) = Δp(0) e−t/τp

Where:

- Δp(t) = excess hole concentration at time t (cm−3)

- Δp(0) = excess hole concentration at switch-off, t = 0 (cm−3)

- t = time (s)

- τp = minority-carrier (hole) lifetime (s)

τp is the minority-carrier lifetime: the average time an extra minority carrier survives before it recombines. After one lifetime, 37 % (1/e) of the excess remains; after five lifetimes, under 1 %.

Typical values: very pure Si, 1 μs to 1 ms; gold-doped Si for fast switching, 1–10 ns; GaAs, 1–10 ns (fast radiative recombination).

If several mechanisms act together, their rates add: 1/τ = 1/τSRH + 1/τradiative + 1/τAuger.

Under steady illumination the excess holds at Δp = GLτp. When the light is switched off it decays exponentially, falling to 1/e in one lifetime.

### Steady-state excess carrier injection

Now keep the light on, generating GL pairs per cm3 per second uniformly. The excess builds up until recombination exactly balances generation:

dΔp/dt = GL − Δp/τp = 0 ⇒ Δp = Δn = GLτp

Where:

- Δp, Δn = steady-state excess hole and electron concentrations (cm−3)

- GL = generation rate by light (pairs per cm3 per second, cm−3s−1)

- τp = minority-carrier (hole) lifetime (s)

The excess equals the generation rate times the lifetime. A long lifetime lets a large excess build up.

The extra carriers raise the conductivity, called photoconductivity:

Δσ = q(μn + μp) Δn = q(μn + μp) GLτ

Where:

- Δσ = increase in conductivity caused by the light (S/cm)

- q = electronic charge, 1.6×10−19 C

- μn, μp = electron and hole mobilities (cm2/V·s)

- Δn = excess carrier concentration, equal to Δp (cm−3)

- GL = generation rate (cm−3s−1)

- τ = minority-carrier lifetime (s)

#### Example 8.3: photoconductivity

Question. n-type silicon with ND = 1×1015 cm−3 and τp = 10 μs is uniformly illuminated, generating GL = 1×1020 electron–hole pairs per cm3 per second. Calculate the steady-state excess carrier concentration, the increase in conductivity, and compare it with the dark conductivity.

Given: ND = 1×1015 cm−3, τp = 10 μs = 1×10−5 s, GL = 1×1020 cm−3s−1, μn = 1350, μp = 480 cm2/V·s.

Find: Δn, Δσ and σ0.

Formula:

Δn = Δp = GLτp, Δσ = q(μn + μp)Δn, σ0 = qNDμn

Solution.

Step 1. Steady state, generation = recombination:

Δn = Δp = GLτp = 1020 × 10−5 = 1×1015 cm−3

Step 2. Extra conductivity:

Δσ = q(μn + μp)Δn = 1.6×10−19 × (1350 + 480) × 1015 = 0.293 S/cm

Step 3. Dark conductivity:

σ0 = qNDμn = 1.6×10−19 × 1015 × 1350 = 0.216 S/cm

Answer: Δn = 1015 cm−3, Δσ = 0.293 S/cm, against σ0 = 0.216 S/cm: the conductivity more than doubles in the light.

What this means: the total conductivity in the light is 0.216 + 0.293 = 0.509 S/cm, about 2.4 times the dark value, so the sample's resistance falls to about 40 % of its dark value. The 10 μs lifetime is what lets so many extra carriers build up; with a 1 μs lifetime the effect would be ten times smaller.

This is how a light-dependent resistor works. (Here Δp equals n0, so this is not low-level injection, and the single-lifetime formula is only approximate.)

### Quasi-Fermi levels

Out of equilibrium, np ≠ ni2, so a single Fermi level cannot describe both carriers. Instead we use two: one for electrons, EFn, and one for holes, EFp:

n = ni e(EFn − Ei)/kT, p = ni e(Ei − EFp)/kT, np = ni2 e(EFn − EFp)/kT

Where:

- n, p = electron and hole concentrations out of equilibrium (cm−3)

- ni = intrinsic carrier concentration, 1×1010 cm−3 in Si at 300 K

- EFn, EFp = quasi-Fermi levels for electrons and holes (eV)

- Ei = intrinsic Fermi level, close to mid-gap (eV)

- kT = thermal energy, 0.0259 eV at 300 K

The gap between them, EFn − EFp, measures how far from equilibrium the material is. In a forward-biased diode it equals qV; in a solar cell it sets the open-circuit voltage. In equilibrium they merge back into one Fermi level.

## Key points of Week 8

- At high fields drift velocity saturates at vsat ≈ 107 cm/s (optical-phonon emission).

- Hot carriers cause impact ionisation (avalanche) and oxide damage in MOSFETs; LDD reduces them.

- Excess carriers: n = n0 + Δn. Under low-level injection only the minority concentration changes much.

- Recombination: band-to-band (light, GaAs), SRH via traps (heat, dominant in Si), Auger (high density).

- SRH rate U = (np − ni2)/[τp(n + n1) + τn(p + p1)]: mid-gap traps are most effective; τ = 1/(σvthNt).

- Low-level n-type: U = Δp/τp; after switch-off Δp(t) = Δp(0)e−t/τp; under steady light Δp = GLτp.

## Examination questions solved (Q41–Q44)

### Q41. Explain velocity saturation and hot-carrier effects in semiconductors.

Velocity saturation. At low fields, drift velocity is proportional to the field, vd = μE, because carriers lose the energy they gain from the field to the lattice (acoustic phonons) and stay near thermal equilibrium. As the field increases (above about 103–104 V/cm in Si), carriers gain energy faster than acoustic-phonon scattering can remove it. Once their energy reaches the optical-phonon energy (≈ 0.063 eV in Si), they emit optical phonons very rapidly, which transfers energy to the lattice efficiently and limits further gain. The drift velocity therefore stops increasing and approaches a saturation velocity:

vsat ≈ 107 cm/s (Si, 300 K)

and is described empirically by vd = μE/[1 + (μE/vsat)β]1/β. The effective mobility vd/E falls at high field. In GaAs the electron velocity peaks at about 2×107 cm/s then decreases (negative differential mobility) because electrons transfer to the heavier L-valley.

Consequences: in short-channel MOSFETs the drain current becomes proportional to (VGS − VT) rather than (VGS − VT)2, and the maximum transconductance and transit-time-limited speed are set by vsat: fT ≈ vsat/(2πL).

Hot-carrier effects. Under high fields, carriers acquire an average kinetic energy far greater than the thermal value (3/2)kT; they are described by an effective electron temperature Te ≫ T. These "hot" carriers cause:

- Impact ionisation: carriers with energy above about 1.5Eg break bonds and create electron–hole pairs, leading to avalanche multiplication and avalanche breakdown of junctions.

- Hot-carrier injection into gate oxides: hot electrons near the drain of a MOSFET surmount the 3.1 eV Si/SiO2 barrier, become trapped in the oxide or create interface traps. The threshold voltage shifts and transconductance degrades over the device's life (hot-carrier degradation).

- Substrate and gate currents: impact-generated holes flow to the substrate, which can forward-bias source junctions and trigger parasitic bipolar action or CMOS latch-up.

- Velocity overshoot: in very short channels carriers transit before scattering brings them to steady state, briefly exceeding vsat.

- Increased noise and light emission.

Mitigation: lightly doped drain (LDD) structures to reduce the peak field, reduced supply voltage, graded junctions, and nitrided or hardened gate oxides.

### Q42. What is meant by generation and recombination of charge carriers?

Generation is any process that creates free electron–hole pairs (or a free carrier from a dopant or trap) by giving an electron enough energy to move from the valence band (or a localised state) into the conduction band. The rate G is the number of pairs created per unit volume per unit time (cm−3s−1). Mechanisms:

- Thermal generation by lattice vibrations, directly or through trap levels in the gap.

- Optical generation by absorption of photons with hν ≥ Eg (photodetectors, solar cells).

- Impact ionisation by energetic carriers in high fields (avalanche).

- Tunnelling generation at very high fields (Zener).

Recombination is the reverse: a conduction-band electron falls back to the valence band and fills a hole, so both carriers are annihilated. The released energy Eg appears as a photon, as heat (phonons), or as kinetic energy of a third carrier. The rate R has the same units. Mechanisms:

- Direct (band-to-band, radiative) recombination, emitting a photon; dominant in direct-gap materials.

- Indirect (trap-assisted, SRH) recombination through defect or impurity levels in the gap, releasing heat; dominant in Si.

- Auger recombination, energy given to a third carrier; dominant at high carrier density.

- Surface recombination through surface states.

Equilibrium and non-equilibrium. In thermal equilibrium the two processes balance (Gth = Rth), giving n0p0 = ni2. If excess carriers are introduced (np > ni2), net recombination U = R − G > 0 restores equilibrium; if carriers are removed (np < ni2, e.g. a reverse-biased depletion region), net generation occurs. For low-level injection the net recombination rate is U = Δp/τp (n-type), where τp is the minority-carrier lifetime.

Generation and recombination govern the leakage current of diodes, the operation of solar cells, LEDs and photodetectors, the gain of BJTs and the switching speed of p-n junctions.

### Q43. Explain the Shockley-Read-Hall (SRH) recombination mechanism.

Principle. SRH (trap-assisted or indirect) recombination occurs through localised energy levels Et in the forbidden gap introduced by crystal defects or impurities (e.g. Au, Fe, Cu, vacancies, dislocations). Instead of crossing the whole gap in one step, which in an indirect semiconductor requires an unlikely phonon-assisted transition, the electron makes two smaller steps via the trap, and the energy is released as lattice vibrations (phonons).

The four processes at a trap (density Nt, occupation probability ft):

| Process | Description | Rate |
| --- | --- | --- |
| (a) Electron capture | CB electron captured by an empty trap | ra = vthσn n Nt(1 − ft) |
| (b) Electron emission | Trapped electron emitted to CB | rb = en Nt ft |
| (c) Hole capture | Trapped electron drops to VB, annihilating a hole | rc = vthσp p Nt ft |
| (d) Hole emission | VB electron captured by empty trap, leaving a hole | rd = ep Nt(1 − ft) |

Recombination = (a) then (c). Generation = (d) then (b).

Derivation outline. In steady state the trap occupation is constant, so the net electron capture rate equals the net hole capture rate: ra − rb = rc − rd = U. The emission coefficients follow from detailed balance in equilibrium: en = vthσn n1 and ep = vthσp p1. Solving for ft and substituting gives:

U = (np − ni2) / [ τp(n + n1) + τn(p + p1) ]

with τn = 1/(σn vth Nt), τp = 1/(σp vth Nt), n1 = ni e(Et − Ei)/kT, p1 = ni e(Ei − Et)/kT.

Interpretation.

- The driving force is (np − ni2): positive for excess carriers (recombination), negative for depletion (generation), zero in equilibrium.

- U is maximum when Et is near mid-gap (Et ≈ Ei). Shallow levels near a band edge just re-emit carriers and are ineffective. Deep, mid-gap levels are the effective recombination centres.

- U ∝ Nt: more traps give faster recombination and shorter lifetime.

- For low-level injection in n-type material (n ≫ p, n1, p1): U = (p − p0)/τp = Δp/τp. The rate is limited by capture of the minority carrier.

- In a reverse-biased depletion region (n, p ≈ 0): U = −ni/(τp + τn) ≈ −ni/2τ0, a net generation that produces the generation leakage current Jgen = qniW/2τ0.

Applications: gold or platinum doping, or electron irradiation, is deliberately used to reduce lifetime in fast-switching diodes and thyristors. Conversely, gettering and clean processing reduce trap densities for long lifetimes in solar cells, CCDs and low-leakage devices.

### Q44. Define minority-carrier lifetime and explain its significance in semiconductor devices.

Definition. The minority-carrier lifetime is the average time an excess minority carrier exists in a semiconductor before it recombines with a majority carrier. For low-level injection, τp (holes in n-type) or τn (electrons in p-type) is defined by

U = Δp / τp

so that, when generation stops, the excess density decays exponentially:

Δp(t) = Δp(0) e−t/τp

τp is the time for the excess to fall to 1/e (37 %) of its initial value. With SRH recombination, τp = 1/(σp vth Nt): lifetime is inversely proportional to the trap density. Typical values: 1 ns to 1 ms in Si depending on purity.

Significance:

- Diffusion length. Injected minority carriers diffuse an average distance L = √(Dτ) before recombining. In Si with Dp = 12 cm2/s and τp = 1 μs, Lp = √(12 × 10−6) = 35 μm. L determines how far carriers travel and therefore device dimensions.

- Diode current. The saturation current Js = qni2(Dp/(LpND) + Dn/(LnNA)) depends on lifetime through L. Short lifetime raises leakage; generation current in the depletion region is ∝ 1/τ.

- Switching speed. When a forward-biased diode is turned off, the stored minority charge Q = Iτ must be removed; the reverse-recovery time is ≈ τ. Fast-recovery and switching diodes are gold- or platinum-doped to cut τ to nanoseconds.

- BJT current gain. Electrons injected into a p-type base must cross it before recombining. The base transport factor ≈ 1 − WB2/2Ln2, so long lifetime (Ln ≫ WB) gives high β.

- Solar cells and photodetectors. Photogenerated carriers must reach the junction before recombining; long lifetime (long L) means higher collection efficiency, current and efficiency.

- LEDs and lasers. The radiative fraction of recombination, and the modulation speed (bandwidth ∝ 1/τ), depend on lifetime.

- Power devices. In p-i-n diodes and IGBTs, long lifetime gives conductivity modulation and low on-state voltage but slow switching; there is a design trade-off.

- Material quality indicator. Lifetime is very sensitive to metallic contamination, so it is measured (photoconductive decay, μ-PCD) to monitor crystal growth and process cleanliness.

## Practice questions

These extra questions practise this week's ideas. Work each one on paper before reading the solution; the calculation questions follow the same Question, Given, Find, Solution, Answer layout as the worked examples.

#### Practice 8.1: when does velocity saturate?

Question. Estimate the field at which electron drift in silicon starts to saturate (μn = 1350 cm2/V·s, vsat = 1×107 cm/s). Is a 100 nm MOSFET channel with 1 V across it saturated?

Given: μn = 1350 cm2/V·s, vsat = 107 cm/s, V = 1 V over L = 100 nm = 10−5 cm.

Find: E where μE = vsat; the channel field.

Solution.

Esat ≈ vsat/μn = 107/1350 = 7.4×103 V/cm
Channel field ≈ V/L = 1/10−5 = 105 V/cm

Answer: Esat ≈ 7.4 kV/cm; the channel field (100 kV/cm) is over ten times larger, so the carriers are fully velocity-saturated.

#### Practice 8.2: gold as a lifetime killer

Question. A switching diode is doped with 1×1015 cm−3 gold atoms (σ = 1×10−15 cm2, vth = 1×107 cm/s). Find the minority-carrier lifetime.

Given: Nt = 1015 cm−3, σ = 10−15 cm2, vth = 107 cm/s.

Find: τ.

Solution.

τ = 1/(σvthNt) = 1/(10−15 × 107 × 1015) = 10−7 s

Answer: τ = 100 ns, short enough for a fast-recovery diode.

#### Practice 8.3: how long until the excess is gone?

Question. After the light is switched off, excess holes in n-type silicon decay with τp = 5 μs. How long does it take for the excess to fall to 1 % of its initial value?

Given: τp = 5 μs, Δp(t)/Δp(0) = 0.01.

Find: t.

Solution.

e−t/τ = 0.01 ⇒ t = τ ln(100) = 5 μs × 4.61 = 23 μs

Answer: t ≈ 23 μs (about 4.6 lifetimes).

#### Practice 8.4: steady-state injection level

Question. n-type silicon (ND = 1×1016 cm−3, τp = 20 μs) is uniformly illuminated with GL = 5×1019 cm−3s−1. Find Δp and decide whether this is low-level injection.

Given: GL = 5×1019 cm−3s−1, τp = 2×10−5 s, ND = 1016 cm−3.

Find: Δp and Δp/n0.

Solution.

Δp = GLτp = 5×1019 × 2×10−5 = 1×1015 cm−3
Δp/n0 = 1015/1016 = 0.1

Answer: Δp = 1015 cm−3, 10 % of n0: borderline but usually treated as low-level injection.

#### Practice 8.5: quasi-Fermi level splitting

Question. n-type silicon with ND = 1×1016 cm−3 is illuminated so that Δn = Δp = 1×1014 cm−3. Find EFn − Ei, Ei − EFp and the splitting EFn − EFp at 300 K.

Given: n = 1.01×1016, p ≈ 1014 cm−3, ni = 1010 cm−3, kT = 0.0259 eV.

Find: the quasi-Fermi levels and their splitting.

Solution.

EFn − Ei = kT ln(n/ni) = 0.0259 ln(1.01×106) = 0.358 eV
Ei − EFp = kT ln(p/ni) = 0.0259 ln(104) = 0.239 eV
EFn − EFp = 0.358 + 0.239 = 0.597 eV

Answer: EFn = Ei + 0.358 eV, EFp = Ei − 0.239 eV, splitting ≈ 0.60 eV. The electron level hardly moves; the hole level moves a long way.

#### Practice 8.6: generation current in a depletion region

Question. A reverse-biased silicon junction has a depletion width of 1 μm, area 10−3 cm2 and effective lifetime τ0 = 1 μs. Estimate the generation leakage current, Jgen = qniW/2τ0.

Given: W = 10−4 cm, A = 10−3 cm2, τ0 = 10−6 s, ni = 1010 cm−3.

Find: Jgen and Igen.

Solution.

Jgen = qniW/(2τ0) = 1.6×10−19 × 1010 × 10−4 / (2×10−6) = 8×10−8 A/cm2
Igen = JgenA = 8×10−11 A

Answer: Jgen = 8×10−8 A/cm2, Igen = 80 pA. In silicon this generation current usually exceeds the ideal diffusion leakage.

#### Practice 8.7: Auger versus SRH

Question. Explain why Auger recombination is important in heavily doped emitters but not in lightly doped bulk silicon.

Answer. Auger recombination needs three carriers to meet (the recombining electron and hole plus a third carrier that takes the energy), so its rate grows as n2p or np2, much faster than SRH, which grows only linearly with the excess. In lightly doped silicon carrier densities are low and three-carrier encounters are rare, so SRH dominates. In emitters doped to 1019–1020 cm−3 the majority density is enormous, Auger becomes the fastest path and it limits the minority-carrier lifetime.

## Objectives check

Use this table to confirm you have met this week's objectives. Cover the Answer column and answer each check question from memory. If you cannot, go back to the section in the last column before moving on.

| # | Objective | Check yourself | Answer | Where it is taught |
| --- | --- | --- | --- | --- |
| 1 | Explain velocity saturation and its effect on devices. | What is the saturation velocity in Si and what causes it? | About 107 cm/s; optical-phonon emission by energetic carriers. | Velocity saturation |
| 2 | Explain hot-carrier effects and how they are reduced. | How does a hot carrier cause avalanche breakdown? | It impact-ionises, creating new pairs that are accelerated and do the same. | Hot-carrier effects |
| 3 | Explain excess carriers and low-level injection. | Under low-level injection in n-type material, which carrier concentration changes significantly? | The minority (hole) concentration. | Equilibrium and excess carriers; Example 8.1 |
| 4 | Describe the generation and recombination mechanisms. | Which recombination mechanism dominates in silicon? | Shockley–Read–Hall (trap-assisted). | Generation; recombination; the three recombination mechanisms compared |
| 5 | Explain SRH recombination and calculate lifetime from trap data. | Why are mid-gap traps the most effective recombination centres? | They capture electrons and holes with similar ease; shallow traps just re-emit carriers. | SRH; Example 8.2 |
| 6 | Calculate decay of excess carriers and steady-state injection levels. | With GL = 1019 cm−3s−1 and τ = 2 μs, find Δp. | Δp = GLτ = 2×1013 cm−3. | Part C; Example 8.3 |

Week 9 · Module 3 · Carrier Transport & Injection Phenomena

# Continuity Equation and Surface Phenomena

Plan: derivation and application of the minority-carrier continuity equation; semiconductor surface states and surface recombination velocity.

## Learning objectives

By the end of this week you should be able to:

- Derive the continuity equation for holes and electrons.

- Write and interpret the minority-carrier diffusion equation.

- Solve the diffusion equation for the standard cases.

- Calculate diffusion lengths and explain their importance.

- Explain surface states and surface recombination velocity.

- Calculate the effective lifetime of a wafer with recombining surfaces.

## Symbols and abbreviations used this week

Every symbol, constant and abbreviation on this page is listed here, even if an earlier week already defined it, so you can study this page on its own.

Constants and units

| Symbol | Meaning | Units / typical value |
| --- | --- | --- |
| q | Magnitude of the electronic charge | 1.6×10−19 C |
| eV | Electron-volt, a unit of energy | 1 eV = 1.6×10−19 J |
| μm | Micrometre (micron) | 1 μm = 10−4 cm = 10−6 m |

Symbols

| Symbol | Meaning | Units / typical value |
| --- | --- | --- |
| Eg | Band-gap energy, Ec − Ev | eV; Si 1.12, Ge 0.66, GaAs 1.42 at 300 K |
| n | Electron concentration (free electrons per cm3) | cm−3 |
| p | Hole concentration (holes per cm3) | cm−3 |
| ND | Donor concentration | cm−3 |
| Δn, Δp | Excess electron and hole concentrations above equilibrium | cm−3 |
| D | Diffusion coefficient (dopants in a furnace, or carriers) | cm2/s |
| Rp | Projected range: average depth at which implanted ions stop | μm |
| μ, μn, μp | Mobility: drift velocity per unit field (electrons, holes) | cm2/(V·s); Si μn 1350, μp 480 |
| vth | Thermal velocity of carriers | ≈ 107 cm/s at 300 K |
| J, Jn, Jp | Current density (total, electrons, holes) | A/cm2 |
| Dn, Dp | Diffusion coefficients of electrons and holes | cm2/s; Si 35 and 12.4 |
| G, GL | Generation rate of electron–hole pairs (GL: by light) | cm−3s−1 |
| R | Recombination rate | cm−3s−1 |
| U | Net recombination rate, R − G | cm−3s−1 |
| τ, τn, τp | Minority-carrier lifetime (τeff: effective, including surfaces) | s; Si 1 ns – 1 ms |
| σn, σp | Capture cross-section of a trap for electrons, holes | cm2 |
| L, Ln, Lp | Diffusion length √(Dτ): distance a minority carrier travels before recombining | μm or cm |
| S | Surface recombination velocity | cm/s |
| Nst | Density of surface traps | cm−2 |
| Us | Recombination rate per unit area at a surface | cm−2s−1 |
| W | Depletion-region width (in Week 13 WB, WE are base and emitter widths; in Week 14 W is channel width) | μm or cm |
| xn, xp | Parts of the depletion region on the n side and on the p side | μm |
| A (area) | Device or contact area | cm2 |
| NE, WE, DE; NB, WB, DB | Doping, width and minority diffusion coefficient of the emitter; of the base | cm−3; μm; cm2/s |
| Gth, Rth | Thermal generation and recombination rates (equal in equilibrium) | cm−3s−1 |
| Gn, Gp, Rn, Rp | Generation and recombination rates of electrons and holes | cm−3s−1 |
| τb (τbulk), τsurface | Lifetime from bulk recombination only; from surface recombination only | s |
| Us, ps, Δps | Surface recombination rate; hole density and excess at the surface | cm−2s−1; cm−3 |
| t | Time (or a thickness, where the text says so) | s (or cm) |

Abbreviations

| Abbreviation | Meaning |
| --- | --- |
| Si | Silicon |
| SiO2 | Silicon dioxide (silica), the oxide insulator |
| SRH | Shockley–Read–Hall (trap-assisted) recombination |
| MOS | Metal–oxide–semiconductor |
| MOSFET | Metal–oxide–semiconductor field-effect transistor |
| BJT | Bipolar junction transistor |
| TCAD | Technology computer-aided design (device simulation software) |

## Key terms

Every important word used this week is defined here, so you can read this week on its own.

Band gap (Eg). The range of energies between the top of the valence band and the bottom of the conduction band in which a perfect crystal has no allowed electron states. For silicon it is 1.12 eV at 300 K.

Electron and hole. An electron is a free negative charge carrier in the conduction band. A hole is an empty state left in the valence band when an electron leaves it; it moves like a positive charge carrier.

Doping (n-type, p-type). Adding small, controlled amounts of impurity atoms to a semiconductor. Donor atoms give electrons and make the material n-type; acceptor atoms take electrons, create holes and make it p-type.

Majority and minority carriers. In n-type material electrons are the majority carriers and holes the minority carriers; in p-type material it is the other way round. Minority carriers are few, but they control most device currents.

Why it matters: the continuity equation this week is almost always solved for the minority carriers.

Excess carriers (Δn, Δp). Carriers present above the equilibrium (dark, no-bias) number, for example created by light or injected by a junction.

Δp = p − p0

Where:

- Δp = excess hole concentration (cm−3)

- p = actual hole concentration (cm−3)

- p0 = hole concentration in thermal equilibrium (cm−3)

Low-level injection. The condition in which the excess carrier density is much smaller than the majority-carrier density, so the majority density is hardly changed. It makes the recombination rate simply proportional to the excess, Δp/τ.

Generation and recombination (G, R). Generation is the creation of electron–hole pairs (by heat or light); recombination is their destruction when an electron drops back into a hole. Both are counted per cm3 per second.

Trap (SRH recombination). A defect or impurity with an energy level inside the band gap that captures an electron and then a hole, so that the pair recombines in two easy steps. This Shockley–Read–Hall process is the main recombination route in silicon.

Minority-carrier lifetime (τ). The average time an excess minority carrier survives before it recombines. In silicon it ranges from about 1 ns to 1 ms, depending on how many traps there are.

Why it matters: the lifetime, together with the diffusion coefficient, sets how far carriers travel and hence how much current a diode or transistor carries.

Drift and diffusion. The two ways carriers move. Drift is motion pushed by an electric field; diffusion is the spreading of carriers from where there are many to where there are few, with no field needed.

Diffusion coefficient (D). A measure of how quickly carriers spread out by diffusion, in cm2/s. For lightly doped silicon Dn ≈ 35 cm2/s and Dp ≈ 12 cm2/s.

Continuity equation. The book-keeping equation for carriers: in any small volume, the rate of change of the carrier density equals the net inflow carried by current, plus generation, minus recombination.

∂p/∂t = −(1/q) ∂Jp/∂x + Gp − Rp

Where:

- ∂p/∂t = rate of change of hole concentration with time (cm−3s−1)

- q = electronic charge, 1.6×10−19 C

- Jp = hole current density (A/cm2); ∂Jp/∂x is its change with position x (cm)

- Gp, Rp = generation and recombination rates of holes (cm−3s−1)

Why it matters: every diode and transistor current in this course comes from solving this equation.

Minority-carrier diffusion equation. The continuity equation written for minority carriers in a region with almost no electric field (a quasi-neutral region), using diffusion for the current and Δp/τ for the recombination.

Diffusion length (L). The average distance an excess minority carrier diffuses before it recombines.

Lp = √(Dp τp)

Where:

- Lp = hole diffusion length (cm)

- Dp = hole diffusion coefficient (cm2/s)

- τp = hole lifetime (s)

Why it matters: a device region much shorter than L lets almost every carrier cross it; a region much longer than L loses most of them.

Surface states (dangling bonds). Energy levels inside the band gap located at a surface, caused mainly by surface atoms whose bonds point out into nothing (dangling bonds). They act as traps.

Surface recombination velocity (S). A measure, in cm/s, of how fast a surface destroys excess carriers: the recombination per unit area equals S times the excess density at the surface.

Us = S Δp(0)

Where:

- Us = recombination rate per unit area of surface (cm−2s−1)

- S = surface recombination velocity (cm/s)

- Δp(0) = excess minority density at the surface (cm−3)

Why it matters: a poor surface (large S) can destroy carriers faster than the whole bulk does.

Effective lifetime (τeff). The lifetime actually measured in a sample, which includes losses both in the bulk and at the surfaces. It is always shorter than the bulk lifetime.

Passivation. Treating a surface (for example growing an oxide or depositing a nitride film) so that its dangling bonds are tied up and S becomes small.

## The big picture

Weeks 7 and 8 gave us all the separate pieces: carriers flow (drift and diffusion), and carriers are created and destroyed (generation and recombination). The continuity equation puts the pieces together into one equation.

It is nothing more than book-keeping, like a bank account:

change in balance = money in − money out + interest earned − charges paid

For carriers in a small slice of semiconductor:

change in carriers = carriers flowing in − carriers flowing out + carriers generated − carriers recombined

Solve this equation and you know where the carriers are and how they change with time. That is how we will get the diode equation in Week 10 and the transistor currents in Week 13.

The second half of the week is about surfaces, where the crystal ends and carriers get lost much faster than inside.

## Deriving the continuity equation

Take a thin slice of semiconductor between x and x + dx, with cross-section area A. Count the holes in it. The number changes for three reasons:

- Flow. Holes enter at x carried by the current Jp(x), and leave at x + dx carried by Jp(x + dx). Dividing a current by q turns it into a number of carriers per second, so the net inflow is [Jp(x) − Jp(x + dx)]A/q.

- Generation inside the slice: Gp per cm3 per second, times the volume A dx.

- Recombination inside the slice: Rp per cm3 per second, times A dx.

So:

(rate of change of p) × A dx = [Jp(x) − Jp(x + dx)] A/q + (Gp − Rp) A dx

Divide by A dx. As dx → 0, [Jp(x) − Jp(x + dx)]/dx becomes −∂Jp/∂x:

∂p/∂t = −(1/q) ∂Jp/∂x + Gp − Rp

For electrons the sign of the flow term is opposite, because the electron charge is negative:

∂n/∂t = +(1/q) ∂Jn/∂x + Gn − Rn

Where:

- p, n = hole and electron concentrations (cm−3); t = time (s)

- q = electronic charge, 1.6×10−19 C

- Jp, Jn = hole and electron current densities (A/cm2); x = position (cm)

- Gp, Gn = generation rates of holes and electrons (cm−3s−1)

- Rp, Rn = recombination rates of holes and electrons (cm−3s−1)

Reading it. If more current flows into the slice than out of it (current decreasing with x), carriers pile up. If generation beats recombination, carriers build up. Otherwise they fall.

## The minority-carrier diffusion equation

Now apply it to the case that matters most: holes as minority carriers in an n-type region, with low-level injection.

- From Week 7, the hole current is Jp = qpμpE − qDp ∂p/∂x.

- From Week 8, the net recombination is Δp/τp.

- In a neutral region of a device the field is small, so the drift term can usually be dropped.

Substituting gives the minority-carrier diffusion equation:

∂Δp/∂t = Dp ∂2Δp/∂x2 − Δp/τp + GL

Where:

- Δp = excess hole concentration (cm−3), a function of position x (cm) and time t (s)

- Dp = hole diffusion coefficient (cm2/s); about 12 cm2/s in lightly doped Si

- τp = hole (minority-carrier) lifetime (s)

- GL = generation rate by external light (cm−3s−1)

| Term | Meaning |
| --- | --- |
| ∂Δp/∂t | how fast the excess changes at this point |
| Dp ∂2Δp/∂x2 | diffusion: carriers spread from where there are more to where there are fewer |
| −Δp/τp | recombination: excess carriers die off with lifetime τp |
| GL | external generation, e.g. by light |

(If there is a field, add −μpE ∂Δp/∂x for drift.) For electrons in p-type: ∂Δn/∂t = Dn ∂2Δn/∂x2 − Δn/τn + GL.

### The four standard solutions

| Situation | Equation becomes | Solution |
| --- | --- | --- |
| Uniform sample, light switched off at t = 0 | dΔp/dt = −Δp/τp | Δp(t) = Δp(0) e−t/τp (exponential decay in time) |
| Uniform sample, steady light | 0 = GL − Δp/τp | Δp = GLτp |
| Steady injection at x = 0 into a long sample | 0 = Dp d2Δp/dx2 − Δp/τp | Δp(x) = Δp(0) e−x/Lp (exponential decay in space) |
| Steady injection into a short sample, W ≪ Lp | d2Δp/dx2 ≈ 0 | Δp(x) = Δp(0)(1 − x/W), a straight line |

(In the last row W is the length of the short sample, in cm.)

#### Example 9.1: steady illumination and decay after the light is switched off

Question. A uniform n-type silicon sample (ND = 1×1016 cm−3) has a hole lifetime of 2 μs. It is illuminated uniformly so that light generates 1×1020 electron–hole pairs per cm3 per second. Find the steady excess hole concentration, check that this is low-level injection, and find how long after the light is switched off the excess falls to 10 % of its steady value.

Given: τp = 2 μs = 2×10−6 s, GL = 1×1020 cm−3s−1, ND = 1×1016 cm−3 (so the electron density is about 1016 cm−3).

Find: Δp in the steady state; the time t at which Δp(t) = 0.1 Δp(0).

Formula: the first two rows of the table above (the sample is uniform, so there is no diffusion):

Δp = GL τp (steady light)

Δp(t) = Δp(0) e−t/τp (after switch-off)

Solution.

Step 1. Steady state:

Δp = 1×1020 × 2×10−6 = 2×1014 cm−3

Step 2. Low-level check: 2×1014 cm−3 is only 2 % of the electron density 1016 cm−3, so the injection is low-level and the simple Δp/τp recombination term is valid.

Step 3. Decay: set e−t/τp = 0.1, so t = τp ln 10:

t = 2×10−6 × 2.303 = 4.6×10−6 s

Answer: Δp = 2×1014 cm−3 (low-level injection), and it falls to 10 % of this 4.6 μs after the light is switched off.

What this means: the excess builds up until recombination (Δp/τp) exactly balances generation, so a longer lifetime gives a larger steady excess. Timing the decay after a light pulse is exactly how lifetime is measured (photoconductive decay): it takes about 2.3 lifetimes to fall by a factor of ten.

### The diffusion length

The third case introduces the diffusion length:

Lp = √(Dp τp), Ln = √(Dn τn)

Where:

- Lp, Ln = diffusion lengths of holes and electrons (cm; often quoted in μm)

- Dp, Dn = diffusion coefficients of holes and electrons (cm2/s)

- τp, τn = lifetimes of holes and electrons as minority carriers (s)

It is the average distance an injected minority carrier diffuses before it recombines. The excess falls to 1/e (37 %) at one diffusion length, and to under 1 % at five.

Steady-state profile when minority carriers are injected at x = 0 into a long n-type bar: an exponential decay with characteristic length Lp.

In plain words. Inject carriers at one end of a bar and they spread out by diffusion, but they also keep dying by recombination. They spread a typical distance Lp before they die. The longer they live (τ) and the faster they spread (D), the further they get.

#### Example 9.2: diffusion length

Question. Holes are injected into n-type silicon in which Dp = 12 cm2/s and the hole lifetime is 1 μs. Calculate the hole diffusion length, and the fraction of the injected excess remaining 100 μm from the injection point.

Given: Dp = 12 cm2/s, τp = 1 μs = 1×10−6 s, x = 100 μm.

Find: Lp, and Δp(100 μm)/Δp(0).

Formula:

Lp = √(Dpτp), Δp(x) = Δp(0) e−x/Lp

Solution.

Step 1. Lp = √(Dpτp) = √(12 × 10−6) = 3.46×10−3 cm = 34.6 μm

Step 2. Δp(x)/Δp(0) = e−x/Lp:

e−100/34.6 = e−2.89 = 0.056

Answer: Lp = 34.6 μm; only 5.6 % of the excess survives 100 μm from the injection point.

What this means: a typical hole lives long enough to spread only about 35 μm, a third of the width of a human hair. A device region much thinner than this (such as a transistor base) is crossed by almost every carrier; a region several diffusion lengths long loses nearly all of them to recombination.

The hole current at the injection point comes from the slope of the profile there:

Jp(0) = −qDp dΔp/dx |0 = qDpΔp(0)/Lp

Where:

- Jp(0) = hole diffusion current density at the injection point (A/cm2)

- q = electronic charge, 1.6×10−19 C

- Dp = hole diffusion coefficient (cm2/s)

- Δp(0) = excess hole concentration at the injection point (cm−3)

- Lp = hole diffusion length (cm)

This is exactly the formula that, applied at the edge of a junction, gives the Shockley diode equation (Week 10). The fourth case (straight-line profile in a short region) is what happens in a transistor's thin base (Week 13).

### Where the continuity equation is used

- Diodes: the exponential profile in each neutral region gives the diode current (Week 10).

- Bipolar transistors: the straight-line profile in the thin base gives the collector current and the gain (Week 13).

- Measuring lifetime: the exponential decay after a light pulse (photoconductive decay) gives τ directly.

- Haynes–Shockley experiment: a pulse of carriers drifts and spreads; timing it gives μ, D and τ.

- Solar cells and photodiodes: with generation GL(x) = G0e−αx, the solution gives how many carriers are collected.

- Device simulators solve these equations numerically for every chip design.

## Surfaces and surface states

### Why surfaces are special

Inside the crystal, every silicon atom is bonded to four neighbours. At a surface the crystal simply stops: the surface atoms have bonds pointing out into nothing, called dangling bonds. Adsorbed impurities and defects in any oxide on top add more problems.

These create a high density of surface states: energy levels inside the band gap, located at the surface (typically 1010–1015 per cm2). They:

- act as SRH traps (Week 8), so carriers recombine much faster at the surface than in the bulk;

- trap charge, which bends the bands near the surface even with no voltage applied;

- cause noise and instability, and shift the threshold voltage in MOSFETs.

### Surface recombination velocity

Recombination at a surface happens in an extremely thin layer, so it is counted per unit area, not per unit volume:

Us = S × Δp(0) [carriers per cm2 per second]

Where:

- Us = recombination rate per unit area of surface (cm−2s−1)

- S = surface recombination velocity (cm/s)

- Δp(0) = excess minority (here hole) concentration at the surface (cm−3)

In plain words. Imagine the excess carriers near the surface rushing into it at speed S and vanishing. A surface with S = 100 cm/s swallows carriers as fast as if they flowed into a drain at 100 cm/s. A perfect surface has S = 0; a surface that destroys every carrier that reaches it has S → ∞.

For surface traps of density Nst (per cm2):

S = σp vth Nst

Where:

- S = surface recombination velocity (cm/s)

- σp = capture cross-section of a surface trap for holes (cm2); typically about 10−15 cm2

- vth = thermal velocity of carriers, about 107 cm/s at 300 K

- Nst = density of surface traps (cm−2)

It enters the diffusion equation as a boundary condition: the carriers arriving at the surface by diffusion must equal the carriers recombining there,

Dp dΔp/dx |surface = S Δp(0)

Where:

- Dp dΔp/dx |surface = diffusion flow of holes towards the surface, per cm2 per second (Dp in cm2/s, dΔp/dx in cm−4)

- S Δp(0) = rate at which they recombine at the surface (cm−2s−1)

#### Example 9.3: surface recombination velocity from the trap density

Question. A silicon surface has surface traps with a hole capture cross-section of 1×10−15 cm2. Find the surface recombination velocity (a) for a well-oxidised surface with 1×1010 traps per cm2, and (b) for a bare surface with 1×1013 traps per cm2. For case (a), find the recombination rate per cm2 if the excess hole concentration at the surface is 1×1013 cm−3.

Given: σp = 1×10−15 cm2, vth = 1×107 cm/s, Nst = 1010 cm−2 (a) and 1013 cm−2 (b), Δp(0) = 1×1013 cm−3.

Find: S in each case; Us for case (a).

Formula:

S = σp vth Nst, Us = S Δp(0)

Solution.

Step 1. Oxidised surface:

S = 1×10−15 × 1×107 × 1×1010 = 100 cm/s

Step 2. Bare surface:

S = 1×10−15 × 1×107 × 1×1013 = 1×105 cm/s

Step 3. Recombination rate at the oxidised surface:

Us = 100 × 1×1013 = 1×1015 cm−2s−1

Answer: S = 100 cm/s for the oxidised surface and 1×105 cm/s for the bare surface; at the oxidised surface Us = 1×1015 carriers per cm2 per second.

What this means: S is simply proportional to the number of surface traps, so cutting the trap density a thousandfold by growing a good oxide cuts the surface loss a thousandfold. These two values match the "thermally oxidised" and "bare" rows of the table below.

| Surface | Typical S (cm/s) |
| --- | --- |
| Bare or freshly etched Si | 104 – 106 |
| Thermally oxidised Si | 10 – 100 |
| Best passivated Si (Al2O3, SiNx, annealed SiO2) | below 10 |
| Ohmic metal contact | → ∞ (Δp forced to 0) |

### How surfaces shorten the lifetime

In a wafer of thickness W with both surfaces recombining, the measured (effective) lifetime combines bulk and surface losses:

1/τeff = 1/τbulk + 2S/W (for small S: SW/2D ≪ 1)

Where:

- τeff = effective (measured) lifetime of the wafer (s)

- τbulk = lifetime set by recombination in the bulk alone (s)

- S = surface recombination velocity, the same on both faces (cm/s)

- W = wafer thickness (cm)

The term 2S/W is 1/τsurface: two surfaces, each removing carriers at speed S, shared over a thickness W.

The diffusion limit. The simple formula assumes carriers reach the surfaces easily, so the excess is almost uniform through the wafer. That is true only while SW/2D ≪ 1 (D is the minority-carrier diffusion coefficient). If S is very large, the surfaces swallow carriers faster than diffusion can bring them, and the loss is limited by the time carriers take to diffuse to a surface. A good approximation covering both cases is:

τsurface ≈ W/(2S) + W2/(π2D), 1/τeff = 1/τbulk + 1/τsurface

Where:

- τsurface = lifetime set by surface recombination alone (s)

- W/(2S) = time for the surfaces to remove the carriers once they arrive (s)

- W2/(π2D) = time for carriers to diffuse to the surfaces (s); it is the shortest τsurface can ever be

- D = minority-carrier diffusion coefficient (cm2/s)

For small S the first term dominates and this reduces to 1/τsurface = 2S/W.

#### Example 9.4: how surfaces reduce the lifetime

Question. An n-type silicon wafer 300 μm thick has a bulk lifetime of 100 μs and a hole diffusion coefficient of 12 cm2/s. Both surfaces are oxidised, giving a surface recombination velocity of 100 cm/s. Calculate the effective lifetime. Repeat for unprotected surfaces with S = 105 cm/s.

Given: τbulk = 100 μs = 1×10−4 s, W = 300 μm = 0.03 cm, Dp = 12 cm2/s, S = 100 cm/s (then 105 cm/s).

Find: τeff in each case.

Formula:

1/τeff = 1/τbulk + 2S/W (valid when SW/2D ≪ 1)

τsurface ≈ W/(2S) + W2/(π2D), 1/τeff = 1/τbulk + 1/τsurface (any S)

Solution.

Step 1. Oxidised surfaces. Check: SW/2D = 100 × 0.03/24 = 0.13, small, so the simple formula applies.

2S/W = 2 × 100/0.03 = 6.7×103 s−1, 1/τbulk = 1×104 s−1

1/τeff = 1.67×104 s−1 ⇒ τeff = 60 μs

Step 2. Bare surfaces. Check: SW/2D = 105 × 0.03/24 = 125, not small, so the simple formula would give a wrong answer (it predicts 0.15 μs). Use the full form:

W/(2S) = 0.03/(2 × 105) = 1.5×10−7 s = 0.15 μs

W2/(π2D) = (0.03)2/(9.87 × 12) = 7.6×10−6 s = 7.6 μs

τsurface ≈ 0.15 + 7.6 = 7.75 μs

1/τeff = 1/100 μs + 1/7.75 μs ⇒ τeff ≈ 7.2 μs

Answer: τeff = 60 μs with oxidised surfaces, but only about 7.2 μs with bare surfaces.

What this means: with a good oxide the wafer keeps most of its bulk lifetime, but with bare surfaces the surfaces, not the bulk, control the lifetime. Once S is this large, making the surface even worse hardly matters: the loss is limited by how fast holes can diffuse 150 μm to the nearest surface.

Reducing surface recombination (passivation): grow thermal SiO2 and anneal in hydrogen to tie up dangling bonds; deposit silicon nitride or aluminium oxide; add a heavily doped surface layer that repels minority carriers (a "back-surface field" in solar cells); and keep surfaces clean and damage-free.

### Bulk and surface recombination compared

|  | Bulk recombination | Surface recombination |
| --- | --- | --- |
| Where it happens | Throughout the volume of the crystal | In a very thin layer at the surface |
| Cause | Traps from impurities and crystal defects (SRH), plus band-to-band and Auger processes | Surface states, mainly dangling bonds, adsorbed impurities and oxide defects |
| How it is counted | Rate per unit volume, Δp/τbulk (cm−3s−1) | Rate per unit area, Us = SΔp(0) (cm−2s−1) |
| Key parameter | Bulk lifetime τbulk (s) | Surface recombination velocity S (cm/s) |
| Where it enters the equations | The −Δp/τp term of the diffusion equation | A boundary condition: Dp dΔp/dx = SΔp(0) at the surface |
| Most important when | Thick devices, poor-quality or contaminated crystal | Thin wafers, small devices, light absorbed near the surface |
| How it is reduced | Purer crystal, gettering of impurities, fewer defects | Passivation: thermal oxide with H2 anneal, SiNx or Al2O3 films, back-surface field |

## Key points of Week 9

- Continuity equation = carrier book-keeping: ∂p/∂t = −(1/q)∂Jp/∂x + G − R.

- Minority-carrier diffusion equation: ∂Δp/∂t = Dp∂2Δp/∂x2 − Δp/τp + GL.

- Standard solutions: decay in time e−t/τ; steady light Δp = GLτ; long bar e−x/L; short region a straight line.

- Diffusion length L = √(Dτ): how far a minority carrier travels before recombining.

- Surfaces have dangling bonds → surface states → fast recombination, measured by S (cm/s).

- 1/τeff = 1/τbulk + 2S/W for small S; for very large S the loss is limited by diffusion to the surfaces (τsurface cannot fall below W2/π2D). Passivation keeps S small.

## Examination questions solved (Q45–Q46)

### Q45. Explain the continuity equation for minority carriers and discuss its application to semiconductor devices.

Statement. The continuity equation expresses conservation of carriers: in any small volume, the rate of increase of carrier concentration equals the net inflow due to current, plus generation, minus recombination.

∂p/∂t = −(1/q) ∂Jp/∂x + Gp − Rp (holes)
∂n/∂t = +(1/q) ∂Jn/∂x + Gn − Rn (electrons)

Derivation. For a slab of area A and thickness dx, the number of holes increases at the rate (1/q)[Jp(x) − Jp(x + dx)]A from current flow and at (Gp − Rp)A dx from generation and recombination. Dividing by A dx and taking the limit gives the equations above.

Minority-carrier form. For holes in an n-type region, substitute the hole current Jp = qμppE − qDp ∂p/∂x and, for low-level injection, the recombination rate Rp − Gth = Δp/τp. With uniform doping:

∂Δp/∂t = Dp ∂2Δp/∂x2 − μpE ∂Δp/∂x − μp p ∂E/∂x + GL − Δp/τp

In a quasi-neutral region E ≈ 0, giving the ambipolar / minority-carrier diffusion equation:

∂Δp/∂t = Dp ∂2Δp/∂x2 − Δp/τp + GL

For electrons in p-type material: ∂Δn/∂t = Dn ∂2Δn/∂x2 − Δn/τn + GL.

Applications:

- p-n junction diode. In the neutral regions under steady forward bias, 0 = Dp d2Δp/dx2 − Δp/τp gives Δp(x) = Δp(xn)e−(x − xn)/Lp. The diffusion current at the depletion edge leads directly to the Shockley diode equation (Week 10).

- Bipolar transistor. In a narrow base (WB ≪ Ln), solving the equation gives a nearly linear minority-carrier profile; the slope gives collector current, and the small recombination loss gives the base transport factor and current gain.

- Photoconductive decay and lifetime measurement. For uniform illumination switched off at t = 0, Δp(t) = Δp(0)e−t/τp; measuring the decay of conductivity gives τ.

- Haynes–Shockley experiment. A pulse of minority carriers drifts and spreads; the time-dependent solution, a moving and broadening Gaussian, gives μp, Dp and τp and was used to verify the Einstein relation.

- Solar cells and photodiodes. With GL(x) = G0e−αx, the solution gives the collection efficiency and photocurrent and shows why the diffusion length must exceed the absorption depth.

- Switching transients. The time-dependent equation gives stored charge and the reverse-recovery time of diodes.

- Device simulation. Together with Poisson's equation and the current equations, the continuity equations are solved numerically in every TCAD simulator.

### Q46. What is surface recombination velocity? Explain how semiconductor surface states affect carrier lifetime.

Surface recombination velocity. At a semiconductor surface, recombination happens in a very thin layer through surface states. It is described per unit area as

Us = S · Δps (cm−2 s−1)

where Δps is the excess minority-carrier density at the surface and S is the surface recombination velocity (cm/s). It is the effective velocity at which excess carriers move into the surface and are annihilated. For surface traps of density Nst (cm−2) with capture cross-section σp:

S = σp vth Nst

S enters the boundary condition for the diffusion equation: Dp dΔp/dx = SΔp at the surface. S = 0 means an ideal surface; S → ∞ means every carrier arriving recombines (Δps = 0, like an Ohmic contact). Typical values: unpassivated Si 104–106 cm/s; thermally oxidised Si 10–103 cm/s; well-passivated Si < 10 cm/s.

Surface states. The crystal periodicity ends at the surface, leaving unsaturated (dangling) bonds, as well as adsorbed atoms, oxide defects and contamination. These produce a high density of localised energy levels distributed throughout the band gap, many near mid-gap.

How they affect lifetime:

- Additional recombination path. Mid-gap surface states are efficient SRH centres. Carriers that diffuse to the surface recombine there quickly, so the measured (effective) lifetime is lower than the bulk lifetime: 1/τeff = 1/τbulk + 1/τsurface, with 1/τsurface ≈ 2S/W for a wafer of thickness W recombining at both surfaces (valid while SW/2D ≪ 1; for very large S, τsurface ≈ W/2S + W2/π2D, limited by diffusion to the surfaces). In thin wafers and small devices surface recombination can dominate: a 300 μm n-type wafer with τbulk = 100 μs falls to τeff ≈ 60 μs at S = 100 cm/s and to about 7 μs at S = 105 cm/s (Example 9.4).

- Carrier depletion near the surface. The excess carrier density falls towards the surface, creating a gradient that pulls more carriers there, so even carriers generated deep in the material are lost.

- Surface band bending. Charge in surface states bends the bands, creating depletion or inversion layers. Under depletion, both electrons and holes are present in similar numbers near the surface, which maximises SRH recombination and generation.

- Leakage and noise. Surface generation adds to reverse leakage current of junctions where they meet the surface; trapping and detrapping produces 1/f noise; charged states cause threshold-voltage drift and instability in MOS devices.

- Device performance. High S reduces solar-cell efficiency (especially for blue light absorbed near the surface), reduces BJT current gain (surface recombination at the emitter–base perimeter), and degrades photodetector response.

Reduction (passivation): thermal oxidation (SiO2) with forming-gas (H2) anneal to tie up dangling bonds; silicon nitride and Al2O3 films with fixed charge for field-effect passivation; heavily doped surface layers (back-surface field) that repel minority carriers; and clean, damage-free surface preparation.

## Practice questions

These extra questions practise this week's ideas. Work each one on paper before reading the solution; the calculation questions follow the same Question, Given, Find, Solution, Answer layout as the worked examples.

#### Practice 9.1: electron diffusion length

Question. Electrons in p-type silicon have Dn = 25 cm2/s and τn = 10 μs. Find the diffusion length.

Given: Dn = 25 cm2/s, τn = 10−5 s.

Find: Ln.

Solution.

Ln = √(Dnτn) = √(25 × 10−5) = 1.58×10−2 cm = 158 μm

Answer: Ln ≈ 160 μm.

What this means: electrons in this p-type material survive long enough to cross a region about 0.16 mm thick, so a p-type layer a few micrometres thick loses almost none of them.

#### Practice 9.2: injected profile and current

Question. Holes are injected at x = 0 into a long n-type bar with Δp(0) = 1×1014 cm−3, Dp = 12 cm2/s and Lp = 30 μm. Find the hole current density at x = 0 and the excess hole concentration at x = 60 μm.

Given: Δp(0) = 1014 cm−3, Dp = 12 cm2/s, Lp = 3×10−3 cm.

Find: Jp(0) and Δp(60 μm).

Solution.

Jp(0) = qDpΔp(0)/Lp = 1.6×10−19 × 12 × 1014 / 3×10−3 = 0.064 A/cm2
Δp(60 μm) = Δp(0) e−60/30 = 1014 × e−2 = 1.35×1013 cm−3

Answer: Jp(0) = 64 mA/cm2, Δp(60 μm) = 1.35×1013 cm−3.

#### Practice 9.3: diffusion across a short region

Question. Electrons are injected into a p-type region only 2 μm wide (much shorter than Ln), with Δn = 1×1015 cm−3 at one side and Δn = 0 at the other. Find the electron current density (Dn = 25 cm2/s).

Given: W = 2×10−4 cm, Δn(0) = 1015 cm−3, Δn(W) = 0, Dn = 25 cm2/s.

Find: Jn.

Solution. In a short region the profile is a straight line, so the gradient is Δn(0)/W:

Jn = qDnΔn(0)/W = 1.6×10−19 × 25 × 1015 / 2×10−4 = 20 A/cm2

Answer: Jn = 20 A/cm2. This is exactly the situation in a BJT base (Week 13).

#### Practice 9.4: how good must the surface be?

Question. A 200 μm thick wafer has a bulk lifetime of 200 μs. What surface recombination velocity can be tolerated if the effective lifetime must be at least 50 μs?

Given: τbulk = 2×10−4 s, τeff = 5×10−5 s, W = 0.02 cm.

Find: S.

Solution.

2S/W = 1/τeff − 1/τbulk = 2×104 − 5×103 = 1.5×104 s−1
S = 1.5×104 × 0.02 / 2 = 150 cm/s

Answer: S ≤ 150 cm/s, achievable with a good thermal oxide.

What this means: for silicon (D ≈ 12–35 cm2/s), SW/2D = 150 × 0.02/(2D) is at most about 0.13, so the simple formula is valid here. Even a "good" surface takes away three quarters of the lifetime of a 200 μm wafer.

#### Practice 9.5: surface recombination current

Question. At a surface with S = 1000 cm/s the excess hole concentration is 1×1013 cm−3. Find the recombination rate per unit area and the equivalent current density lost to the surface.

Given: S = 103 cm/s, Δps = 1013 cm−3.

Find: Us and J = qUs.

Solution.

Us = SΔps = 103 × 1013 = 1016 cm−2s−1
J = qUs = 1.6×10−19 × 1016 = 1.6×10−3 A/cm2

Answer: Us = 1016 cm−2s−1, J = 1.6 mA/cm2.

#### Practice 9.6: no recombination

Question. What does the steady-state minority-carrier profile look like if the lifetime is infinite (no recombination) and there is no field or generation? Why?

Answer. The diffusion equation reduces to Dp d2Δp/dx2 = 0, so the second derivative is zero and Δp is a straight line. With no recombination, every carrier that enters a slice must leave it, so the current, and hence the slope, is the same everywhere.

## Objectives check

Use this table to confirm you have met this week's objectives. Cover the Answer column and answer each check question from memory. If you cannot, go back to the section in the last column before moving on.

| # | Objective | Check yourself | Answer | Where it is taught |
| --- | --- | --- | --- | --- |
| 1 | Derive the continuity equation for holes and electrons. | Write the continuity equation for holes. | ∂p/∂t = −(1/q)∂Jp/∂x + Gp − Rp. | Deriving the continuity equation |
| 2 | Write and interpret the minority-carrier diffusion equation. | What does the term −Δp/τp represent? | Loss of excess holes by recombination. | The minority-carrier diffusion equation |
| 3 | Solve the diffusion equation for the standard cases. | What is the steady-state profile for injection into a long bar? | Δp(x) = Δp(0)e−x/Lp. | The four standard solutions; Example 9.1 |
| 4 | Calculate diffusion lengths and explain their importance. | Find Ln for Dn = 30 cm2/s, τn = 10 μs. | Ln = √(30 × 10−5) = 1.7×10−2 cm = 173 μm. | Diffusion length; Example 9.2 |
| 5 | Explain surface states and surface recombination velocity. | What value of S corresponds to an Ohmic metal contact? | S → ∞ (Δp forced to zero). | Surfaces and surface states; Example 9.3 |
| 6 | Calculate the effective lifetime of a wafer with recombining surfaces. | Write 1/τeff for a wafer of thickness W (small S). | 1/τeff = 1/τbulk + 2S/W, valid while SW/2D ≪ 1. | How surfaces shorten the lifetime; Example 9.4 |

Week 10 · Module 4 · Junctions, Interfaces & Characterisation

# The p-n Junction Diode

Plan: built-in potential, depletion width and electric-field profile; ideal diode (Shockley) equation derivation under forward and reverse bias.

## Learning objectives

By the end of this week you should be able to:

- Explain the formation of the depletion region in a p-n junction.

- Derive and calculate the built-in potential.

- Calculate the depletion width and electric-field profile.

- Explain the junction under forward and reverse bias and the law of the junction.

- Derive and use the Shockley diode equation.

- Explain breakdown and junction capacitance.

## Symbols and abbreviations used this week

Every symbol, constant and abbreviation on this page is listed here, even if an earlier week already defined it, so you can study this page on its own.

Constants and units

| Symbol | Meaning | Units / typical value |
| --- | --- | --- |
| q | Magnitude of the electronic charge | 1.6×10−19 C |
| k | Boltzmann constant | 8.617×10−5 eV/K = 1.381×10−23 J/K |
| kT | Thermal energy | 0.0259 eV (often 0.02585 eV) at 300 K |
| kT/q | Thermal voltage | 0.0259 V (about 26 mV) at 300 K |
| T | Absolute temperature | kelvin (K); room temperature = 300 K |
| εs (εsi) | Permittivity of silicon, 11.7ε0 | 1.04×10−12 F/cm |
| eV | Electron-volt, a unit of energy | 1 eV = 1.6×10−19 J |
| μm | Micrometre (micron) | 1 μm = 10−4 cm = 10−6 m |

Symbols

| Symbol | Meaning | Units / typical value |
| --- | --- | --- |
| Ec (EC) | Energy of the bottom of the conduction band | eV |
| Ev (EV) | Energy of the top of the valence band | eV |
| Eg | Band-gap energy, Ec − Ev | eV; Si 1.12, Ge 0.66, GaAs 1.42 at 300 K |
| EF | Fermi level: the energy at which a state has a 50 % chance of being occupied | eV |
| Ei | Intrinsic Fermi level, close to mid-gap | eV |
| p | Hole concentration (holes per cm3) | cm−3 |
| ni | Intrinsic carrier concentration (n = p = ni in pure material) | cm−3; Si ≈ 1×1010 at 300 K |
| pn0, np0 | Equilibrium minority concentrations: holes on the n side, electrons on the p side | cm−3; pn0 = ni2/ND |
| ND | Donor concentration | cm−3 |
| NA | Acceptor concentration | cm−3 |
| ND+, NA− | Concentrations of ionised donors and acceptors | cm−3 |
| Δn, Δp | Excess electron and hole concentrations above equilibrium | cm−3 |
| E (field) | Electric field (on band diagrams, E is energy instead) | V/cm |
| μ, μn, μp | Mobility: drift velocity per unit field (electrons, holes) | cm2/(V·s); Si μn 1350, μp 480 |
| J, Jn, Jp | Current density (total, electrons, holes) | A/cm2 |
| Dn, Dp | Diffusion coefficients of electrons and holes | cm2/s; Si 35 and 12.4 |
| τ, τn, τp | Minority-carrier lifetime (τeff: effective, including surfaces) | s; Si 1 ns – 1 ms |
| L, Ln, Lp | Diffusion length √(Dτ): distance a minority carrier travels before recombining | μm or cm |
| Vbi | Built-in potential of a junction or Schottky contact | V; typically 0.5–1 V |
| V, Va | Applied voltage (positive for forward bias) | V |
| W | Depletion-region width (in Week 13 WB, WE are base and emitter widths; in Week 14 W is channel width) | μm or cm |
| xn, xp | Parts of the depletion region on the n side and on the p side | μm |
| Emax | Peak electric field, at the junction | V/cm |
| Is, Js (IS) | Saturation current (density) of a diode or transistor | A; A/cm2 |
| I | Current | A |
| A (area) | Device or contact area | cm2 |
| η | Ideality factor of a diode, 1 (ideal) to 2 | dimensionless |
| C, Cj | Capacitance (junction or depletion capacitance) | F (pF = 10−12 F) |
| VBR | Breakdown voltage | V |
| nn0, pp0, pn0, np0 | Equilibrium densities: majority (nn0, pp0) and minority (pn0 holes on n side, np0 electrons on p side) | cm−3 |
| Δpn, Δnp | Excess minority carriers at the depletion edges (holes on n side, electrons on p side) | cm−3 |
| pn, np | Minority-carrier density: holes on the n side, electrons on the p side | cm−3 |
| ΔV, ΔVBE | A small change in a voltage | V |

Abbreviations

| Abbreviation | Meaning |
| --- | --- |
| Si | Silicon |
| Ge | Germanium |
| C-V | Capacitance–voltage (measurement or characteristic) |
| MOSFET | Metal–oxide–semiconductor field-effect transistor |
| BJT | Bipolar junction transistor |
| LED | Light-emitting diode |
| n+ | Very heavily doped n-type (similarly p+) |

## Key terms

Every important word used this week is defined here, so you can read this week on its own.

Band gap (Eg). The range of energies between the top of the valence band (Ev) and the bottom of the conduction band (Ec) in which a perfect crystal has no allowed electron states. For silicon it is 1.12 eV at 300 K.

Electron and hole. An electron is a free negative charge carrier in the conduction band. A hole is an empty state left in the valence band when an electron leaves it; it moves like a positive charge carrier.

Intrinsic carrier concentration (ni). The density of electrons (equal to the density of holes) in a pure, undoped semiconductor, created by heat alone. For silicon at 300 K it is about 1×1010 cm−3; it rises very steeply with temperature.

Doping (ND, NA). Adding small, controlled amounts of impurity atoms. Donors (density ND) give electrons and make the material n-type; acceptors (density NA) take electrons, create holes and make it p-type. Once they have given up or taken an electron, the donor and acceptor ions are charged and fixed in the crystal.

Majority and minority carriers. In n-type material electrons are the majority carriers and holes the minority carriers; in p-type material it is the other way round. In equilibrium the minority density follows from the mass-action law np = ni2.

pn0 = ni2/ND, np0 = ni2/NA

Where:

- pn0 = equilibrium hole (minority) density on the n side (cm−3)

- np0 = equilibrium electron (minority) density on the p side (cm−3)

- ni = intrinsic carrier concentration (cm−3)

- ND, NA = donor and acceptor concentrations (cm−3)

Why it matters: the diode current is carried by minority carriers, so it is set by these tiny densities.

Fermi level (EF). The energy at which an electron state has a 50 % chance of being occupied. In n-type material it lies near Ec, in p-type near Ev. In equilibrium it is flat (the same energy) everywhere in a connected system.

Drift and diffusion. The two ways carriers move. Drift is motion pushed by an electric field; diffusion is the spreading of carriers from where there are many to where there are few.

p-n junction. The boundary between a p-type region and an n-type region in one continuous crystal. On its own it forms a diode, which conducts easily in one direction only (rectification).

Depletion region (W). The thin layer on both sides of the junction that has lost almost all its mobile carriers, leaving only the fixed charged donor and acceptor ions. It is also called the space-charge region and is typically 0.1–10 μm wide.

Why it matters: all the applied voltage appears across this region, and its width sets the junction capacitance and the breakdown voltage.

Built-in potential (Vbi). The voltage that appears across the depletion region in equilibrium, created by the fixed ion charges. It is the barrier that stops further diffusion of majority carriers.

Vbi = (kT/q) ln( NAND / ni2 )

Where:

- Vbi = built-in potential (V)

- kT/q = thermal voltage, 0.0259 V at 300 K

- NA, ND = acceptor and donor concentrations (cm−3)

- ni = intrinsic carrier concentration, 1×1010 cm−3 for Si at 300 K

Depletion approximation. The simplifying assumption that the depletion region contains no mobile carriers at all and has sharp edges, while the regions outside it are exactly neutral.

Forward and reverse bias (Va). Forward bias makes the p side positive (Va > 0) and lowers the barrier to Vbi − Va; reverse bias makes the p side negative (Va < 0) and raises the barrier to Vbi + |Va|.

Minority-carrier injection (law of the junction). Under forward bias, majority carriers cross the lowered barrier and become minority carriers on the other side. The minority density at the edge of the depletion region rises exponentially with voltage.

pn(xn) = pn0 eqVa/kT

Where:

- pn(xn) = hole density at the n-side edge of the depletion region (cm−3)

- pn0 = equilibrium hole density on the n side (cm−3)

- Va = applied voltage (V), positive for forward bias

- kT/q = 0.0259 V at 300 K

Minority-carrier lifetime and diffusion length (τ, L). The lifetime τ is the average time an injected minority carrier survives before it recombines; the diffusion length L = √(Dτ) is the average distance it diffuses in that time (D is the diffusion coefficient, cm2/s).

Saturation current (Is). The small, almost voltage-independent current that flows under reverse bias, carried by minority carriers that diffuse to the depletion region and are swept across. In small silicon diodes it is about 10−15–10−12 A.

Shockley (ideal diode) equation. The current–voltage law of an ideal p-n junction, obtained by adding up the minority-carrier diffusion currents on both sides.

I = Is ( eqV/kT − 1 )

Where:

- I = diode current (A), positive in the forward direction

- Is = saturation current (A)

- V = applied voltage (V), positive for forward bias

- kT/q = thermal voltage, 0.0259 V at 300 K

Why it matters: it explains rectification: current grows tenfold for every 60 mV of forward bias but stays at −Is in reverse.

Breakdown (VBR). The sudden, large rise of reverse current at a high enough reverse voltage VBR, caused either by avalanche multiplication or by Zener tunnelling. It is not destructive if the current is limited.

Junction capacitance (Cj). The capacitance of the depletion region, which acts like a parallel-plate capacitor whose plate spacing W grows with reverse bias.

Cj = εsA/W

Where:

- Cj = junction (depletion) capacitance (F)

- εs = permittivity of silicon, 1.04×10−12 F/cm

- A = junction area (cm2)

- W = depletion width (cm)

## The big picture

A p-n junction is what you get when one part of a single crystal is p-type and the part next to it is n-type. It is the most important structure in electronics: it is a diode on its own, two of them make a bipolar transistor, and it appears in every MOSFET, solar cell, LED and laser.

Its key property is that it conducts easily one way and hardly at all the other way (rectification). This week explains why, using only ideas you already have:

- Diffusion (Week 7) makes carriers cross the junction, leaving fixed charges behind.

- Those charges create an electric field and a built-in voltage, which stops further diffusion.

- An applied voltage raises or lowers that barrier. Lowering it lets minority carriers be injected, and they diffuse and recombine (Weeks 8–9). Adding up that diffusion gives the diode equation.

## Forming the junction: where the depletion region comes from

Imagine joining p-type silicon (lots of holes, doping NA) and n-type silicon (lots of electrons, doping ND) in one crystal.

- Diffusion starts. There are many holes on the p side and very few on the n side, so holes diffuse from p into n. Electrons diffuse the other way, from n into p.

- Fixed charges are uncovered. Each hole that leaves the p side leaves behind a negative acceptor ion (NA−), which is locked in the crystal and cannot move. Each electron that leaves the n side leaves behind a positive donor ion (ND+). The carriers that cross also recombine with the majority carriers on the other side and disappear.

- A charged layer forms. Near the junction there is now a layer of negative ions on the p side and positive ions on the n side, with almost no mobile carriers in it. This is the depletion region (also called the space-charge region).

- The charges create a field. Positive charge on the n side and negative on the p side create an electric field pointing from n to p.

- The field pushes back. That field drives holes back to the p side and electrons back to the n side: a drift current opposite to the diffusion current.

- Balance. The depletion region grows until, for each type of carrier, drift exactly cancels diffusion. Now no net current flows. The Fermi level is flat across the whole junction, as it must be in equilibrium (Week 5).

The abrupt p-n junction in equilibrium. Top: the fixed charge in the depletion region (negative on the p side, positive on the n side). Middle: the electric field, strongest at the junction. Bottom: the band diagram; the Fermi level is flat and the bands bend by qVbi.

In plain words. Two crowds on either side of a line start mixing. But everyone who crosses leaves a tied-up dog behind, and the dogs bark at anyone trying to follow. Soon the barking (the field) is strong enough to stop the crossing. The strip full of dogs and empty of people is the depletion region.

## The built-in potential

The field in the depletion region corresponds to a voltage across it, the built-in potential Vbi. The n side is at a higher potential than the p side. In the band diagram, the bands on the p side sit higher than on the n side by qVbi.

We can find Vbi from the Fermi-level positions of Week 5. On the p side, EF is kT ln(NA/ni) below Ei. On the n side it is kT ln(ND/ni) above Ei. In the joined junction EF is one flat line, so the bands must bend by the sum:

qVbi = kT ln(NA/ni) + kT ln(ND/ni)

Vbi = (kT/q) ln( NA ND / ni2 )

Where:

- Vbi = built-in potential (V)

- kT/q = thermal voltage, 0.0259 V at 300 K (kT = 0.0259 eV is the thermal energy)

- NA = acceptor concentration on the p side (cm−3)

- ND = donor concentration on the n side (cm−3)

- ni = intrinsic carrier concentration, 1×1010 cm−3 for Si at 300 K

#### Example 10.1: built-in potential

Question. A silicon p-n junction has NA = 1×1017 cm−3 on the p side and ND = 1×1016 cm−3 on the n side. Calculate the built-in potential at 300 K.

Given: NA = 1×1017 cm−3, ND = 1×1016 cm−3, ni = 1×1010 cm−3, kT/q = 0.0259 V.

Find: Vbi.

Formula:

Vbi = (kT/q) ln( NAND / ni2 )

Solution.

Vbi = (kT/q) ln(NAND/ni2) = 0.0259 × ln(1017 × 1016 / 1020)

= 0.0259 × ln(1013) = 0.0259 × 29.93 = 0.775 V

Answer: Vbi = 0.775 V.

What this means: a majority carrier must climb an energy barrier of 0.775 eV, about 30 times the thermal energy kT, to cross the junction, so in equilibrium almost none do. The barrier is less than the band gap (1.12 eV), as it always is for non-degenerate doping.

You cannot measure Vbi with a voltmeter across a diode: where the wires meet the semiconductor, contact potentials appear that exactly cancel it. It is an internal barrier, not a battery.

## Depletion width and field: the depletion approximation

To calculate the width of the depletion region we make the depletion approximation: inside the region (from −xp on the p side to xn on the n side) there are no mobile carriers at all, only the fixed ions; outside it the material is neutral. Then Poisson's equation (the link between charge and field) gives:

Charge balance. The total negative charge equals the total positive charge:

NA xp = ND xn

Where:

- NA, ND = acceptor and donor concentrations (cm−3)

- xp = width of the depletion region on the p side (cm)

- xn = width of the depletion region on the n side (cm)

So the depletion region extends further into the more lightly doped side. If NA = 10 × ND, then xn = 10 × xp.

Width.

W = xn + xp = √( (2εs/q)(Vbi − Va)(1/NA + 1/ND) )

with xn = W NA/(NA + ND) and xp = W ND/(NA + ND).

Where:

- W = total depletion width, xn + xp (cm)

- εs = permittivity of silicon, 11.7 × 8.854×10−14 = 1.04×10−12 F/cm

- q = electronic charge, 1.6×10−19 C

- Vbi = built-in potential (V)

- Va = applied voltage (V), positive for forward bias, negative for reverse bias

- NA, ND = acceptor and donor concentrations (cm−3)

Peak field (at the junction):

Emax = qND xn/εs = qNA xp/εs, and Vbi − Va = ½ Emax W

Where:

- Emax = peak electric field, at the metallurgical junction (V/cm)

- q, NA, ND, xn, xp, εs, Vbi, Va, W = as above

The field is a triangle: zero at the edges of the depletion region, rising linearly to Emax at the junction. The area of that triangle, ½EmaxW, is the voltage across the region.

For a one-sided p+n junction (NA ≫ ND), almost all of W is on the n side: W ≈ √(2εs(Vbi − Va)/qND).

#### Example 10.2: depletion width and peak field

Question. For the junction of Example 10.1 at zero bias, calculate the total depletion width, how much of it lies on each side, and the peak electric field.

Given: Vbi = 0.775 V, NA = 1017 cm−3, ND = 1016 cm−3, εs = 1.04×10−12 F/cm, q = 1.6×10−19 C, Va = 0.

Find: W, xn, xp and Emax.

Formula:

W = √( (2εs/q)(Vbi − Va)(1/NA + 1/ND) ), xn = W NA/(NA + ND), Emax = qND xn/εs

Solution.

Step 1. Total width:

W = √( (2εs/q) Vbi (1/NA + 1/ND) )

= √( 2 × 1.04×10−12 × 0.775 × (10−17 + 10−16) / 1.6×10−19 ) = √(1.10×10−9) = 3.32×10−5 cm

Step 2. Split, using xn = W NA/(NA + ND):

xn = 0.332 × 10/11 = 0.30 μm, xp = 0.332 − 0.30 = 0.03 μm

Step 3. Peak field at the junction:

Emax = qNDxn/εs = 1.6×10−19 × 1016 × 3.0×10−5 / 1.04×10−12 = 4.7×104 V/cm

Answer: W = 0.33 μm (0.30 μm on the n side, 0.03 μm on the p side), Emax = 4.7×104 V/cm.

What this means: the region is only a third of a micrometre wide, and 90 % of it lies in the more lightly doped n side. Yet the field in it, 47 kV/cm (4.7 MV/m), is enormous by everyday standards; it is this strong field that sweeps any carrier arriving at the depletion region straight across.

## The junction under bias

Forward bias (p side made positive, Va > 0). The applied voltage opposes the built-in voltage, so the barrier falls to Vbi − Va and the depletion region narrows. Diffusion now wins over drift. Holes pour from p into n, and electrons from n into p. On arrival they are minority carriers: they are injected. They diffuse away from the junction and recombine (Week 9). The current rises steeply (exponentially) with voltage.

Reverse bias (p side negative, Va < 0). The applied voltage adds to the built-in voltage. The barrier rises to Vbi + |Va| and the depletion region widens. Diffusion is shut off. The only current left is the tiny drift of the few minority carriers that happen to wander to the edge of the depletion region and get swept across. This is the reverse saturation current, almost independent of voltage, until breakdown.

The law of the junction. The barrier controls how many carriers can be injected. At the edges of the depletion region, the minority-carrier concentrations become:

pn(xn) = pn0 eqVa/kT, np(−xp) = np0 eqVa/kT

Where:

- pn(xn) = hole density at the n-side edge of the depletion region (cm−3)

- np(−xp) = electron density at the p-side edge of the depletion region (cm−3)

- pn0 = ni2/ND and np0 = ni2/NA = equilibrium minority concentrations (cm−3)

- Va = applied voltage (V), positive for forward bias

- kT/q = thermal voltage, 0.0259 V at 300 K

Forward bias multiplies the minority densities by eqVa/kT; reverse bias makes them almost zero. Every 60 mV of forward bias multiplies the injected minority carriers by 10.

### Forward and reverse bias compared

The numbers in the depletion-width row are for the junction of Examples 10.1 and 10.2 (NA = 1017, ND = 1016 cm−3, Vbi = 0.775 V).

|  | Forward bias | Reverse bias |
| --- | --- | --- |
| Connection | p side positive, n side negative (Va > 0) | p side negative, n side positive (Va < 0) |
| Barrier height | Lowered to Vbi − Va | Raised to Vbi + ¦Va¦ |
| Depletion width | Narrower (0.20 μm at Va = +0.5 V) | Wider (0.91 μm at Va = −5 V); W ∝ √(Vbi + ¦Va¦) |
| Peak field | Smaller | Larger |
| Minority carriers at the depletion edges | Increased by eqVa/kT: carriers are injected | Reduced almost to zero: carriers are extracted |
| Dominant current | Diffusion of injected minority carriers | Drift of the few minority carriers that reach the depletion region |
| Current size | Large; rises tenfold every 60 mV, I ≈ Is eqV/kT | Tiny and nearly constant, I ≈ −Is, until breakdown |
| Resistance | Low | Very high |
| Main capacitance | Diffusion capacitance (from stored minority carriers) | Junction (depletion) capacitance Cj = εsA/W, falling as ¦Va¦ rises |
| Typical uses | Rectifier conduction, LEDs, the emitter junction of a BJT | Blocking in rectifiers, photodiodes, varactors, Zener regulators, the collector junction of a BJT |

## The ideal diode (Shockley) equation, in words

The full derivation is worked in exam question Q48 below. The idea in four steps:

- Injection. The law of the junction gives the excess minority carriers at each edge of the depletion region: Δp = pn0(eqV/kT − 1) on the n side.

- Diffusion and recombination. In each neutral region the excess decays exponentially over a diffusion length (Week 9): Δp(x) = Δp(xn)e−(x − xn)/Lp.

- Current at the edge. The diffusion current at the edge is qDp × slope = (qDp/Lp)Δp(xn). Same for electrons on the p side.

- Add them. The total current is the sum of the hole and electron diffusion currents:

I = Is ( eqV/kT − 1 ), Is = qA ni2 ( Dp/(LpND) + Dn/(LnNA) )

Where:

- I = diode current (A), positive in the forward direction

- Is = saturation current (A)

- V = applied voltage (V), positive for forward bias

- kT/q = thermal voltage, 0.0259 V at 300 K

- q = electronic charge, 1.6×10−19 C

- A = junction area (cm2)

- ni = intrinsic carrier concentration, 1×1010 cm−3 for Si at 300 K

- Dp, Dn = diffusion coefficients of holes (in the n region) and electrons (in the p region) (cm2/s)

- Lp, Ln = diffusion lengths of holes and electrons, √(Dpτp) and √(Dnτn) (cm)

- ND, NA = donor and acceptor concentrations (cm−3)

The ideal diode characteristic. Forward current grows ten times for every 60 mV at 300 K; reverse current is a tiny −Is.

What the equation says:

- Forward (V > about 0.1 V): the −1 is negligible and I ≈ Is eqV/kT. Because Is is tiny (10−15–10−12 A for small Si diodes), a noticeable current needs about 0.6–0.7 V in Si (0.2–0.3 V in Ge).

- Reverse (V negative, more than a few kT/q): eqV/kT → 0 and I ≈ −Is, tiny and constant.

- Is ∝ ni2, so it rises steeply with temperature and is much larger in small-gap materials (Ge diodes leak far more than Si).

#### Example 10.3: saturation current and forward current of a diode

Question. A silicon p+n diode has ND = 1×1016 cm−3 on the n side, hole diffusion coefficient Dp = 10 cm2/s, hole lifetime τp = 1 μs and area 10−4 cm2. Calculate the saturation current, and the forward current at 0.6 V and at 0.7 V (300 K).

Given: ND = 1016 cm−3, Dp = 10 cm2/s, τp = 10−6 s, A = 10−4 cm2, ni = 1010 cm−3, kT/q = 0.0259 V.

Find: Is, I(0.6 V), I(0.7 V).

Formula:

Lp = √(Dpτp), Is ≈ qAni2Dp/(LpND) (p+n: hole term only), I ≈ Is eqV/kT

Solution.

Step 1. Diffusion length: Lp = √(Dpτp) = √(10 × 10−6) = 3.16×10−3 cm

Step 2. For a p+n diode only the hole term matters:

Is ≈ qAni2Dp/(LpND) = 1.6×10−19 × 10−4 × 1020 × 10 / (3.16×10−3 × 1016) = 5.1×10−16 A

Step 3. Forward current, I ≈ Is eqV/kT:

I(0.6 V) = 5.1×10−16 × e0.6/0.0259 = 5.1×10−16 × 1.15×1010 = 5.9×10−6 A

I(0.7 V) = 5.1×10−16 × e0.7/0.0259 = 5.1×10−16 × 5.45×1011 = 2.8×10−4 A

Answer: Is = 5.1×10−16 A; I = 5.9 μA at 0.6 V and 280 μA at 0.7 V. An extra 0.1 V multiplies the current by about 47.

What this means: the saturation current is less than a femtoampere, so nothing useful flows until the forward voltage reaches about 0.6 V. Above that the current rises so steeply that a silicon diode conducting anything from microamps to milliamps always shows a forward drop of roughly 0.6–0.7 V.

## Breakdown

At large reverse voltage the current suddenly rises. Two mechanisms:

- Avalanche breakdown. Carriers crossing the strong depletion field gain enough energy to knock new electron–hole pairs out of the lattice (impact ionisation, Week 8), which multiply in a chain reaction. Typical of lightly doped junctions; breakdown voltage above about 6 V; rises with temperature.

- Zener breakdown. In very heavily doped junctions the depletion region is extremely thin, and electrons tunnel straight through from the p-side valence band to the n-side conduction band. Breakdown voltage below about 4 V; falls with temperature. Used in Zener voltage regulators.

Between about 4 V and 6 V both mechanisms act together, and their opposite temperature effects nearly cancel; this is why diodes rated near 5–6 V have the most temperature-stable breakdown voltage.

### Avalanche and Zener breakdown compared

|  | Avalanche breakdown | Zener breakdown |
| --- | --- | --- |
| Mechanism | Impact ionisation: accelerated carriers knock out new electron–hole pairs, which multiply in a chain | Quantum-mechanical tunnelling of electrons straight through the thin barrier, from the p-side valence band to the n-side conduction band |
| Doping | Lightly or moderately doped (at least one side) | Very heavily doped on both sides (p+n+) |
| Depletion width | Wide; carriers need distance to gain energy | Very narrow (of order 10 nm) so tunnelling is possible |
| Breakdown voltage | Above about 6 V (up to thousands of volts) | Below about 4 V |
| Field needed | Of order 3×105 V/cm in Si, reached over a wide region | About 106 V/cm, reached across a very thin region |
| Temperature coefficient of VBR | Positive: VBR rises with temperature (more phonon scattering, carriers lose energy) | Negative: VBR falls with temperature (band gap shrinks, tunnelling easier) |
| Onset | Sharp knee | Softer, more gradual knee |
| Uses | High-voltage rectifiers, avalanche photodiodes, surge-protection diodes | Low-voltage reference and regulator ("Zener") diodes |

## Junction capacitance

The depletion region is a layer of stored charge between two conducting regions, so it behaves as a capacitor with plate separation W:

Cj = εsA/W

Where:

- Cj = junction (depletion) capacitance (F)

- εs = permittivity of silicon, 1.04×10−12 F/cm

- A = junction area (cm2)

- W = depletion width at the operating voltage (cm)

Since W grows with reverse bias, Cj falls as the reverse voltage increases. Diodes used deliberately as voltage-controlled capacitors (in radio tuning) are called varactors. Measuring Cj against voltage is also how doping is measured (C-V profiling, Week 12). Under forward bias the stored minority carriers add a larger diffusion capacitance.

## Key points of Week 10

- Diffusion across the junction uncovers fixed ions: the depletion region, with a field from n to p.

- Equilibrium: drift balances diffusion, EF is flat, and the bands bend by qVbi = kT ln(NAND/ni2).

- NAxp = NDxn: the depletion region lies mostly on the lightly doped side. W = √((2εs/q)(Vbi − V)(1/NA + 1/ND)).

- Forward bias lowers the barrier and injects minority carriers (law of the junction); reverse bias raises it.

- Shockley equation: I = Is(eqV/kT − 1), from minority-carrier diffusion in the neutral regions.

- Breakdown by avalanche (lightly doped) or Zener tunnelling (heavily doped); Cj = εsA/W.

## Examination questions solved (Q47–Q48)

### Q47. Explain the formation of the depletion region and built-in potential in a p-n junction.

Formation of the depletion region.

- When p-type and n-type regions are formed in one crystal, the p side has a high hole concentration (pp0 ≈ NA) and the n side a high electron concentration (nn0 ≈ ND). The steep concentration gradients cause holes to diffuse from p to n and electrons from n to p.

- Holes leaving the p side near the junction leave behind immobile negative acceptor ions; electrons leaving the n side leave behind immobile positive donor ions. Diffusing carriers also recombine with the majority carriers on the other side.

- A region on both sides of the metallurgical junction is therefore stripped of mobile carriers and contains only fixed ionic charge: negative on the p side, positive on the n side. This is the depletion region or space-charge region, typically 0.1–10 μm wide.

- The two charge layers are equal in magnitude, NA xp = ND xn, so the depletion region extends further into the more lightly doped side.

- The space charge produces an electric field directed from the positive (n) side to the negative (p) side, maximum at the junction: Emax = qND xn/εs.

- This field drives drift currents of holes back to p and electrons back to n, opposing the diffusion. The depletion region grows until drift exactly balances diffusion for both carriers and the net current is zero. In equilibrium the Fermi level is constant throughout.

Built-in potential. The field corresponds to an electrostatic potential difference across the depletion region, the built-in potential Vbi, with the n side positive with respect to the p side. In the band diagram, the bands bend by qVbi so that the flat Fermi level is near Ev on the p side and near Ec on the n side. It forms a potential barrier that majority carriers must surmount to cross.

Its value follows from the Fermi-level positions: q Vbi = (Ei − EF)p + (EF − Ei)n = kT ln(NA/ni) + kT ln(ND/ni), so

Vbi = (kT/q) ln( NA ND / ni2 )

Width of the depletion region:

W = √( (2εs Vbi / q)(NA + ND)/(NA ND) )

Example (Si, NA = 1017, ND = 1016 cm−3): Vbi = 0.0259 ln(1013) = 0.775 V; W = 0.33 μm, of which 0.30 μm is on the n side; Emax ≈ 4.7×104 V/cm.

The built-in potential cannot drive current in an external circuit, because in equilibrium it is exactly balanced by the contact potentials at the metal–semiconductor contacts. Applied bias changes the barrier to Vbi − Va, which is the basis of rectification.

### Q48. Derive the ideal Shockley diode equation and explain the effect of forward and reverse bias.

Assumptions (Shockley):

- Abrupt junction; depletion approximation (no carriers in the depletion region, neutral elsewhere).

- Boltzmann statistics apply (non-degenerate).

- Low-level injection: injected minority densities are much smaller than majority densities.

- No generation or recombination inside the depletion region, so electron and hole currents are each constant across it.

- All applied voltage V appears across the depletion region; neutral regions have negligible resistance (zero field).

- Long neutral regions (longer than the diffusion lengths) terminated by Ohmic contacts.

Step 1: law of the junction. In equilibrium nn0/np0 = exp(qVbi/kT). With bias V the barrier becomes Vbi − V, and (quasi-equilibrium across the depletion region) the minority densities at its edges become:

pn(xn) = pn0 exp(qV/kT), np(−xp) = np0 exp(qV/kT)

So the excess minority densities at the edges are:

Δpn(xn) = pn0 [ exp(qV/kT) − 1 ], Δnp(−xp) = np0 [ exp(qV/kT) − 1 ]

Step 2: minority-carrier diffusion in the neutral n region. With E = 0 and steady state, the continuity equation reduces to

Dp d2Δpn/dx2 − Δpn/τp = 0

For a long region (Δp → 0 as x → ∞) the solution is

Δpn(x) = Δpn(xn) exp( −(x − xn)/Lp ), Lp = √(Dpτp)

Step 3: hole diffusion current at x = xn. With no field, the hole current is pure diffusion:

Jp(xn) = −qDp dΔpn/dx |xn = (qDp/Lp) Δpn(xn) = (qDp pn0/Lp) [ exp(qV/kT) − 1 ]

Step 4: electron current at x = −xp. Similarly in the p region:

Jn(−xp) = (qDn np0/Ln) [ exp(qV/kT) − 1 ]

Step 5: total current. With no recombination in the depletion region, Jn is the same at xn as at −xp, so the total current (constant everywhere) is the sum of the two minority diffusion currents at the depletion edges:

J = Jp(xn) + Jn(−xp) = [ qDp pn0/Lp + qDn np0/Ln ] [ exp(qV/kT) − 1 ]

Using pn0 = ni2/ND and np0 = ni2/NA:

J = Js [ exp(qV/kT) − 1 ], Js = q ni2 ( Dp/(Lp ND) + Dn/(Ln NA) )

or, for area A, I = Is [ exp(qV/kT) − 1 ] with Is = AJs. This is the ideal Shockley diode equation.

Ideal diode characteristic. Forward current grows by a factor of 10 for every 60 mV at 300 K; reverse current saturates at −Is.

Effect of forward bias (V > 0, p side positive):

- The barrier is lowered to Vbi − V and the depletion region narrows.

- Minority carriers are injected: the edge densities increase by exp(qV/kT).

- For V ≫ kT/q (above about 0.1 V) the −1 is negligible: I ≈ Is exp(qV/kT). Current increases by a decade every 2.3kT/q ≈ 60 mV.

- Significant current flows only above the "cut-in" voltage (≈ 0.6–0.7 V in Si, ≈ 0.2–0.3 V in Ge), because Is is so small.

Effect of reverse bias (V < 0):

- The barrier rises to Vbi + |V|; the depletion region widens.

- The edge minority densities fall almost to zero (exp(qV/kT) → 0). Carriers are extracted rather than injected.

- For |V| ≫ kT/q: I ≈ −Is, a small, voltage-independent reverse saturation current (Si, about 10−15–10−12 A for small diodes) carried by minority carriers generated within a diffusion length of the junction.

- In real diodes, generation in the depletion region adds a current ∝ W ∝ √|V|, and at large |V| avalanche or Zener breakdown occurs.

Numerical example. A Si p+n diode with ND = 1016 cm−3, Dp = 10 cm2/s, τp = 1 μs, area 10−4 cm2: Lp = √(10 × 10−6) = 3.16×10−3 cm; Js ≈ qni2Dp/(LpND) = (1.6×10−19)(1020)(10)/(3.16×10−3 × 1016) = 5.1×10−12 A/cm2, so Is = 5.1×10−16 A. At V = 0.6 V, I = Is e0.6/0.0259 = 5.1×10−16 × 1.15×1010 ≈ 5.9 μA, and at 0.7 V it is about 280 μA.

Real diodes deviate: recombination in the depletion region at low forward bias (I ∝ eqV/2kT), high-level injection at high current, series resistance, and generation current and breakdown in reverse. These are summarised by I = Is(eqV/ηkT − 1), with ideality factor η between 1 and 2.

## Practice questions

These extra questions practise this week's ideas. Work each one on paper before reading the solution; the calculation questions follow the same Question, Given, Find, Solution, Answer layout as the worked examples.

#### Practice 10.1: built-in potential of a germanium junction

Question. A germanium junction has NA = ND = 1×1016 cm−3. Find Vbi at 300 K (ni = 2.4×1013 cm−3) and compare with silicon.

Given: NA = ND = 1016 cm−3, ni = 2.4×1013 cm−3, kT/q = 0.0259 V.

Find: Vbi.

Solution.

Vbi = 0.0259 ln(1032/5.76×1026) = 0.0259 ln(1.74×105) = 0.0259 × 12.06 = 0.31 V

Answer: Vbi = 0.31 V, against 0.72 V for silicon with the same doping: the smaller gap gives a smaller barrier.

#### Practice 10.2: reverse-biased depletion width and field

Question. A silicon p+n junction has ND = 1×1015 cm−3 and Vbi = 0.7 V. Find the depletion width and peak field at a reverse bias of 5 V.

Given: ND = 1015 cm−3, Vbi − V = 0.7 + 5 = 5.7 V, εs = 1.04×10−12 F/cm.

Find: W and Emax.

Solution.

W = √(2εs(Vbi − V)/qND) = √(2 × 1.04×10−12 × 5.7 / (1.6×10−19 × 1015)) = 2.72×10−4 cm
Emax = 2(Vbi − V)/W = 2 × 5.7/2.72×10−4 = 4.2×104 V/cm

Answer: W = 2.7 μm, Emax = 4.2×104 V/cm.

What this means: light doping and reverse bias together make the depletion region several micrometres wide, which is why lightly doped junctions can withstand large reverse voltages before the field reaches the avalanche level.

#### Practice 10.3: junction capacitance

Question. Find the junction capacitance of the diode in Practice 10.2 if its area is 1×10−3 cm2.

Given: W = 2.72×10−4 cm, A = 10−3 cm2, εs = 1.04×10−12 F/cm.

Find: Cj.

Solution.

Cj = εsA/W = 1.04×10−12 × 10−3 / 2.72×10−4 = 3.8×10−12 F

Answer: Cj = 3.8 pF.

What this means: increasing the reverse bias widens W and lowers Cj further; this voltage-controlled capacitance is what a varactor diode uses to tune a radio circuit.

#### Practice 10.4: saturation current with both sides

Question. A silicon diode has NA = 1×1017 cm−3, ND = 1×1016 cm−3, Dn = 20 cm2/s, Ln = 20 μm, Dp = 10 cm2/s, Lp = 10 μm. Find Js and the fraction carried by holes.

Given: the values above, ni = 1010 cm−3.

Find: Js and the hole fraction.

Solution.

Dp/(LpND) = 10/(10−3 × 1016) = 1.0×10−12
Dn/(LnNA) = 20/(2×10−3 × 1017) = 1.0×10−13
Js = qni2(1.0×10−12 + 1.0×10−13) = 1.6×10−19 × 1020 × 1.1×10−12 = 1.76×10−11 A/cm2
hole fraction = 1.0/1.1 = 91 %

Answer: Js = 1.8×10−11 A/cm2, 91 % carried by holes injected into the lightly doped n side.

#### Practice 10.5: temperature and the saturation current

Question. By roughly what factor does Is of a silicon diode increase when the temperature rises from 300 K to 310 K? (Take Is ∝ ni2 and ignore other temperature effects.)

Given: ni ∝ T3/2e−Eg/2kT, Eg = 1.12 eV.

Find: Is(310)/Is(300).

Solution.

ni(310)/ni(300) = (310/300)3/2 × exp[6499 × (1/300 − 1/310)] = 1.050 × e0.699 = 2.11
Is ratio = 2.112 = 4.5

Answer: about 4.5 times for a 10 K rise: reverse leakage is very temperature-sensitive.

#### Practice 10.6: forward voltage per decade

Question. How much must the forward voltage of an ideal diode increase to multiply the current by 10 at 300 K? If I = 1 mA at 0.60 V, what is I at 0.66 V?

Given: I ∝ eqV/kT, kT/q = 0.0259 V.

Find: ΔV per decade; I at 0.66 V.

Solution.

ΔV = (kT/q) ln 10 = 0.0259 × 2.303 = 59.6 mV
I(0.66) = 1 mA × e0.06/0.0259 = 1 × 10.1 = 10.1 mA

Answer: about 60 mV per decade; I ≈ 10 mA at 0.66 V.

#### Practice 10.7: avalanche or Zener?

Question. A diode breaks down at 3.3 V and its breakdown voltage falls as it warms up. Another breaks down at 50 V and its breakdown voltage rises with temperature. Identify the mechanism in each and explain the temperature behaviour.

Answer. The 3.3 V diode is Zener breakdown: it is heavily doped, its depletion region is very thin, and electrons tunnel across the gap. Heating shrinks the band gap, making tunnelling easier, so VBR falls. The 50 V diode is avalanche breakdown: carriers gain energy across a wide depletion region and impact-ionise. Heating increases lattice vibration, so carriers lose more energy to phonons between collisions and need a larger field to ionise, so VBR rises.

## Objectives check

Use this table to confirm you have met this week's objectives. Cover the Answer column and answer each check question from memory. If you cannot, go back to the section in the last column before moving on.

| # | Objective | Check yourself | Answer | Where it is taught |
| --- | --- | --- | --- | --- |
| 1 | Explain the formation of the depletion region in a p-n junction. | Why is the depletion region empty of mobile carriers? | Carriers diffused across and recombined, leaving only fixed donor and acceptor ions. | Forming the junction |
| 2 | Derive and calculate the built-in potential. | Find Vbi for NA = ND = 1016 cm−3 in Si. | 0.0259 ln(1012) = 0.716 V. | The built-in potential; Example 10.1 |
| 3 | Calculate the depletion width and electric-field profile. | If NA = 100 ND, where does most of the depletion region lie? | On the n side (xn = 100 xp). | Depletion approximation; Example 10.2 |
| 4 | Explain the junction under forward and reverse bias and the law of the junction. | By what factor does forward bias of 0.12 V multiply the injected minority carriers? | e0.12/0.0259 ≈ 100. | The junction under bias; Forward and reverse bias compared |
| 5 | Derive and use the Shockley diode equation. | Write the ideal diode equation and its saturation current density. | I = Is(eqV/kT − 1); Js = qni2(Dp/LpND + Dn/LnNA). | Shockley equation; Example 10.3; Q48 |
| 6 | Explain breakdown and junction capacitance. | Which breakdown mechanism occurs in very heavily doped junctions, and how does its VBR change with temperature? | Zener (tunnelling) breakdown; VBR falls as temperature rises. | Breakdown; Avalanche and Zener breakdown compared; junction capacitance |

Week 11 · Module 4 · Junctions, Interfaces & Characterisation

# Metal–Semiconductor Interfaces

Plan: Schottky barrier diode physics versus Ohmic contact mechanisms; energy band diagrams under equilibrium and bias.

## Learning objectives

By the end of this week you should be able to:

- Define work function and electron affinity and relate them.

- Explain how a Schottky barrier forms and calculate ΦB and Vbi.

- Explain thermionic emission and calculate Schottky diode currents.

- Draw Schottky band diagrams in equilibrium and under bias.

- Explain the two ways of making Ohmic contacts.

- Describe the stability problems of metal contacts.

- Compare Schottky and ohmic contacts, their advantages, limitations and applications.

## Symbols and abbreviations used this week

Every symbol, constant and abbreviation on this page is listed here, even if an earlier week already defined it, so you can study this page on its own.

Constants and units

| Symbol | Meaning | Units / typical value |
| --- | --- | --- |
| q | Magnitude of the electronic charge | 1.6×10−19 C |
| k | Boltzmann constant | 8.617×10−5 eV/K = 1.381×10−23 J/K |
| kT | Thermal energy | 0.0259 eV (often 0.02585 eV) at 300 K |
| kT/q | Thermal voltage | 0.0259 V (about 26 mV) at 300 K |
| T | Absolute temperature | kelvin (K); room temperature = 300 K |
| ε0 | Permittivity of free space | 8.854×10−14 F/cm |
| εs (εsi) | Permittivity of silicon, 11.7ε0 | 1.04×10−12 F/cm |
| eV | Electron-volt, a unit of energy | 1 eV = 1.6×10−19 J |
| μm | Micrometre (micron) | 1 μm = 10−4 cm = 10−6 m |

Symbols

| Symbol | Meaning | Units / typical value |
| --- | --- | --- |
| Ec (EC) | Energy of the bottom of the conduction band | eV |
| Ev (EV) | Energy of the top of the valence band | eV |
| Eg | Band-gap energy, Ec − Ev | eV; Si 1.12, Ge 0.66, GaAs 1.42 at 300 K |
| EF | Fermi level: the energy at which a state has a 50 % chance of being occupied | eV |
| Nc | Effective density of states in the conduction band | cm−3; Si 2.8×1019 at 300 K |
| ND | Donor concentration | cm−3 |
| NA | Acceptor concentration | cm−3 |
| Q | Dose: dopant atoms per unit area (in Weeks 13–14, Q also means charge) | atoms/cm2 (C or C/cm2 for charge) |
| E (field) | Electric field (on band diagrams, E is energy instead) | V/cm |
| μ, μn, μp | Mobility: drift velocity per unit field (electrons, holes) | cm2/(V·s); Si μn 1350, μp 480 |
| τ, τn, τp | Minority-carrier lifetime (τeff: effective, including surfaces) | s; Si 1 ns – 1 ms |
| Vbi | Built-in potential of a junction or Schottky contact | V; typically 0.5–1 V |
| V, Va | Applied voltage (positive for forward bias) | V |
| W | Depletion-region width (in Week 13 WB, WE are base and emitter widths; in Week 14 W is channel width) | μm or cm |
| Emax | Peak electric field, at the junction | V/cm |
| Is, Js (IS) | Saturation current (density) of a diode or transistor | A; A/cm2 |
| I | Current | A |
| A (area) | Device or contact area | cm2 |
| η | Ideality factor of a diode, 1 (ideal) to 2 | dimensionless |
| Φm | Work function of a metal | eV; Al 4.28, Au 5.1 |
| Φs | Work function of a semiconductor, χ + (Ec − EF) | eV |
| χ | Electron affinity: energy from Ec up to the vacuum level | eV; Si 4.05 |
| ΦB | Schottky barrier height seen from the metal | eV (or V) |
| A∗∗ | Effective Richardson constant | A/(cm2·K2); n-Si ≈ 110 |
| ρc | Specific contact resistance | Ω·cm2 |
| Evac | Vacuum level: energy of an electron just free of the material | eV |
| Rc | Contact resistance | Ω (specific: Ω·cm2) |
| ΦBn, ΦBp | Schottky barrier height for electrons (n-type) and for holes (p-type) | eV |

Abbreviations

| Abbreviation | Meaning |
| --- | --- |
| Si | Silicon |
| Ge | Germanium |
| GaAs | Gallium arsenide |
| SiO2 | Silicon dioxide (silica), the oxide insulator |
| I-V | Current–voltage (measurement or characteristic) |
| MESFET | Metal–semiconductor field-effect transistor |
| IC | Integrated circuit |
| RF | Radio frequency |
| n+ | Very heavily doped n-type (similarly p+) |

## Key terms

Every important word used this week is defined here, so you can read this week on its own.

Metal. A material with a very large number of free electrons (about 1022 cm−3), so it conducts electricity very easily. Its electron states are filled up to the Fermi level, and there are empty states immediately above it. Examples: aluminium, gold, platinum, titanium, tungsten.

Semiconductor. A material whose conductivity lies between a metal's and an insulator's, and can be controlled by doping, temperature, light and electric fields. Examples: silicon (Si), germanium (Ge), gallium arsenide (GaAs).

Doping; n-type and p-type. Doping is adding a small, controlled amount of impurity atoms to a semiconductor. Donor atoms (e.g. phosphorus in Si, concentration ND) give free electrons and make it n-type. Acceptor atoms (e.g. boron, concentration NA) create holes and make it p-type.

Majority and minority carriers. The carrier that is in the majority: electrons in n-type material, holes in p-type. The other carrier is the minority carrier. A Schottky diode works with majority carriers only.

Conduction band edge (Ec) and valence band edge (Ev). Ec is the lowest energy a free electron can have in the semiconductor. Ev is the highest energy of the (almost full) valence band, where holes live.

Band gap (Eg). The energy gap between the conduction and valence bands, in which electrons cannot sit.

Eg = Ec − Ev

Where:

- Eg = band-gap energy (eV); 1.12 eV for Si at 300 K

- Ec = conduction-band edge (eV)

- Ev = valence-band edge (eV)

Fermi level (EF). The energy at which a state has a 50 % chance of being occupied by an electron. It marks how "full" a material is with electrons. In n-type material it lies near Ec, in p-type near Ev. At equilibrium the Fermi level is flat (the same everywhere) across any set of materials in contact. For n-type silicon:

Ec − EF = kT ln(Nc/ND)

Where:

- kT = thermal energy, 0.0259 eV at 300 K (0.02585 eV is used in this week's calculations)

- Nc = effective density of states in the conduction band, 2.8×1019 cm−3 for Si

- ND = donor concentration (cm−3)

Why it matters: the Fermi level sets the semiconductor's work function, and lining up the two Fermi levels is what bends the bands at a contact.

Vacuum level (Evac). The energy of an electron at rest just outside the material, free of it. Every other energy this week is measured down from this level.

Work function (Φ). The minimum energy needed to remove an electron from the Fermi level and take it to the vacuum level. Φm is the metal's work function, Φs the semiconductor's.

Φm = Evac − EF,m, Φs = Evac − EF,s

Where:

- Φm, Φs = work functions of the metal and of the semiconductor (eV)

- EF,m, EF,s = Fermi levels of the metal and of the semiconductor (eV)

Metal values (eV): Al 4.28, Ti 4.33, Cr 4.5, W 4.55, Au 5.1, Ni 5.15, Pt 5.65.

Why it matters: the sign of Φm − Φs decides whether a contact is rectifying or ohmic.

Electron affinity (χ). The energy from the bottom of the conduction band up to the vacuum level. Unlike Φs, it does not change with doping, so it is a fixed property of the material: Si 4.05 eV, GaAs 4.07 eV, Ge 4.0 eV.

χ = Evac − Ec

Metal–semiconductor contact (interface). The boundary formed where a metal touches a semiconductor. Every device has several, because every device must be wired to the circuit with metal.

Schottky contact (Schottky barrier). A metal–semiconductor contact that has an energy barrier to majority carriers, so it rectifies: current flows easily in one direction and hardly at all in the other. A diode made this way is a Schottky barrier diode (SBD).

Ohmic contact. A metal–semiconductor contact with no significant barrier, so current flows equally easily in both directions and the I-V graph is a straight line through the origin (V = IRc). Its job is to connect a device to the circuit while adding almost no resistance.

Rectifying. Conducting much better in one direction (forward bias) than the other (reverse bias).

Schottky barrier height (ΦB). The height of the barrier an electron in the metal must climb to enter the semiconductor. It is fixed by the interface and does not change with bias.

Depletion region (width W). A layer next to the interface emptied of free carriers, leaving only the fixed, charged dopant ions (positive donor ions in n-type). Those charges create an electric field and a voltage across the layer.

Built-in potential (Vbi). The voltage across the depletion region at equilibrium; the barrier an electron in the semiconductor must climb to reach the metal.

Band bending. The upward or downward curving of Ec and Ev near the interface, caused by the voltage across the depletion (or accumulation) region. Upward bending in n-type = a barrier to electrons.

Accumulation layer. A thin layer at the interface with extra majority carriers (the opposite of depletion). The bands bend downward in n-type, and there is no barrier.

Forward bias and reverse bias. For a metal on n-type: forward bias makes the metal positive with respect to the semiconductor (current flows easily); reverse bias makes the metal negative (only a small current flows).

Thermionic emission. Current carried by carriers that have enough thermal energy to jump over a barrier. It is how current flows in a Schottky diode.

Tunnelling (field emission). A quantum effect: an electron passes through a barrier that is thin enough (a few nanometres) without having the energy to go over it. It is how most practical ohmic contacts work.

Saturation current (Is, Js) and ideality factor (η). Is is the small current that flows under reverse bias; Js is the same per unit area. The ideality factor η (1 for an ideal diode, 1.0–1.1 for a good Schottky diode) measures how closely a real diode follows the ideal equation.

Fermi-level pinning. At a real interface, defects and surface states hold ("pin") the Fermi level near a fixed energy, so the measured barrier height depends much less on the metal than the ideal rule predicts.

Specific contact resistance (ρc). The resistance of a contact multiplied by its area, in Ω·cm2. It lets contacts of different sizes be compared. Good ohmic contacts have ρc ≈ 10−6–10−8 Ω·cm2.

## The big picture

Every device must be wired to the outside world with metal. You might expect a metal touching a semiconductor to behave like a simple wire connection. Sometimes it does: that is an ohmic contact, which lets current through equally well in both directions. But sometimes the contact itself forms a barrier and conducts in only one direction, like a diode: a Schottky contact.

Which one you get depends on the metal, the semiconductor and its doping. Engineers want ohmic contacts for wiring, and Schottky contacts when they want a very fast diode. A real Schottky diode has both: a Schottky contact on top that does the rectifying and an ohmic contact underneath that lets the current out.

A Schottky diode in cross-section. The metal anode sits on a lightly doped n-type layer: this is the rectifying Schottky contact, with its depletion region under the metal. The n-type layer is grown on a heavily doped n⁺ substrate whose metal back contact is ohmic. The oxide (SiO₂) ring insulates the edges of the metal.

This week explains both contacts with energy band diagrams, using one rule: at equilibrium the Fermi level is flat.

## The energies before contact

Before the metal and semiconductor touch, each has its own Fermi level, and we compare them by measuring everything down from the common vacuum level.

A metal and an n-type semiconductor before contact. The metal's Fermi level is qΦm below the vacuum level. In the semiconductor the conduction band edge is qχ below the vacuum level and the Fermi level qΦs below it. When Φm > Φs, the semiconductor's Fermi level is higher by q(Φm − Φs), so electrons will flow from the semiconductor into the metal on contact.

The semiconductor's work function is the electron affinity plus the gap between Ec and EF:

Φs = χ + (Ec − EF)

Where:

- Φs = work function of the semiconductor (eV)

- χ = electron affinity (eV); 4.05 eV for Si

- Ec − EF = how far the Fermi level lies below the conduction band edge (eV); it shrinks as ND increases

#### Example 11.1: work function of doped silicon

Question. Calculate the work function of n-type silicon doped with ND = 1×1016 cm−3 at 300 K. The electron affinity of Si is 4.05 eV.

Given: χ = 4.05 eV, ND = 1×1016 cm−3, Nc = 2.8×1019 cm−3, kT = 0.02585 eV.

Find: Φs.

Formula: Ec − EF = kT ln(Nc/ND), then Φs = χ + (Ec − EF).

Solution.

Step 1. Position of EF below Ec:

Ec − EF = 0.02585 × ln(2.8×1019 / 1×1016) = 0.02585 × 7.94 = 0.205 eV

Step 2. Work function:

Φs = 4.05 + 0.205 = 4.26 eV

Answer: Φs = 4.26 eV.

What this means: any metal with Φm above 4.26 eV (gold, nickel, platinum) will tend to form a barrier on this silicon; a metal below it would not.

## The Schottky barrier (rectifying contact)

### How it forms: metal on n-type with Φm > Φs

- Before contact, the semiconductor's Fermi level is higher than the metal's by Φm − Φs (figure above).

- On contact, electrons flow "downhill" from the semiconductor into the metal.

- The electrons that leave uncover positive donor ions near the interface in the semiconductor. These ions cannot move, so a depletion region forms. A thin sheet of extra electrons sits on the metal surface.

- The positive ions and the negative sheet create an electric field in the depletion region, pointing from the semiconductor towards the metal.

- The field makes the semiconductor's bands bend upward towards the interface.

- The flow stops when the two Fermi levels line up: one flat EF through the whole structure. Now the upward bend is a barrier that holds back further electron flow.

Metal on n-type silicon (Φm > Φs) after contact. An electron in the metal sees the barrier qΦB. An electron in the semiconductor sees the smaller built-in barrier qVbi.

There are now two barriers, depending on which side the electron starts from:

seen from the metal (barrier height): ΦB = Φm − χ (the ideal Schottky–Mott rule)
seen from the semiconductor (built-in): Vbi = Φm − Φs = ΦB − (Ec − EF)/q

Where:

- ΦB = Schottky barrier height for electrons (eV, or V when divided by q)

- Φm = metal work function (eV); χ = electron affinity (eV); Φs = semiconductor work function (eV)

- Vbi = built-in potential (V); with energies in eV, the number in eV equals the voltage in V

For a p-type semiconductor everything flips: a rectifying contact needs Φm < Φs, and the barrier for holes is

ΦBp = Eg − (Φm − χ) = Eg − ΦB

Where ΦBp = hole barrier height (eV) and Eg = band gap (eV). For example, aluminium on p-Si: ΦBp = 1.12 − (4.28 − 4.05) = 0.89 eV.

#### Example 11.2: ideal Schottky barrier

Question. Gold (Φm = 5.1 eV) is deposited on the n-type silicon of Example 11.1. Using the ideal Schottky–Mott model, find the barrier height seen from the metal and the built-in potential seen from the semiconductor. Is the contact rectifying or ohmic?

Given: Φm = 5.1 eV, χ = 4.05 eV, Φs = 4.26 eV.

Find: ΦB, Vbi, and the type of contact.

Formula: ΦB = Φm − χ; Vbi = Φm − Φs.

Solution.

ΦB = 5.1 − 4.05 = 1.05 eV

Vbi = 5.1 − 4.26 = 0.84 V

Φm > Φs on n-type silicon, so a depletion region forms: the contact is rectifying.

Answer: ΦB = 1.05 eV, Vbi = 0.84 V: a rectifying (Schottky) contact.

What this means: an electron in the metal faces a 1.05 eV climb, about 40 kT, so very few cross from the metal: that is why the reverse current is small. In practice Fermi-level pinning gives a measured ΦB of about 0.8 eV for Au on n-Si.

### The depletion region

The depletion region under the metal is exactly like the n side of a very one-sided (p+n) junction, because the metal holds its compensating charge in a sheet at its surface. With the depletion approximation (no free carriers in the region, uniform doping):

W = √( 2εs(Vbi − V) / qND ), Emax = qND W / εs

Where:

- W = depletion width (cm)

- εs = permittivity of silicon, 11.7ε0 = 1.04×10−12 F/cm

- Vbi = built-in potential (V); V = applied voltage (positive for forward bias)

- q = 1.6×10−19 C; ND = donor concentration (cm−3)

- Emax = peak electric field, at the interface (V/cm)

Rearranged at zero bias, Vbi = qND W2 / 2εs. Note that W ∝ 1/√ND: more doping means a thinner depletion region. This is the key to ohmic contacts below.

#### Example 11.3: depletion width under a gold contact

Question. For the gold contact of Example 11.2 (Vbi = 0.84 V, ND = 1×1016 cm−3), calculate the depletion width and the peak field at zero bias.

Given: Vbi = 0.84 V, V = 0, ND = 1×1016 cm−3, εs = 1.04×10−12 F/cm, q = 1.6×10−19 C.

Find: W and Emax.

Formula: W = √(2εsVbi/qND); Emax = qND W/εs.

Solution.

W = √( 2 × 1.04×10−12 × 0.84 / (1.6×10−19 × 1016) ) = √(1.09×10−9) = 3.3×10−5 cm = 0.33 μm

Emax = 1.6×10−19 × 1016 × 3.3×10−5 / 1.04×10−12 = 5.1×104 V/cm

Answer: W = 0.33 μm, Emax = 5.1×104 V/cm.

What this means: the barrier is about 0.33 μm thick, far too thick for electrons to tunnel through, so they must go over it by thermionic emission. The contact rectifies.

### How current flows: thermionic emission

In a Schottky diode the current is carried by majority carriers (electrons in n-type) jumping over the barrier. Only electrons with enough thermal energy can get over, so the current depends exponentially on the barrier height:

J = Js ( eqV/ηkT − 1 ), Js = A∗∗ T2 e−qΦB/kT

Where:

- J = current density (A/cm2); I = J × A for a diode of area A

- Js = saturation current density (A/cm2)

- V = applied voltage, positive for forward bias (metal positive on n-type) (V)

- η = ideality factor: 1 for the ideal model, 1.0–1.1 for good diodes

- kT/q = thermal voltage, 0.0259 V at 300 K

- A∗∗ = effective Richardson constant: about 110 A/cm2K2 for n-Si, 8 for n-GaAs

- T = absolute temperature (K)

- ΦB = barrier height (eV in qΦB/kT with kT in eV)

The shape is the same as a p-n diode, but Js is far larger, so the diode turns on at a lower voltage.

#### Example 11.4: Schottky saturation current

Question. A Schottky diode on n-type silicon has a barrier height of 0.8 eV. Taking A∗∗ = 110 A/cm2K2, calculate the saturation current density at 300 K and the forward voltage needed for 1 A/cm2.

Given: ΦB = 0.8 eV, A∗∗ = 110 A/cm2K2, T = 300 K, kT = 0.0259 eV, J = 1 A/cm2, η = 1.

Find: Js, and V at J = 1 A/cm2.

Formula: Js = A∗∗T2e−qΦB/kT; V = (kT/q) ln(J/Js) (forward bias, J ≫ Js).

Solution.

Step 1. Saturation current density:

Js = 110 × 3002 × e−0.8/0.0259 = 9.9×106 × 3.9×10−14 = 3.8×10−7 A/cm2

Step 2. Forward voltage:

V = 0.0259 × ln(1/3.8×10−7) = 0.0259 × 14.8 = 0.38 V

Answer: Js = 3.8×10−7 A/cm2; 1 A/cm2 flows at about 0.38 V.

What this means: a silicon p-n diode needs about 0.7 V for the same current, because its Js is about 105 times smaller. The Schottky diode wastes less power as heat when it conducts.

#### Example 11.5: forward current of a Schottky diode

Question. An ideal Schottky diode has a saturation current of 2 μA. Calculate its current at 300 K when a forward voltage of 0.20 V is applied.

Given: Is = 2×10−6 A, V = 0.20 V, η = 1, T = 300 K, kT/q = 0.02585 V.

Find: I.

Formula: I = Is ( eqV/ηkT − 1 ).

Solution.

Step 1. Exponent: qV/kT = 0.20 / 0.02585 = 7.737

Step 2. Exponential: e7.737 = 2291

Step 3. Current:

I = 2×10−6 × (2291 − 1) = 4.58×10−3 A

Answer: I = 4.58 mA.

What this means: only 0.2 V multiplies the current more than two-thousand-fold above Is. Every extra 0.1 V multiplies it by a further e0.1/0.0259 ≈ 48. In a real diode the series resistance and η > 1 make the current somewhat smaller.

### Schottky diode versus p-n diode

|  | Schottky diode | p-n junction diode |
| --- | --- | --- |
| Current carried by | Majority carriers only | Minority carriers injected and diffusing |
| Mechanism | Thermionic emission over the barrier | Diffusion |
| Stored minority charge | Practically none | Q = Iτ |
| Switching speed | Very fast, no reverse-recovery delay | Slower (recovery time ≈ τ) |
| Turn-on voltage (Si) | 0.2–0.4 V | 0.6–0.7 V |
| Reverse leakage | Higher | Lower |
| Breakdown voltage | Lower | Higher |
| Uses | Fast rectifiers in power supplies, microwave mixers and detectors, clamps, MESFET gates | General rectification, high voltage, low leakage |

Current–voltage curves. An ohmic contact gives a straight line through the origin (current both ways). A Schottky diode turns on at about 0.3 V, a silicon p-n diode at about 0.65 V; both pass very little current in reverse.

## Band diagrams under bias

Take the metal on n-type Si. The key rule: the barrier seen from the metal, qΦB, never changes, because it is fixed by the interface. The applied voltage appears across the depletion region and changes only the barrier seen from the semiconductor. Under bias the two sides are no longer in equilibrium, so there is no single flat Fermi level: the semiconductor's Fermi level moves by qV relative to the metal's.

|  | Equilibrium (V = 0) | Forward bias (metal +, V > 0) | Reverse bias (metal −, V < 0) |
| --- | --- | --- | --- |
| Fermi levels | One flat EF | Semiconductor EF raised by qV relative to the metal | Semiconductor EF lowered by q¦V¦ |
| Band bending | qVbi | q(Vbi − V), smaller | q(Vbi + ¦V¦), larger |
| Depletion width | W0 = √(2εsVbi/qND) | Narrower | Wider |
| Electrons semiconductor → metal | Balanced by metal → semiconductor | Increase by eqV/kT | Suppressed |
| Electrons metal → semiconductor | Small, over ΦB | Unchanged (ΦB fixed) | Unchanged: this is the saturation current |
| Net current | 0 | Js(eqV/ηkT − 1), large | ≈ −Js, small |

The same Schottky contact in equilibrium, forward bias and reverse bias. The barrier from the metal (qΦB) stays fixed. Forward bias shrinks the semiconductor-side barrier to q(Vbi − V); reverse bias raises it to q(Vbi + |V|).

In plain words. The metal side of the hill never changes height. Forward bias lowers the semiconductor side of the hill, so a flood of electrons pours over it into the metal. Reverse bias raises the semiconductor side, stopping that flow, and only the small trickle from the metal side remains.

At large reverse voltage the field becomes strong enough to cause breakdown. Real diodes also show some extra leakage from image-force lowering (the barrier is pulled down slightly by the high field) and a voltage drop across their series resistance.

## Ohmic contacts

An ohmic contact has a straight-line, symmetric I-V characteristic and a resistance negligible compared with the device. Current passes freely in both directions.

V = I Rc, Rc = ρc / A

Where:

- V = voltage across the contact (V); I = current through it (A)

- Rc = contact resistance (Ω)

- ρc = specific contact resistance (Ω·cm2)

- A = contact area (cm2)

An ohmic contact is not necessarily a contact with no barrier. It may have a barrier that is so low, or so thin, that it does not restrict the current. There are three ways to make one.

Two ways to an ohmic contact on n-type silicon. (a) A metal with Φm < Φs: electrons flow into the semiconductor, the bands bend down into an accumulation layer, and there is no barrier. (b) Heavy doping: a barrier is still there, but it is only a few nanometres thick, so electrons tunnel straight through it.

1. Choose a low-barrier metal. For n-type, use a metal with Φm < Φs (for p-type, Φm > Φs). Now electrons flow from the metal into the semiconductor on contact, piling up an accumulation layer instead of a depletion layer. The bands bend downward, and there is no barrier for electrons in either direction. In practice Fermi-level pinning makes suitable metals rare for Si and GaAs, so the second method is used.

2. Dope heavily so that electrons tunnel (the practical method). Dope the semiconductor very heavily just under the contact (n+ or p+, above about 1019 cm−3). A barrier still exists, but because W ∝ 1/√ND the depletion width shrinks to a few nanometres. A barrier that thin is no obstacle: electrons tunnel straight through it in both directions.

3. Engineer the interface. Clean the surface, then deposit and anneal (heat) the metal so that it reacts with the semiconductor and forms a stable compound with a low barrier: a silicide (TiSi2, CoSi2, NiSi) on silicon, or an alloyed Au–Ge–Ni contact on n-GaAs.

In plain words. A wall that is high but paper-thin is no barrier to a quantum particle: it goes straight through. Heavy doping makes the barrier paper-thin.

|  | Thermionic emission | Tunnelling (field emission) |
| --- | --- | --- |
| How the electron crosses | Over the top of the barrier | Through the barrier |
| Needs | Enough thermal energy | A thin barrier (a few nm) |
| Doping under the contact | Light to moderate (≤ 1017 cm−3) | Heavy (≥ 1019 cm−3) |
| Temperature dependence | Strong (∝ T2e−qΦB/kT) | Weak |
| Gives | Schottky (rectifying) contact | Ohmic contact |

#### Example 11.6: why heavy doping makes a contact ohmic

Question. The voltage across the depletion region under a contact on n-type silicon is 0.60 V. Calculate the depletion width for ND = 1×1016 cm−3 and for ND = 1×1019 cm−3, and say which contact will be ohmic.

Given: Vbi − V = 0.60 V, εs = 1.04×10−12 F/cm, q = 1.6×10−19 C, ND = 1016 and 1019 cm−3.

Find: W for each doping.

Formula: W = √( 2εs(Vbi − V)/qND ).

Solution.

Step 1. Light doping:

W = √( 2 × 1.04×10−12 × 0.60 / (1.6×10−19 × 1016) ) = 2.79×10−5 cm = 279 nm

Step 2. Heavy doping: ND is 1000 times larger, so W is √1000 = 31.6 times smaller:

W = 279 nm / 31.6 = 8.8 nm

Answer: W = 279 nm at 1016 cm−3 and 8.8 nm at 1019 cm−3.

What this means: electrons cannot tunnel through 279 nm, so the lightly doped contact rectifies. A barrier under about 10 nm thick lets a large tunnelling current through, so the heavily doped contact behaves as ohmic, even though the barrier height has not changed.

## Schottky contact versus ohmic contact, and where each is used

| Feature | Schottky contact | Ohmic contact |
| --- | --- | --- |
| Electrical behaviour | Rectifying | Non-rectifying |
| I-V curve | Exponential, asymmetric | Straight line through the origin |
| Barrier | Significant: limits the current | Low, or thin enough to tunnel through |
| Main transport mechanism | Thermionic emission | Tunnelling, or flow over a small barrier |
| Doping under the contact | Moderate | Heavy (n+ or p+) |
| Used for | Fast rectifiers, clamps, RF detectors and mixers, MESFET gates | Transistor terminals, solar-cell contacts, every IC connection |
| Advantages | Fast switching (majority carriers, no stored charge); low forward voltage | Low resistance; current collected efficiently in both directions |
| Limitations | Higher reverse leakage; lower breakdown voltage | Needs heavy doping and careful processing; resistance rises if fabrication is poor |

Both are needed together: a Schottky diode has a rectifying contact on one side and an ohmic contact on the other. In a solar cell, every contact must be ohmic: an accidental barrier adds series resistance, lowers the fill factor and reduces the output power.

Fermi-level pinning (what really happens). Measured barriers depend much less on the metal than ΦB = Φm − χ predicts, because surface states at the interface hold ("pin") the Fermi level near a fixed energy. For example, gold on n-Si gives ΦB ≈ 0.8 eV, not 1.05 eV; on n-GaAs almost every metal gives about 0.8 eV. In calculations, use the measured ΦB if it is given.

## Stability of contacts

Contacts must keep working through hot processing steps and years of operation:

- Aluminium spiking: silicon dissolves into aluminium and aluminium spikes into the silicon, which can short out a shallow junction. Prevented by adding 1 % Si to the Al, or by a barrier layer (TiN, TiW).

- Electromigration: at high current density the flowing electrons gradually push metal atoms along, forming voids and breaks. Reduced by Al–Cu alloys or copper wiring.

- Interdiffusion and chemical reaction at high temperature change the barrier height; silicides are used because they form a clean, stable interface.

- Contamination and native oxide at the interface raise ρc and change ΦB.

## Key points of Week 11

- Φs = χ + (Ec − EF). Metal on n-type with Φm > Φs → Schottky barrier; Φm < Φs (or heavy doping) → ohmic.

- Schottky: electrons leave the semiconductor, a depletion region forms, bands bend up, Fermi levels align. ΦB = Φm − χ (ideally), Vbi = Φm − Φs, W = √(2εsVbi/qND).

- Current by thermionic emission of majority carriers: J = A∗∗T2e−qΦB/kT(eqV/ηkT − 1). Fast, low turn-on voltage, higher leakage.

- Under bias, qΦB is fixed; only the semiconductor-side barrier changes.

- Ohmic contacts: accumulation (low barrier), tunnelling through a thin barrier made by heavy doping (W ∝ 1/√ND), or a silicide. An ohmic contact may still have a barrier; what matters is that it does not limit the current.

## Examination question solved (Q49)

### Q49. Differentiate between a Schottky barrier diode and an Ohmic contact. Explain their energy-band characteristics.

Both are metal–semiconductor junctions. The difference is whether a significant potential barrier to majority-carrier flow exists at the interface.

Schottky barrier diode (rectifying contact).

Condition: n-type semiconductor with Φm > Φs (or p-type with Φm < Φs), moderate doping (≤ 1017 cm−3).

Energy-band characteristics:

- Before contact, EF in the n-semiconductor lies above EF in the metal by Φm − Φs.

- On contact, electrons flow from semiconductor to metal until the Fermi levels align. A depletion region of ionised donors forms in the semiconductor and the bands bend upward at the interface.

- A barrier of height qΦB = q(Φm − χ) opposes electron flow from metal to semiconductor; a built-in barrier qVbi = q(Φm − Φs) opposes flow from semiconductor to metal. (In practice ΦB is fixed by Fermi-level pinning, e.g. ≈ 0.8 eV for Au on n-Si.)

- Forward bias (metal positive) lowers the semiconductor-side barrier to Vbi − V, and electrons are thermionically emitted into the metal: current rises exponentially. Reverse bias raises it to Vbi + |V| while ΦB stays the same, so only a small saturation current flows.

I-V: rectifying, J = A∗∗T2e−qΦB/kT[eqV/ηkT − 1].

Features: majority-carrier device, negligible minority storage, very fast switching, low forward drop (0.2–0.4 V on Si), higher leakage than a p-n diode.

Ohmic contact.

Condition: either n-type with Φm < Φs (p-type with Φm > Φs), or, in practice, any metal on a very heavily doped (n+ or p+, > 1019 cm−3) surface layer.

Energy-band characteristics:

- Low-barrier case: electrons flow from the metal into the semiconductor on contact, forming an accumulation layer; the bands bend downward. There is no barrier for electrons in either direction.

- Tunnelling case: a barrier exists, but heavy doping makes the depletion region only a few nanometres thick (W ∝ 1/√ND). Electrons tunnel through it freely in both directions (field emission).

I-V: linear and symmetric, V = IRc, with very low specific contact resistance (ρc ≈ 10−6–10−8 Ω·cm2).

| Feature | Schottky barrier | Ohmic contact |
| --- | --- | --- |
| Work-function condition (n-type) | Φm > Φs | Φm < Φs (or heavy doping) |
| Semiconductor doping | Moderate (1015–1017 cm−3) | Heavy (> 1019 cm−3) |
| Band bending at interface (n-type) | Upward, depletion layer | Downward (accumulation) or very thin barrier |
| Barrier to majority carriers | Yes, qΦB and qVbi | None, or transparent to tunnelling |
| Conduction mechanism | Thermionic emission | Free flow or field-emission tunnelling |
| I-V characteristic | Rectifying, exponential | Linear, symmetric |
| Resistance | Depends on bias and polarity | Small, constant |
| Purpose | Fast rectifier, detector, MESFET gate | Connecting devices to the circuit |
| Examples | Au, Pt, W, PtSi on n-Si; Ti/Au on n-GaAs | Al or silicide on n+/p+ Si; Au–Ge–Ni on n+-GaAs |

## Practice questions

These extra questions practise this week's ideas. Work each one on paper before reading the solution; the calculation questions follow the same Question, Given, Find, Solution, Answer layout as the worked examples.

#### Practice 11.1: tungsten on n-type silicon

Question. Tungsten (Φm = 4.55 eV) is deposited on n-type silicon with ND = 1×1015 cm−3 (χ = 4.05 eV). Using the ideal model, find ΦB, Φs and Vbi.

Given: Φm = 4.55 eV, χ = 4.05 eV, ND = 1015 cm−3, Nc = 2.8×1019 cm−3.

Find: ΦB, Φs, Vbi.

Solution.

ΦB = Φm − χ = 4.55 − 4.05 = 0.50 eV
Ec − EF = 0.02585 ln(2.8×1019/1015) = 0.265 eV
Φs = 4.05 + 0.265 = 4.315 eV
Vbi = Φm − Φs = 4.55 − 4.315 = 0.235 V

Answer: ΦB = 0.50 eV, Φs = 4.32 eV, Vbi = 0.24 V.

#### Practice 11.2: choosing a metal for an Ohmic contact

Question. n-type silicon with ND = 1×1016 cm−3 has Φs = 4.26 eV. Using the ideal theory, which of Al (4.28), Ti (4.33), Au (5.1) would give an Ohmic contact? What is done in practice?

Given: Φs = 4.26 eV; an Ohmic contact on n-type needs Φm < Φs.

Find: a suitable metal.

Solution. All three have Φm > Φs (Al only just, by 0.02 eV), so none meets the ideal Ohmic condition; Au, with the largest Φm, would give the strongest barrier.

Answer: None, strictly. In practice the silicon under the contact is doped n+ (above 1019 cm−3) so the barrier becomes thin enough to tunnel through, and Al or a silicide is used.

#### Practice 11.3: Schottky forward voltage

Question. A Schottky diode on n-Si has ΦB = 0.65 eV. Find Js at 300 K (A∗∗ = 110 A/cm2K2) and the forward voltage at 10 A/cm2.

Given: ΦB = 0.65 eV, A∗∗ = 110 A/cm2K2, T = 300 K, J = 10 A/cm2.

Find: Js and V.

Solution.

Js = 110 × 3002 × e−0.65/0.0259 = 9.9×106 × 1.26×10−11 = 1.25×10−4 A/cm2
V = 0.0259 ln(10/1.25×10−4) = 0.0259 × 11.29 = 0.29 V

Answer: Js = 1.25×10−4 A/cm2, V ≈ 0.29 V.

#### Practice 11.4: why heavy doping gives tunnelling

Question. Find the zero-bias depletion width under a contact with Vbi = 0.6 V for ND = 1×1016 cm−3 and for ND = 1×1020 cm−3. Explain the result.

Given: Vbi = 0.6 V, εs = 1.04×10−12 F/cm.

Find: W for each doping.

Solution.

W(1016) = √(2 × 1.04×10−12 × 0.6 / (1.6×10−19 × 1016)) = 2.8×10−5 cm = 0.28 μm
W(1020) = W(1016)/√104 = 2.8×10−7 cm = 2.8 nm

Answer: 0.28 μm and 2.8 nm. A 2.8 nm barrier is thin enough for electrons to tunnel through, so the heavily doped contact is Ohmic even though the barrier is still there.

#### Practice 11.5: contact resistance of a small contact

Question. A contact has specific contact resistance ρc = 1×10−6 Ω·cm2 and measures 1 μm × 1 μm. Find its resistance.

Given: ρc = 10−6 Ω·cm2, A = (10−4 cm)2 = 10−8 cm2.

Find: Rc.

Solution.

Rc = ρc/A = 10−6/10−8 = 100 Ω

Answer: Rc = 100 Ω, large for a small transistor, which is why modern processes need ρc near 10−8 Ω·cm2.

#### Practice 11.6: an Ohmic contact by accumulation

Question. Describe the band diagram of an ideal Ohmic contact formed by a low work-function metal (Φm < Φs) on n-type silicon.

Answer. Before contact the metal's Fermi level is higher than the semiconductor's. On contact, electrons flow from the metal into the semiconductor until the Fermi levels align. The extra electrons form an accumulation layer at the interface, and the semiconductor bands bend downward towards it. There is no depletion region and no barrier to electrons in either direction, so current flows freely both ways and the I-V characteristic is linear.

## Objectives check

Use this table to confirm you have met this week's objectives. Cover the Answer column and answer each check question from memory. If you cannot, go back to the section in the last column before moving on.

| # | Objective | Check yourself | Answer | Where it is taught |
| --- | --- | --- | --- | --- |
| 1 | Define work function and electron affinity and relate them. | Write Φs in terms of χ. | Φs = χ + (Ec − EF). | Key terms; The energies before contact; Example 11.1 |
| 2 | Explain how a Schottky barrier forms and calculate ΦB and Vbi. | Al (4.28 eV) on n-Si (χ = 4.05 eV): find the ideal barrier height. | ΦB = 4.28 − 4.05 = 0.23 eV. | The Schottky barrier; Examples 11.2–11.3 |
| 3 | Explain thermionic emission and calculate Schottky diode currents. | Why does a Schottky diode switch faster than a p-n diode? | It is a majority-carrier device with no stored minority charge. | How current flows: thermionic emission; Examples 11.4–11.5 |
| 4 | Draw Schottky band diagrams in equilibrium and under bias. | Which barrier stays constant under bias? | qΦB, the barrier seen from the metal. | Band diagrams under bias |
| 5 | Explain the two ways of making Ohmic contacts. | Why does heavy doping make a contact Ohmic? | The depletion layer becomes so thin that electrons tunnel through it. | Ohmic contacts; Example 11.6 |
| 6 | Describe the stability problems of metal contacts. | What is electromigration? | Gradual movement of metal atoms by the flowing electrons, forming voids and opens. | Stability of contacts |
| 7 | Compare Schottky and ohmic contacts, their advantages, limitations and applications. | Give one advantage and one limitation of a Schottky diode, and one use of an ohmic contact. | Advantage: fast switching (or low forward voltage). Limitation: higher reverse leakage (or lower breakdown voltage). Ohmic use: transistor terminals or solar-cell contacts. | Schottky contact versus ohmic contact |

Week 12 · Module 4 · Junctions, Interfaces & Characterisation

# Interface Characterisation and CAT 2

Plan: methods of characterisation (capacitance–voltage C-V profiling, current–voltage I-V analysis); Continuous Assessment Test 2.

## Learning objectives

By the end of this week you should be able to:

- Describe I-V measurement and extract Is, η and Rs.

- Explain how the Schottky barrier height is obtained from I-V data.

- Explain the principle of C-V measurement.

- Extract doping and built-in potential from a Mott–Schottky plot.

- Explain doping profiling and the MOS C-V measurement.

## Symbols and abbreviations used this week

Every symbol, constant and abbreviation on this page is listed here, even if an earlier week already defined it, so you can study this page on its own.

Constants and units

| Symbol | Meaning | Units / typical value |
| --- | --- | --- |
| q | Magnitude of the electronic charge | 1.6×10−19 C |
| k | Boltzmann constant | 8.617×10−5 eV/K = 1.381×10−23 J/K |
| kT | Thermal energy | 0.0259 eV (often 0.02585 eV) at 300 K |
| kT/q | Thermal voltage | 0.0259 V (about 26 mV) at 300 K |
| T | Absolute temperature | kelvin (K); room temperature = 300 K |
| εs (εsi) | Permittivity of silicon, 11.7ε0 | 1.04×10−12 F/cm |
| εox | Permittivity of SiO2, 3.9ε0 | 3.45×10−13 F/cm |
| eV | Electron-volt, a unit of energy | 1 eV = 1.6×10−19 J |
| μm | Micrometre (micron) | 1 μm = 10−4 cm = 10−6 m |

Symbols

| Symbol | Meaning | Units / typical value |
| --- | --- | --- |
| p | Hole concentration (holes per cm3) | cm−3 |
| ni | Intrinsic carrier concentration (n = p = ni in pure material) | cm−3; Si ≈ 1×1010 at 300 K |
| ND | Donor concentration | cm−3 |
| NA | Acceptor concentration | cm−3 |
| Δn, Δp | Excess electron and hole concentrations above equilibrium | cm−3 |
| C(x, t) | Dopant concentration at depth x and time t | cm−3 |
| Rs | Sheet resistance (or diode series resistance in Week 12) | Ω/□ (ohms per square); Ω |
| E (field) | Electric field (on band diagrams, E is energy instead) | V/cm |
| μ, μn, μp | Mobility: drift velocity per unit field (electrons, holes) | cm2/(V·s); Si μn 1350, μp 480 |
| σ | Conductivity, q(nμn + pμp) (in Week 8, σ is also a capture cross-section) | S/cm (siemens per cm) |
| ρ | Resistivity, 1/σ | Ω·cm |
| J, Jn, Jp | Current density (total, electrons, holes) | A/cm2 |
| Dn, Dp | Diffusion coefficients of electrons and holes | cm2/s; Si 35 and 12.4 |
| R | Recombination rate | cm−3s−1 |
| τ, τn, τp | Minority-carrier lifetime (τeff: effective, including surfaces) | s; Si 1 ns – 1 ms |
| L, Ln, Lp | Diffusion length √(Dτ): distance a minority carrier travels before recombining | μm or cm |
| Vbi | Built-in potential of a junction or Schottky contact | V; typically 0.5–1 V |
| V, Va | Applied voltage (positive for forward bias) | V |
| W | Depletion-region width (in Week 13 WB, WE are base and emitter widths; in Week 14 W is channel width) | μm or cm |
| Emax | Peak electric field, at the junction | V/cm |
| Is, Js (IS) | Saturation current (density) of a diode or transistor | A; A/cm2 |
| I | Current | A |
| A (area) | Device or contact area | cm2 |
| η | Ideality factor of a diode, 1 (ideal) to 2 | dimensionless |
| C, Cj | Capacitance (junction or depletion capacitance) | F (pF = 10−12 F) |
| ΦB | Schottky barrier height seen from the metal | eV (or V) |
| A∗∗ | Effective Richardson constant | A/(cm2·K2); n-Si ≈ 110 |
| Cox | Gate-oxide capacitance per unit area, εox/tox | F/cm2 |
| tox | Gate-oxide thickness | nm |
| VT (Vth) | Threshold voltage of a MOSFET | V |
| VFB | Flat-band voltage | V |
| VGS, VDS, VSB, VG | Gate–source, drain–source, source–body and gate voltages | V |
| ID | Drain current | A (mA) |
| Vjunction | Part of the applied voltage that appears across the junction itself | V |
| N(x), N(W) | Doping concentration at depth x (or at the depletion edge W), from C-V profiling | cm−3 |
| ΔV, ΔVBE | A small change in a voltage | V |

Abbreviations

| Abbreviation | Meaning |
| --- | --- |
| Si | Silicon |
| I-V | Current–voltage (measurement or characteristic) |
| C-V | Capacitance–voltage (measurement or characteristic) |
| LCR | Inductance–capacitance–resistance meter |
| MOS | Metal–oxide–semiconductor |
| MOSFET | Metal–oxide–semiconductor field-effect transistor |
| BJT | Bipolar junction transistor |
| CAT | Continuous Assessment Test |
| DC | Direct current (steady) |
| AC | Alternating current (small signal) |
| n+ | Very heavily doped n-type (similarly p+) |

## Key terms

Every important word used this week is defined here, so you can read this week on its own.

Doping (ND, NA). Adding a small, controlled amount of impurity atoms to a semiconductor to set its electrical properties. Donors (concentration ND) give electrons and make the material n-type; acceptors (concentration NA) take electrons, create holes and make it p-type. Doping is measured in atoms per cm3.

Majority and minority carriers. In n-type material electrons are the more numerous (majority) carriers and holes the less numerous (minority) carriers; in p-type material it is the other way round.

Depletion region (W). The thin layer on each side of a p-n junction, or under a metal–semiconductor contact, from which the mobile carriers have been swept away, leaving only the fixed charge of the ionised dopant atoms. Its width W grows when a reverse bias is applied.

Built-in potential (Vbi). The voltage that appears across the depletion region of a junction or Schottky contact with no applied bias. It is the barrier that stops majority carriers flowing across in equilibrium, typically 0.5–1 V in silicon.

One-sided junction. A p-n junction with one side much more heavily doped than the other (p+n or n+p). Almost all of the depletion region then lies in the lightly doped side, so measurements on it describe that side alone. A Schottky diode behaves the same way.

Schottky diode and barrier height (ΦB). A Schottky diode is a rectifying metal–semiconductor contact. Its barrier height ΦB is the energy step an electron in the metal must climb to enter the semiconductor; it fixes how much current the diode can leak.

Why it matters: ΦB cannot be seen directly, but it sets the saturation current, so it can be found from an I-V measurement.

Saturation current (Is, Js). The small current that a diode carries under reverse bias, and the scale factor in front of the exponential in the diode equation. Js = Is/A is the same quantity per unit area.

Ideality factor (η). A number between 1 and 2 that says how closely a real diode follows the ideal diode equation. η = 1 means the current is pure diffusion (or, in a Schottky diode, pure thermionic emission); η near 2 means recombination in the depletion region dominates.

I = Is ( eqV/ηkT − 1 )

Where:

- I = diode current (A)

- Is = saturation current (A)

- V = applied voltage, positive for forward bias (V)

- η = ideality factor (dimensionless)

- kT/q = thermal voltage, 0.0259 V at 300 K

Why it matters: η tells you which current mechanism is at work, and so how good the junction is.

Series resistance (Rs). The resistance of the bulk semiconductor, contacts and leads in series with the junction itself. It wastes part of the applied voltage, so at high current the diode needs more voltage than the ideal equation predicts.

I-V characterisation. Measuring the current through a device as the applied voltage is stepped, and comparing the curve with theory to extract Is, η, Rs, leakage, breakdown and, for a Schottky diode, ΦB.

Semi-log plot. A graph of the natural logarithm of a quantity (here ln I) against a linear quantity (here V). An exponential law becomes a straight line on it, so slope and intercept can be read off.

Effective Richardson constant (A∗∗). The material constant in the thermionic-emission law that links a Schottky diode's saturation current density to its barrier height and temperature; about 110 A/(cm2·K2) for n-type Si.

Arrhenius plot. A graph of the logarithm of a temperature-dependent quantity against 1/T. A process with an energy barrier gives a straight line whose slope gives the barrier energy.

Depletion (junction) capacitance (C, Cj). The capacitance of a reverse-biased junction, which behaves like a parallel-plate capacitor with the depletion region as the gap between the plates. It falls as the reverse bias widens the depletion region.

C-V characterisation. Measuring the small-signal capacitance of a reverse-biased junction, Schottky diode or MOS capacitor as the DC bias is stepped, to find the doping, its profile with depth and the built-in potential.

Mott–Schottky plot. A graph of 1/C2 against V for a one-sided junction or Schottky diode. Uniform doping gives a straight line: its slope gives the doping and its voltage-axis intercept gives Vbi.

Why it matters: it is the standard way of measuring doping electrically, without damaging the sample.

Doping profile (N(x)). The way the doping concentration changes with depth x below the surface, for example after diffusion or ion implantation.

MOS capacitor. A metal (or polysilicon) plate on a thin oxide on a semiconductor: the gate structure of a MOSFET. Its C-V curve reveals the oxide thickness, the flat-band and threshold voltages and the quality of the oxide.

## The big picture

After a device is made, how do you know what is inside it? You cannot see the doping or the barrier height. But you can measure electrically and compare the results with the theory of Weeks 10–11. Two measurements do most of the work:

- I-V (current against voltage) tells you how current flows: the saturation current, how ideal the junction is, the series resistance, leakage and breakdown, and for a Schottky diode the barrier height.

- C-V (capacitance against voltage) tells you how charge is arranged: the doping concentration (and how it changes with depth) and the built-in potential.

The trick in both cases is to plot the data so that the theory predicts a straight line, then read the answers from the slope and the intercept.

| Feature | I-V measurement | C-V measurement |
| --- | --- | --- |
| What is applied | DC voltage, swept from reverse to forward bias | DC reverse bias, plus a small AC signal (10–50 mV, about 1 MHz) |
| What is measured | DC current | Small-signal capacitance |
| Instrument | Source-measure unit (or supply, resistor and meters) | LCR (capacitance) meter |
| Physics probed | How carriers flow across the junction | How fixed charge is arranged in the depletion region |
| Straight-line plot | ln I against V (semi-log) | 1/C2 against V (Mott–Schottky) |
| Slope gives | Ideality factor η | Doping N |
| Intercept gives | Saturation current Is (and ΦB for a Schottky diode) | Built-in potential Vbi |
| Also gives | Rs, leakage, breakdown, Ohmic or rectifying contact | Doping profile N(x); for MOS: tox, VFB, VT, oxide charge |
| Main sources of error | Series resistance, heating, leakage paths at the edges | Stray capacitance, series resistance, uncertain area (N ∝ 1/A2), traps |
| Barrier height ΦB | From Is via thermionic emission: sensitive to barrier lowering and patches of low barrier | From Vbi: measures the average barrier, usually slightly higher than the I-V value |

## I-V characterisation

### The measurement

A source-measure unit (or a power supply with a series resistor and two meters) applies a voltage to the device in steps, from reverse to forward bias, and records the current at each step. Currents from picoamps to amps may need measuring, often on a probe station, sometimes at several temperatures.

### Turning the curve into a straight line

For a real diode,

I = Is ( eqV/ηkT − 1 )

Where:

- I = diode current (A)

- Is = saturation current (A)

- V = applied voltage, positive for forward bias (V)

- η = ideality factor (dimensionless, 1 to 2)

- q = electronic charge, 1.6×10−19 C; kT = thermal energy, so kT/q = 0.0259 V at 300 K

η (the ideality factor) is 1 for a perfect diffusion-current diode and up to 2 when recombination in the depletion region dominates. Above about 0.1 V the −1 is negligible, so take the natural log:

ln I = ln Is + (q/ηkT) V

That is a straight line if you plot ln I against V (a semi-log plot):

- the intercept at V = 0 gives ln Is, so the saturation current Is;

- the slope is q/(ηkT), so η = (q/kT) / slope.

#### Example 12.1: ideality factor and saturation current from I-V data

Question. A silicon diode carries 0.9 μA at a forward voltage of 0.30 V and 40 μA at 0.40 V. Assuming both points lie on the straight part of the semi-log plot, find the ideality factor and the saturation current (300 K).

Given: I1 = 0.9 μA at V1 = 0.30 V; I2 = 40 μA at V2 = 0.40 V; kT/q = 0.0259 V.

Find: η and Is.

Formula:

slope = ln(I2/I1)/(V2 − V1), η = (q/kT)/slope, Is = I1 e−slope × V1

Solution.

Step 1. Slope of ln I against V:

slope = ln(I2/I1)/(V2 − V1) = ln(40/0.9)/0.10 = 3.79/0.10 = 37.9 V−1

Step 2. Ideality factor, slope = q/(ηkT):

η = 1/(0.0259 × 37.9) = 1.02

Step 3. Extrapolate back to V = 0:

Is = I1 / eslope × V1 = 0.9×10−6 / e37.9 × 0.30 = 0.9×10−6 / 8.7×104 = 1.0×10−11 A

Answer: η = 1.02 (almost ideal diffusion current), Is ≈ 1×10−11 A.

What this means: the current rises by a factor of about 44 for only 0.1 V, almost exactly the 60 mV per decade of an ideal diode, so nearly all the current is diffusion current and depletion-region recombination is negligible. The tiny Is (10 pA) is what makes the diode switch on only above about 0.5 V.

### What else the I-V curve shows

- Series resistance Rs: at high current the curve bends away from the straight line, because part of the voltage is dropped across the resistance of the bulk and contacts: V = Vjunction + IRs. Rs = (extra voltage)/I.

- Reverse leakage and breakdown voltage from the reverse branch.

- Schottky barrier height from Is (see below). Measuring at several temperatures and plotting ln(Is/T2) against 1/T (an Arrhenius plot) gives a straight line of slope −qΦB/k.

- Ohmic contacts: the I-V between two contacts should be a straight line through the origin, the same in both directions.

Transistors are characterised the same way: MOSFET ID–VGS curves give the threshold voltage and mobility (Week 14, Practical 4), and BJT curves give the current gain.

### Barrier height from the saturation current

In a Schottky diode the current is carried by electrons that have enough thermal energy to jump over the barrier (thermionic emission). The saturation current density is

Js = Is/A = A∗∗ T2 e−qΦB/kT

Where:

- Js = saturation current density (A/cm2)

- Is = saturation current, from the intercept of the semi-log plot (A)

- A = diode (contact) area (cm2)

- A∗∗ = effective Richardson constant, 110 A/(cm2·K2) for n-Si

- T = absolute temperature (K)

- ΦB = Schottky barrier height (eV, or V when multiplied by q)

- kT/q = thermal voltage, 0.0259 V at 300 K

Taking logarithms and solving for the barrier:

ΦB = (kT/q) ln( A∗∗ T2 / Js ) = (kT/q) ln( A∗∗ A T2 / Is )

Because ΦB depends only on the logarithm of Is, even a factor-of-two error in the area or in A∗∗ changes ΦB by only 0.0259 × ln 2 ≈ 18 meV. That is why this is the standard I-V method for barrier height.

#### Example 12.2: barrier height from the saturation current

Question. A Schottky diode on n-type silicon has an area of 2×10−4 cm2. Its semi-log forward I-V plot is straight with η = 1.03, and extrapolates to Is = 1.2×10−10 A at V = 0 (300 K). Find the saturation current density, the barrier height, and the forward voltage needed for 1 mA (take η ≈ 1 for this last part).

Given: A = 2×10−4 cm2, Is = 1.2×10−10 A, T = 300 K, A∗∗ = 110 A/(cm2·K2), kT/q = 0.0259 V.

Find: Js, ΦB and V at I = 1 mA.

Formula:

Js = Is/A, ΦB = (kT/q) ln( A∗∗T2/Js ), V = (kT/q) ln( I/Is + 1 )

Solution.

Step 1. Saturation current density:

Js = 1.2×10−10 / 2×10−4 = 6.0×10−7 A/cm2

Step 2. A∗∗T2 = 110 × (300)2 = 9.9×106 A/cm2, so

ΦB = 0.0259 × ln( 9.9×106 / 6.0×10−7 ) = 0.0259 × ln(1.65×1013) = 0.0259 × 30.43 = 0.79 eV

Step 3. Forward voltage for 1 mA:

V = 0.0259 × ln( 10−3/1.2×10−10 + 1 ) = 0.0259 × 15.94 = 0.41 V

Answer: Js = 6.0×10−7 A/cm2, ΦB ≈ 0.79 eV, V ≈ 0.41 V at 1 mA.

What this means: an η so close to 1 shows that thermionic emission over the barrier is the main current mechanism, so the formula applies. A 0.79 eV barrier is typical of a good rectifying contact on n-Si, and the diode turns on at about 0.4 V, well below the 0.6–0.7 V of a silicon p-n diode.

## C-V characterisation

### The measurement

An LCR meter applies a small AC voltage (10–50 mV, typically at 1 MHz) on top of a DC bias, and measures the capacitance. The DC bias is stepped through a range of reverse voltages.

### The theory: a capacitor whose plates move

A reverse-biased one-sided junction (p+n) or Schottky diode has a depletion region with no mobile carriers, between two conducting regions. It is a parallel-plate capacitor whose plate separation is the depletion width W:

C = εs A / W

Where:

- C = depletion (junction) capacitance (F)

- εs = permittivity of silicon, 1.04×10−12 F/cm

- A = junction area (cm2)

- W = depletion-region width (cm)

From Week 10, W = √(2εs(Vbi − V)/qN), where N is the doping on the lightly doped side. As the reverse voltage increases, W gets bigger and C gets smaller. Substituting:

C = A √( qεsN / 2(Vbi − V) )

Where:

- q = electronic charge, 1.6×10−19 C

- N = doping on the lightly doped side (cm−3)

- Vbi = built-in potential (V)

- V = applied voltage, negative for reverse bias (V)

- C, A, εs as above

### Turning it into a straight line: the Mott–Schottky plot

Square both sides and turn upside down:

1/C2 = 2(Vbi − V) / (qεsNA2)

Where:

- 1/C2 = inverse square of the measured capacitance (F−2)

- Vbi = built-in potential (V); V = applied voltage (V)

- q = 1.6×10−19 C; εs = 1.04×10−12 F/cm

- N = doping on the lightly doped side (cm−3); A = area (cm2)

So if you plot 1/C2 against V, uniform doping gives a straight line:

- Slope = −2/(qεsNA2), which gives the doping N (equation below).

- Intercept on the voltage axis (where 1/C2 = 0) is at V = Vbi: the built-in potential.

Rearranging the slope for the doping:

N = 2 / ( qεs A2 × |slope| )

Where:

- N = doping concentration on the lightly doped side (cm−3)

- |slope| = magnitude of the slope of the 1/C2 against V line (F−2V−1)

- q = 1.6×10−19 C; εs = 1.04×10−12 F/cm; A = area (cm2)

Mott–Schottky plot. For uniform doping the points fall on a straight line; the slope gives the doping and the voltage-axis intercept gives Vbi.

In plain words. Reverse bias pushes the edge of the depletion region deeper into the semiconductor. How much extra charge is uncovered as the edge moves tells you how many dopant atoms are there. The capacitance measures exactly that.

#### Example 12.3: doping and built-in potential from a C-V plot

Question. A silicon Schottky diode of area 1×10−3 cm2 gives a straight 1/C2 against V plot with slope −1.2×1021 F−2V−1 that meets the voltage axis at +0.60 V. Find the doping concentration and the built-in potential. Also find the capacitance and depletion width at a reverse bias of 5 V.

Given: A = 1×10−3 cm2, slope = −1.2×1021 F−2V−1, intercept 0.60 V, εs = 1.036×10−12 F/cm, q = 1.602×10−19 C, V = −5 V.

Find: ND, Vbi, and C and W at −5 V.

Formula:

ND = 2/(qεsA2|slope|), C = A√( qεsND / 2(Vbi − V) ), W = εsA/C

Solution.

Step 1. Doping from the slope:

ND = 2/(qεsA2|slope|) = 2 / (1.602×10−19 × 1.036×10−12 × (10−3)2 × 1.2×1021) = 2/1.99×10−16 = 1.0×1016 cm−3

Step 2. Built-in potential from the intercept: Vbi = 0.60 V

Step 3. At V = −5 V, Vbi − V = 5.6 V:

C = A√(qεsND / 2(Vbi − V)) = 10−3 × √(1.66×10−15 / 11.2) = 1.22×10−11 F

W = εsA/C = 1.036×10−15 / 1.22×10−11 = 8.5×10−5 cm

Answer: ND = 1.0×1016 cm−3, Vbi = 0.60 V; at −5 V, C = 12.2 pF and W = 0.85 μm.

What this means: the semiconductor is moderately doped n-type, about one dopant atom for every 5 million silicon atoms, found without cutting or etching the sample. At −5 V the depletion edge sits 0.85 μm below the contact, so this is the depth at which the doping is being sampled at that bias.

### Doping profiles

If the doping is not uniform, the 1/C2 plot curves. The local slope at each bias still gives the doping at the edge of the depletion region, and the capacitance tells you where that edge is:

N(W) = 2 / ( qεsA2 × |d(1/C2)/dV| ), W = εsA/C

Where:

- N(W) = doping at the edge of the depletion region, at depth W (cm−3)

- |d(1/C2)/dV| = magnitude of the local slope of the 1/C2 curve at that bias (F−2V−1)

- W = depletion width, the depth being probed (cm)

- C = measured capacitance at that bias (F)

- q = 1.6×10−19 C; εs = 1.04×10−12 F/cm; A = area (cm2)

Sweeping the bias moves W deeper and maps out the doping profile N(x). This only works for one-sided junctions (p+n, n+p) or Schottky diodes, where the depletion region is all on one side.

### MOS C-V

For a MOS capacitor (Week 14), the C-V curve shows accumulation (C = Cox), depletion (C falling) and inversion. It gives the oxide thickness (from Cox = εoxA/tox), the flat-band and threshold voltages, the substrate doping, the charge trapped in the oxide, and the density of interface traps. It is the main tool for checking the quality and stability of gate oxides.

### Getting accurate C-V results

- Measure only in reverse bias (forward bias adds a large diffusion capacitance).

- Subtract stray and probe-pad capacitance (an open-circuit correction).

- Correct for series resistance.

- Keep the AC signal small.

- Choose the frequency so that deep traps do not respond (or so that they do, if you want to measure them).

- Know the device area accurately: N depends on 1/A2.

## Key points of Week 12

- I-V: plot ln I against V. Intercept → Is; slope → η = (q/kT)/slope; bending at high current → Rs; Arrhenius plot → ΦB.

- Schottky barrier height from one I-V curve: ΦB = (kT/q) ln(A∗∗T2/Js), with Js = Is/A and A∗∗ = 110 A/(cm2·K2) for n-Si.

- C-V: a reverse-biased junction is a capacitor C = εsA/W, with W growing with reverse bias.

- Mott–Schottky: 1/C2 = 2(Vbi − V)/(qεsNA2). Slope → N = 2/(qεsA2|slope|); intercept → Vbi.

- Non-uniform doping: local slope gives N at depth W = εsA/C.

- MOS C-V gives tox, VFB, VT, substrate doping and oxide quality.

## Examination question solved (Q50)

### Q50. Explain the principles of I-V and C-V characterisation of semiconductor devices and describe how C-V measurements can be used to estimate doping concentration.

I-V characterisation: principle. A known DC voltage is applied across the device (swept in steps from reverse to forward bias) and the resulting current is measured with a source-measure unit, usually on a probe station and sometimes at several temperatures. Comparing the measured curve with device theory gives the transport parameters.

For a diode, I = Is[exp(qV/ηkT) − 1]. From a semi-log plot of ln I versus V:

- the intercept gives the saturation current Is (and, for Schottky diodes, the barrier height ΦB = (kT/q) ln(AA∗∗T2/Is));

- the slope gives the ideality factor η (1 for ideal diffusion current, approaching 2 when depletion-region recombination dominates);

- deviation at high current gives the series resistance;

- the reverse branch gives leakage current and breakdown voltage;

- for contacts, a linear symmetric I-V confirms an Ohmic contact and gives contact resistance.

I-V curves of transistors give threshold voltage, transconductance, output resistance, mobility and current gain, and repeated I-V measurement after stress is used to test stability and reliability.

C-V characterisation: principle. A reverse-biased p-n junction or Schottky barrier has a depletion region free of carriers between two conducting regions; it behaves like a parallel-plate capacitor with dielectric εs and plate separation W:

C = εs A / W

The DC reverse bias is swept, and the small-signal capacitance is measured with a small AC voltage (typically 1 MHz, a few tens of mV) using an LCR meter. Since W increases with reverse bias, C decreases.

Using C-V to estimate doping. For a one-sided abrupt junction (p+n or Schottky on n-type) with uniform doping N:

W = √( 2εs(Vbi − V)/qN ) ⇒ C = A √( qεsN / 2(Vbi − V) )

Rearranging:

1/C2 = 2(Vbi − V) / (qεs N A2)

- Measure C at a series of reverse biases V.

- Plot 1/C2 against V (the Mott–Schottky plot). For uniform doping it is a straight line.

- The slope is −2/(qεsNA2), so the doping concentration is N = 2/(qεsA2·|slope|).

- The intercept on the V axis gives the built-in potential Vbi (and from it the Schottky barrier height).

- For non-uniform doping, use the local slope: N(W) = 2/(qεsA2 d(1/C2)/dV) evaluated at each bias, and the depth W = εsA/C. This gives the doping profile N(x) as a function of depth.

Example. A diode of area 10−3 cm2 on Si (εs = 1.036×10−12 F/cm) gives a 1/C2 slope magnitude of 1.2×1021 F−2V−1:

N = 2 / (1.602×10−19 × 1.036×10−12 × 10−6 × 1.2×1021) = 1.0×1016 cm−3

Advantages and limits. C-V is non-destructive, fast and needs only a simple diode, but only measures the doping on the lightly doped side, only to depths reachable before breakdown, and with resolution limited by the Debye length. Accuracy requires a correct area, correction for stray capacitance and series resistance, and a frequency at which deep traps do not respond.

## CAT 2 practice test (60 minutes)

Covers Weeks 7–12. Practice questions, not the actual CAT. Use q = 1.6×10−19 C, kT/q = 0.0259 V, Si: ni = 1×1010 cm−3, εs = 1.04×10−12 F/cm.

- An n-type Si bar (ND = 1016 cm−3, μn = 1200 cm2/V·s) is 1 cm long with 10−3 cm2 cross-section. Find its resistance and the current at 5 V.

- Find the hole diffusion coefficient in Si if μp = 450 cm2/V·s, and the diffusion length if τp = 2 μs.

- Holes injected into n-Si fall from 1014 cm−3 at x = 0 with Lp = 30 μm. Find the hole diffusion current density at x = 0 (Dp = 11.6 cm2/s).

- A Si p+n junction has ND = 5×1015 cm−3 and NA = 1018 cm−3. Find Vbi, the depletion width at zero bias and at −10 V, and the peak field at −10 V.

- The diode of Q4 has area 10−3 cm2 and Is = 1×10−14 A. Find the current at 0.6 V and the voltage for 1 mA.

- A Schottky diode on n-Si has ΦB = 0.7 eV. Find Js at 300 K (A∗∗ = 110 A/cm2K2) and the forward voltage for J = 10 A/cm2.

- A 1/C2 plot for a one-sided junction of area 2×10−3 cm2 has slope magnitude 4.0×1020 F−2V−1. Find the doping.

## CAT 2 solutions

### 1. Resistance of a bar

Question. An n-type Si bar (ND = 1016 cm−3, μn = 1200 cm2/V·s) is 1 cm long with 10−3 cm2 cross-section. Find its resistance and the current at 5 V.

Given: ND = 1016 cm−3, μn = 1200 cm2/V·s, L = 1 cm, A = 10−3 cm2, V = 5 V.

Find: R and I.

Formula:

σ = qNDμn, ρ = 1/σ, R = ρL/A, I = V/R

Solution.

σ = qNDμn = 1.6×10−19 × 1016 × 1200 = 1.92 S/cm, ρ = 0.521 Ω·cm
R = ρL/A = 0.521 × 1 / 10−3 = 521 Ω
I = V/R = 5/521 = 9.6 mA

Answer: R ≈ 521 Ω, I ≈ 9.6 mA.

What this means: with 1016 donors per cm3 the silicon conducts several hundred thousand times better than pure silicon, but a long thin bar is still a resistor of several hundred ohms; this is how diffused resistors in integrated circuits work.

### 2. Einstein relation and diffusion length

Question. Find the hole diffusion coefficient in Si if μp = 450 cm2/V·s, and the diffusion length if τp = 2 μs.

Given: μp = 450 cm2/V·s, τp = 2×10−6 s, kT/q = 0.0259 V.

Find: Dp and Lp.

Formula:

Dp = (kT/q)μp, Lp = √(Dpτp)

Solution.

Dp = (kT/q)μp = 0.0259 × 450 = 11.7 cm2/s
Lp = √(Dpτp) = √(11.7 × 2×10−6) = 4.83×10−3 cm = 48 μm

Answer: Dp ≈ 11.7 cm2/s, Lp ≈ 48 μm.

What this means: an injected hole typically wanders about 48 μm before it recombines, far more than the width of a transistor base, so almost all holes injected into a thin region survive to cross it.

### 3. Diffusion current at the injection point

Question. Holes injected into n-Si fall from 1014 cm−3 at x = 0 with Lp = 30 μm. Find the hole diffusion current density at x = 0 (Dp = 11.6 cm2/s).

Given: Δp(0) = 1014 cm−3, Lp = 30 μm = 3×10−3 cm, Dp = 11.6 cm2/s.

Find: Jp at x = 0.

Formula:

Δp(x) = Δp(0)e−x/Lp, Jp = −qDp dp/dx

Solution.

Δp(x) = Δp(0)e−x/Lp, so dp/dx at x = 0 is −Δp(0)/Lp.

Jp = −qDp dp/dx = qDpΔp(0)/Lp = 1.6×10−19 × 11.6 × 1014 / 3×10−3
= 0.062 A/cm2

Answer: Jp ≈ 0.062 A/cm2 (62 mA/cm2), flowing in the +x direction.

What this means: with no electric field at all, a concentration difference alone drives a sizeable current; the steeper the fall-off (the shorter Lp), the larger the current.

### 4. Junction parameters

Question. A Si p+n junction has ND = 5×1015 cm−3 and NA = 1018 cm−3. Find Vbi, the depletion width at zero bias and at −10 V, and the peak field at −10 V.

Given: ND = 5×1015 cm−3, NA = 1018 cm−3, ni = 1010 cm−3, εs = 1.04×10−12 F/cm, kT/q = 0.0259 V.

Find: Vbi, W(0), W(−10 V), Emax(−10 V).

Formula:

Vbi = (kT/q) ln(NAND/ni2), W = √(2εs(Vbi − V)/qND), Emax = 2(Vbi − V)/W

Solution.

Vbi = 0.0259 ln(1018 × 5×1015 / 1020) = 0.0259 ln(5×1013) = 0.0259 × 31.54 = 0.817 V

One-sided (NA ≫ ND): W = √(2εs(Vbi − V)/qND).

V = 0: W = √(2 × 1.04×10−12 × 0.817 / (1.6×10−19 × 5×1015)) = √(2.12×10−9) = 4.6×10−5 cm = 0.46 μm
V = −10: W = √(2 × 1.04×10−12 × 10.817 / 8×10−4) = √(2.81×10−8) = 1.68×10−4 cm = 1.68 μm
Emax = 2(Vbi − V)/W = 2 × 10.817 / 1.68×10−4 = 1.29×105 V/cm

Answer: Vbi = 0.817 V; W = 0.46 μm at 0 V and 1.68 μm at −10 V; Emax = 1.29×105 V/cm.

What this means: the depletion region lies almost entirely in the lightly doped n side and grows as the square root of the voltage. The peak field is still below the roughly 3×105 V/cm at which silicon breaks down, so the junction safely blocks 10 V.

### 5. Diode current

Question. The diode of Q4 has area 10−3 cm2 and Is = 1×10−14 A. Find the current at 0.6 V and the voltage for 1 mA.

Given: Is = 10−14 A, kT/q = 0.0259 V, ideal diode (η = 1).

Find: I at 0.6 V; V at 1 mA.

Formula:

I = Is(eqV/kT − 1), V = (kT/q) ln(I/Is + 1)

Solution.

I(0.6 V) = 10−14 (e0.6/0.0259 − 1) = 10−14 × 1.15×1010 = 0.115 mA
V(1 mA) = 0.0259 ln(10−3/10−14 + 1) = 0.0259 × 25.33 = 0.656 V

Answer: I = 0.115 mA at 0.6 V; V = 0.656 V for 1 mA.

What this means: raising the voltage by only 56 mV multiplies the current by almost nine, which is why a silicon diode looks as if it "turns on" sharply at about 0.6–0.7 V.

### 6. Schottky diode

Question. A Schottky diode on n-Si has ΦB = 0.7 eV. Find Js at 300 K (A∗∗ = 110 A/cm2K2) and the forward voltage for J = 10 A/cm2.

Given: ΦB = 0.7 eV, T = 300 K, A∗∗ = 110 A/(cm2·K2), J = 10 A/cm2, kT/q = 0.0259 V.

Find: Js and V.

Formula:

Js = A∗∗T2 e−qΦB/kT, V = (kT/q) ln(J/Js)

Solution.

Js = A∗∗T2e−qΦB/kT = 110 × 9×104 × e−0.7/0.0259 = 9.9×106 × 1.82×10−12 = 1.8×10−5 A/cm2
V = 0.0259 ln(10/1.8×10−5) = 0.0259 × 13.23 = 0.343 V

Answer: Js ≈ 1.8×10−5 A/cm2; V ≈ 0.34 V for 10 A/cm2.

What this means: a p-n diode needs about 0.7 V for a similar current density, which is why Schottky diodes are used where a low forward drop matters.

### 7. Doping from C-V

Question. A 1/C2 plot for a one-sided junction of area 2×10−3 cm2 has slope magnitude 4.0×1020 F−2V−1. Find the doping.

Given: A = 2×10−3 cm2, |slope| = 4.0×1020 F−2V−1, q = 1.6×10−19 C, εs = 1.04×10−12 F/cm.

Find: N.

Formula:

N = 2/(qεsA2|slope|)

Solution.

N = 2/(qεsA2|slope|) = 2 / (1.6×10−19 × 1.04×10−12 × (2×10−3)2 × 4.0×1020)
= 2 / (2.66×10−16) = 7.5×1015 cm−3

Answer: N ≈ 7.5×1015 cm−3 (the doping of the lightly doped side).

What this means: a shallower 1/C2 line means heavier doping; because N depends on 1/A2, a 10 % error in the measured area would give about a 20 % error in this doping.

## Practice questions

These extra questions practise this week's ideas. Work each one on paper before reading the solution; the calculation questions follow the same Question, Given, Find, Solution, Answer layout as the worked examples.

#### Practice 12.1: ideality factor

Question. A diode carries 1 mA at 0.55 V and 10 mA at 0.62 V. Find its ideality factor.

Given: a decade of current over ΔV = 0.07 V, kT/q = 0.0259 V.

Find: η.

Solution.

slope = ln 10 / 0.07 = 32.9 V−1
η = 1/(0.0259 × 32.9) = 1.17

Answer: η ≈ 1.17: some depletion-region recombination current is present.

#### Practice 12.2: series resistance

Question. At 50 mA a diode's measured voltage is 0.80 V, while the straight line of the semi-log plot predicts 0.70 V at that current. Find the series resistance.

Given: I = 50 mA, ΔV = 0.80 − 0.70 = 0.10 V.

Find: Rs.

Solution.

Rs = ΔV/I = 0.10/0.05 = 2 Ω

Answer: Rs = 2 Ω.

#### Practice 12.3: barrier height from the saturation current

Question. A Schottky diode of area 1×10−4 cm2 has Is = 2×10−9 A at 300 K. Find the barrier height (A∗∗ = 110 A/cm2K2).

Given: Is = 2×10−9 A, A = 10−4 cm2, A∗∗ = 110 A/cm2K2, T = 300 K.

Find: ΦB.

Solution.

ΦB = (kT/q) ln(A∗∗AT2/Is) = 0.0259 × ln(110 × 10−4 × 9×104 / 2×10−9)
= 0.0259 × ln(4.95×1011) = 0.0259 × 26.93 = 0.70 eV

Answer: ΦB ≈ 0.70 eV.

What this means: a 2 nA leakage from such a small contact points to a moderate barrier; a diode with ΦB only 0.1 eV lower would leak about 50 times more.

#### Practice 12.4: doping from two C-V points

Question. A one-sided silicon junction of area 1×10−3 cm2 has C = 20 pF at −1 V and 12 pF at −4 V. Assuming uniform doping, find N and Vbi.

Given: C(−1 V) = 20 pF, C(−4 V) = 12 pF, A = 10−3 cm2, εs = 1.04×10−12 F/cm.

Find: N and Vbi.

Solution.

1/C2 at −1 V = 1/(20×10−12)2 = 2.50×1021 F−2
1/C2 at −4 V = 1/(12×10−12)2 = 6.94×1021 F−2
|slope| = (6.94 − 2.50)×1021 / 3 = 1.48×1021 F−2V−1
N = 2/(qεsA2|slope|) = 2/(1.6×10−19 × 1.04×10−12 × 10−6 × 1.48×1021) = 8.1×1015 cm−3
1/C2 = |slope|(Vbi − V): 2.50×1021 = 1.48×1021 (Vbi + 1) ⇒ Vbi = 0.69 V

Answer: N = 8.1×1015 cm−3, Vbi = 0.69 V.

What this means: two capacitance readings are enough to estimate both the doping and the built-in potential, but only if the doping is uniform; a real profile needs many points so that the curvature of the 1/C2 plot can be seen.

#### Practice 12.5: oxide thickness from MOS C-V

Question. A MOS capacitor of area 1×10−3 cm2 shows a capacitance of 345 pF in accumulation. Find the oxide thickness.

Given: C = 345 pF, A = 10−3 cm2, εox = 3.45×10−13 F/cm.

Find: tox.

Solution.

Cox = C/A = 345×10−12 / 10−3 = 3.45×10−7 F/cm2
tox = εox/Cox = 3.45×10−13 / 3.45×10−7 = 1×10−6 cm

Answer: tox = 10 nm.

#### Practice 12.6: why one-sided?

Question. Why is C-V profiling done on a p+n (or n+p) junction or a Schottky diode rather than a junction with similar doping on both sides?

Answer. The formula N = 2/(qεsA2|d(1/C2)/dV|) assumes that the depletion region grows into one side only, so that the change in charge measures one doping. In a one-sided junction or Schottky diode, almost all of W lies in the lightly doped side, and the measurement gives that side's doping at depth W. If both sides were similarly doped, W would grow into both at once, and the result would be a mixture (an effective NAND/(NA + ND)) that cannot be assigned to either side or to a depth.

## Objectives check

Use this table to confirm you have met this week's objectives. Cover the Answer column and answer each check question from memory. If you cannot, go back to the section in the last column before moving on.

| # | Objective | Check yourself | Answer | Where it is taught |  |  |
| --- | --- | --- | --- | --- | --- | --- |
| 1 | Describe I-V measurement and extract Is, η and Rs. | What plot gives a straight line for a diode, and what does its slope give? | ln I against V; slope = q/(ηkT). | I-V characterisation; Example 12.1; I-V vs C-V table (The big picture) |  |  |
| 2 | Explain how the Schottky barrier height is obtained from I-V data. | What is plotted in an Arrhenius plot of a Schottky diode? | ln(Is/T2) against 1/T; slope = −qΦB/k. | What else the I-V curve shows; Barrier height from the saturation current; Example 12.2 |  |  |
| 3 | Explain the principle of C-V measurement. | Why does the junction capacitance fall with reverse bias? | The depletion width W grows, and C = εsA/W. | C-V characterisation |  |  |
| 4 | Extract doping and built-in potential from a Mott–Schottky plot. | What gives N and what gives Vbi in a 1/C2 plot? | N from the slope, N = 2/(qεsA2 | slope | ); Vbi from the voltage intercept. | Mott–Schottky plot; Example 12.3 |
| 5 | Explain doping profiling and the MOS C-V measurement. | Where is the doping being measured at each bias? | At the depletion edge, depth W = εsA/C. | Doping profiles; MOS C-V |  |  |

Week 13 · Module 5 · Advanced Device Technology

# Bipolar Junction Transistors (BJTs)

Plan: operational physics; minority-carrier profiles in the active regions; emitter efficiency, base transport factor and current gains (α, β). This page follows your lecturer's Weeks 13–15 note (sections 13.1–13.13) and solves its review questions.

## Learning objectives

By the end of this week you should be able to:

- Explain the structure and operating principle of NPN and PNP transistors.

- Describe injection, diffusion, recombination and collection in the forward-active region.

- Sketch and explain the minority-carrier profiles.

- Define emitter injection efficiency and base transport factor.

- Derive α and β and relate them to γ and αT.

- Solve problems on transistor currents and gains.

## Symbols and abbreviations used this week

Every symbol, constant and abbreviation on this page is listed here, even if an earlier week already defined it, so you can study this page on its own.

Constants and units

| Symbol | Meaning | Units / typical value |
| --- | --- | --- |
| q | Magnitude of the electronic charge | 1.6×10−19 C |
| k | Boltzmann constant | 8.617×10−5 eV/K = 1.381×10−23 J/K |
| kT | Thermal energy | 0.0259 eV (often 0.02585 eV) at 300 K |
| kT/q | Thermal voltage | 0.0259 V (about 26 mV) at 300 K |
| μm | Micrometre (micron) | 1 μm = 10−4 cm = 10−6 m |

Symbols

| Symbol | Meaning | Units / typical value |
| --- | --- | --- |
| ni | Intrinsic carrier concentration (n = p = ni in pure material) | cm−3; Si ≈ 1×1010 at 300 K |
| pn0, np0 | Equilibrium minority concentrations: holes on the n side, electrons on the p side | cm−3; pn0 = ni2/ND |
| NB (CB) | Background doping of the wafer (in Week 13, NB is the base doping) | cm−3 |
| μ, μn, μp | Mobility: drift velocity per unit field (electrons, holes) | cm2/(V·s); Si μn 1350, μp 480 |
| J, Jn, Jp | Current density (total, electrons, holes) | A/cm2 |
| Dn, Dp | Diffusion coefficients of electrons and holes | cm2/s; Si 35 and 12.4 |
| τ, τn, τp | Minority-carrier lifetime (τeff: effective, including surfaces) | s; Si 1 ns – 1 ms |
| L, Ln, Lp | Diffusion length √(Dτ): distance a minority carrier travels before recombining | μm or cm |
| V, Va | Applied voltage (positive for forward bias) | V |
| Is, Js (IS) | Saturation current (density) of a diode or transistor | A; A/cm2 |
| A (area) | Device or contact area | cm2 |
| IE, IB, IC | Emitter, base and collector currents | A (mA) |
| VBE, VCE, VCB | Base–emitter, collector–emitter and collector–base voltages | V |
| α | Common-base current gain, IC/IE | dimensionless; 0.98–0.999 |
| β | Common-emitter current gain, IC/IB (also hFE) | dimensionless; 50–500 |
| γ (BJT) | Emitter injection efficiency | dimensionless, close to 1 |
| αT | Base transport factor | dimensionless, close to 1 |
| NE, WE, DE; NB, WB, DB | Doping, width and minority diffusion coefficient of the emitter; of the base | cm−3; μm; cm2/s |
| VA | Early voltage | V |
| ro | Output resistance | Ω |
| τB | Base transit time, WB2/2Dn | s |
| fT | Transition (cut-off) frequency | Hz |
| nn0, pp0, pn0, np0 | Equilibrium densities: majority (nn0, pp0) and minority (pn0 holes on n side, np0 electrons on p side) | cm−3 |
| IE,n, IE,p, IC,n | Electron and hole parts of the emitter and collector currents | A |
| nB(x) | Minority-electron density in the base of an NPN transistor | cm−3 |
| VEB, VBC (VCB) | Emitter–base and base–collector voltages | V |
| ΔV, ΔVBE | A small change in a voltage | V |
| IC1, IC2 | Collector currents at two operating points | A |

Abbreviations

| Abbreviation | Meaning |
| --- | --- |
| Si | Silicon |
| CB | Conduction band |
| MOSFET | Metal–oxide–semiconductor field-effect transistor |
| BJT | Bipolar junction transistor |
| NPN | BJT with n-type emitter, p-type base, n-type collector |
| PNP | BJT with p-type emitter, n-type base, p-type collector |
| E–B | Emitter–base (junction) |
| C–B | Collector–base (junction) |
| n+ | Very heavily doped n-type (similarly p+) |

## Key terms

Every important word used this week is defined here, so you can read this week on its own.

Doping (NE, NB). Adding a small, controlled amount of impurity atoms to a semiconductor. Donors give electrons and make it n-type; acceptors create holes and make it p-type. In a transistor, NE and NB are the doping concentrations of the emitter and the base (atoms per cm3).

Majority and minority carriers. The more numerous carrier in a region is the majority carrier (electrons in n-type, holes in p-type); the less numerous one is the minority carrier. Electrons injected into a p-type base are minority carriers there.

Why it matters: the main current of a BJT is carried by minority carriers crossing the base.

p-n junction and depletion region. The boundary between a p-type and an n-type region. Around it lies a thin depletion region, emptied of mobile carriers and containing a strong electric field.

Forward and reverse bias. A junction is forward biased when the p side is made positive with respect to the n side: the barrier is lowered and carriers are injected across it. It is reverse biased when the p side is made negative: the barrier rises, almost no current flows, and the field sweeps across any minority carriers that reach the depletion edge.

Diffusion. The movement of carriers from where they are concentrated to where they are sparse, caused only by their random thermal motion. Its strength is measured by the diffusion coefficient D (cm2/s).

Minority-carrier lifetime (τn, τp) and diffusion length (Ln, Lp). The lifetime τ is the average time a minority carrier survives before it recombines with a majority carrier. The diffusion length is the average distance it diffuses in that time.

Ln = √(Dn τn)

Where:

- Ln = electron diffusion length (cm)

- Dn = electron diffusion coefficient (cm2/s)

- τn = electron lifetime (s)

Bipolar junction transistor (BJT). A three-terminal device made of three alternately doped regions, emitter (E), base (B) and collector (C), forming two back-to-back p-n junctions. It is called bipolar because both electrons and holes carry current. It is built as NPN or PNP.

Emitter, base and collector. The emitter is the heavily doped region that injects carriers; the base is the thin, lightly doped middle region they cross; the collector is the moderately doped region that gathers them.

Forward-active mode. The normal amplifying condition: emitter–base junction forward biased, collector–base junction reverse biased. The collector current is then set by VBE (or IB) and hardly depends on the collector voltage.

Emitter injection efficiency (γ). The fraction of the emitter current that is carried by the useful carriers injected from the emitter into the base (electrons in an NPN), rather than by carriers injected backwards from the base into the emitter.

Why it matters: only the carriers injected into the base can reach the collector, so γ sets an upper limit on the gain.

Base transport factor (αT). The fraction of the carriers injected into the base that cross it without recombining and reach the collector.

Common-base current gain (α). The ratio of collector current to emitter current, α = IC/IE. It is just below 1 (typically 0.98–0.999).

Common-emitter current gain (β, hFE). The ratio of collector current to base current, β = IC/IB; typically 50–500.

β = α / (1 − α)

Where:

- β = common-emitter current gain (dimensionless)

- α = common-base current gain (dimensionless)

Why it matters: because α is so close to 1, a tiny base current controls a collector current about β times larger, which is amplification.

Saturation current of a transistor (IS). The scale factor in the collector-current law IC = IS eqVBE/kT. It is set by the base doping, base width and device area, and is typically 10−16–10−14 A.

Early effect and Early voltage (VA). In the active mode, raising VCE widens the collector depletion region into the base and makes the neutral base thinner, so IC rises slightly. Extended backwards, the sloping output curves meet the VCE axis at −VA, the Early voltage.

Output resistance (ro). The small-signal resistance seen looking into the collector, ΔVCE/ΔIC, approximately VA/IC. A large ro means the transistor behaves like a good current source.

## The big picture

A transistor is a device in which a small current or voltage controls a large current. That is all amplification is.

In a BJT the trick is geometry. Two p-n junctions (Week 10) are built back to back, with a very thin middle layer. One junction pushes carriers into the thin layer; the other junction, a fraction of a micrometre away, pulls them out the other side. Because the middle layer is so thin, almost every carrier that goes in comes out at the far side. A small current into the middle layer (the base) is enough to keep this going, while a large current flows straight through. The physics is the minority-carrier diffusion you met in Weeks 7–9.

## 13.1 Introduction and BJT structure

A bipolar junction transistor (BJT) is a three-terminal semiconductor device in which both electrons and holes take part in current conduction. That is why it is called "bipolar". The three terminals are the emitter (E), base (B) and collector (C). A BJT contains two p-n junctions, arranged either as NPN or PNP.

| Region | Typical doping | Main function |
| --- | --- | --- |
| Emitter | Heavily doped (n+ in an NPN) | Injects majority carriers into the base |
| Base | Lightly doped and very thin | Controls carrier transport and limits recombination |
| Collector | Moderately doped | Collects carriers and supports the voltage |

Why each choice?

- The emitter is heavily doped so that, when its junction is forward biased, it can inject a large concentration of carriers into the base, and so that the base injects very few carriers back into it.

- The base is very thin (often well under 1 μm) and lightly doped, so that most injected carriers cross it before they have time to recombine.

- The collector is moderately doped and physically larger, so that it can collect the carriers and withstand a relatively high reverse voltage without breaking down.

## 13.2 BJT biasing and operational physics

For normal forward-active operation of an NPN transistor:

- the emitter–base junction is forward biased;

- the collector–base junction is reverse biased.

What happens, step by step:

- Injection. The forward-biased E–B junction lowers its barrier. Electrons flow from the n-type emitter into the p-type base. In the base they are minority carriers.

- Diffusion across the base. There are many injected electrons at the emitter side of the base and almost none at the collector side, so they diffuse across. Because the base is thin, most of them get across.

- Recombination (a small loss). A small fraction of the electrons meet holes in the base and recombine.

- Collection. The electrons that reach the collector side are swept into the collector by the strong electric field of the reverse-biased C–B junction. They form most of the collector current.

- Base current. The base current is mainly associated with (a) recombination in the base, which must be replaced by holes flowing in through the base lead, and (b) holes injected from the base into the emitter.

For a PNP transistor the carrier polarities are reversed: holes are injected from the p-type emitter into the n-type base and are collected by the p-type collector. All currents and voltages change sign.

| Feature | NPN | PNP |
| --- | --- | --- |
| Layers (E–B–C) | n+ – p – n | p+ – n – p |
| Carriers injected into the base | Electrons (minority carriers in the p-type base) | Holes (minority carriers in the n-type base) |
| Main E-to-C current carried by | Electrons | Holes |
| Base current carried by | Holes (recombination and back-injection into the emitter) | Electrons |
| Forward-active bias | VBE ≈ +0.7 V (base above emitter); VCB > 0 | VEB ≈ +0.7 V (emitter above base); VBC > 0 |
| Conventional current | IC and IB flow in; IE flows out of the emitter | IE flows into the emitter; IC and IB flow out |
| Emitter arrow in the symbol | Points out | Points in |
| Speed and gain for the same size | Higher: electrons have the larger mobility and diffusion coefficient (Dn ≈ 35 against Dp ≈ 12.4 cm2/s in Si) | Lower |
| Typical use | Most amplifiers and switches; integrated circuits | Complementary (push–pull) stages with NPN, high-side switches, current sources and mirrors from the positive supply |

In plain words. The emitter is a crowd pushing through a door (the forward-biased junction) into a narrow corridor (the base). At the other end of the corridor is a slide (the reverse-biased junction) that carries everyone who reaches it away. The corridor is so short that nearly everyone makes it. The base current is the small trickle of people who get lost in the corridor, plus a few who wander back the wrong way.

## 13.3 Minority-carrier concentration profiles

In a forward-active NPN transistor, electrons are minority carriers in the p-type base. Their concentration is highest at the emitter side of the base (because of injection) and almost zero at the collector side (because the collector removes them as fast as they arrive). In a thin, uniformly doped base with little recombination, the profile in between is approximately a straight line:

nB(x) ≈ nB(0) − [ nB(0) − nB(WB) ] x/WB

| Symbol | Meaning |
| --- | --- |
| WB | neutral base width |
| x | distance measured from the emitter side of the base |
| nB(0) | minority-electron concentration at the emitter edge of the base, nB(0) = np0 eqVBE/kT |
| nB(WB) | minority-electron concentration at the collector edge, ≈ 0 |

Minority carriers in an NPN transistor in the forward-active mode. Electrons in the base fall almost linearly from nB(0) to about zero at the collector edge. Holes injected back into the emitter decay away from the junction.

The concentration gradient drives electron diffusion through the base. By Fick's law the electron diffusion current density is

Jn = q Dn (dn/dx)

where q is the magnitude of the electronic charge and Dn the electron diffusion coefficient (the sign depends on the direction you take as positive). For the straight-line profile, dn/dx = −nB(0)/WB, so

|Jn| = q Dn nB(0) / WB

Where:

- Jn = electron diffusion current density in the base (A/cm2)

- q = electronic charge, 1.6×10−19 C

- Dn = electron diffusion coefficient in the base (cm2/s)

- nB(0) = electron concentration at the emitter edge of the base, np0 eqVBE/kT (cm−3)

- np0 = equilibrium electron concentration in the base, ni2/NB (cm−3)

- WB = neutral base width (cm)

This is the collector current density. It is controlled by VBE through nB(0) = np0 eqVBE/kT, and it is larger for a thinner base.

At the collector–base junction, the electric field in the reverse-biased depletion region rapidly sweeps the carriers into the collector. Because the collector only has to collect whatever arrives, the collector current is almost independent of the collector voltage in the active region, provided the transistor stays away from breakdown and saturation. This is what makes the BJT behave like a current source.

## 13.4 Emitter injection efficiency γ

The emitter current is made of two parts:

- IE,n: electrons injected from emitter into base (useful: these become the collector current);

- IE,p: holes injected from base into emitter (wasted: they only add to base current).

Emitter injection efficiency γ (gamma) measures what fraction of the emitter current is the useful kind:

γ = IE,n / (IE,n + IE,p)

Where:

- γ = emitter injection efficiency (dimensionless, just below 1)

- IE,n = electron current injected from the emitter into the base (A)

- IE,p = hole current injected from the base into the emitter (A)

A well-designed transistor has γ very close to 1. The electrons injected into the base are limited by the base doping, and the holes injected into the emitter by the emitter doping: the more heavily a side is doped, the fewer carriers the other side can inject into it. This gives

γ ≈ 1 / [ 1 + (DE NB WB) / (DB NE WE) ]

Where:

- NE, NB = emitter and base doping concentrations (cm−3)

- WE, WB = neutral emitter and base widths (cm or μm; only their ratio matters)

- DE = diffusion coefficient of the minority carriers in the emitter (holes in an NPN) (cm2/s)

- DB = diffusion coefficient of the minority carriers in the base (electrons in an NPN) (cm2/s)

This form assumes both the emitter and the base are much thinner than their minority-carrier diffusion lengths. Making NE ≫ NB makes the fraction small and γ close to 1.

Factors that improve emitter efficiency:

- heavy emitter doping relative to base doping;

- appropriate semiconductor material and junction design (for example a wider-gap emitter in a heterojunction transistor);

- proper control of emitter and base widths;

- minimising unwanted carrier injection.

## 13.5 Base transport factor αT

Of the electrons injected into the base, a few recombine before reaching the collector. The base transport factor αT is the fraction that make it:

αT = IC,n / IE,n

Where:

- αT = base transport factor (dimensionless, just below 1)

- IC,n = electron current reaching the collector (A)

- IE,n = electron current injected into the base by the emitter (A)

If recombination in the base is negligible, αT approaches 1. If the base is thick, or the minority-carrier lifetime is short, more carriers recombine and αT falls. Quantitatively,

αT ≈ 1 − WB2 / (2Ln2), Ln = √(Dn τn)

Where:

- WB = neutral base width (cm)

- Ln = diffusion length of electrons in the base (cm)

- Dn = electron diffusion coefficient in the base (cm2/s)

- τn = electron lifetime in the base (s)

The transport factor depends on base width WB, the minority-carrier diffusion coefficient Dn and the minority-carrier lifetime τn. A thin base and a long lifetime give αT close to one. For example WB = 1 μm and Ln = 20 μm give αT = 1 − 1/800 = 0.99875.

## 13.6 Common-base current gain α

The common-base current gain is the ratio of collector current to emitter current:

α = IC / IE

Where:

- α = common-base current gain (dimensionless)

- IC = collector current (A)

- IE = emitter current (A)

The collector current is slightly less than the emitter current (a little is lost to the base), so α is always less than 1, but for a good transistor it is very close to 1, typically 0.98–0.999.

Physically, a current must survive two losses to get from emitter to collector: it must be the right kind of carrier (γ) and it must survive the trip (αT). So

α ≈ γ αT

Where:

- α = common-base current gain

- γ = emitter injection efficiency

- αT = base transport factor (all dimensionless)

#### Example 13.1: α from γ and αT

Question. A transistor has an emitter injection efficiency of 0.995 and a base transport factor of 0.990. Estimate its common-base current gain.

Given: γ = 0.995, αT = 0.990.

Find: α.

Formula:

α ≈ γαT

Solution.

α ≈ γαT = 0.995 × 0.990 = 0.98505

Answer: α ≈ 0.985.

What this means: about 1.5 % of the emitter current never reaches the collector: 0.5 % is lost as holes injected back into the emitter and about 1 % as electrons that recombine in the base. That missing 1.5 % is the base current.

## 13.7 Common-emitter current gain β

The common-emitter current gain β (also called hFE under specified conditions) is the ratio of collector current to base current:

β = IC / IB

Where:

- β = common-emitter current gain (dimensionless)

- IC = collector current (A)

- IB = base current (A)

Deriving the relation between α and β. Kirchhoff's current law at the transistor: everything that enters at the emitter leaves at the collector or the base,

IE = IC + IB

Start from α:

α = IC/IE = IC/(IC + IB)

Divide top and bottom by IB, and use β = IC/IB:

α = (IC/IB) / (IC/IB + 1) = β/(β + 1)

Solve for β: α(β + 1) = β ⇒ αβ + α = β ⇒ α = β(1 − α) ⇒

β = α / (1 − α)

Where:

- β = common-emitter current gain, IC/IB (dimensionless)

- α = common-base current gain, IC/IE (dimensionless)

Because α is close to 1, the denominator 1 − α is a small number, so a small change in α produces a large change in β:

| α | 0.98 | 0.99 | 0.995 | 0.999 |
| --- | --- | --- | --- | --- |
| β = α/(1 − α) | 49 | 99 | 199 | 999 |

#### Example 13.2: γ, αT, α and β of a PNP transistor from its design

Question. A silicon p+np transistor has emitter doping NE = 5×1018 cm−3 and base doping NB = 1×1017 cm−3. The neutral emitter is 0.5 μm wide and the neutral base 0.8 μm. The electron diffusion coefficient in the emitter is 5 cm2/s, the hole diffusion coefficient in the base is 8 cm2/s, and the hole lifetime in the base is 0.5 μs. Find γ, αT, α and β, and say which factor limits the gain.

Given: NE = 5×1018 cm−3, NB = 1017 cm−3, WE = 0.5 μm, WB = 0.8 μm = 8×10−5 cm, DE = 5 cm2/s (electrons in the emitter), DB = 8 cm2/s (holes in the base), τp = 0.5×10−6 s.

Find: γ, αT, α, β.

Formula: the same as for an NPN, with the roles of electrons and holes swapped (the base minority carriers are now holes, so Lp replaces Ln):

γ ≈ 1/[1 + (DE NB WB)/(DB NE WE)], αT ≈ 1 − WB2/(2Lp2), Lp = √(DB τp)

α ≈ γαT, β = α/(1 − α)

Solution.

Step 1. Emitter injection efficiency:

(DE NB WB)/(DB NE WE) = (5 × 1017 × 0.8)/(8 × 5×1018 × 0.5) = 4×1017/2×1019 = 0.020
γ = 1/1.020 = 0.9804

Step 2. Diffusion length and base transport factor:

Lp = √(8 × 0.5×10−6) = 2.0×10−3 cm = 20 μm
αT = 1 − (0.8)2/(2 × 202) = 1 − 0.64/800 = 0.9992

Step 3. Current gains:

α = 0.9804 × 0.9992 = 0.9796
β = 0.9796/(1 − 0.9796) = 0.9796/0.0204 ≈ 48

Answer: γ = 0.980, αT = 0.9992, α = 0.980, β ≈ 48. The emitter injection efficiency limits the gain.

What this means: only 0.08 % of the holes are lost by recombination in the base, but 2 % of the emitter current is electrons injected backwards into the emitter, because the emitter is only 50 times more heavily doped than the base and is thin. Doping the emitter more heavily (or using a wider-band-gap emitter) would raise β far more than making the base thinner.

## 13.8 BJT current relationships

| Quantity | Expression | Meaning |
| --- | --- | --- |
| Emitter current | IE = IC + IB | Total transistor current at the emitter |
| Common-base gain | α = IC/IE | Collector current relative to emitter current |
| Common-emitter gain | β = IC/IB | Collector current relative to base current |
| Relation | β = α/(1 − α) | Converts α to β |
| Relation | α = β/(β + 1) | Converts β to α |
| Physics of α | α ≈ γαT | Injection efficiency × transport factor |
| Collector current | IC = IS eqVBE/kT | Set by the base–emitter voltage |

The last line comes from multiplying the diffusion current density of section 13.3 by the emitter area, using nB(0) = np0 eqVBE/kT and np0 = ni2/NB:

IC = IS eqVBE/kT, IS = q A DB ni2 / (NB WB)

Where:

- IC = collector current (A)

- IS = saturation current of the transistor (A)

- VBE = base–emitter voltage (V); kT/q = 0.0259 V at 300 K

- A = emitter (junction) area (cm2)

- DB = minority-carrier diffusion coefficient in the base (cm2/s)

- ni = intrinsic carrier concentration, 1×1010 cm−3 for Si

- NB = base doping (cm−3); WB = neutral base width (cm)

Because IC depends exponentially on VBE, every increase of (kT/q) ln 10 ≈ 60 mV in VBE multiplies IC by 10.

#### Example 13.3: collector and base currents from IS and VBE

Question. An NPN transistor has IS = 5×10−16 A and β = 150. At VBE = 0.68 V (300 K), find IC, IB and IE. By how much must VBE rise to increase IC tenfold?

Given: IS = 5×10−16 A, β = 150, VBE = 0.68 V, kT/q = 0.0259 V.

Find: IC, IB, IE and ΔVBE for a ×10 change in IC.

Formula:

IC = IS eqVBE/kT, IB = IC/β, IE = IC + IB, ΔVBE = (kT/q) ln(IC2/IC1)

Solution.

Step 1. Collector current:

qVBE/kT = 0.68/0.0259 = 26.25, e26.25 = 2.53×1011
IC = 5×10−16 × 2.53×1011 = 1.26×10−4 A = 0.126 mA

Step 2. Base and emitter currents:

IB = 0.126 mA / 150 = 0.84 μA
IE = 0.126 + 0.00084 = 0.127 mA

Step 3. Voltage for a tenfold increase:

ΔVBE = 0.0259 × ln 10 = 0.0596 V ≈ 60 mV

Answer: IC ≈ 0.126 mA, IB ≈ 0.84 μA, IE ≈ 0.127 mA; VBE must rise by about 60 mV (to 0.74 V) for 1.26 mA.

What this means: the transistor is a very sensitive voltage-controlled device: a sub-microamp base current and a change of only 60 mV at the input change the output current by a factor of ten. This is why VBE stays near 0.6–0.7 V over a wide range of collector currents.

## 13.9 Worked example 1: finding α

Question. A BJT has an emitter current of 5 mA and a collector current of 4.9 mA. Determine α and the base current.

Given: IE = 5 mA, IC = 4.9 mA.

Find: α and IB.

Formula:

α = IC/IE, IB = IE − IC

Solution.

α = IC/IE = 4.9/5 = 0.98
IB = IE − IC = 5 − 4.9 = 0.1 mA

Answer: α = 0.98, IB = 0.1 mA. (And β = 4.9/0.1 = 49.)

What this means: 98 % of the emitter current reaches the collector; the 2 % that flows out of the base lead is the "control" current, and 0.1 mA of it governs 4.9 mA of output.

## 13.10 Worked example 2: finding β from α

Question. A transistor has α = 0.98. Determine β. If the base current is 0.2 mA, determine the collector and emitter currents.

Given: α = 0.98, IB = 0.2 mA.

Find: β, IC, IE.

Formula:

β = α/(1 − α), IC = βIB, IE = IC + IB

Solution.

β = α/(1 − α) = 0.98/0.02 = 49
IC = βIB = 49 × 0.2 mA = 9.8 mA
IE = IC + IB = 9.8 + 0.2 = 10.0 mA

Answer: β = 49, IC = 9.8 mA, IE = 10 mA.

What this means: in the common-emitter connection the 0.2 mA base current is amplified 49 times; a modest α of 0.98 already gives useful current gain.

## 13.11 Worked example 3: injection efficiency and transport factor

Question. An NPN transistor has emitter injection efficiency γ = 0.995 and base transport factor αT = 0.990. Estimate α and β.

Given: γ = 0.995, αT = 0.990.

Find: α and β.

Formula:

α ≈ γαT, β = α/(1 − α)

Solution.

α ≈ γαT = 0.995 × 0.990 = 0.98505
β = α/(1 − α) = 0.98505/0.01495 ≈ 65.9

Answer: α ≈ 0.985, β ≈ 65.9.

What this means: neither loss is large on its own (0.5 % and 1 %), yet together they hold β down to 66, because β depends on how small 1 − α is.

## Worked example 4: from device design to gain

Question. An NPN silicon transistor has NE = 1019 cm−3, NB = 1017 cm−3, WE = 1 μm, WB = 0.5 μm, DE (holes in the emitter) = 2.5 cm2/s, DB (electrons in the base) = 25 cm2/s, base lifetime τn = 1 μs and area 10−4 cm2. Calculate the emitter injection efficiency γ, the base transport factor αT, the current gains α and β, and the collector and base currents at VBE = 0.65 V.

Given: the dopings, widths, diffusion coefficients and lifetime above; ni = 1010 cm−3, kT/q = 0.0259 V.

Find: γ, αT, α, β, IC and IB.

Formula:

γ ≈ 1/[1 + (DE NB WB)/(DB NE WE)], αT ≈ 1 − WB2/(2Ln2), Ln = √(DB τn)

α ≈ γαT, β = α/(1 − α), IS = qADBni2/(NBWB), IC = IS eqVBE/kT, IB = IC/β

Solution.

γ = 1 / [1 + (2.5 × 1017 × 0.5)/(25 × 1019 × 1)] = 1/(1 + 5×10−4) = 0.99950
Ln = √(25 × 10−6) = 5×10−3 cm = 50 μm
αT = 1 − 0.52/(2 × 502) = 1 − 5×10−5 = 0.99995
α = γαT = 0.99945, β = 0.99945/0.00055 ≈ 1800

IS = qADBni2/(NBWB) = (1.6×10−19)(10−4)(25)(1020)/(1017 × 5×10−5) = 8×10−15 A
IC = 8×10−15 × e0.65/0.0259 = 8×10−15 × 7.9×1010 = 0.63 mA, IB = IC/β ≈ 0.35 μA

Answer: γ = 0.9995, αT = 0.99995, α = 0.99945, β ≈ 1800; IC ≈ 0.63 mA and IB ≈ 0.35 μA at VBE = 0.65 V.

What this means: here the emitter efficiency limits β: the back-injection loss (5×10−4) is ten times the recombination loss in the base (5×10−5). Real devices have lower β (typically 100–300) because of recombination in the E–B depletion region and other non-ideal effects.

## 13.12 BJT operating regions

| Region | Emitter–base junction | Collector–base junction | Typical use |
| --- | --- | --- | --- |
| Cut-off | Reverse biased | Reverse biased | OFF (switching) |
| Forward active | Forward biased | Reverse biased | Amplification |
| Saturation | Forward biased | Forward biased | ON (switching) |
| Reverse active | Reverse biased | Forward biased | Limited, reverse operation |

- Cut-off: no injection, so essentially no current flows: an open switch.

- Forward active: IC = βIB, controlled by the base: an amplifier.

- Saturation: both junctions inject; the collector can no longer collect everything independently, IC < βIB, and VCE is small (about 0.2 V): a closed switch.

- Reverse active: emitter and collector swap roles; gain is poor because the collector was not designed to inject.

Early effect. In the active region, increasing VCE widens the collector depletion region slightly into the base, making WB smaller. A thinner base means a steeper profile and a larger IC, so the output curves slope upward slightly. Extrapolated backwards they meet at −VA, the Early voltage.

In the active region this is described by

IC = IS eqVBE/kT (1 + VCE/VA), ro = ΔVCE/ΔIC ≈ VA/IC

Where:

- IC = collector current (A); IS = saturation current (A)

- VBE = base–emitter voltage (V); kT/q = 0.0259 V at 300 K

- VCE = collector–emitter voltage (V)

- VA = Early voltage, typically 50–200 V (V)

- ro = small-signal output resistance (Ω)

A large VA (flat output curves) means a high output resistance, so the transistor is a better current source and an amplifier stage can have a higher voltage gain. A lightly doped base, which the collector depletion region can push into easily, gives a smaller VA.

#### Example 13.4: Early voltage and output resistance from the output curve

Question. With the base current held constant, an NPN transistor carries IC = 2.00 mA at VCE = 2 V and IC = 2.10 mA at VCE = 7 V. Find its output resistance and Early voltage, and predict IC at VCE = 12 V.

Given: IC = 2.00 mA at 2 V, 2.10 mA at 7 V, same base drive.

Find: ro, VA and IC at 12 V.

Formula:

ro = ΔVCE/ΔIC, VA = IC/(slope) − VCE (the extrapolated line meets IC = 0 at VCE = −VA)

Solution.

Step 1. Slope of the output curve and output resistance:

slope = ΔIC/ΔVCE = (2.10 − 2.00) mA / (7 − 2) V = 0.02 mA/V
ro = 1/slope = 1/(2×10−5 A/V) = 50 kΩ

Step 2. Extrapolate the straight line back to IC = 0:

IC = 2.00 mA + 0.02 mA/V × (VCE − 2 V) = 0 ⇒ VCE = 2 − 100 = −98 V
VA = 98 V

Step 3. Current at 12 V (same straight line):

IC(12 V) = 2.00 + 0.02 × (12 − 2) = 2.20 mA

Check: VA/IC = 98 V / 2 mA = 49 kΩ, close to the measured ro (the small difference is because the exact relation is ro = (VA + VCE)/IC).

Answer: ro = 50 kΩ, VA ≈ 98 V, IC ≈ 2.20 mA at 12 V.

What this means: raising VCE sixfold, from 2 V to 12 V, raises IC by only 10 %, so the collector behaves almost like an ideal current source. The finite 50 kΩ output resistance is what limits the voltage gain of a single-transistor amplifier.

## 13.13 Summary of Week 13

- A BJT uses two p-n junctions and three semiconductor regions (emitter, base, collector).

- In forward-active operation the E–B junction is forward biased and the C–B junction reverse biased.

- The thin base lets most injected minority carriers reach the collector; their profile across the base is nearly a straight line.

- Emitter injection efficiency γ measures the desired carrier injection relative to the total emitter current.

- Base transport factor αT measures the fraction of injected carriers that cross the base without recombining.

- α = IC/IE ≈ γαT is the common-base gain; β = IC/IB is the common-emitter gain.

- The key relationship is β = α/(1 − α).

## Review questions, Week 13, solved

### 1. Define a BJT and explain why it is called a bipolar device.

A bipolar junction transistor is a three-terminal semiconductor device consisting of two p-n junctions formed by three alternately doped regions, emitter, base and collector, arranged as NPN or PNP. A small base current (or base–emitter voltage) controls a much larger collector current, so it can amplify and switch. It is called bipolar because current is carried by both kinds of carrier: in an NPN, electrons carry the main emitter-to-collector current while holes carry the base current (recombination in the base and injection into the emitter). In contrast, a MOSFET is unipolar: its channel current is carried by one carrier type only.

### 2. Draw and label an NPN transistor and indicate the direction of conventional current and electron flow.

Draw three blocks side by side: n+ emitter | p base | n collector, with terminal leads E, B and C. Mark the E–B junction "forward biased" (base positive with respect to emitter, VBE ≈ 0.7 V) and the C–B junction "reverse biased" (collector positive with respect to base).

- Electron flow: from the emitter, through the thin base, into the collector (left to right). A small number recombine with holes in the base; the holes they use up flow in through the base lead.

- Conventional current: opposite to electron flow. IC flows into the collector, IB flows into the base, and IE = IC + IB flows out of the emitter. In the circuit symbol, the arrow on the emitter points outwards for an NPN, showing the direction of conventional emitter current.

### 3. Explain the operation of a BJT in the forward-active region.

With the E–B junction forward biased, the emitter barrier is lowered and the heavily doped n+ emitter injects a large number of electrons into the p-type base, where they become minority carriers with concentration nB(0) = np0eqVBE/kT at the emitter edge. The reverse-biased collector holds the electron concentration at the collector edge of the base at almost zero. The resulting nearly linear concentration gradient makes the electrons diffuse across the thin base. Since the base is much thinner than the diffusion length, only a small fraction recombine. On reaching the C–B depletion region, the electrons are swept into the collector by its electric field, forming the collector current IC = αIE. The base supplies holes to replace those lost in recombination and those injected into the emitter, which is the small base current IB = IC/β. Because IC depends on VBE but hardly on VCB, the transistor acts as a controlled current source, which allows amplification.

### 4. What is emitter injection efficiency? Why should it be close to unity?

Emitter injection efficiency γ = IE,n/(IE,n + IE,p) is the fraction of the emitter current carried by carriers injected from the emitter into the base (electrons in an NPN), rather than by carriers injected from the base back into the emitter (holes). It should be close to unity because only the injected electrons can reach the collector and form useful output current; the back-injected holes simply add to the base current without contributing to IC. Since α ≈ γαT and β = α/(1 − α), even a small reduction of γ below 1 sharply reduces the current gain. γ is made close to 1 by doping the emitter much more heavily than the base.

### 5. Define the base transport factor and state two factors that affect it.

The base transport factor αT = IC,n/IE,n is the fraction of minority carriers injected into the base that cross it without recombining and reach the collector. It is approximately αT ≈ 1 − WB2/(2Ln2). Factors that affect it (any two):

- Base width WB: a thinner base gives fewer recombinations and a higher αT.

- Minority-carrier lifetime τn in the base: a longer lifetime (fewer traps, cleaner material) increases Ln and αT.

- Minority-carrier diffusion coefficient Dn: faster diffusion means less time in the base and higher αT.

- Base doping: heavier doping shortens lifetime and lowers mobility, reducing αT.

### 6. Derive β = α/(1 − α) from the definitions of α and β.

Definitions: α = IC/IE and β = IC/IB. By Kirchhoff's current law, IE = IC + IB.

α = IC/IE = IC/(IC + IB)

Dividing numerator and denominator by IB:

α = (IC/IB)/(IC/IB + 1) = β/(β + 1)

Rearranging: α(β + 1) = β ⇒ αβ + α = β ⇒ α = β − αβ = β(1 − α), so

β = α/(1 − α)

### 7. A transistor has IE = 12 mA and IC = 11.76 mA. Calculate α, IB and β.

Question. A transistor has IE = 12 mA and IC = 11.76 mA. Calculate α, IB and β.

Given: IE = 12 mA, IC = 11.76 mA.

Find: α, IB, β.

Formula:

α = IC/IE, IB = IE − IC, β = IC/IB

Solution.

α = IC/IE = 11.76/12 = 0.98
IB = IE − IC = 12 − 11.76 = 0.24 mA
β = IC/IB = 11.76/0.24 = 49

Check: α/(1 − α) = 0.98/0.02 = 49. ✓

Answer: α = 0.98, IB = 0.24 mA, β = 49.

What this means: a base current of a quarter of a milliamp controls almost 12 mA; any two of the three currents fix the third, and α and β always satisfy β = α/(1 − α).

### 8. Explain the difference between cut-off, active and saturation regions.

|  | Cut-off | Forward active | Saturation |
| --- | --- | --- | --- |
| E–B junction | Reverse (or zero) biased | Forward biased | Forward biased |
| C–B junction | Reverse biased | Reverse biased | Forward biased |
| Currents | IB ≈ 0, IC ≈ 0 (leakage only) | IC = βIB | IC < βIB; IC set by the external circuit |
| VCE | Large (≈ supply voltage) | Intermediate | Small, VCE(sat) ≈ 0.1–0.3 V |
| Behaves as | Open switch (OFF) | Current-controlled current source | Closed switch (ON) |
| Use | Digital OFF state | Amplifiers | Digital ON state |

In cut-off there is no injection, so no carriers cross the base. In the active region the collector collects all carriers that arrive, independently of its voltage. In saturation the collector junction is also forward biased and starts injecting carriers back into the base, so the collector current can no longer rise with base current; the transistor is fully ON.

## Practice questions

These extra questions practise this week's ideas. Work each one on paper before reading the solution; the calculation questions follow the same Question, Given, Find, Solution, Answer layout as the worked examples.

#### Practice 13.1: currents from β

Question. A transistor has β = 80 and IC = 4 mA. Find IB, IE and α.

Given: β = 80, IC = 4 mA.

Find: IB, IE, α.

Solution.

IB = IC/β = 4/80 = 0.05 mA = 50 μA
IE = IC + IB = 4.05 mA
α = β/(β + 1) = 80/81 = 0.988

Answer: IB = 50 μA, IE = 4.05 mA, α = 0.988.

#### Practice 13.2: from doping to gain

Question. An NPN transistor has NE = 5×1018 cm−3, NB = 5×1016 cm−3, equal emitter and base widths, DE = 3 cm2/s and DB = 20 cm2/s. Its base transport factor is 0.995. Find γ, α and β.

Given: NE, NB, DE, DB above, WE = WB, αT = 0.995.

Find: γ, α, β.

Solution.

DENBWB/(DBNEWE) = (3 × 5×1016)/(20 × 5×1018) = 1.5×10−3
γ = 1/(1 + 1.5×10−3) = 0.9985
α = γαT = 0.9985 × 0.995 = 0.9935
β = α/(1 − α) = 0.9935/0.0065 = 153

Answer: γ = 0.9985, α = 0.9935, β ≈ 153.

What this means: the recombination loss in the base (0.5 %) is more than three times the back-injection loss (0.15 %), so here a thinner base or a longer lifetime would raise β most.

#### Practice 13.3: base transport factor

Question. A BJT has a base width of 1 μm and an electron diffusion length in the base of 10 μm. Find αT. What base width would give αT = 0.999?

Given: WB = 1 μm, Ln = 10 μm.

Find: αT, and WB for αT = 0.999.

Solution.

αT = 1 − WB2/(2Ln2) = 1 − 1/(2 × 100) = 0.995
For 0.999: WB2/(2Ln2) = 0.001 ⇒ WB = Ln√0.002 = 10 × 0.0447 = 0.45 μm

Answer: αT = 0.995; a 0.45 μm base gives 0.999.

#### Practice 13.4: collector current and VBE

Question. A transistor has IS = 1×10−15 A. Find IC at VBE = 0.70 V, and the VBE needed for IC = 5 mA.

Given: IS = 10−15 A, kT/q = 0.0259 V.

Find: IC(0.70 V) and VBE(5 mA).

Solution.

IC = IS eVBE/0.0259 = 10−15 × e27.03 = 10−15 × 5.5×1011 = 0.55 mA
VBE = 0.0259 ln(5×10−3/10−15) = 0.0259 × 29.24 = 0.757 V

Answer: IC = 0.55 mA at 0.70 V; VBE = 0.76 V for 5 mA.

What this means: a ninefold rise in current needs only about 57 mV more on the base, the familiar 60 mV per decade of a BJT.

#### Practice 13.5: the Early effect

Question. A transistor has an Early voltage of 100 V and IC = 1 mA at VCE = 5 V. Find its output resistance and IC at VCE = 10 V (same base drive).

Given: VA = 100 V, IC(5 V) = 1 mA.

Find: ro and IC(10 V).

Solution.

ro = VA/IC = 100/10−3 = 100 kΩ
IC(10 V) = IC(5 V) × (1 + 10/100)/(1 + 5/100) = 1 × 1.10/1.05 = 1.048 mA

Answer: ro = 100 kΩ; IC rises to 1.05 mA.

#### Practice 13.6: base transit time

Question. An NPN transistor has a 0.2 μm base and Dn = 20 cm2/s. Find the base transit time and the upper limit it places on fT.

Given: WB = 2×10−5 cm, Dn = 20 cm2/s.

Find: τB and fT.

Solution.

τB = WB2/(2Dn) = (2×10−5)2/40 = 1×10−11 s
fT ≲ 1/(2πτB) = 1.6×1010 Hz

Answer: τB = 10 ps, fT up to about 16 GHz. Thin bases make fast transistors.

#### Practice 13.7: why the reverse-active gain is poor

Question. Explain why a BJT has a much lower current gain in the reverse-active mode.

Answer. In reverse-active mode the collector acts as the emitter. But the collector is only moderately (lightly) doped and much larger, while the base is more heavily doped than it. The injection efficiency is therefore poor (the base injects many holes back into the collector), and the collector-side geometry collects carriers badly. The result is a reverse β of typically only 1–5.

## Objectives check

Use this table to confirm you have met this week's objectives. Cover the Answer column and answer each check question from memory. If you cannot, go back to the section in the last column before moving on.

| # | Objective | Check yourself | Answer | Where it is taught |
| --- | --- | --- | --- | --- |
| 1 | Explain the structure and operating principle of NPN and PNP transistors. | Why is the base made very thin? | So that injected carriers cross it before they recombine. | 13.1–13.2; NPN vs PNP table |
| 2 | Describe injection, diffusion, recombination and collection in the forward-active region. | Which junction is forward biased in forward-active operation? | The emitter–base junction (collector–base is reverse biased). | 13.2 |
| 3 | Sketch and explain the minority-carrier profiles. | What shape is the electron profile in a thin base, and what does its slope set? | Almost a straight line; its slope sets the collector current. | 13.3; 13.8 (IC = IS eqVBE/kT) |
| 4 | Define emitter injection efficiency and base transport factor. | How is γ made close to 1? | By doping the emitter much more heavily than the base. | 13.4–13.5; Example 13.2 |
| 5 | Derive α and β and relate them to γ and αT. | Write β in terms of α. | β = α/(1 − α). | 13.6–13.8 |
| 6 | Solve problems on transistor currents and gains. | β = 100, IC = 5 mA: find IB and IE. | IB = 50 μA, IE = 5.05 mA. | Examples 13.1–13.4; worked examples 1–4; review Q7 |

Week 14 · Module 5 · Advanced Device Technology

# Field-Effect Transistors (MOSFETs)

Plan: ideal MOS capacitor physics (accumulation, depletion, inversion); MOSFET threshold voltage; linear and saturation operating regions. This page follows your lecturer's note (sections 14.1–14.17) and solves its review questions 9–17.

## Learning objectives

By the end of this week you should be able to:

- Describe the structure of an ideal MOS capacitor and calculate Cox.

- Explain accumulation, depletion and inversion.

- Explain how a MOS capacitor becomes a MOSFET, and enhancement versus depletion mode.

- Define the threshold voltage and calculate it.

- Determine the operating region and calculate drain current.

- Compare BJTs and MOSFETs.

## Symbols and abbreviations used this week

Every symbol, constant and abbreviation on this page is listed here, even if an earlier week already defined it, so you can study this page on its own.

Constants and units

| Symbol | Meaning | Units / typical value |
| --- | --- | --- |
| q | Magnitude of the electronic charge | 1.6×10−19 C |
| k | Boltzmann constant | 8.617×10−5 eV/K = 1.381×10−23 J/K |
| kT | Thermal energy | 0.0259 eV (often 0.02585 eV) at 300 K |
| kT/q | Thermal voltage | 0.0259 V (about 26 mV) at 300 K |
| ε0 | Permittivity of free space | 8.854×10−14 F/cm |
| εs (εsi) | Permittivity of silicon, 11.7ε0 | 1.04×10−12 F/cm |
| εox | Permittivity of SiO2, 3.9ε0 | 3.45×10−13 F/cm |
| εr | Relative permittivity (dielectric constant) | Si 11.7, SiO2 3.9, GaAs 12.9 |
| μm | Micrometre (micron) | 1 μm = 10−4 cm = 10−6 m |

Symbols

| Symbol | Meaning | Units / typical value |
| --- | --- | --- |
| Ev (EV) | Energy of the top of the valence band | eV |
| EF | Fermi level: the energy at which a state has a 50 % chance of being occupied | eV |
| Ei | Intrinsic Fermi level, close to mid-gap | eV |
| ni | Intrinsic carrier concentration (n = p = ni in pure material) | cm−3; Si ≈ 1×1010 at 300 K |
| ND | Donor concentration | cm−3 |
| NA | Acceptor concentration | cm−3 |
| ψ | Wave function (¦ψ¦2 is the probability density) | — |
| λ | Wavelength | μm or nm; λ(μm) = 1.24/E(eV) |
| μ, μn, μp | Mobility: drift velocity per unit field (electrons, holes) | cm2/(V·s); Si μn 1350, μp 480 |
| G, GL | Generation rate of electron–hole pairs (GL: by light) | cm−3s−1 |
| S | Surface recombination velocity | cm/s |
| W | Depletion-region width (in Week 13 WB, WE are base and emitter widths; in Week 14 W is channel width) | μm or cm |
| A (area) | Device or contact area | cm2 |
| IE, IB, IC | Emitter, base and collector currents | A (mA) |
| α | Common-base current gain, IC/IE | dimensionless; 0.98–0.999 |
| β | Common-emitter current gain, IC/IB (also hFE) | dimensionless; 50–500 |
| γ (BJT) | Emitter injection efficiency | dimensionless, close to 1 |
| ro | Output resistance | Ω |
| Cox | Gate-oxide capacitance per unit area, εox/tox | F/cm2 |
| tox | Gate-oxide thickness | nm |
| φF, ψs (φs) | Bulk Fermi potential (kT/q)ln(NA/ni); surface potential (band bending) | V |
| Wd, Wdmax, Qdmax | MOS depletion width, its maximum at inversion, and the depletion charge then | μm; C/cm2 |
| VT (Vth) | Threshold voltage of a MOSFET | V |
| VFB | Flat-band voltage | V |
| Φms, Qf | Gate–substrate work-function difference; fixed oxide charge | V; C/cm2 |
| γ (MOSFET) | Body-effect coefficient √(2qεsiNA)/Cox | V1/2 |
| VGS, VDS, VSB, VG | Gate–source, drain–source, source–body and gate voltages | V |
| ID | Drain current | A (mA) |
| W/L | Channel width-to-length ratio | dimensionless |
| gm | Transconductance, ∂ID/∂VGS | S (A/V) |
| k (MOSFET) | Device parameter μnCox(W/L) | A/V2 (mA/V2) |
| λ (MOSFET) | Channel-length modulation parameter | V−1 |
| ΔVT | Shift in threshold voltage (e.g. from body bias) | V |

Abbreviations

| Abbreviation | Meaning |
| --- | --- |
| Si | Silicon |
| SiO2 | Silicon dioxide (silica), the oxide insulator |
| MOS | Metal–oxide–semiconductor |
| MOSFET | Metal–oxide–semiconductor field-effect transistor |
| CMOS | Complementary MOS (n- and p-channel MOSFETs together) |
| BJT | Bipolar junction transistor |
| RF | Radio frequency |
| DC | Direct current (steady) |
| n+ | Very heavily doped n-type (similarly p+) |

## Key terms

Every important word used this week is defined here, so you can read this week on its own.

Electron and hole. The two kinds of mobile charge in a semiconductor. A free electron (negative) moves in the conduction band; a hole (positive) is an empty electron place in the valence band that moves like a positive particle.

Doping (NA, ND). Adding a small, controlled amount of impurity atoms to a pure semiconductor. Acceptor atoms (concentration NA, e.g. boron in Si) give p-type material with many holes; donor atoms (ND, e.g. phosphorus) give n-type material with many electrons.

Majority and minority carriers. The majority carriers are the more numerous kind of mobile charge in a doped region (holes in p-type); the minority carriers are the far fewer other kind (electrons in p-type).

Why it matters: the MOSFET channel on a p-type substrate is made of minority electrons pulled to the surface by the gate.

Fermi level (EF) and intrinsic level (Ei). The Fermi level is the energy at which a state has a 50 % chance of being occupied by an electron; it is flat through a material in equilibrium. The intrinsic level Ei is where EF would sit in undoped material, close to the middle of the band gap. In p-type material EF lies below Ei; in n-type it lies above.

Bulk Fermi potential (φF). How far, in volts, the Fermi level lies below the intrinsic level deep inside a p-type substrate.

φF = (kT/q) ln(NA/ni)

Where:

- φF = bulk Fermi potential (V)

- kT/q = thermal voltage, 0.0259 V at 300 K

- NA = substrate acceptor concentration (cm−3)

- ni = intrinsic carrier concentration, 1×1010 cm−3 for Si at 300 K

Surface potential (ψs). The amount, in volts, by which the energy bands bend at the silicon surface compared with the bulk. The gate voltage controls it.

MOS capacitor. A metal (or polysilicon) gate, a thin insulating oxide (SiO2) and a semiconductor substrate stacked on top of each other. It is a parallel-plate capacitor whose lower "plate" is the silicon surface.

Gate-oxide capacitance (Cox). The capacitance of the oxide layer per unit area: how much charge the gate induces in the silicon per volt.

Cox = εox / tox

Where:

- Cox = oxide capacitance per unit area (F/cm2)

- εox = permittivity of SiO2, 3.45×10−13 F/cm

- tox = oxide thickness (cm; 1 nm = 10−7 cm)

Why it matters: a thinner oxide gives a larger Cox, a lower threshold voltage and more drain current for the same gate voltage.

Accumulation. The state of a MOS capacitor on p-type silicon when the gate is negative: extra holes (majority carriers) are pulled to the surface.

Depletion region (Wd). A layer next to the surface from which the mobile majority carriers have been pushed away, leaving only the fixed charge of ionised dopant atoms. Its thickness is the depletion width Wd.

Inversion and strong inversion. Inversion is the state in which the gate has pulled so many minority electrons to the surface of p-type silicon that the surface behaves as n-type. Strong inversion is reached when the surface is as n-type as the bulk is p-type, which happens when ψs = 2φF.

Flat-band voltage (VFB). The gate voltage that makes the energy bands flat right up to the surface (no band bending, no surface charge). It is zero for an ideal MOS capacitor.

VFB = Φms − Qf/Cox

Where:

- VFB = flat-band voltage (V)

- Φms = work-function difference between gate and substrate (V)

- Qf = fixed positive charge in the oxide, per unit area (C/cm2)

- Cox = oxide capacitance per unit area (F/cm2)

Threshold voltage (VT). The gate-to-source voltage at which strong inversion starts, so that a conducting channel joins source and drain and the transistor begins to turn on.

Why it matters: every MOSFET current formula is written in terms of how far VGS is above VT.

MOSFET (source, drain, gate, channel). A metal–oxide–semiconductor field-effect transistor: a MOS capacitor with two heavily doped regions, the source and the drain, at either side of the gate. The inversion layer under the gate is the channel that carries current between them; the gate voltage controls it through an electric field, with no DC gate current.

Enhancement and depletion mode. An enhancement-mode MOSFET has no channel at VGS = 0 and needs a gate voltage beyond VT to create one. A depletion-mode MOSFET is built with a channel already present at VGS = 0 and needs a gate voltage of the opposite sign to remove it.

Pinch-off and saturation. Pinch-off is the point, at VDS = VGS − VT, where the channel charge at the drain end falls to zero. For larger VDS the transistor is in saturation: the drain current stays almost constant, set by VGS alone.

Transconductance (gm). The change in drain current per unit change in gate voltage, gm = ∂ID/∂VGS, in siemens (A/V). It measures how good the transistor is as an amplifier.

Body effect. The rise in threshold voltage that occurs when the source is at a higher voltage than the substrate (body), because a wider depletion region must then be supported before inversion.

## The big picture

A BJT is controlled by a current. A MOSFET is controlled by a voltage, and the control works through an electric field, without any current flowing into the control terminal.

The idea: put a metal plate (the gate) just above the silicon surface, separated by a very thin insulator. Put a positive voltage on the plate, and it attracts electrons to the silicon surface just beneath it, the same way a charged comb attracts bits of paper. With enough voltage, those electrons form a thin conducting sheet, a channel, connecting two contacts (source and drain). Remove the voltage and the channel disappears. The gate switches the channel on and off, and nothing flows into the gate. That is why billions of MOSFETs can sit on one chip without melting it.

## 14.1 Introduction to MOSFETs

A metal-oxide-semiconductor field-effect transistor (MOSFET) is a voltage-controlled semiconductor device. The gate voltage controls the conductivity of a channel between the source and drain terminals. The gate is separated from the semiconductor by a thin insulating oxide layer, so ideally the DC gate current is essentially zero.

The basic MOS structure is:

gate (metal or polysilicon) / oxide (SiO2 insulator) / semiconductor substrate

In an n-channel MOSFET the substrate is normally p-type, and an electron inversion layer forms when the gate voltage is sufficiently positive. In a p-channel MOSFET the polarities are reversed: n-type substrate, hole inversion layer, negative gate voltage.

## 14.2 The ideal MOS capacitor

A MOS capacitor can be viewed as a parallel-plate capacitor: one plate is the gate, the other is the semiconductor surface, and the oxide is the dielectric between them. The gate voltage creates an electric field through the oxide and changes the distribution of charge near the semiconductor surface.

Cox = εox / tox

| Symbol | Meaning |
| --- | --- |
| Cox | oxide capacitance per unit area (F/cm2) |
| εox | oxide permittivity, εox = εr ε0 with εr ≈ 3.9 for SiO2: εox = 3.45×10−13 F/cm |
| tox | oxide thickness (cm; 1 nm = 10−7 cm) |

A thinner oxide gives a larger capacitance per unit area, so the same gate voltage induces more charge: stronger electrostatic control of the channel. For tox = 10 nm = 10−6 cm, Cox = 3.45×10−13/10−6 = 3.45×10−7 F/cm2.

"Ideal" means: no charge trapped in the oxide, no trap states at the interface, no difference between the gate and semiconductor work functions, and an oxide that conducts no current at all.

For the p-type substrate we also need the bulk Fermi potential φF, which is how far the Fermi level lies below the intrinsic level in the bulk (from Week 5, Ei − EF = kT ln(NA/ni)):

φF = (kT/q) ln(NA/ni)

Where:

- φF = bulk Fermi potential (V)

- kT/q = thermal voltage, 0.0259 V at 300 K

- NA = substrate acceptor concentration (cm−3)

- ni = intrinsic carrier concentration, 1×1010 cm−3 for Si at 300 K

For NA = 1017 cm−3: φF = 0.0259 ln(107) = 0.417 V.

## 14.3 Accumulation

Take a p-type silicon substrate and apply a negative gate voltage relative to it. The negative gate attracts the positive majority carriers, holes, towards the semiconductor–oxide interface. The surface now contains more holes than it does in equilibrium. This is accumulation.

- p-type substrate + negative gate voltage → hole accumulation.

- The surface majority-carrier concentration increases.

- The surface becomes more strongly p-type.

- In the band diagram the bands bend upward at the surface (Ev moves closer to EF).

## 14.4 Depletion

Apply a small positive gate voltage. Holes are now repelled from the surface. The region near the oxide is depleted of mobile majority carriers. What remains is the fixed negative charge of the ionised acceptor atoms, which cannot move. This is the depletion region.

- p-type substrate + moderately positive gate voltage → depletion.

- Mobile holes are pushed away from the surface.

- A negative space-charge region of ionised acceptors remains, of width Wd.

- The bands bend downward at the surface by the surface potential ψs.

The depletion width grows with the band bending:

Wd = √( 2εsi ψs / qNA )

Where:

- Wd = depletion width below the oxide (cm)

- εsi = permittivity of silicon, 1.04×10−12 F/cm

- ψs = surface potential: the band bending at the surface (V)

- q = electronic charge, 1.6×10−19 C

- NA = substrate acceptor concentration (cm−3)

## 14.5 Inversion

As the positive gate voltage is increased further, the surface potential becomes positive enough to attract electrons (the minority carriers of the p-type substrate) towards the surface. When the electron concentration at the surface becomes large enough that the surface behaves as n-type, the semiconductor is said to be inverted. This is inversion.

For an ideal p-type substrate, strong inversion is conventionally defined as the point where the surface is as strongly n-type as the bulk is p-type. That happens when the band bending is twice the bulk Fermi potential:

ψs ≈ 2φF

Why 2φF? In the bulk, EF is φF below Ei. Bending the bands down by φF brings Ei down to EF (the surface is intrinsic). Bending by another φF puts Ei φF below EF, which is exactly the mirror image of the bulk: n-type to the same degree.

Once strong inversion is reached, the depletion width stops growing at its maximum

Wdmax = √( 4εsi φF / qNA )

Where:

- Wdmax = maximum depletion width, reached at strong inversion (cm)

- εsi = permittivity of silicon, 1.04×10−12 F/cm

- φF = bulk Fermi potential (V)

- q = electronic charge, 1.6×10−19 C

- NA = substrate acceptor concentration (cm−3)

and any further gate voltage simply adds electrons to the inversion layer. This electron layer is the channel of the MOSFET.

The exact sign conventions for φF and ψs differ between textbooks. The physical idea is what matters: the gate field first depletes the surface, then attracts minority carriers until an inversion layer forms.

Band diagrams of an ideal MOS capacitor on p-type silicon. Accumulation: bands bend up and holes gather at the surface. Depletion: bands bend down and holes are pushed away, leaving negative acceptor ions. Inversion: the bands bend so far that the surface becomes n-type.

#### Example 14.1: oxide capacitance and maximum depletion width

Question. A MOS capacitor has a 7 nm SiO2 gate oxide on p-type silicon with NA = 1×1016 cm−3. At 300 K find (a) the oxide capacitance per unit area, (b) the bulk Fermi potential, (c) the maximum depletion width at strong inversion and (d) the depletion charge per unit area then.

Given: tox = 7 nm = 7×10−7 cm, NA = 1×1016 cm−3, εox = 3.45×10−13 F/cm, εsi = 1.04×10−12 F/cm, ni = 1010 cm−3, kT/q = 0.0259 V, q = 1.6×10−19 C.

Find: Cox, φF, Wdmax and Qdmax.

Formula:

Cox = εox/tox, φF = (kT/q) ln(NA/ni), Wdmax = √(4εsiφF/qNA), |Qdmax| = qNAWdmax

Solution.

Step 1. Oxide capacitance:

Cox = 3.45×10−13 / 7×10−7 = 4.93×10−7 F/cm2

Step 2. Bulk Fermi potential:

φF = 0.0259 ln(1016/1010) = 0.0259 × 13.82 = 0.358 V

Step 3. Maximum depletion width:

Wdmax = √(4 × 1.04×10−12 × 0.358 / (1.6×10−19 × 1016)) = 3.05×10−5 cm = 0.305 μm

Step 4. Depletion charge at strong inversion:

|Qdmax| = 1.6×10−19 × 1016 × 3.05×10−5 = 4.88×10−8 C/cm2

Answer: Cox = 4.93×10−7 F/cm2, φF = 0.358 V, Wdmax = 0.305 μm, |Qdmax| = 4.88×10−8 C/cm2.

What this means: the depletion layer under the gate never grows beyond about 0.3 μm, roughly 40 times the oxide thickness. Holding up its charge needs only |Qdmax|/Cox ≈ 0.10 V across this thin oxide, so on a lightly doped substrate most of the threshold voltage goes into band bending (2φF = 0.72 V) rather than into the depletion charge.

## 14.6 From MOS capacitor to MOSFET

In an n-channel enhancement MOSFET, two heavily doped n+ regions form the source and drain inside a p-type substrate. The gate lies above the region between them, which has length L (channel length) and width W.

- With VGS below threshold there is no channel. Source and drain are two n+ islands in p-type silicon, i.e. two back-to-back p-n junctions: no current flows.

- With a sufficiently positive gate-to-source voltage, an electron inversion channel forms and connects source to drain.

- Applying a drain-to-source voltage VDS then makes electrons drift from source to drain. Conventional drain current flows from drain to source.

The gate voltage controls whether the channel exists and how strongly it conducts. This is the fundamental reason the MOSFET is a field-effect device.

Enhancement and depletion mode. In an enhancement-mode device (the normal kind) there is no channel at VGS = 0; a gate voltage above VT must be applied to create (enhance) one. A depletion-mode device is built with a channel already present at VGS = 0 (by doping the surface n-type); a negative gate voltage is needed to remove (deplete) it, so its VT is negative.

The same two choices exist for p-channel devices, with every polarity reversed. The four kinds of MOSFET compare as follows:

| Feature | n-channel enhancement | n-channel depletion | p-channel enhancement | p-channel depletion |
| --- | --- | --- | --- | --- |
| Substrate (body) | p-type | p-type | n-type | n-type |
| Source and drain | n+ | n+ | p+ | p+ |
| Channel carriers | Electrons | Electrons | Holes | Holes |
| Channel at VGS = 0? | No (normally off) | Yes (normally on) | No (normally off) | Yes (normally on) |
| Sign of VT | Positive | Negative | Negative | Positive |
| Gate voltage to turn on harder | More positive | More positive | More negative | More negative |
| Normal sign of VDS | Positive | Positive | Negative | Negative |
| Typical use | Digital logic (CMOS), switches, amplifiers | Constant-current sources, loads, some RF circuits | Partner of nMOS in CMOS logic | Rare; special analogue circuits |

Because electrons have a higher mobility than holes (1350 against 480 cm2/V·s in bulk Si), an n-channel transistor carries about 2–3 times more current than a p-channel transistor of the same size. That is why the nMOS is the main device, and why pMOS transistors in CMOS logic are drawn wider.

## 14.7 Threshold voltage

The threshold voltage VT is the gate-to-source voltage at which a strong inversion channel forms and significant conduction begins in an enhancement-mode MOSFET.

A commonly used long-channel expression for an ideal nMOS is:

VT = VFB + 2φF + γ √(2φF)

with the body-effect coefficient

γ = √(2qεsi NA) / Cox

| Symbol | Meaning |
| --- | --- |
| VT | threshold voltage (V) |
| VFB | flat-band voltage: the gate voltage that makes the bands flat; zero for an ideal MOS, VFB = Φms − Qf/Cox in a real one (V) |
| 2φF | the band bending needed for strong inversion (V) |
| γ | body-effect coefficient (V1/2) |
| γ√(2φF) | the voltage dropped across the oxide to support the depletion charge, ¦Qdmax¦/Cox (V) |
| q | electronic charge, 1.6×10−19 C |
| NA | substrate acceptor concentration (cm−3) |
| εsi | silicon permittivity, 11.7ε0 = 1.04×10−12 F/cm |
| Cox | oxide capacitance per unit area, εox/tox (F/cm2) |

Reading the formula. The gate voltage has three jobs: get to flat bands (VFB), bend the bands by 2φF, and hold up the charge of the depletion region across the oxide. Heavier substrate doping raises both φF and the depletion charge, so VT rises. A thinner oxide (larger Cox) lowers VT.

(This γ is not the same as the emitter injection efficiency γ of Week 13; the same Greek letter is used for different things.)

For simplified ideal MOSFET problems, the threshold voltage may simply be given. Always use the convention and parameters supplied in the question.

#### Example 14.2: calculating the threshold voltage

Question. An n-channel MOSFET is built on p-type silicon with NA = 1×1017 cm−3, a 10 nm SiO2 gate oxide and an n+ polysilicon gate, for which VFB = −0.98 V. There is no oxide charge. Calculate the threshold voltage at 300 K.

Given: NA = 1×1017 cm−3, tox = 10 nm = 1×10−6 cm, VFB = −0.98 V, εox = 3.45×10−13 F/cm, εsi = 1.04×10−12 F/cm, ni = 1010 cm−3, kT/q = 0.0259 V.

Find: the threshold voltage VT.

Formula:

VT = VFB + 2φF + γ√(2φF), φF = (kT/q) ln(NA/ni), γ = √(2qεsiNA)/Cox, Cox = εox/tox

Solution.

Step 1. Bulk Fermi potential:

φF = 0.0259 ln(1017/1010) = 0.417 V, 2φF = 0.834 V

Step 2. Oxide capacitance:

Cox = 3.45×10−13 / 10−6 = 3.45×10−7 F/cm2

Step 3. Body-effect coefficient:

γ = √(2 × 1.6×10−19 × 1.04×10−12 × 1017) / 3.45×10−7 = 1.824×10−7 / 3.45×10−7 = 0.529 V1/2

γ√(2φF) = 0.529 × √0.834 = 0.529 × 0.913 = 0.483 V

Step 4. Add the three terms:

VT = −0.98 + 0.834 + 0.483 = 0.34 V

Answer: VT ≈ 0.34 V.

What this means: the band bending (0.83 V) and the depletion charge (0.48 V) together need 1.32 V of gate voltage, but the n+ polysilicon gate's work function supplies −0.98 V of it for free. The result, about 0.3 V, is a typical threshold for a modern low-voltage logic transistor.

Body effect. The formula above assumes the source is at the same voltage as the body (substrate). If the source is raised VSB above the body, the channel must be inverted relative to a source that is VSB higher, so the band bending needed at the surface becomes 2φF + VSB, the depletion region widens and more depletion charge must be supported. The threshold voltage therefore rises:

VT(VSB) = VFB + 2φF + γ√(2φF + VSB), ΔVT = γ[ √(2φF + VSB) − √(2φF) ]

Where:

- VT(VSB) = threshold voltage with source–body bias VSB (V)

- ΔVT = rise in threshold voltage caused by the body bias (V)

- VSB = source-to-body voltage, positive when the source is above the body in an nMOS (V)

- γ = body-effect coefficient √(2qεsiNA)/Cox (V1/2)

- φF = bulk Fermi potential (V); VFB = flat-band voltage (V)

#### Example 14.3: the body effect

Question. The transistor of Example 14.2 is used with its source 1 V above its substrate (VSB = 1 V). Find its new threshold voltage.

Given: VT(0) = 0.338 V, γ = 0.529 V1/2, 2φF = 0.834 V, VSB = 1 V.

Find: ΔVT and VT(VSB = 1 V).

Formula:

ΔVT = γ[ √(2φF + VSB) − √(2φF) ]

Solution.

Step 1. The two square roots:

√(0.834 + 1) = √1.834 = 1.355 V1/2, √0.834 = 0.914 V1/2

Step 2. Rise in threshold:

ΔVT = 0.529 × (1.355 − 0.914) = 0.529 × 0.441 = 0.233 V

Step 3. New threshold:

VT = 0.338 + 0.233 = 0.57 V

Answer: ΔVT ≈ 0.23 V, so VT rises from 0.34 V to about 0.57 V.

What this means: a 1 V source–body bias raises the threshold by about two-thirds. In a chip, transistors stacked on top of one another have their sources above ground, so they switch on later and carry less current; designers must allow for this, and a thinner oxide (smaller γ) reduces the effect.

## 14.8 MOSFET regions of operation

For a long-channel enhancement nMOS transistor, the region depends on VGS compared with VT, and on VDS compared with VGS − VT (called the overdrive voltage).

| Condition | Operating region | Physical condition |
| --- | --- | --- |
| VGS < VT | Cut-off | No strong inversion channel |
| VGS > VT and VDS < VGS − VT | Linear (triode) | Channel exists along the entire length |
| VGS > VT and VDS ≥ VGS − VT | Saturation | Channel pinches off near the drain |

## 14.9 Cut-off region

When VGS ≤ VT, an enhancement nMOS has no strong inversion channel. Ideally the drain current is zero, apart from small leakage:

ID ≈ 0

## 14.10 Linear (triode) region

When VGS > VT and VDS is smaller than VGS − VT, the channel exists all the way from source to drain. The long-channel drain current is:

ID = μn Cox (W/L) [ (VGS − VT) VDS − VDS2/2 ]

| Symbol | Meaning |
| --- | --- |
| ID | drain current (A) |
| μn | electron mobility in the channel (cm2/V·s) |
| Cox | oxide capacitance per unit area (F/cm2) |
| W, L | channel width and length (cm or μm; only their ratio W/L matters) |
| VGS, VDS | gate-to-source and drain-to-source voltages (V) |
| VT | threshold voltage (V) |

Where it comes from (in words). The amount of electron charge in the channel per unit area is Cox × (how far the gate is above threshold). At the source end that is Cox(VGS − VT); at the drain end the channel is at VDS, so the gate is only VGS − VDS above it and the charge is Cox(VGS − VT − VDS). The current is (charge per area) × (width) × (drift velocity μ × field). Adding this up along the channel gives the formula; the −VDS2/2 term is the effect of the channel thinning towards the drain.

For small VDS the VDS2 term is negligible, and

ID ≈ μnCox(W/L)(VGS − VT) VDS

The current is proportional to VDS: the transistor behaves as a voltage-controlled resistor whose resistance is set by the gate.

## 14.11 Saturation region

As VDS is increased, the channel becomes progressively thinner near the drain. When

VDS = VGS − VT

the channel charge at the drain end falls to zero: this is the onset of pinch-off. For larger VDS the device is in saturation. The extra voltage is dropped across a short pinched-off region near the drain, and the current stops rising. Ignoring channel-length modulation:

ID = ½ μn Cox (W/L) (VGS − VT)2

Where:

- ID = saturation drain current (A)

- μn = electron mobility in the channel (cm2/V·s)

- Cox = oxide capacitance per unit area (F/cm2)

- W/L = channel width-to-length ratio (dimensionless)

- VGS = gate-to-source voltage (V)

- VT = threshold voltage (V); VGS − VT is the overdrive voltage

This is one of the most important MOSFET equations for examination calculations. In saturation the current depends on VGS but (ideally) not on VDS: the MOSFET is a voltage-controlled current source, which is what an amplifier needs.

Output characteristics of an n-channel MOSFET. Each curve rises (linear region) until VDS = VGS − VT (dashed line), then flattens (saturation).

## 14.12 Transconductance

In saturation the small-signal transconductance is

gm = ∂ID/∂VGS

For the ideal long-channel saturation equation:

gm = μnCox (W/L)(VGS − VT) = 2ID/(VGS − VT)

Where:

- gm = transconductance (S = A/V)

- μnCox(W/L) = device parameter k (A/V2)

- VGS − VT = overdrive voltage (V)

- ID = saturation drain current at that bias (A)

Transconductance measures how strongly the drain current responds to a small change in gate voltage (unit: siemens, A/V). It plays the role for a MOSFET that β plays for a BJT.

#### Example 14.4: saturation current and transconductance from device data

Question. An n-channel MOSFET has the threshold voltage of Example 14.2 (VT = 0.34 V), the same 10 nm oxide, a channel mobility μn = 400 cm2/V·s and W/L = 10. It is biased at VGS = 1.34 V and VDS = 2 V. Find (a) the device parameter k, (b) the drain current and (c) the transconductance.

Given: VT = 0.34 V, Cox = 3.45×10−7 F/cm2, μn = 400 cm2/V·s, W/L = 10, VGS = 1.34 V, VDS = 2 V.

Find: k, ID and gm.

Formula:

k = μnCox(W/L), ID = ½k(VGS − VT)2, gm = k(VGS − VT) = 2ID/(VGS − VT)

Solution.

Step 1. Device parameter:

k = 400 × 3.45×10−7 × 10 = 1.38×10−3 A/V2 = 1.38 mA/V2

Step 2. Check the region. The overdrive is VGS − VT = 1.34 − 0.34 = 1.0 V, and VDS = 2 V ≥ 1.0 V, so the transistor is in saturation.

Step 3. Drain current:

ID = ½ × 1.38 × (1.0)2 = 0.69 mA

Step 4. Transconductance:

gm = 1.38 × 1.0 = 1.38 mS (check: 2 × 0.69/1.0 = 1.38 mS)

Answer: k = 1.38 mA/V2, ID = 0.69 mA, gm = 1.38 mS.

What this means: a gate change of 10 mV shifts the drain current by about 14 μA (1.38 mS × 10 mV). Note that the channel mobility (400) is much lower than bulk mobility (1350) because electrons in the channel scatter off the rough Si/SiO2 interface; using the bulk value would overestimate the current more than threefold.

## 14.13 Worked example 1: determining the operating region

Question. An nMOS transistor has VT = 1 V, VGS = 3 V and VDS = 1 V. Determine its operating region.

Given: VT = 1 V, VGS = 3 V, VDS = 1 V.

Find: the region of operation.

Formula: cut-off if VGS < VT; linear if VGS > VT and VDS < VGS − VT; saturation if VGS > VT and VDS ≥ VGS − VT.

Solution.

VGS > VT (3 > 1), so a channel exists.
VGS − VT = 3 − 1 = 2 V
VDS = 1 V < 2 V

Answer: The transistor is in the linear (triode) region.

What this means: the channel still reaches all the way from source to drain, so the transistor behaves like a gate-controlled resistor; VDS would have to rise above 2 V before the channel pinches off and the current levels out.

## 14.14 Worked example 2: saturation current

Question. An nMOS transistor has μnCox(W/L) = 2 mA/V2, VT = 1 V and VGS = 4 V. Find the saturation drain current.

Given: k = μnCox(W/L) = 2 mA/V2, VT = 1 V, VGS = 4 V.

Find: ID(sat).

Formula:

ID(sat) = ½ μnCox(W/L)(VGS − VT)2

Solution.

ID = ½ × 2 × (4 − 1)2 mA = 1 × 9 = 9 mA

Answer: ID = 9 mA.

What this means: as long as VDS is at least VGS − VT = 3 V, the drain current stays at about 9 mA whatever the drain voltage; the gate alone sets it, which is what makes the MOSFET useful as a current source and amplifier.

## 14.15 Worked example 3: linear-region current

Question. An nMOS transistor has μnCox(W/L) = 1 mA/V2, VT = 1 V, VGS = 3 V and VDS = 0.5 V. Calculate the drain current.

Given: k = 1 mA/V2, VT = 1 V, VGS = 3 V, VDS = 0.5 V.

Find: ID.

Formula:

ID = μnCox(W/L)[ (VGS − VT)VDS − VDS2/2 ]

Solution.

First check the region: VGS − VT = 2 V > VDS = 0.5 V, so it is linear.

ID = 1 × [ (3 − 1)(0.5) − (0.5)2/2 ] mA = [1 − 0.125] mA = 0.875 mA

Answer: ID = 0.875 mA.

What this means: the channel behaves roughly as a resistor of VDS/ID = 0.5 V/0.875 mA ≈ 570 Ω. The −VDS2/2 term cuts the current by 12.5 % compared with a pure resistor, because the channel is already thinner at the drain end.

## 14.16 Comparison of BJT and MOSFET

| Feature | BJT | MOSFET |
| --- | --- | --- |
| Control | Mainly current-controlled (base current) | Voltage-controlled (gate voltage) |
| Input current | Requires base current | Ideally zero DC gate current |
| Carriers | Electrons and holes (bipolar) | Majority-carrier conduction in the channel (unipolar) |
| Input impedance | Moderate | Very high |
| Typical use | Amplification, switching, analogue | Digital logic, switching, amplification, power |
| Key gain parameter | β or α | gm |

## 14.17 Summary of Week 14

- An ideal MOS capacitor has three electrostatic conditions: accumulation, depletion and inversion.

- On a p-type substrate: negative gate → accumulation; moderate positive gate → depletion; sufficiently positive gate → inversion.

- The MOSFET uses the inversion layer as a controllable channel between source and drain.

- Threshold voltage is the gate voltage at the onset of strong inversion, VT = VFB + 2φF + γ√(2φF).

- For an nMOS enhancement device: VGS < VT gives cut-off; VGS > VT and VDS < VGS − VT gives the linear region; VGS > VT and VDS ≥ VGS − VT gives saturation.

- Linear: ID = μCox(W/L)[(VGS − VT)VDS − VDS2/2]. Saturation: ID = ½μCox(W/L)(VGS − VT)2.

## Review questions, Week 14, solved

### 9. What is a MOS capacitor? Draw and label its basic structure.

A MOS (metal-oxide-semiconductor) capacitor is a three-layer structure in which a conducting gate electrode is separated from a semiconductor substrate by a thin insulating oxide. It acts as a parallel-plate capacitor whose capacitance per unit area is Cox = εox/tox in accumulation; the gate voltage controls the charge at the semiconductor surface.

Sketch (top to bottom): a gate contact (metal or n+ polysilicon) labelled G; a thin layer of SiO2 with thickness tox marked; the p-type Si substrate (doping NA); a metal substrate (body) contact at the bottom labelled B. Mark VG applied between G and B.

### 10. Explain accumulation, depletion and inversion for a p-type silicon substrate.

- Accumulation (VG < 0): the negative gate attracts the majority holes to the oxide–silicon interface. The surface becomes more strongly p-type; the bands bend upward.

- Depletion (small VG > 0): the positive gate repels holes from the surface, leaving a layer of fixed negative acceptor ions of width Wd. There are almost no mobile carriers in this layer; the bands bend downward.

- Inversion (VG > VT): the downward band bending becomes large enough (ψs ≈ 2φF) to attract minority electrons to the surface in large numbers. The surface becomes n-type: an electron inversion layer forms, which is the MOSFET channel. The depletion width stops growing at Wdmax.

### 11. Why is an oxide layer used between the gate and the semiconductor?

- It insulates the gate from the channel, so the gate draws essentially no DC current. This gives the MOSFET its very high input impedance and low power consumption.

- It lets the gate control the surface through the electric field only, as the dielectric of a capacitor. A thin oxide gives a large Cox and strong control.

- SiO2 forms a very clean, stable interface with silicon (few interface traps), so the surface carriers have good mobility and VT is stable.

- It passivates and protects the silicon surface.

### 12. Define threshold voltage.

The threshold voltage VT is the gate-to-source voltage at which the semiconductor surface reaches strong inversion (surface potential ψs ≈ 2φF), so that a conducting inversion channel forms between source and drain and significant drain current begins to flow. For an ideal nMOS, VT = VFB + 2φF + γ√(2φF), with γ = √(2qεsiNA)/Cox.

### 13. State the conditions for cut-off, linear and saturation operation of an nMOS transistor.

- Cut-off: VGS < VT. No channel, ID ≈ 0.

- Linear (triode): VGS > VT and VDS < VGS − VT. ID = μnCox(W/L)[(VGS − VT)VDS − VDS2/2].

- Saturation: VGS > VT and VDS ≥ VGS − VT. ID = ½μnCox(W/L)(VGS − VT)2.

### 14. Derive the condition VDS ≥ VGS − VT for saturation.

Physical argument. An inversion channel exists at a point in the channel only where the gate is more than VT above the local channel voltage. At the source end the channel voltage is 0, so the gate–channel voltage is VGS. At the drain end the channel voltage is VDS, so the gate–channel voltage is VGD = VGS − VDS. The channel at the drain end disappears (pinches off) when this falls to threshold:

VGS − VDS = VT ⇒ VDS = VGS − VT

For any VDS larger than this, the drain end stays pinched off and the device is saturated. Hence saturation requires VDS ≥ VGS − VT.

Mathematical argument. The linear-region equation ID = k[(VGS − VT)VDS − VDS2/2] is a parabola in VDS. Its maximum is where

dID/dVDS = k[(VGS − VT) − VDS] = 0 ⇒ VDS = VGS − VT

Beyond this point the equation would predict a falling current, which does not happen physically; instead the current stays at its maximum value, ID = ½k(VGS − VT)2. So saturation begins at VDS = VGS − VT.

### 15. Calculate the saturation current when μnCox(W/L) = 1.5 mA/V2, VGS = 5 V and VT = 2 V.

Given: k = μnCox(W/L) = 1.5 mA/V2, VGS = 5 V, VT = 2 V (saturation assumed, as the question states).

Find: ID(sat).

Formula:

ID(sat) = ½ μnCox(W/L)(VGS − VT)2

Solution.

ID = ½ × 1.5 × (5 − 2)2 = 0.75 × 9 = 6.75 mA

Answer: ID = 6.75 mA.

What this means: the current grows with the square of the overdrive: with VGS − VT = 3 V it is 6.75 mA, but halving the overdrive to 1.5 V would cut it to a quarter, about 1.7 mA. This holds for any VDS ≥ 3 V.

### 16. Calculate the linear-region current for μnCox(W/L) = 2 mA/V2, VGS = 4 V, VT = 1 V and VDS = 0.8 V.

Given: k = μnCox(W/L) = 2 mA/V2, VGS = 4 V, VT = 1 V, VDS = 0.8 V.

Find: ID.

Formula:

ID = μnCox(W/L)[ (VGS − VT)VDS − VDS2/2 ]

Solution.

Check the region: VGS − VT = 3 V > VDS = 0.8 V, so linear.

ID = 2 × [ (4 − 1)(0.8) − (0.8)2/2 ] = 2 × [2.4 − 0.32] = 2 × 2.08 = 4.16 mA

Answer: ID = 4.16 mA.

What this means: this is well below the 9 mA the same transistor would carry in saturation (½ × 2 × 32), because at VDS = 0.8 V the channel is still open along its whole length and the current is limited by the small drain voltage.

### 17. Compare a BJT and a MOSFET in terms of input impedance and control mechanism.

- Control mechanism. A BJT is current-controlled: the collector current is set by the base current (IC = βIB), or equivalently by the base–emitter voltage through carrier injection across a forward-biased junction. A MOSFET is voltage-controlled: the gate voltage creates an electric field across the oxide that induces the channel charge, with no carrier injection from the gate.

- Input impedance. The BJT's base–emitter junction is forward biased and must be supplied with base current, so its input impedance is moderate (typically kΩ). The MOSFET's gate is insulated by the oxide and draws essentially no DC current, so its input impedance is extremely high (1012 Ω or more), limited only by the gate capacitance at high frequency.

## Practice questions

These extra questions practise this week's ideas. Work each one on paper before reading the solution; the calculation questions follow the same Question, Given, Find, Solution, Answer layout as the worked examples.

#### Practice 14.1: oxide capacitance of a thin gate

Question. Find Cox for a 3 nm SiO2 gate oxide.

Given: tox = 3×10−7 cm, εox = 3.45×10−13 F/cm.

Find: Cox.

Solution.

Cox = εox/tox = 3.45×10−13 / 3×10−7 = 1.15×10−6 F/cm2

Answer: Cox = 1.15 μF/cm2.

#### Practice 14.2: bulk potential and maximum depletion width

Question. For p-type silicon with NA = 5×1016 cm−3, find φF and the maximum depletion width at strong inversion.

Given: NA = 5×1016 cm−3, ni = 1010 cm−3, εsi = 1.04×10−12 F/cm.

Find: φF and Wdmax.

Solution.

φF = 0.0259 ln(5×106) = 0.400 V
Wdmax = √(4εsiφF/qNA) = √(4 × 1.04×10−12 × 0.400 / (1.6×10−19 × 5×1016)) = 1.44×10−5 cm

Answer: φF = 0.40 V, Wdmax = 0.144 μm.

#### Practice 14.3: threshold voltage of an ideal MOSFET

Question. Using the substrate of Practice 14.2 with a 20 nm oxide and an ideal gate (VFB = 0), find the threshold voltage.

Given: φF = 0.400 V, Wdmax = 1.44×10−5 cm, tox = 2×10−6 cm.

Find: VT = VFB + 2φF + qNAWdmax/Cox.

Solution.

Cox = 3.45×10−13/2×10−6 = 1.725×10−7 F/cm2
qNAWdmax = 1.6×10−19 × 5×1016 × 1.44×10−5 = 1.15×10−7 C/cm2
VT = 0 + 0.80 + 1.15×10−7/1.725×10−7 = 0.80 + 0.67 = 1.47 V

Answer: VT ≈ 1.47 V. A thinner oxide or a real n+ poly gate (negative VFB) would lower it.

#### Practice 14.4: current in both regions

Question. An nMOS has μnCox(W/L) = 0.5 mA/V2 and VT = 0.8 V, with VGS = 2.0 V. Find ID at VDS = 0.4 V and at VDS = 2.0 V.

Given: k = 0.5 mA/V2, VT = 0.8 V, VGS = 2.0 V (overdrive 1.2 V).

Find: ID at each VDS.

Solution.

VDS = 0.4 V < 1.2 V → linear: ID = 0.5 × [1.2 × 0.4 − 0.42/2] = 0.5 × 0.40 = 0.20 mA
VDS = 2.0 V ≥ 1.2 V → saturation: ID = ½ × 0.5 × 1.22 = 0.36 mA

Answer: 0.20 mA (linear) and 0.36 mA (saturation).

#### Practice 14.5: transconductance

Question. Find the transconductance of the transistor of Practice 14.4 in saturation.

Given: ID = 0.36 mA, VGS − VT = 1.2 V.

Find: gm.

Solution.

gm = 2ID/(VGS − VT) = 2 × 0.36/1.2 = 0.60 mS
(check: gm = k(VGS − VT) = 0.5 × 1.2 = 0.60 mS)

Answer: gm = 0.60 mS.

#### Practice 14.6: body effect

Question. A MOSFET has γ = 0.5 V1/2 and 2φF = 0.8 V. By how much does its threshold voltage rise when the source is 2 V above the body?

Given: γ = 0.5 V1/2, 2φF = 0.8 V, VSB = 2 V.

Find: ΔVT.

Solution.

ΔVT = γ(√(2φF + VSB) − √(2φF)) = 0.5 × (√2.8 − √0.8) = 0.5 × (1.673 − 0.894) = 0.39 V

Answer: VT rises by 0.39 V.

#### Practice 14.7: sizing a transistor

Question. A MOSFET must carry 1 mA in saturation with an overdrive of 0.5 V. If μnCox = 200 μA/V2, what W/L is needed?

Given: ID = 1 mA, VGS − VT = 0.5 V, μnCox = 200×10−6 A/V2.

Find: W/L.

Solution.

W/L = 2ID / (μnCox (VGS − VT)2) = 2 × 10−3 / (200×10−6 × 0.25) = 40

Answer: W/L = 40.

#### Practice 14.8: channel-length modulation

Question. Why does a real MOSFET's saturation current rise slightly with VDS?

Answer. Beyond pinch-off, increasing VDS moves the pinch-off point slightly towards the source, so the effective channel length becomes L − ΔL. Since ID ∝ 1/L, the current rises a little. This is channel-length modulation, written ID = ID(sat)(1 + λVDS). It is the MOSFET's equivalent of the BJT's Early effect and gives a finite output resistance ro ≈ 1/(λID).

## Objectives check

Use this table to confirm you have met this week's objectives. Cover the Answer column and answer each check question from memory. If you cannot, go back to the section in the last column before moving on.

| # | Objective | Check yourself | Answer | Where it is taught |
| --- | --- | --- | --- | --- |
| 1 | Describe the structure of an ideal MOS capacitor and calculate Cox. | Find Cox for a 5 nm SiO2 layer. | 3.45×10−13/5×10−7 = 6.9×10−7 F/cm2. | 14.2; Example 14.1 |
| 2 | Explain accumulation, depletion and inversion. | On p-type Si, what forms at the surface in inversion? | A layer of electrons (the surface becomes n-type). | 14.3–14.5 |
| 3 | Explain how a MOS capacitor becomes a MOSFET, and enhancement versus depletion mode. | Does an enhancement-mode nMOS conduct at VGS = 0? | No: a gate voltage above VT is needed to create the channel. | 14.6 (table of the four MOSFET types) |
| 4 | Define the threshold voltage and calculate it. | What three contributions make up VT? | VFB, the band bending 2φF, and the depletion-charge term γ√(2φF). | 14.7; Examples 14.2–14.3 |
| 5 | Determine the operating region and calculate drain current. | VT = 1 V, VGS = 2 V, VDS = 3 V: which region? | Saturation (VDS ≥ VGS − VT = 1 V). | 14.8–14.15; Example 14.4 |
| 6 | Compare BJTs and MOSFETs. | Which has the higher input impedance, and why? | The MOSFET: its gate is insulated by the oxide and draws no DC current. | 14.16; review Q17 |

Week 15 · Module 5 · Advanced Device Technology

# Revision and Final Exam Preparation

Plan: overview of the entire curriculum, problem-solving clinic and past-question review. The sections follow the Week 15 headings in your lecturer's note: course overview, formula sheet, problem-solving clinic, past-question style exercises, final examination checklist and comprehensive revision questions.

## Learning objectives

By the end of this week you should be able to:

- Summarise the whole course and how its ideas connect.

- Recall and apply the key formulas.

- Answer definitions, derivations and calculations in examination style.

- Solve mixed past-question style problems.

- Check readiness for the final examination.

## Symbols and abbreviations used this week

Every symbol, constant and abbreviation on this page is listed here, even if an earlier week already defined it, so you can study this page on its own.

Constants and units

| Symbol | Meaning | Units / typical value |
| --- | --- | --- |
| q | Magnitude of the electronic charge | 1.6×10−19 C |
| k | Boltzmann constant | 8.617×10−5 eV/K = 1.381×10−23 J/K |
| kT | Thermal energy | 0.0259 eV (often 0.02585 eV) at 300 K |
| kT/q | Thermal voltage | 0.0259 V (about 26 mV) at 300 K |
| h | Planck constant | 6.626×10−34 J·s |
| ħ | Reduced Planck constant, h/2π | 1.055×10−34 J·s |
| m0 | Free-electron mass | 9.11×10−31 kg |
| ε0 | Permittivity of free space | 8.854×10−14 F/cm |
| εs (εsi) | Permittivity of silicon, 11.7ε0 | 1.04×10−12 F/cm |
| εox | Permittivity of SiO2, 3.9ε0 | 3.45×10−13 F/cm |
| εr | Relative permittivity (dielectric constant) | Si 11.7, SiO2 3.9, GaAs 12.9 |
| eV | Electron-volt, a unit of energy | 1 eV = 1.6×10−19 J |
| Å | Ångström, a unit of length | 1 Å = 10−10 m = 0.1 nm |
| μm | Micrometre (micron) | 1 μm = 10−4 cm = 10−6 m |

Symbols

| Symbol | Meaning | Units / typical value |
| --- | --- | --- |
| Ec (EC) | Energy of the bottom of the conduction band | eV |
| Ev (EV) | Energy of the top of the valence band | eV |
| Eg | Band-gap energy, Ec − Ev | eV; Si 1.12, Ge 0.66, GaAs 1.42 at 300 K |
| EF | Fermi level: the energy at which a state has a 50 % chance of being occupied | eV |
| Ei | Intrinsic Fermi level, close to mid-gap | eV |
| Ea | Activation energy of dopant diffusion | eV; about 3–4 eV |
| f(E) | Fermi–Dirac function: probability that a state at energy E is occupied | dimensionless, 0 to 1 |
| g(E), gc, gv | Density of states: allowed states per unit energy per unit volume | states/(eV·cm3) |
| Nc | Effective density of states in the conduction band | cm−3; Si 2.8×1019 at 300 K |
| Nv | Effective density of states in the valence band | cm−3; Si 1.04×1019 at 300 K |
| n | Electron concentration (free electrons per cm3) | cm−3 |
| p | Hole concentration (holes per cm3) | cm−3 |
| ni | Intrinsic carrier concentration (n = p = ni in pure material) | cm−3; Si ≈ 1×1010 at 300 K |
| ND | Donor concentration | cm−3 |
| NA | Acceptor concentration | cm−3 |
| Δn, Δp | Excess electron and hole concentrations above equilibrium | cm−3 |
| m∗, mn∗, mp∗ | Effective mass of electrons or holes | kg, or as a multiple of m0 |
| ψ | Wave function (¦ψ¦2 is the probability density) | — |
| k (wave vector) | Wave vector, 2π/λ; measures the electron's momentum, p = ħk | m−1 or cm−1 |
| α (Kronig–Penney) | √(2mE)/ħ, set by the electron energy | m−1 |
| P (Kronig–Penney) | Barrier strength mV0ba/ħ2 | dimensionless |
| λ | Wavelength | μm or nm; λ(μm) = 1.24/E(eV) |
| a | Lattice constant: edge length of the cubic unit cell | Å; Si 5.43, Ge and GaAs 5.65 |
| (h k l), {h k l} | Miller indices of a plane; family of equivalent planes | integers |
| dhkl | Spacing between neighbouring (h k l) planes, a/√(h2 + k2 + l2) | Å |
| rnn | Nearest-neighbour distance | Å; Si 2.35 |
| k0 | Segregation coefficient, Cs/Cl at the freezing interface | dimensionless; B 0.8, P 0.35 |
| Cs | Surface concentration of a diffusion (or solid concentration when freezing) | cm−3 |
| Cl, C0 | Concentration in the melt (liquid); C0 at the start | cm−3 |
| C(x, t) | Dopant concentration at depth x and time t | cm−3 |
| D | Diffusion coefficient (dopants in a furnace, or carriers) | cm2/s |
| D0 | Diffusion constant in D = D0e−Ea/kT | cm2/s |
| F | Particle flux in Fick's law | particles/(cm2·s) |
| Q | Dose: dopant atoms per unit area (in Weeks 13–14, Q also means charge) | atoms/cm2 (C or C/cm2 for charge) |
| Φ (dose) | Implanted dose (ions per cm2) | cm−2 |
| erfc | Complementary error function, erfc(u) = 1 − erf(u); read from a table | dimensionless |
| xj | Junction depth: where the dopant concentration equals the background | μm |
| NB (CB) | Background doping of the wafer (in Week 13, NB is the base doping) | cm−3 |
| Rp | Projected range: average depth at which implanted ions stop | μm |
| ΔRp | Straggle: spread of the implanted ions' stopping depths | μm |
| Np | Peak concentration of an implanted profile | cm−3 |
| E (field) | Electric field (on band diagrams, E is energy instead) | V/cm |
| μ, μn, μp | Mobility: drift velocity per unit field (electrons, holes) | cm2/(V·s); Si μn 1350, μp 480 |
| μL, μI | Mobility limited by lattice scattering, by ionised-impurity scattering | cm2/(V·s) |
| vd | Drift velocity | cm/s |
| vsat | Saturation velocity at high field | ≈ 107 cm/s in Si |
| τm | Mean free time between collisions | s; about 0.1–1 ps |
| σ | Conductivity, q(nμn + pμp) (in Week 8, σ is also a capture cross-section) | S/cm (siemens per cm) |
| ρ | Resistivity, 1/σ | Ω·cm |
| J, Jn, Jp | Current density (total, electrons, holes) | A/cm2 |
| Dn, Dp | Diffusion coefficients of electrons and holes | cm2/s; Si 35 and 12.4 |
| G, GL | Generation rate of electron–hole pairs (GL: by light) | cm−3s−1 |
| R | Recombination rate | cm−3s−1 |
| U | Net recombination rate, R − G | cm−3s−1 |
| τ, τn, τp | Minority-carrier lifetime (τeff: effective, including surfaces) | s; Si 1 ns – 1 ms |
| Nt | Density of traps (recombination centres) | cm−3 |
| n1, p1 | SRH parameters nie(Et − Ei)/kT and nie(Ei − Et)/kT | cm−3 |
| L, Ln, Lp | Diffusion length √(Dτ): distance a minority carrier travels before recombining | μm or cm |
| S | Surface recombination velocity | cm/s |
| Nst | Density of surface traps | cm−2 |
| Us | Recombination rate per unit area at a surface | cm−2s−1 |
| Vbi | Built-in potential of a junction or Schottky contact | V; typically 0.5–1 V |
| V, Va | Applied voltage (positive for forward bias) | V |
| W | Depletion-region width (in Week 13 WB, WE are base and emitter widths; in Week 14 W is channel width) | μm or cm |
| xn, xp | Parts of the depletion region on the n side and on the p side | μm |
| Emax | Peak electric field, at the junction | V/cm |
| Is, Js (IS) | Saturation current (density) of a diode or transistor | A; A/cm2 |
| I | Current | A |
| A (area) | Device or contact area | cm2 |
| η | Ideality factor of a diode, 1 (ideal) to 2 | dimensionless |
| C, Cj | Capacitance (junction or depletion capacitance) | F (pF = 10−12 F) |
| Φm | Work function of a metal | eV; Al 4.28, Au 5.1 |
| Φs | Work function of a semiconductor, χ + (Ec − EF) | eV |
| χ | Electron affinity: energy from Ec up to the vacuum level | eV; Si 4.05 |
| ΦB | Schottky barrier height seen from the metal | eV (or V) |
| A∗∗ | Effective Richardson constant | A/(cm2·K2); n-Si ≈ 110 |
| IE, IB, IC | Emitter, base and collector currents | A (mA) |
| VBE, VCE, VCB | Base–emitter, collector–emitter and collector–base voltages | V |
| α | Common-base current gain, IC/IE | dimensionless; 0.98–0.999 |
| β | Common-emitter current gain, IC/IB (also hFE) | dimensionless; 50–500 |
| γ (BJT) | Emitter injection efficiency | dimensionless, close to 1 |
| αT | Base transport factor | dimensionless, close to 1 |
| NE, WE, DE; NB, WB, DB | Doping, width and minority diffusion coefficient of the emitter; of the base | cm−3; μm; cm2/s |
| τB | Base transit time, WB2/2Dn | s |
| Cox | Gate-oxide capacitance per unit area, εox/tox | F/cm2 |
| tox | Gate-oxide thickness | nm |
| φF, ψs (φs) | Bulk Fermi potential (kT/q)ln(NA/ni); surface potential (band bending) | V |
| Wd, Wdmax, Qdmax | MOS depletion width, its maximum at inversion, and the depletion charge then | μm; C/cm2 |
| VT (Vth) | Threshold voltage of a MOSFET | V |
| VFB | Flat-band voltage | V |
| Φms, Qf | Gate–substrate work-function difference; fixed oxide charge | V; C/cm2 |
| γ (MOSFET) | Body-effect coefficient √(2qεsiNA)/Cox | V1/2 |
| VGS, VDS, VSB, VG | Gate–source, drain–source, source–body and gate voltages | V |
| ID | Drain current | A (mA) |
| W/L | Channel width-to-length ratio | dimensionless |
| gm | Transconductance, ∂ID/∂VGS | S (A/V) |
| k (MOSFET) | Device parameter μnCox(W/L) | A/V2 (mA/V2) |
| μi, τi (μL, μI, NI) | Mobility and scattering time for one scattering mechanism (L: lattice, I: ionised impurity); NI = ionised-impurity density | cm2/(V·s); s; cm−3 |
| Jdrift, Jdiff | Drift and diffusion parts of the current density | A/cm2 |
| Gn, Gp, Rn, Rp | Generation and recombination rates of electrons and holes | cm−3s−1 |
| τb (τbulk), τsurface | Lifetime from bulk recombination only; from surface recombination only | s |
| Us, ps, Δps | Surface recombination rate; hole density and excess at the surface | cm−2s−1; cm−3 |
| pn, np | Minority-carrier density: holes on the n side, electrons on the p side | cm−3 |
| erfc(u), erfc−1 | Complementary error function, 1 − erf(u), and its inverse (read from a table) | dimensionless |
| N(x), N(W) | Doping concentration at depth x (or at the depletion edge W), from C-V profiling | cm−3 |
| t | Time (or a thickness, where the text says so) | s (or cm) |

Abbreviations

| Abbreviation | Meaning |
| --- | --- |
| Si | Silicon |
| Ge | Germanium |
| GaAs | Gallium arsenide |
| SiO2 | Silicon dioxide (silica), the oxide insulator |
| FCC | Face-centred cubic lattice |
| BCC | Body-centred cubic lattice |
| SC | Simple cubic lattice |
| APF | Atomic packing factor |
| MG-Si | Metallurgical-grade silicon (≈ 98 % pure) |
| EG-Si | Electronic-grade silicon (99.9999999 % or better) |
| CZ | Czochralski crystal growth |
| VPE | Vapour-phase epitaxy |
| LPE | Liquid-phase epitaxy |
| MBE | Molecular-beam epitaxy |
| SRH | Shockley–Read–Hall (trap-assisted) recombination |
| I-V | Current–voltage (measurement or characteristic) |
| C-V | Capacitance–voltage (measurement or characteristic) |
| MOS | Metal–oxide–semiconductor |
| MOSFET | Metal–oxide–semiconductor field-effect transistor |
| BJT | Bipolar junction transistor |
| PGD | Postgraduate Diploma |
| n+ | Very heavily doped n-type (similarly p+) |

## Key terms

Every important word used this week is defined here, so you can read this week on its own. These are the most important terms of the whole course; each week's own Key terms section gives more detail.

Semiconductor. A solid whose electrical conductivity lies between that of a metal and an insulator and can be controlled over many orders of magnitude by temperature, light and added impurities. Silicon (Si), germanium (Ge) and gallium arsenide (GaAs) are the main examples.

Energy band and band gap (Eg). In a crystal the allowed electron energies form bands. The valence band (top edge Ev) is normally full; the conduction band (bottom edge Ec) is normally nearly empty. The band gap Eg = Ec − Ev is the forbidden energy range between them: 1.12 eV for Si.

Electron and hole. The two kinds of mobile charge. A free electron (negative) moves in the conduction band; a hole (positive) is an empty electron place in the valence band that moves like a positive particle.

Intrinsic carrier concentration (ni). The electron (and equal hole) concentration in a pure, undoped semiconductor, created only by heat lifting electrons across the gap. For Si at 300 K, ni = 1×1010 cm−3; it rises very steeply with temperature.

Doping (donor, acceptor). Adding a small, controlled amount of impurity atoms. Donors (concentration ND, e.g. phosphorus) each give a free electron, making n-type material; acceptors (NA, e.g. boron) each take an electron, leaving a hole, making p-type material.

Majority and minority carriers. The majority carriers are the more numerous kind of mobile charge in a doped region (electrons in n-type, holes in p-type); the minority carriers are the far fewer other kind.

Mass-action law. In equilibrium the product of the electron and hole concentrations is fixed by the material and temperature, whatever the doping: np = ni2. So in n-type Si with n = ND, the hole concentration is p = ni2/ND.

Fermi level (EF). The energy at which a state has a 50 % chance of being occupied by an electron; it is flat through any material or device in equilibrium. It lies at the intrinsic level Ei (near mid-gap) in pure material and moves towards Ec with donor doping and towards Ev with acceptor doping.

EF − Ei = kT ln(ND/ni) (n-type); Ei − EF = kT ln(NA/ni) (p-type)

Where:

- EF, Ei = Fermi level and intrinsic level (eV)

- kT = thermal energy, 0.0259 eV at 300 K

- ND, NA = donor and acceptor concentrations (cm−3)

- ni = intrinsic carrier concentration (cm−3)

Miller indices (h k l). Three whole numbers that name a plane in a crystal: take the plane's intercepts on the axes in units of the lattice constant, take reciprocals, and clear fractions.

Czochralski (CZ) growth and epitaxy. CZ growth pulls a large single-crystal ingot of silicon slowly out of a melt using a seed crystal. Epitaxy grows a thin new crystalline layer on top of a crystal wafer, continuing its lattice (VPE from a gas, LPE from a liquid, MBE from molecular beams in vacuum).

Dopant diffusion and ion implantation. The two ways of putting dopants into a wafer. In diffusion, dopant atoms spread in from the surface in a hot furnace, giving an erfc or Gaussian profile; in ion implantation, ions are fired into the wafer, giving a Gaussian profile centred at the projected range Rp.

Junction depth (xj). The depth at which the added dopant concentration equals the background doping of the wafer, so the material changes type.

Drift and mobility (μ). Drift is the motion of carriers caused by an electric field. Mobility is the drift velocity per unit field, vd = μE, in cm2/(V·s); for lightly doped Si μn = 1350 and μp = 480.

Conductivity (σ) and resistivity (ρ). How easily a material carries current, and its inverse.

σ = q(nμn + pμp), ρ = 1/σ

Where:

- σ = conductivity (S/cm); ρ = resistivity (Ω·cm)

- q = electronic charge, 1.6×10−19 C

- n, p = electron and hole concentrations (cm−3)

- μn, μp = electron and hole mobilities (cm2/V·s)

Diffusion current and the Einstein relation. Diffusion current flows when carriers spread from where they are concentrated to where they are scarce, even with no field. The diffusion coefficient D and the mobility are linked by the Einstein relation D/μ = kT/q (0.0259 V at 300 K).

Recombination and minority-carrier lifetime (τ). Recombination is an electron falling back into a hole, removing both. The lifetime τ is the average time an extra (excess) minority carrier survives before it recombines; in Si it ranges from about 1 ns to 1 ms.

Diffusion length (L). The average distance an excess minority carrier diffuses before recombining.

L = √(Dτ)

Where:

- L = diffusion length (cm)

- D = minority-carrier diffusion coefficient (cm2/s)

- τ = minority-carrier lifetime (s)

p-n junction and depletion region. A p-n junction is the boundary between p-type and n-type regions of one crystal. Next to it is the depletion region (width W), a layer emptied of mobile carriers that contains only fixed ionised dopants and therefore a strong electric field.

Built-in potential (Vbi). The voltage that appears across the depletion region of a junction in equilibrium, which stops further diffusion of carriers across it.

Vbi = (kT/q) ln( NAND / ni2 )

Where:

- Vbi = built-in potential (V)

- kT/q = thermal voltage, 0.0259 V at 300 K

- NA, ND = acceptor and donor concentrations on the two sides (cm−3)

- ni = intrinsic carrier concentration (cm−3)

Forward and reverse bias. Forward bias (p side positive) lowers the junction barrier and lets a large current flow; reverse bias (p side negative) raises it, widens the depletion region and allows only a tiny current.

Shockley diode equation (Is, η). The current–voltage law of a diode, I = Is(eqV/ηkT − 1). The saturation current Is is the tiny reverse current; the ideality factor η is 1 for an ideal diode and up to 2 when recombination in the depletion region matters.

Schottky contact and barrier height (ΦB). A rectifying metal–semiconductor contact. Electrons crossing from the metal face a barrier of height ΦB = Φm − χ, where Φm is the metal's work function and χ the semiconductor's electron affinity.

Ohmic contact. A metal–semiconductor contact that passes current equally easily in both directions with a straight-line I-V graph, usually made by doping the semiconductor so heavily (≳ 1019 cm−3) that electrons tunnel through the barrier.

C-V profiling. Measuring a reverse-biased junction's capacitance C against voltage V. A plot of 1/C2 against V is a straight line whose slope gives the doping and whose voltage intercept gives Vbi.

Bipolar junction transistor (BJT) and current gains (α, β). A three-layer (n-p-n or p-n-p) device in which a small base current controls a much larger collector current. α = IC/IE is the common-base gain (just below 1); β = IC/IB = α/(1 − α) is the common-emitter gain (typically 50–500).

MOS capacitor and inversion. A MOS capacitor is a gate, a thin oxide and a semiconductor stacked together. On p-type silicon a negative gate gives accumulation (more holes at the surface), a small positive gate gives depletion, and a large positive gate gives inversion: the surface fills with electrons and becomes n-type.

Threshold voltage (VT). The gate-to-source voltage at which strong inversion starts and a MOSFET's channel forms, VT = VFB + 2φF + γ√(2φF).

MOSFET and its operating regions. A metal–oxide–semiconductor field-effect transistor: a MOS capacitor with a source and a drain on either side of the gate, whose inversion layer forms the conducting channel. It is cut off for VGS < VT, linear for VDS < VGS − VT, and saturated for VDS ≥ VGS − VT.

ID(sat) = ½ μnCox(W/L)(VGS − VT)2

Where:

- ID(sat) = drain current in saturation (A)

- μn = channel electron mobility (cm2/V·s)

- Cox = gate-oxide capacitance per unit area, εox/tox (F/cm2)

- W/L = channel width-to-length ratio

- VGS = gate-to-source voltage; VT = threshold voltage (V)

Why it matters: this, with the diode equation and Vbi, is among the formulas most often examined.

## 15.1 Course overview

The whole course tells one story: how do we make, control and use the free charges in a crystal?

| Module | Weeks | The question it answers | The one idea to carry into the exam |
| --- | --- | --- | --- |
| 1. Material physics and growth | 1–3 | What is a semiconductor, and how do we make and dope it? | Conductivity is controllable because of a moderate band gap and doping. Crystals are grown pure by CZ and epitaxy, and doped by diffusion (erfc or Gaussian) or implantation (Gaussian at Rp). |
| 2. Bands and statistics | 4–6 | How many electrons and holes are there? | n = Nce−(Ec−EF)/kT, p = Nve−(EF−Ev)/kT, np = ni2. EF moves 60 mV per decade of doping, and back to mid-gap when hot. |
| 3. Transport and injection | 7–9 | How do the carriers move, and how long do extra ones last? | J = qnμE + qD dn/dx, D/μ = kT/q. Excess minority carriers recombine with lifetime τ and spread over L = √(Dτ). |
| 4. Junctions and interfaces | 10–12 | What happens where two materials meet? | Vbi = (kT/q) ln(NAND/ni2); I = Is(eqV/kT − 1); Schottky ΦB = Φm − χ; 1/C2 against V gives the doping. |
| 5. Devices | 13–15 | How do transistors work? | BJT: β = α/(1 − α), α = γαT. MOSFET: VT = VFB + 2φF + γ√(2φF); ID(sat) = ½μCox(W/L)(VGS − VT)2. |

How the ideas connect. Doping (Week 3) sets n and p (Week 5). n and p set conductivity (Week 7). Joining p and n regions creates a built-in field (Week 10). Forward bias injects minority carriers that diffuse and recombine (Weeks 7–9), which gives the diode equation. Two junctions close together give the BJT (Week 13); a field-induced inversion layer gives the MOSFET (Week 14).

## 15.2 Formula sheet

### Physical constants

| Quantity | Symbol | Value |
| --- | --- | --- |
| Electronic charge | q | 1.602×10−19 C |
| Boltzmann constant | k | 1.381×10−23 J/K = 8.617×10−5 eV/K |
| Thermal energy at 300 K | kT | 0.0259 eV |
| Thermal voltage at 300 K | kT/q | 0.0259 V (25.9 mV) |
| Planck constant | h | 6.626×10−34 J·s |
| Reduced Planck constant | ħ | 1.055×10−34 J·s |
| Free electron mass | m0 | 9.109×10−31 kg |
| Permittivity of free space | ε0 | 8.854×10−14 F/cm |
| Speed of light | c | 3×1010 cm/s |
| Electron-volt | 1 eV | 1.602×10−19 J |
| Photon wavelength | λ | 1.24/E (μm, with E in eV) |

### Material data at 300 K

|  | Si | Ge | GaAs |
| --- | --- | --- | --- |
| Crystal | Diamond | Diamond | Zinc blende |
| Lattice constant a (Å) | 5.43 | 5.65 | 5.65 |
| Atoms/cm3 | 5.0×1022 | 4.4×1022 | 4.4×1022 |
| Eg (eV) | 1.12 (indirect) | 0.66 (indirect) | 1.42 (direct) |
| ni (cm−3) | 1×1010 | 2.4×1013 | 2×106 |
| Nc (cm−3) | 2.8×1019 | 1.04×1019 | 4.7×1017 |
| Nv (cm−3) | 1.04×1019 | 6.0×1018 | 7.0×1018 |
| μn (cm2/V·s) | 1350 | 3900 | 8500 |
| μp (cm2/V·s) | 480 | 1900 | 400 |
| Dn, Dp (cm2/s) | 35, 12.4 | 101, 49 | 220, 10 |
| εr | 11.7 | 16.0 | 12.9 |
| χ (eV) | 4.05 | 4.0 | 4.07 |
| vsat (cm/s) | 1×107 | 6×106 | ≈ 1×107 (peak 2×107) |
| Melting point (°C) | 1414 | 937 | 1238 |

### Crystals and Miller indices

Miller indices: intercepts → reciprocals → clear fractions → (h k l)
dhkl = a / √(h2 + k2 + l2) (cubic)
Diamond: 8 atoms/cell, coordination 4, rnn = (√3/4)a, APF = 0.34
SC 1, BCC 2, FCC 4 atoms/cell; APF 0.52, 0.68, 0.74

### Growth and doping

SiO2 + 2C → Si + 2CO; Si + 3HCl → SiHCl3 + H2; SiHCl3 + H2 → Si + 3HCl
Segregation: k0 = Cs/Cl; Cs = k0C0(1 − f)k0 − 1
Fick 1: F = −D ∂C/∂x; Fick 2: ∂C/∂t = D ∂2C/∂x2; D = D0 e−Ea/kT
Constant source: C = Cs erfc(x/2√(Dt)); Q = (2/√π)Cs√(Dt)
Limited source: C = (Q/√(πDt)) exp(−x2/4Dt)
Implant: N(x) = (Φ/√(2π)ΔRp) exp(−(x − Rp)2/2ΔRp2); Np ≈ 0.4Φ/ΔRp; Φ = It/qA

### Bands and statistics

Schrödinger: −(ħ2/2m) d2ψ/dx2 + Vψ = Eψ
Kronig–Penney: P sin(αa)/(αa) + cos(αa) = cos(ka)
1/m∗ = (1/ħ2) d2E/dk2
f(E) = 1/(1 + e(E − EF)/kT)
gc(E) = (4π(2mn∗)3/2/h3)√(E − Ec)
n = Nc e−(Ec − EF)/kT; p = Nv e−(EF − Ev)/kT
Nc = 2(2πmn∗kT/h2)3/2
ni = √(NcNv) e−Eg/2kT; np = ni2
n = ni e(EF − Ei)/kT; p = ni e(Ei − EF)/kT
n = (ND − NA)/2 + √(((ND − NA)/2)2 + ni2)
EF − Ei = kT ln(ND/ni); Ei − EF = kT ln(NA/ni)

### Transport

vd = μE; μ = qτm/m∗; 1/μ = 1/μL + 1/μI
Jdrift = q(nμn + pμp)E; σ = q(nμn + pμp); ρ = 1/σ
Jn = qnμnE + qDn dn/dx; Jp = qpμpE − qDp dp/dx
Einstein: D/μ = kT/q
vd = μE/[1 + (μE/vsat)β]1/β

### Recombination and continuity

SRH: U = (np − ni2)/[τp(n + n1) + τn(p + p1)]; τ = 1/(σvthNt)
Low-level, n-type: U = Δp/τp; Δp(t) = Δp(0)e−t/τp
∂Δp/∂t = Dp ∂2Δp/∂x2 − μpE ∂Δp/∂x + GL − Δp/τp
L = √(Dτ); Δp(x) = Δp(0)e−x/Lp
Surface: Us = SΔps; S = σvthNst; 1/τeff = 1/τb + 2S/W

### Junctions and contacts

Vbi = (kT/q) ln(NAND/ni2)
W = √((2εs/q)(Vbi − V)(1/NA + 1/ND)); NAxp = NDxn; Emax = qNDxn/εs
I = Is(eqV/kT − 1); Js = qni2(Dp/(LpND) + Dn/(LnNA))
Cj = εsA/W; 1/C2 = 2(Vbi − V)/(qεsNA2); N = 2/(qεsA2|d(1/C2)/dV|)
Schottky: ΦB = Φm − χ; Vbi = Φm − Φs; Js = A∗∗T2e−qΦB/kT
Ohmic (tunnelling): ND ≳ 1019 cm−3

### Devices

BJT: IC = IS eqVBE/kT, IS = qADBni2/(NBWB)
γ = 1/[1 + DENBWB/(DBNEWE)], αT ≈ 1 − WB2/2Ln2
α = γαT, β = α/(1 − α), IE = IC + IB, τB = WB2/2DB
MOS: Cox = εox/tox, φF = (kT/q)ln(NA/ni), Wdmax = √(4εsφF/qNA)
VT = VFB + 2φF + √(4qεsNAφF)/Cox, VFB = Φms − Qf/Cox
Linear: ID = μCox(W/L)[(VGS − VT)VDS − VDS2/2]
Saturation: ID = ½μCox(W/L)(VGS − VT)2, gm = μCox(W/L)(VGS − VT)

### Rules of thumb

- Each decade of doping moves EF by 60 mV; each 60 mV of forward bias raises diode current tenfold (300 K).

- ni(Si) roughly doubles every 8 °C.

- Doping 1016 cm−3 in Si = 1 dopant per 5×106 Si atoms; ρ ≈ 0.5 Ω·cm (n-type), 1.4 Ω·cm (p-type).

- Diffusion length in good Si: tens to hundreds of μm.

## 15.3 Problem-solving clinic

### How to answer each type of question

- Definitions (2–3 marks). One clear sentence, then an example, then the formula if there is one. "The Fermi level is the energy at which the probability of occupation is ½; in n-type Si it lies near Ec; EF − Ei = kT ln(ND/ni)."

- "Explain" and "describe" questions want the mechanism, not just a list. Use the pattern: what happens physically → the equation → the consequence.

- Derivations. List the assumptions first, number the steps, and box the final result. Examiners give marks for the assumptions.

- Calculations. Write the formula, substitute with units, give the answer to 2–3 significant figures with units. Then sanity-check the size of the answer.

- Comparisons. Use a table with three to six rows.

- Diagrams earn marks: band diagrams, carrier profiles, the CZ puller, MOS band bending, BJT and MOSFET cross-sections, I-V curves.

### Unit traps that cost marks

| Trap | Fix |
| --- | --- |
| Mixing μm and cm | 1 μm = 10−4 cm. Convert depths and widths to cm before using cm2/s, cm−3 |
| Mixing eV and J | kT = 0.02585 eV at 300 K; only convert to joules (× 1.6×10−19) when multiplying by something in SI |
| Forgetting the factor ½ | ID(sat) = ½μCox(W/L)(VGS − VT)2 |
| Using the wrong form of diffusion length | Use the form the question gives: √(Dt), √(2Dt) or 2√(Dt) |
| Natural log against log10 | All the semiconductor formulas use ln. ln(10n) = 2.303n |
| Dose units | Dose is per cm2 (atoms/cm2); concentration is per cm3 |

### Sanity checks

| Quantity | Typical size |
| --- | --- |
| Carrier concentrations | 104 – 1020 cm−3 |
| ni (Si, 300 K) | 1010 cm−3 |
| EF − Ei | 0.2 – 0.5 eV |
| Diffusion coefficients (dopants in a furnace) | 10−15 – 10−12 cm2/s |
| Carrier diffusion coefficients | 1 – 100 cm2/s |
| Built-in voltage | 0.5 – 1.0 V |
| Depletion width | 0.01 – 10 μm |
| BJT β | 20 – 500 |
| MOSFET VT | 0.2 – 2 V |

## 15.4 Past-question style exercises (with solutions)

### E1. Find the Miller indices of a plane with intercepts 4a, 2b and ∞c.

Given: intercepts 4, 2 and ∞ (in units of the lattice constants a, b, c).

Find: the Miller indices (h k l).

Formula: intercepts → reciprocals → multiply by the smallest number that clears the fractions → (h k l).

Solution. Reciprocals 1/4, 1/2, 0. Multiply by 4: 1, 2, 0.

Answer: (1 2 0).

What this means: the zero index says the plane never meets the z-axis: it is parallel to it.

### E2. Constant-source diffusion with Cs = 5×1019 cm−3, D = 2×10−13 cm2/s, t = 2 h. Find the concentration at 0.3 μm.

Given: Cs = 5×1019 cm−3, D = 2×10−13 cm2/s, t = 2 h = 7200 s, x = 0.3 μm = 3×10−5 cm.

Find: C(x, t).

Formula:

C(x, t) = Cs erfc( x / 2√(Dt) )

Where:

- C(x, t) = dopant concentration at depth x after time t (cm−3)

- Cs = surface concentration, held constant (cm−3)

- D = dopant diffusion coefficient at the furnace temperature (cm2/s)

- x = depth (cm); t = diffusion time (s)

Solution.

√(Dt) = √(2×10−13 × 7200) = √(1.44×10−9) = 3.79×10−5 cm
u = x/2√(Dt) = 3×10−5 / (2 × 3.79×10−5) = 0.395
erfc(0.395) = 0.576
C = 5×1019 × 0.576 = 2.88×1019 cm−3

Answer: C(0.3 μm) ≈ 2.9×1019 cm−3.

What this means: 0.3 μm is only about 0.4 of the characteristic diffusion length 2√(Dt) = 0.76 μm, so the concentration there is still more than half the surface value; the junction will lie much deeper.

### E3. Silicon is doped with NA = 2×1016 cm−3 at 300 K (ni = 1010 cm−3). Find p, n and the Fermi level relative to Ei.

Given: NA = 2×1016 cm−3, ni = 1010 cm−3, kT = 0.02585 eV.

Find: p, n and Ei − EF.

Formula:

p ≈ NA, n = ni2/p, Ei − EF = kT ln(p/ni)

Where:

- p, n = hole and electron concentrations (cm−3)

- NA = acceptor concentration (cm−3); ni = intrinsic concentration (cm−3)

- Ei − EF = distance of the Fermi level below the intrinsic level (eV); kT = thermal energy (eV)

Solution.

p ≈ NA = 2×1016 cm−3
n = ni2/p = 1020/(2×1016) = 5×103 cm−3
Ei − EF = kT ln(p/ni) = 0.02585 ln(2×106) = 0.02585 × 14.51 = 0.375 eV

Answer: p = 2×1016 cm−3, n = 5×103 cm−3; EF lies 0.375 eV below Ei.

What this means: there are 4×1012 holes for every electron, so the electrons are true minority carriers; EF sits about two-thirds of the way from mid-gap down to Ev (which is 0.56 eV below Ei).

### E4. Find the resistivity of n-type Si with ND = 1015 cm−3 and μn = 1350 cm2/V·s.

Given: n ≈ ND = 1015 cm−3, μn = 1350 cm2/V·s, q = 1.6×10−19 C.

Find: ρ.

Formula:

σ = qnμn (holes negligible), ρ = 1/σ

Where:

- σ = conductivity (S/cm); ρ = resistivity (Ω·cm)

- q = electronic charge (C); n = electron concentration (cm−3); μn = electron mobility (cm2/V·s)

Solution.

σ = qNDμn = 1.6×10−19 × 1015 × 1350 = 0.216 S/cm
ρ = 1/σ = 4.63 Ω·cm

Answer: ρ ≈ 4.6 Ω·cm.

What this means: one donor per 5×107 silicon atoms lowers the resistivity from about 3×105 Ω·cm (pure Si) to under 5 Ω·cm, a factor of about 70 000.

### E5. Holes in n-Si have μp = 450 cm2/V·s and lifetime 5 μs. Find Dp and the diffusion length Lp.

Given: μp = 450 cm2/V·s, τp = 5×10−6 s, kT/q = 0.02585 V.

Find: Dp and Lp.

Formula:

Dp = (kT/q)μp, Lp = √(Dpτp)

Where:

- Dp = hole diffusion coefficient (cm2/s); μp = hole mobility (cm2/V·s)

- kT/q = thermal voltage (V)

- Lp = hole diffusion length (cm); τp = hole lifetime (s)

Solution.

Dp = (kT/q)μp = 0.02585 × 450 = 11.6 cm2/s
Lp = √(Dpτp) = √(11.6 × 5×10−6) = 7.6×10−3 cm = 76 μm

Answer: Dp = 11.6 cm2/s, Lp ≈ 76 μm.

What this means: holes injected into this n-type silicon travel on average about 76 μm before recombining, far more than the width of a typical depletion region or transistor base.

### E6. A Si p+n junction has NA = 1017 cm−3 and ND = 1015 cm−3. Find Vbi and the zero-bias depletion width.

Given: NA = 1017 cm−3, ND = 1015 cm−3, ni = 1010 cm−3, kT/q = 0.02585 V, εs = 1.04×10−12 F/cm.

Find: Vbi and W at V = 0.

Formula:

Vbi = (kT/q) ln(NAND/ni2), W ≈ √(2εsVbi/qND) (one-sided junction)

Where:

- Vbi = built-in potential (V); kT/q = thermal voltage (V)

- NA, ND = acceptor and donor concentrations (cm−3); ni = intrinsic concentration (cm−3)

- W = depletion width (cm); εs = permittivity of Si (F/cm); q = electronic charge (C)

Solution.

Vbi = (kT/q) ln(NAND/ni2) = 0.02585 ln(1032/1020) = 0.02585 × 27.63 = 0.714 V

One-sided junction, so the depletion region is almost all on the lightly doped n side:

W ≈ √(2εsVbi/qND) = √(2 × 1.04×10−12 × 0.714 / (1.6×10−19 × 1015)) = 9.6×10−5 cm = 0.96 μm

Answer: Vbi = 0.714 V, W ≈ 0.96 μm.

What this means: because the p side is 100 times more heavily doped, about 99 % of the 0.96 μm depletion region lies in the n side; the light side controls both the width and the capacitance.

### E7. A diode has Is = 2×10−14 A. Find the current at V = 0.65 V and 300 K.

Given: Is = 2×10−14 A, V = 0.65 V, kT/q = 0.02585 V, ideal diode (η = 1).

Find: I.

Formula:

I = Is(eqV/kT − 1)

Where:

- I = diode current (A); Is = saturation current (A)

- V = applied forward voltage (V); kT/q = thermal voltage (V)

Solution.

I = Is(eqV/kT − 1) = 2×10−14 × e0.65/0.02585 = 2×10−14 × 8.3×1010 = 1.66 mA

Answer: I ≈ 1.7 mA.

What this means: a saturation current of only 2×10−14 A becomes a useful milliamp current at 0.65 V, because each extra 60 mV of forward bias multiplies the current by ten.

### E8. A BJT has β = 150 and IB = 20 μA. Find IC, IE and α.

Given: β = 150, IB = 20 μA.

Find: IC, IE and α.

Formula:

IC = βIB, IE = IC + IB, α = β/(β + 1)

Where:

- IC, IB, IE = collector, base and emitter currents (A)

- β = common-emitter current gain; α = common-base current gain (dimensionless)

Solution.

IC = βIB = 150 × 20 μA = 3.00 mA
IE = IC + IB = 3.02 mA
α = β/(β + 1) = 150/151 = 0.9934

Answer: IC = 3.00 mA, IE = 3.02 mA, α = 0.993.

What this means: 99.3 % of the electrons leaving the emitter reach the collector; the 0.7 % lost in the base is the base current, and that small loss is what lets 20 μA control 3 mA.

### E9. An nMOS has μnCox(W/L) = 0.8 mA/V2 and VT = 0.7 V, with VGS = 2 V. Find ID for VDS = 0.5 V and for VDS = 3 V.

Given: k = μnCox(W/L) = 0.8 mA/V2, VT = 0.7 V, VGS = 2 V, VDS = 0.5 V and 3 V.

Find: ID at each VDS.

Formula:

Linear (VDS < VGS − VT): ID = k[(VGS − VT)VDS − VDS2/2]
Saturation (VDS ≥ VGS − VT): ID = ½k(VGS − VT)2

Where:

- ID = drain current (A); k = μnCox(W/L), the device parameter (A/V2)

- VGS, VDS = gate–source and drain–source voltages (V); VT = threshold voltage (V)

Solution.

VGS − VT = 1.3 V.

VDS = 0.5 V < 1.3 V → linear: ID = 0.8 × [1.3 × 0.5 − 0.52/2] = 0.8 × 0.525 = 0.42 mA
VDS = 3 V ≥ 1.3 V → saturation: ID = ½ × 0.8 × 1.32 = 0.4 × 1.69 = 0.676 mA

Answer: ID = 0.42 mA at VDS = 0.5 V (linear) and 0.68 mA at VDS = 3 V (saturation).

What this means: raising VDS sixfold increases the current by only about 60 %, because once VDS passes 1.3 V the channel pinches off and the current is fixed by VGS alone.

## 15.5 Final examination checklist

Before the exam, can you:

- [Week 1] compare conductors, semiconductors and insulators; Si, Ge and GaAs; find Miller indices including ∞ and negative intercepts?

- [Week 2] describe MG-Si → EG-Si, the CZ method with its advantages and limitations, and compare VPE, LPE, MBE?

- [Week 3] state Fick's laws; use the erfc and Gaussian profiles; calculate junction depth, implant peak and dose?

- [Week 4] state the Schrödinger equation and explain the Kronig–Penney model; compare direct and indirect gaps; derive ni?

- [Week 5] use the Fermi–Dirac function; calculate n, p and EF for any doping; explain the three temperature regions?

- [Week 7] calculate drift current and conductivity; explain scattering; state and use the Einstein relation?

- [Week 8] explain velocity saturation, hot carriers, SRH recombination and lifetime?

- [Week 9] write the continuity equation and solve it for steady injection; explain surface recombination velocity?

- [Week 10] explain the depletion region; calculate Vbi and W; derive the Shockley equation?

- [Week 11] draw Schottky and Ohmic band diagrams in equilibrium and under bias?

- [Week 12] extract doping and Vbi from a 1/C2 plot; extract Is and η from an I-V plot?

- [Week 13] explain BJT operation and minority-carrier profiles; use γ, αT, α, β?

- [Week 14] explain accumulation, depletion, inversion; use VT; calculate ID in each region?

On the day: bring a scientific calculator (with ex and ln), a ruler for diagrams, and spare pens. Read every question first, start with the one you know best, and leave 10 minutes to check units.

## 15.6 Comprehensive revision questions

Work through these without notes, then check against the week shown. Full worked answers for the 50 PGD examination questions are on the next page (the answer key) and in each week.

- Define a semiconductor and explain why its conductivity rises with temperature. (Week 1)

- Explain covalent bonding in silicon and electron–hole pair generation. (Week 1)

- Find the Miller indices of planes with intercepts (a) a, 2b, 3c; (b) 2a, 3b, ∞c. (Week 1)

- Describe the conversion of MG-Si to EG-Si and the Czochralski method. (Week 2)

- Compare VPE, LPE and MBE. (Week 2)

- State Fick's first and second laws and the two diffusion profiles. (Week 3)

- Compare diffusion and ion implantation. Find the junction depth of an implant with Np = 1018 cm−3, Rp = 0.2 μm, ΔRp = 0.04 μm into NB = 1016 cm−3. (Week 3; answer xj = 0.2 + 0.04√(2 ln 100) = 0.321 μm)

- Explain the Kronig–Penney model and how it gives energy bands. (Week 4)

- Derive ni = √(NcNv)e−Eg/2kT. (Week 4)

- Write the Fermi–Dirac function and describe it at 0 K and 300 K. (Week 5)

- Find n, p and EF for Si with ND = 5×1015 cm−3. (Week 5; n = 5×1015, p = 2×104 cm−3, EF − Ei = 0.339 eV)

- Derive the drift current density and the Einstein relation. (Week 7)

- Explain SRH recombination and define minority-carrier lifetime. (Week 8)

- Derive the minority-carrier continuity equation and solve it for steady injection into a long bar. (Week 9)

- Explain the formation of the depletion region; derive the Shockley diode equation. (Week 10)

- Distinguish Schottky and Ohmic contacts with band diagrams. (Week 11)

- Explain how C-V measurements give the doping concentration. (Week 12)

- Explain BJT operation and derive β = α/(1 − α). (Week 13)

- Explain accumulation, depletion and inversion; derive the saturation condition of a MOSFET. (Week 14)

- Compare a BJT and a MOSFET. (Week 14)

## Practice questions

These extra questions practise this week's ideas. Work each one on paper before reading the solution; the calculation questions follow the same Question, Given, Find, Solution, Answer layout as the worked examples.

#### Practice 15.1: one sample, every property

Question. n-type silicon has ND = 2×1016 cm−3, μn = 1200 cm2/V·s, μp = 420 cm2/V·s and τp = 2 μs. At 300 K find (a) n and p, (b) EF − Ei, (c) the conductivity, (d) Dp and (e) the hole diffusion length.

Given: ND = 2×1016 cm−3, ni = 1010 cm−3, μn = 1200, μp = 420 cm2/V·s, τp = 2×10−6 s.

Find: n, p, EF − Ei, σ, Dp, Lp.

Solution.

(a) n = 2×1016 cm−3, p = 1020/2×1016 = 5×103 cm−3
(b) EF − Ei = 0.0259 ln(2×106) = 0.376 eV
(c) σ = qnμn = 1.6×10−19 × 2×1016 × 1200 = 3.84 S/cm
(d) Dp = 0.0259 × 420 = 10.9 cm2/s
(e) Lp = √(10.9 × 2×10−6) = 4.66×10−3 cm = 46.6 μm

Answer: n = 2×1016, p = 5×103 cm−3; EF = Ei + 0.376 eV; σ = 3.84 S/cm; Dp = 10.9 cm2/s; Lp = 47 μm.

What this means: one number, the doping, fixes almost everything: the electrons carry essentially all the current (the 5×103 holes add nothing to σ), yet it is those few minority holes, with their 47 μm diffusion length, that will set the behaviour of any junction made on this sample.

#### Practice 15.2: a diode made from that sample

Question. A p+n diode (NA = 1×1019 cm−3, area 1×10−3 cm2) is made on the silicon of Practice 15.1. Find Vbi, the zero-bias depletion width, Is and the current at 0.65 V.

Given: NA = 1019, ND = 2×1016 cm−3, Dp = 10.9 cm2/s, Lp = 4.66×10−3 cm, A = 10−3 cm2.

Find: Vbi, W, Is, I(0.65 V).

Solution.

Vbi = 0.0259 ln(1019 × 2×1016/1020) = 0.0259 ln(2×1015) = 0.913 V
W ≈ √(2εsVbi/qND) = √(2 × 1.04×10−12 × 0.913/(1.6×10−19 × 2×1016)) = 2.44×10−5 cm = 0.24 μm
Js ≈ qni2Dp/(LpND) = 1.6×10−19 × 1020 × 10.9/(4.66×10−3 × 2×1016) = 1.87×10−12 A/cm2
Is = 1.87×10−15 A
I(0.65 V) = 1.87×10−15 × e0.65/0.0259 = 1.87×10−15 × 7.9×1010 = 0.15 mA

Answer: Vbi = 0.91 V, W = 0.24 μm, Is = 1.9×10−15 A, I(0.65 V) = 0.15 mA.

What this means: compared with E6, the 20 times heavier n-side doping makes the depletion region about four times narrower (0.24 μm against 0.96 μm). Its Is is about ten times smaller than that of the diode in E7, which is why only 0.15 mA flows at 0.65 V instead of 1.7 mA.

#### Practice 15.3: a complete MOSFET calculation

Question. An nMOS has NA = 1×1017 cm−3, tox = 5 nm, VFB = −0.9 V, μn = 350 cm2/V·s and W/L = 20. Find VT and the saturation current at VGS = 1.2 V.

Given: NA = 1017 cm−3, tox = 5×10−7 cm, VFB = −0.9 V, μn = 350 cm2/V·s, W/L = 20.

Find: VT and ID(sat).

Solution.

Cox = 3.45×10−13/5×10−7 = 6.9×10−7 F/cm2
φF = 0.417 V, 2φF = 0.834 V
γ = √(2qεsiNA)/Cox = 1.824×10−7/6.9×10−7 = 0.264 V1/2, γ√(2φF) = 0.241 V
VT = −0.9 + 0.834 + 0.241 = 0.18 V
k = μnCox(W/L) = 350 × 6.9×10−7 × 20 = 4.83 mA/V2
ID(sat) = ½ × 4.83 × (1.2 − 0.18)2 = 2.5 mA

Answer: VT ≈ 0.18 V, ID(sat) ≈ 2.5 mA.

What this means: the thin 5 nm oxide gives a large Cox, which both lowers VT (the depletion term is only 0.24 V) and raises the current; the negative VFB (typical of an n+ polysilicon gate) cancels most of the band-bending term.

#### Practice 15.4: essay practice

Question. In about one page, explain how a p-n junction diode rectifies, starting from the formation of the depletion region and ending with the Shockley equation. (Use the structure of Week 10 and Q47–Q48.)

Answer outline. (1) Diffusion of holes and electrons across the junction uncovers fixed ions: the depletion region and its field. (2) Equilibrium: drift balances diffusion, EF is flat, Vbi = (kT/q) ln(NAND/ni2). (3) Forward bias lowers the barrier; minority carriers are injected (law of the junction, pn = pn0eqV/kT). (4) They diffuse and recombine over Lp, Ln; the diffusion currents at the depletion edges add to give I = Is(eqV/kT − 1). (5) Reverse bias raises the barrier: only the tiny −Is flows. Hence rectification. Include the band diagram and the I-V sketch.

## Objectives check

Use this table to confirm you have met this week's objectives. Cover the Answer column and answer each check question from memory. If you cannot, go back to the section in the last column before moving on.

| # | Objective | Check yourself | Answer | Where it is taught |
| --- | --- | --- | --- | --- |
| 1 | Summarise the whole course and how its ideas connect. | Trace the chain from doping to the diode equation in one sentence. | Doping sets n and p; a p-n junction forms a barrier; forward bias injects minority carriers that diffuse and recombine, giving I = Is(eqV/kT − 1). | 15.1 |
| 2 | Recall and apply the key formulas. | Write the mass-action law, the Einstein relation and the saturation MOSFET current. | np = ni2; D/μ = kT/q; ID = ½μCox(W/L)(VGS − VT)2. | 15.2 |
| 3 | Answer definitions, derivations and calculations in examination style. | What should a derivation answer begin with? | A list of the assumptions. | 15.3 |
| 4 | Solve mixed past-question style problems. | Find Vbi for NA = 1017 and ND = 1015 cm−3 in Si. | 0.714 V. | 15.4, E6 |
| 5 | Check readiness for the final examination. | Can you tick every line of the checklist in 15.5? | If not, revise the week named on that line. | 15.5–15.6 |

Revision & Practicals

# Answer Key — All 50 Examination Questions

The key point of every PGD examination answer in one or two lines. Cover the right-hand column, say the answer aloud, then check. The full worked answer is in the week shown in brackets.

## Symbols and abbreviations used on this page

Every symbol, constant and abbreviation on this page is listed here, even if an earlier week already defined it, so you can study this page on its own.

Constants and units

| Symbol | Meaning | Units / typical value |
| --- | --- | --- |
| q | Magnitude of the electronic charge | 1.6×10−19 C |
| k | Boltzmann constant | 8.617×10−5 eV/K = 1.381×10−23 J/K |
| kT | Thermal energy | 0.0259 eV (often 0.02585 eV) at 300 K |
| kT/q | Thermal voltage | 0.0259 V (about 26 mV) at 300 K |
| T | Absolute temperature | kelvin (K); room temperature = 300 K |
| ħ | Reduced Planck constant, h/2π | 1.055×10−34 J·s |
| eV | Electron-volt, a unit of energy | 1 eV = 1.6×10−19 J |
| μm | Micrometre (micron) | 1 μm = 10−4 cm = 10−6 m |

Symbols

| Symbol | Meaning | Units / typical value |
| --- | --- | --- |
| Ec (EC) | Energy of the bottom of the conduction band | eV |
| Ev (EV) | Energy of the top of the valence band | eV |
| Eg | Band-gap energy, Ec − Ev | eV; Si 1.12, Ge 0.66, GaAs 1.42 at 300 K |
| EF | Fermi level: the energy at which a state has a 50 % chance of being occupied | eV |
| Ei | Intrinsic Fermi level, close to mid-gap | eV |
| Et | Energy level of a trap (recombination centre) in the gap | eV |
| Ea | Activation energy of dopant diffusion | eV; about 3–4 eV |
| f(E) | Fermi–Dirac function: probability that a state at energy E is occupied | dimensionless, 0 to 1 |
| g(E), gc, gv | Density of states: allowed states per unit energy per unit volume | states/(eV·cm3) |
| Nc | Effective density of states in the conduction band | cm−3; Si 2.8×1019 at 300 K |
| Nv | Effective density of states in the valence band | cm−3; Si 1.04×1019 at 300 K |
| n | Electron concentration (free electrons per cm3) | cm−3 |
| p | Hole concentration (holes per cm3) | cm−3 |
| ni | Intrinsic carrier concentration (n = p = ni in pure material) | cm−3; Si ≈ 1×1010 at 300 K |
| ND | Donor concentration | cm−3 |
| NA | Acceptor concentration | cm−3 |
| Δn, Δp | Excess electron and hole concentrations above equilibrium | cm−3 |
| m∗, mn∗, mp∗ | Effective mass of electrons or holes | kg, or as a multiple of m0 |
| ψ | Wave function (¦ψ¦2 is the probability density) | — |
| α (Kronig–Penney) | √(2mE)/ħ, set by the electron energy | m−1 |
| P (Kronig–Penney) | Barrier strength mV0ba/ħ2 | dimensionless |
| λ | Wavelength | μm or nm; λ(μm) = 1.24/E(eV) |
| (h k l), {h k l} | Miller indices of a plane; family of equivalent planes | integers |
| Cs | Surface concentration of a diffusion (or solid concentration when freezing) | cm−3 |
| C(x, t) | Dopant concentration at depth x and time t | cm−3 |
| D | Diffusion coefficient (dopants in a furnace, or carriers) | cm2/s |
| D0 | Diffusion constant in D = D0e−Ea/kT | cm2/s |
| F | Particle flux in Fick's law | particles/(cm2·s) |
| Q | Dose: dopant atoms per unit area (in Weeks 13–14, Q also means charge) | atoms/cm2 (C or C/cm2 for charge) |
| erfc | Complementary error function, erfc(u) = 1 − erf(u); read from a table | dimensionless |
| Rp | Projected range: average depth at which implanted ions stop | μm |
| Rs | Sheet resistance (or diode series resistance in Week 12) | Ω/□ (ohms per square); Ω |
| μ, μn, μp | Mobility: drift velocity per unit field (electrons, holes) | cm2/(V·s); Si μn 1350, μp 480 |
| vd | Drift velocity | cm/s |
| vsat | Saturation velocity at high field | ≈ 107 cm/s in Si |
| σ | Conductivity, q(nμn + pμp) (in Week 8, σ is also a capture cross-section) | S/cm (siemens per cm) |
| ρ | Resistivity, 1/σ | Ω·cm |
| J, Jn, Jp | Current density (total, electrons, holes) | A/cm2 |
| Dn, Dp | Diffusion coefficients of electrons and holes | cm2/s; Si 35 and 12.4 |
| Te | Electron temperature of hot carriers | K |
| G, GL | Generation rate of electron–hole pairs (GL: by light) | cm−3s−1 |
| R | Recombination rate | cm−3s−1 |
| U | Net recombination rate, R − G | cm−3s−1 |
| τ, τn, τp | Minority-carrier lifetime (τeff: effective, including surfaces) | s; Si 1 ns – 1 ms |
| Nt | Density of traps (recombination centres) | cm−3 |
| n1, p1 | SRH parameters nie(Et − Ei)/kT and nie(Ei − Et)/kT | cm−3 |
| L, Ln, Lp | Diffusion length √(Dτ): distance a minority carrier travels before recombining | μm or cm |
| S | Surface recombination velocity | cm/s |
| Nst | Density of surface traps | cm−2 |
| Us | Recombination rate per unit area at a surface | cm−2s−1 |
| Vbi | Built-in potential of a junction or Schottky contact | V; typically 0.5–1 V |
| W | Depletion-region width (in Week 13 WB, WE are base and emitter widths; in Week 14 W is channel width) | μm or cm |
| Is, Js (IS) | Saturation current (density) of a diode or transistor | A; A/cm2 |
| I | Current | A |
| η | Ideality factor of a diode, 1 (ideal) to 2 | dimensionless |
| C, Cj | Capacitance (junction or depletion capacitance) | F (pF = 10−12 F) |
| Φm | Work function of a metal | eV; Al 4.28, Au 5.1 |
| Φs | Work function of a semiconductor, χ + (Ec − EF) | eV |
| χ | Electron affinity: energy from Ec up to the vacuum level | eV; Si 4.05 |
| ΦB | Schottky barrier height seen from the metal | eV (or V) |
| β | Common-emitter current gain, IC/IB (also hFE) | dimensionless; 50–500 |
| VT (Vth) | Threshold voltage of a MOSFET | V |
| vdn, vdp | Drift velocity of electrons and holes | cm/s |
| μi, τi (μL, μI, NI) | Mobility and scattering time for one scattering mechanism (L: lattice, I: ionised impurity); NI = ionised-impurity density | cm2/(V·s); s; cm−3 |
| Gn, Gp, Rn, Rp | Generation and recombination rates of electrons and holes | cm−3s−1 |
| τb (τbulk), τsurface | Lifetime from bulk recombination only; from surface recombination only | s |
| Us, ps, Δps | Surface recombination rate; hole density and excess at the surface | cm−2s−1; cm−3 |
| pn, np | Minority-carrier density: holes on the n side, electrons on the p side | cm−3 |
| erfc(u), erfc−1 | Complementary error function, 1 − erf(u), and its inverse (read from a table) | dimensionless |
| N(x), N(W) | Doping concentration at depth x (or at the depletion edge W), from C-V profiling | cm−3 |

Abbreviations

| Abbreviation | Meaning |
| --- | --- |
| Si | Silicon |
| Ge | Germanium |
| GaAs | Gallium arsenide |
| InP | Indium phosphide |
| SiO2 | Silicon dioxide (silica), the oxide insulator |
| CB | Conduction band |
| VB | Valence band |
| III–V | Compound of Group III and Group V elements (e.g. GaAs) |
| MG-Si | Metallurgical-grade silicon (≈ 98 % pure) |
| EG-Si | Electronic-grade silicon (99.9999999 % or better) |
| CZ | Czochralski crystal growth |
| FZ | Float-zone crystal growth |
| CVD | Chemical vapour deposition |
| VPE | Vapour-phase epitaxy |
| LPE | Liquid-phase epitaxy |
| MBE | Molecular-beam epitaxy |
| MOCVD | Metal-organic chemical vapour deposition |
| UHV | Ultra-high vacuum (≈ 10−10 Torr) |
| SRH | Shockley–Read–Hall (trap-assisted) recombination |
| LDD | Lightly doped drain |
| I-V | Current–voltage (measurement or characteristic) |
| C-V | Capacitance–voltage (measurement or characteristic) |
| HEMT | High-electron-mobility transistor |
| BJT | Bipolar junction transistor |
| HBT | Heterojunction bipolar transistor |
| IC | Integrated circuit |
| VLSI | Very-large-scale integration |
| LED | Light-emitting diode |
| RF | Radio frequency |
| PGD | Postgraduate Diploma |
| LHS | Left-hand side (of an equation) |
| IR | Infrared |

## Material physics and semiconductor growth (Q1–Q13)

| Q | Key answer |
| --- | --- |
| 1 (Week 1) | Conductivity between metal and insulator, controllable by doping, T, light. Metal: no gap, σ falls with T. Insulator: gap > 4 eV. Semiconductor: gap ≈ 1 eV, two carriers, σ rises with T. |
| 2 (Week 1) | Elemental: one element, Group IV, covalent, e.g. Si, Ge. Compound: two or more elements (III–V, II–VI), tunable and often direct gap, e.g. GaAs, InP. |
| 3 (Week 1) | Abundant and cheap; excellent native SiO2; 1.12 eV gap gives low leakage to 150 °C; large perfect crystals; strong, good thermal conductor; well-understood doping. |
| 4 (Week 1) | Gaps 1.12 / 0.66 / 1.42 eV; indirect / indirect / direct; μn 1350 / 3900 / 8500. Si for ICs and power; Ge for IR and SiGe HBTs; GaAs for RF, LEDs, lasers. |
| 5 (Week 1) | Lattice = periodic array of points; crystal = lattice + basis. Structure sets bands and gap, mobility, anisotropy, doping sites, epitaxy, cleavage and defects. |
| 6 (Week 1) | Smallest integers proportional to reciprocals of intercepts. Steps: intercepts → reciprocals → clear fractions → (h k l). Infinite intercept → 0; negative → bar. |
| 7 (Week 1) | 2, 3, 1 → 1/2, 1/3, 1 → × 6 → (3 2 6). In a cubic crystal d = a/7. |
| 8 (Week 1) | Covalent: shared pairs, directional. Ionic: electron transfer, Coulomb attraction. Metallic: electron sea. Si is covalent: four sp3 bonds, tetrahedral, 109.5°. |
| 9 (Week 2) | SiO2 + 2C → MG-Si (98 %); Si + 3HCl → SiHCl3 (300 °C); fractional distillation; Siemens CVD SiHCl3 + H2 → Si + 3HCl (1100 °C) → EG-Si (9N–11N) polysilicon; then CZ/FZ. |
| 10 (Week 2) | Seed dipped into melt at 1414 °C and slowly pulled (≈ 1 mm/min) with counter-rotation; melt freezes epitaxially on seed; Dash neck removes dislocations; shoulder, body, tail. |
| 11 (Week 2) | Advantages: large diameter, dislocation-free, controlled doping, low cost, oxygen strengthens and getters. Limitations: O and C contamination from crucible (limits resistivity), axial doping variation from segregation. |
| 12 (Week 2) | VPE: gas reacts on hot substrate (SiCl4 + 2H2 → Si + 4HCl). LPE: precipitation from cooling saturated melt. MBE: atomic beams in UHV with shutters, monolayer control. |
| 13 (Week 2) | Temperature VPE 1000–1250 °C > LPE 700–900 °C > MBE 500–650 °C. Precision MBE (atomic) > VPE > LPE. Uses: VPE production Si/MOCVD LEDs; LPE LEDs, thick layers; MBE quantum wells, HEMTs. |

## Impurity control and doping (Q14–Q21)

| Q | Key answer |
| --- | --- |
| 14 (Week 3) | Controlled addition of impurities (1014–1020 cm−3). Needed because intrinsic σ is too low and T-sensitive; sets carrier type, makes junctions, sets Vbi, VT, β, contacts. |
| 15 (Week 3) | n-type: Group V donors, electrons majority, EF near Ec, n ≈ ND. p-type: Group III acceptors, holes majority, EF near Ev, p ≈ NA. |
| 16 (Week 3) | Donor: one extra valence electron, gives it to CB, becomes +, level near Ec (P, As, Sb). Acceptor: one fewer, takes an electron creating a hole, becomes −, level near Ev (B, Al, Ga, In). |
| 17 (Week 3) | Thermally activated jumps down a gradient. Vacancy (substitutional, slow: B, P, As), interstitial (fast: Au, Cu, Fe), interstitialcy. D = D0e−Ea/kT. Predeposition + drive-in. |
| 18 (Week 3) | First law F = −D∂C/∂x (flux ∝ gradient). Second law ∂C/∂t = D∂2C/∂x2 (from continuity), gives the profile's time evolution. |
| 19 (Week 3) | Constant source → C = 1020 erfc(x/2√(Dt)) cm−3. Maximum (1020) at the surface, falling monotonically with depth; penetrates as √t; dose Q = (2/√π)Cs√(Dt). |
| 20 (Week 3) | Ionised, mass-selected dopant ions accelerated (keV–MeV) into the wafer; Gaussian profile at Rp; anneal. Advantages: precise dose, independent depth, low temperature, resist masks, shallow and buried profiles. |
| 21 (Week 3) | Diffusion: high T, surface-peaked erfc/Gaussian, coupled dose/depth, no damage, cheap batch. Implant: room T, peak at Rp, ±1 % dose, damage needs anneal, channelling, costly, standard for VLSI. |

## Energy bands and carrier statistics (Q22–Q34)

| Q | Key answer |
| --- | --- |
| 22 (Week 4) | Wave nature; fixed nuclei (Born–Oppenheimer); perfect periodic potential; independent electrons in average potential; Bloch functions; Pauli principle; effective mass; Fermi–Dirac statistics. |
| 23 (Week 4) | −(ħ2/2m)d2ψ/dx2 + Vψ = Eψ. Kinetic-energy term + potential-energy term = total energy E; ¦ψ¦2 is probability density; E eigenvalues give quantisation. |
| 24 (Week 4) | Periodic square wells and barriers; Bloch condition gives P sin(αa)/αa + cos αa = cos ka. Only energies with LHS between ±1 are allowed → bands and gaps; edges at k = nπ/a. |
| 25 (Week 4) | VB: highest full band at 0 K (bond electrons, holes). CB: lowest empty band (free electrons). Gap Eg = Ec − Ev: no states. |
| 26 (Week 4) | Direct: CB min and VB max at same k, photon only, efficient light (GaAs). Indirect: different k, phonon needed, poor emitter (Si, Ge). λ = 1.24/Eg μm. |
| 27 (Week 4) | Pure, n = p = ni. n = Nce−(Ec−EF)/kT, p = Nve−(EF−Ev)/kT; multiply: ni = √(NcNv) e−Eg/2kT ∝ T3/2e−Eg/2kT. |
| 28 (Week 4) | Intrinsic: thermal only, n = p = ni, strongly T-dependent. Extrinsic: from dopants, n ≠ p, n ≈ ND or p ≈ NA, nearly T-independent. Linked by np = ni2. |
| 29 (Week 4) | n = p and np = ni2 ⇒ n = p = 1.0×1010 cm−3. |
| 30 (Week 5) | f(E) = 1/(1 + e(E−EF)/kT): occupation probability of a state; ½ at EF. Gives n and p, defines EF, constant EF in equilibrium sets junction physics. |
| 31 (Week 5) | At 0 K f is a step: 1 below EF, 0 above. VB full, CB empty, pure semiconductor is an insulator. |
| 32 (Week 5) | g(E) = states per unit energy per unit volume, gc ∝ (mn∗)3/2√(E − Ec). n = ∫g f dE; gives Nc, Nv; zero in gap. |
| 33 (Week 5) | n-type: EF rises toward Ec, EF − Ei = kT ln(ND/ni). p-type: falls toward Ev. 60 mV per decade; degenerate at very high doping; returns to Ei at high T. |
| 34 (Week 4) | n ≈ ND = 5×1016 cm−3. (p = 2×103 cm−3; EF − Ei = 0.40 eV in Si.) |

## Carrier transport and injection (Q35–Q46)

| Q | Key answer |
| --- | --- |
| 35 (Week 7) | μ = vd/E = qτ/m∗. Depends on effective mass, temperature (lattice T−3/2, impurity T3/2), doping, field, defects, surfaces, orientation, strain. |
| 36 (Week 7) | Lattice (acoustic, optical, polar phonons), ionised impurity, neutral impurity, carrier–carrier, defects, surface roughness, alloy, intervalley. Matthiessen 1/μ = Σ1/μi. |
| 37 (Week 7) | vdn = −μnE, vdp = μpE; J = ρv: Jn = qnμnE, Jp = qpμpE; J = q(nμn + pμp)E, σ = q(nμn + pμp). |
| 38 (Week 7) | J = qnμE = 1.602×10−19 × 2×1016 × 1350 × 10 = 43.3 A/cm2. |
| 39 (Week 7) | Current from carriers moving down a concentration gradient by random motion. Fick: F = −D dC/dx. Jn = qDn dn/dx, Jp = −qDp dp/dx. |
| 40 (Week 7) | D/μ = kT/q (0.0259 V). From zero equilibrium current in a non-uniform sample. Si: Dn = 35, Dp = 12.4 cm2/s. |
| 41 (Week 8) | High field: optical-phonon emission caps vd at vsat ≈ 107 cm/s. Hot carriers (Te ≫ T): impact ionisation, avalanche, oxide injection and VT drift, substrate current; LDD as cure. |
| 42 (Week 8) | Generation creates e–h pairs (thermal, optical, impact); recombination annihilates them (radiative, SRH, Auger, surface). Equal in equilibrium; net U = Δp/τ. |
| 43 (Week 8) | Recombination via mid-gap trap: capture/emission of electrons and holes. U = (np − ni2)/[τp(n + n1) + τn(p + p1)]; maximum for Et ≈ Ei; τ = 1/σvthNt. |
| 44 (Week 8) | Average time an excess minority carrier survives: Δp(t) = Δp(0)e−t/τ. Sets L = √(Dτ), diode leakage, switching speed, BJT gain, solar-cell efficiency. |
| 45 (Week 9) | ∂p/∂t = −(1/q)∂Jp/∂x + G − R; minority form ∂Δp/∂t = D∂2Δp/∂x2 − Δp/τ + G. Used for diodes (exponential profile), BJTs, lifetime and Haynes–Shockley, solar cells. |
| 46 (Week 9) | S defined by Us = SΔps (cm/s), S = σvthNst. Dangling-bond surface states are SRH centres: 1/τeff = 1/τb + 2S/W. Passivate with SiO2, SiNx, Al2O3. |

## Junctions, interfaces and characterisation (Q47–Q50)

| Q | Key answer |
| --- | --- |
| 47 (Week 10) | Diffusion of carriers uncovers fixed ions → depletion region and field; drift balances diffusion; flat EF. Vbi = (kT/q) ln(NAND/ni2); W = √(2εsVbi(NA + ND)/qNAND). |
| 48 (Week 10) | Assumptions; law of junction pn = pn0eqV/kT; diffusion equation → exponential decay over Lp; currents at edges; I = Is(eqV/kT − 1), Js = qni2(Dp/LpND + Dn/LnNA). Forward: exponential rise; reverse: −Is. |
| 49 (Week 11) | Schottky: Φm > Φs (n-type), upward bending, depletion, barrier ΦB = Φm − χ, rectifying, thermionic, fast. Ohmic: Φm < Φs or heavy doping, accumulation or tunnelling, linear I-V. |
| 50 (Week 12) | I-V: ln I vs V gives Is, η, Rs, breakdown, ΦB. C-V: C = εsA/W; 1/C2 = 2(Vbi − V)/(qεsNA2); slope gives N = 2/(qεsA2·slope), intercept gives Vbi; local slope gives profile N(W). |

Revision & Practicals

# Laboratory and Practical Component

The course plan requires at least four practical or simulation experiments (3 hours/week). Each practical below gives the aim, theory, procedure, a results table and the analysis. The readings in the tables are example values that show what correct results look like; replace them with your own measurements.

## Symbols and abbreviations used on this page

Every symbol, constant and abbreviation on this page is listed here, even if an earlier week already defined it, so you can study this page on its own.

Constants and units

| Symbol | Meaning | Units / typical value |
| --- | --- | --- |
| q | Magnitude of the electronic charge | 1.6×10−19 C |
| k | Boltzmann constant | 8.617×10−5 eV/K = 1.381×10−23 J/K |
| kT | Thermal energy | 0.0259 eV (often 0.02585 eV) at 300 K |
| kT/q | Thermal voltage | 0.0259 V (about 26 mV) at 300 K |
| T | Absolute temperature | kelvin (K); room temperature = 300 K |
| εs (εsi) | Permittivity of silicon, 11.7ε0 | 1.04×10−12 F/cm |
| eV | Electron-volt, a unit of energy | 1 eV = 1.6×10−19 J |
| μm | Micrometre (micron) | 1 μm = 10−4 cm = 10−6 m |

Symbols

| Symbol | Meaning | Units / typical value |
| --- | --- | --- |
| Eg | Band-gap energy, Ec − Ev | eV; Si 1.12, Ge 0.66, GaAs 1.42 at 300 K |
| EF | Fermi level: the energy at which a state has a 50 % chance of being occupied | eV |
| Ei | Intrinsic Fermi level, close to mid-gap | eV |
| Nc | Effective density of states in the conduction band | cm−3; Si 2.8×1019 at 300 K |
| Nv | Effective density of states in the valence band | cm−3; Si 1.04×1019 at 300 K |
| n | Electron concentration (free electrons per cm3) | cm−3 |
| ni | Intrinsic carrier concentration (n = p = ni in pure material) | cm−3; Si ≈ 1×1010 at 300 K |
| ND | Donor concentration | cm−3 |
| C(x, t) | Dopant concentration at depth x and time t | cm−3 |
| Rs | Sheet resistance (or diode series resistance in Week 12) | Ω/□ (ohms per square); Ω |
| μ, μn, μp | Mobility: drift velocity per unit field (electrons, holes) | cm2/(V·s); Si μn 1350, μp 480 |
| Vbi | Built-in potential of a junction or Schottky contact | V; typically 0.5–1 V |
| V, Va | Applied voltage (positive for forward bias) | V |
| W | Depletion-region width (in Week 13 WB, WE are base and emitter widths; in Week 14 W is channel width) | μm or cm |
| Is, Js (IS) | Saturation current (density) of a diode or transistor | A; A/cm2 |
| I | Current | A |
| A (area) | Device or contact area | cm2 |
| η | Ideality factor of a diode, 1 (ideal) to 2 | dimensionless |
| C, Cj | Capacitance (junction or depletion capacitance) | F (pF = 10−12 F) |
| ΦB | Schottky barrier height seen from the metal | eV (or V) |
| A∗∗ | Effective Richardson constant | A/(cm2·K2); n-Si ≈ 110 |
| Cox | Gate-oxide capacitance per unit area, εox/tox | F/cm2 |
| VT (Vth) | Threshold voltage of a MOSFET | V |
| VFB | Flat-band voltage | V |
| VGS, VDS, VSB, VG | Gate–source, drain–source, source–body and gate voltages | V |
| ID | Drain current | A (mA) |
| W/L | Channel width-to-length ratio | dimensionless |
| gm | Transconductance, ∂ID/∂VGS | S (A/V) |
| k (MOSFET) | Device parameter μnCox(W/L) | A/V2 (mA/V2) |
| ΔID, ΔVGS | Small changes in drain current and gate voltage (their ratio is gm) | A; V |
| N(x), N(W) | Doping concentration at depth x (or at the depletion edge W), from C-V profiling | cm−3 |
| ΔV, ΔVBE | A small change in a voltage | V |

Abbreviations

| Abbreviation | Meaning |
| --- | --- |
| Si | Silicon |
| Ge | Germanium |
| SiO2 | Silicon dioxide (silica), the oxide insulator |
| I-V | Current–voltage (measurement or characteristic) |
| C-V | Capacitance–voltage (measurement or characteristic) |
| LCR | Inductance–capacitance–resistance meter |
| SMU | Source-measure unit |
| MOS | Metal–oxide–semiconductor |
| MOSFET | Metal–oxide–semiconductor field-effect transistor |
| DC | Direct current (steady) |
| AC | Alternating current (small signal) |
| n+ | Very heavily doped n-type (similarly p+) |
| MATLAB | A numerical computing program (alternative to Python) |

## Key terms

Every important word used on this page is defined here, so you can do these practicals without first rereading the weeks they come from.

Fermi level (EF) and intrinsic level (Ei). The Fermi level is the energy at which a state has a 50 % chance of being occupied by an electron. The intrinsic level Ei is where EF lies in pure silicon, close to mid-gap; in n-type material EF lies above Ei by kT ln(n/ni).

Intrinsic temperature. The temperature at which the thermally generated carrier concentration ni rises to equal the doping, so the material stops behaving as doped and EF falls back to mid-gap. Above it a device no longer works properly.

I-V characteristic. A graph of a device's current against the voltage across it. A semi-log plot shows ln I (or log10 I) against V, which turns an exponential law into a straight line.

Saturation current (Is). The small current that a diode's exponential law extrapolates to at V = 0; it is also the reverse current of an ideal diode. It is read from the intercept of the semi-log plot.

Ideality factor (η). A number between 1 and 2 that says how closely a diode follows the ideal exponential law; it is found from the slope of the semi-log plot.

I = Is[ eqV/ηkT − 1 ], η = (q/kT) / slope of ln I against V

Where:

- I = diode current (A); Is = saturation current (A)

- V = voltage across the diode (V)

- η = ideality factor (dimensionless): 1 for pure diffusion current, nearer 2 when recombination in the depletion region dominates

- kT/q = thermal voltage, 0.0259 V at 300 K

Why it matters: η close to 1 shows a good-quality junction; a larger value points to defects or surface leakage.

Series resistance (Rs). The resistance of the bulk semiconductor, contacts and leads in series with the junction. At high current it adds a voltage drop IRs, so the semi-log plot bends away from a straight line.

Rs = ΔV / I

Where:

- Rs = series resistance (Ω)

- ΔV = extra voltage above the extrapolated straight line at current I (V)

- I = forward current at that point (A)

Schottky diode and barrier height (ΦB). A Schottky diode is a rectifying metal–semiconductor contact whose current is carried by majority carriers crossing an energy barrier of height ΦB. A lower ΦB gives a larger Is, a lower turn-on voltage and a larger reverse leakage than a p-n diode.

Turn-on voltage and reverse leakage current. The turn-on voltage is the forward voltage at which a diode's current becomes noticeable (about 0.6 V for a Si p-n diode, 0.2–0.3 V for a Schottky diode). The reverse leakage current is the small current that flows under reverse bias.

Depletion capacitance (C, Cj). The capacitance of a reverse-biased junction: the depletion region of width W acts as the insulating layer between two conducting plates, so C = εsA/W, and C falls as the reverse bias widens the depletion region.

Built-in potential (Vbi). The voltage across a junction's depletion region in equilibrium, typically 0.5–1 V for Si; in C-V profiling it is the voltage at which the straight line of 1/C2 reaches zero.

C-V profiling and the Mott–Schottky plot. C-V profiling is measuring a junction's capacitance against reverse bias to find its doping. A Mott–Schottky plot is the graph of 1/C2 against V: its slope gives the doping N and its intercept gives Vbi. A straight line means uniform doping.

One-sided junction. A junction with one side far more heavily doped than the other (p+n or n+p, or a Schottky contact), so the depletion region lies almost entirely in the lightly doped side and C-V gives that side's doping.

LCR meter. An instrument that measures inductance (L), capacitance (C) and resistance (R) by applying a small AC test signal (here 20–50 mV at 1 MHz), usually with an adjustable DC bias added.

Open-circuit correction (nulling). Measuring the test fixture with no device in place and subtracting that stray capacitance from every later reading, so only the device's capacitance is recorded.

Source-measure unit (SMU) and parameter analyser. An SMU is a precision instrument that applies a chosen voltage (or current) and measures the resulting current (or voltage) at the same time. A semiconductor parameter analyser contains several SMUs and sweeps them automatically to record device characteristics.

Threshold voltage (VT). The gate-to-source voltage at which a MOSFET's channel forms and drain current begins to flow. Here it is found by drawing a straight line through the steepest part of the transfer curve and extending it to ID = 0 (linear extrapolation).

Flat-band voltage (VFB). The gate voltage at which the energy bands in a MOS structure are flat up to the surface (no surface charge). It is the starting point of the threshold voltage, which adds the voltage needed to bend the bands to inversion and to hold the depletion charge.

Transfer and output characteristics. The transfer characteristic is ID plotted against VGS at fixed VDS; the output characteristics are ID against VDS for several fixed values of VGS.

Transconductance (gm). The change in drain current per unit change in gate voltage, measured as the slope of the transfer curve, in siemens (A/V).

gm = ΔID/ΔVGS

Where:

- gm = transconductance (S)

- ΔID = small change in drain current (A)

- ΔVGS = small change in gate-to-source voltage that causes it (V)

Channel (effective) mobility. The mobility of electrons in the thin MOSFET channel, worked out from the measured gm. It is well below the bulk mobility (1350 cm2/V·s in Si) because the electrons scatter off the Si/SiO2 interface, and it falls further at high gate voltage (mobility degradation).

## Practical 1 — Simulation of carrier transport: Fermi-level shifts in Python

Aim. Model how the Fermi level of silicon moves with temperature and with doping, and find the temperature at which a doped sample becomes intrinsic.

Theory (Weeks 4–5).

ni(T) = √(NcNv) e−Eg(T)/2kT, Nc, Nv ∝ T3/2, Eg(T) = 1.17 − 4.73×10−4T2/(T + 636) eV
n = ND/2 + √((ND/2)2 + ni2) (complete ionisation)
EF − Ei = kT ln(n/ni)

Where:

- ni(T) = intrinsic carrier concentration at temperature T (cm−3)

- Nc, Nv = effective densities of states in the conduction and valence bands, 2.8×1019 and 1.04×1019 cm−3 at 300 K

- Eg(T) = band gap of Si at temperature T (eV); T = absolute temperature (K)

- k = Boltzmann constant, 8.617×10−5 eV/K; kT = thermal energy (eV)

- n = electron concentration (cm−3); ND = donor concentration (cm−3)

- EF − Ei = height of the Fermi level above the intrinsic level (eV)

Procedure.

- Run the script below (Python 3 with NumPy and Matplotlib; the same steps work in MATLAB).

- Plot EF − Ei against T from 200 K to 700 K for ND = 1014, 1015, 1016 and 1017 cm−3.

- Plot EF − Ei against ND at 300 K from 1014 to 1018 cm−3 and measure the slope per decade.

- For each doping, record the temperature at which ni = ND.

import numpy as np
import matplotlib.pyplot as plt

k = 8.617e-5                       # Boltzmann constant, eV/K
Nc300, Nv300 = 2.8e19, 1.04e19     # effective densities of states at 300 K, cm^-3

def Eg(T):                         # silicon band gap, eV (Varshni)
    return 1.17 - 4.73e-4 * T**2 / (T + 636)

def ni(T):
    Nc = Nc300 * (T / 300)**1.5
    Nv = Nv300 * (T / 300)**1.5
    raw = np.sqrt(Nc * Nv) * np.exp(-Eg(T) / (2 * k * T))
    return raw * 1e10 / ni_raw300  # scale so n_i(300 K) = 1e10 cm^-3

ni_raw300 = np.sqrt(Nc300 * Nv300) * np.exp(-Eg(300) / (2 * k * 300))

def EF_minus_Ei(T, ND):
    n = ND / 2 + np.sqrt((ND / 2)**2 + ni(T)**2)
    return k * T * np.log(n / ni(T))

T = np.linspace(200, 700, 501)
for ND in (1e14, 1e15, 1e16, 1e17):
    plt.plot(T, EF_minus_Ei(T, ND), label=f"N_D = {ND:.0e} cm^-3")
    Tint = T[np.argmin(abs(ni(T) - ND))]
    print(f"N_D = {ND:.0e}: E_F - E_i at 300 K = {EF_minus_Ei(300, ND):.3f} eV, "
          f"n_i = N_D at about {Tint:.0f} K")
plt.xlabel("T (K)"); plt.ylabel("E_F - E_i (eV)"); plt.legend(); plt.grid()
plt.show()

slope = (EF_minus_Ei(300, 1e17) - EF_minus_Ei(300, 1e16))
print(f"Shift per decade of doping at 300 K: {1000 * slope:.1f} mV")

Results (output of the script):

| ND (cm−3) | EF − Ei at 300 K (eV) | Temperature where ni = ND |
| --- | --- | --- |
| 1014 | 0.238 | ≈ 470 K |
| 1015 | 0.298 | ≈ 550 K |
| 1016 | 0.357 | ≈ 650 K |
| 1017 | 0.417 | above 700 K |

Shift per decade of doping at 300 K: 59.5 mV (= kT ln 10).

Output of Practical 1: Fermi level against temperature for silicon. Each curve falls towards zero (mid-gap) once ni approaches ND.

Discussion points. (1) Why does the curve flatten near zero at high T? (2) Why does heavier doping raise the maximum operating temperature? (3) What would change for germanium (Eg = 0.66 eV)? Germanium reaches ni = 1015 cm−3 at only about 400 K, which is why Ge devices fail at modest temperatures.

## Practical 2 — I-V characterisation of a p-n junction and a Schottky diode

Aim. Measure and plot the forward and reverse characteristics of a silicon p-n diode (e.g. 1N4148) and a Schottky diode (e.g. 1N5817 or BAT85); extract the saturation current, ideality factor and series resistance, and compare the two.

Theory (Weeks 10–12). I = Is[exp(qV/ηkT) − 1]. Above about 0.1 V, ln I = ln Is + qV/(ηkT), so a semi-log plot is a straight line with slope q/(ηkT) and intercept ln Is.

Apparatus. DC supply (0–10 V) or source-measure unit, series resistor (1 kΩ for forward, none for reverse), two digital multimeters, breadboard, diodes.

Procedure.

- Connect supply → resistor → diode (anode to +). Measure the diode voltage V and the current I (from the resistor voltage, or an ammeter).

- Forward: increase the supply so that V rises from 0 to 0.8 V (p-n) or 0 to 0.5 V (Schottky) in 0.05 V steps. Do not exceed the rated current.

- Reverse: reverse the diode, remove the resistor (or use 100 kΩ) and step V from 0 to −10 V, reading the small reverse current (μA range for Schottky, nA range for p-n).

- Plot I against V on linear axes, and ln I (or log10 I) against V for the forward branch.

Example readings (forward):

| V (V) | I, p-n diode | I, Schottky diode |
| --- | --- | --- |
| 0.15 | 0.003 μA | 0.016 mA |
| 0.20 | 0.02 μA | 0.10 mA |
| 0.25 | 0.13 μA | 0.63 mA |
| 0.30 | 0.9 μA | 4.0 mA |
| 0.35 | 5.7 μA | 25 mA |
| 0.40 | 40 μA | (beyond rating) |
| 0.50 | 1.7 mA | — |
| 0.60 | 45 mA (bending: series resistance) | — |

Analysis.

- From the straight part of the p-n semi-log plot: between 0.3 V and 0.4 V, I rises from 0.9 μA to 40 μA, a factor of 44.4, so ln(44.4) = 3.79 per 0.1 V, slope = 37.9 V−1. Then η = 1/(0.0259 × 37.9) = 1.02. Extrapolating to V = 0: Is = 0.9 μA / e3.79×3 ≈ 1×10−11 A.

- Schottky diode: between 0.25 V and 0.35 V the current rises 40 times per 0.1 V, giving η ≈ 1.05 and Is ≈ 0.1 mA / e0.20/0.0272 ≈ 6×10−8 A. It reaches a given current at about 0.25–0.3 V lower voltage than the p-n diode; Is is several orders of magnitude larger, and the reverse current is much larger (μA instead of nA).

- At high current the curves bend away from the straight line: the extra voltage is IRs. Rs = ΔV/I where ΔV is the deviation from the extrapolated line.

- Schottky barrier height: ΦB = (kT/q) ln(A∗∗AT2/Is), using the diode area A from the datasheet.

Discussion. Explain the lower turn-on voltage and higher leakage of the Schottky diode in terms of majority-carrier thermionic emission over ΦB versus minority-carrier diffusion (Weeks 10–11).

## Practical 3 — C-V profiling: doping and built-in potential

Aim. Measure the capacitance of a reverse-biased one-sided junction (a varactor such as BB112, or a Schottky diode) against bias, and extract the doping concentration and the built-in potential.

Theory (Week 12).

C = A √( qεsN / 2(Vbi − V) ) ⇒ 1/C2 = 2(Vbi − V)/(qεsNA2)

Where:

- C = depletion capacitance (F)

- A = junction area (cm2)

- q = electronic charge, 1.6×10−19 C

- εs = permittivity of silicon, 1.04×10−12 F/cm

- N = doping of the lightly doped side (cm−3)

- Vbi = built-in potential (V); V = applied voltage, negative in reverse bias (V)

The plot of 1/C2 against V is a straight line: the slope gives N, the voltage intercept gives Vbi.

Apparatus. LCR meter with DC bias (1 MHz, 20–50 mV AC level), or a capacitance bridge; DC supply; shielded test fixture.

Procedure.

- Null the fixture with the device removed (open-circuit correction) to remove stray capacitance.

- Connect the diode in reverse bias. Record C at V = 0, −1, −2, … −5 V (or the device's rated range).

- Plot C against V and 1/C2 against V. Fit a straight line to 1/C2.

- Take the area A from the datasheet (or measure the contact diameter).

Example readings (A = 1.0×10−3 cm2, Si):

| V (V) | C (pF) | 1/C2 (F−2) |
| --- | --- | --- |
| 0 | 37.2 | 7.2×1020 |
| −1 | 22.8 | 1.92×1021 |
| −2 | 17.9 | 3.12×1021 |
| −3 | 15.2 | 4.33×1021 |
| −4 | 13.4 | 5.57×1021 |
| −5 | 12.2 | 6.72×1021 |

Analysis.

Slope: (6.72×1021 − 7.2×1020)/(−5 − 0) = −1.20×1021 F−2V−1
N = 2/(qεsA2|slope|) = 2/(1.602×10−19 × 1.036×10−12 × 10−6 × 1.20×1021) = 1.0×1016 cm−3
Intercept: 1/C2 = 0 at V = 7.2×1020/1.20×1021 = +0.60 V ⇒ Vbi = 0.60 V
Depletion depth at −5 V: W = εsA/C = 1.036×10−15/12.2×10−12 = 0.85 μm

Mott–Schottky plot of the example readings. A straight line means uniform doping; curvature would reveal a doping profile N(W).

Discussion. Why must the junction be one-sided? What would curvature in 1/C2 tell you? Why measure in reverse bias only?

## Practical 4 — MOSFET parameter extraction: threshold voltage and channel mobility

Aim. Measure the transfer and output characteristics of an n-channel enhancement MOSFET (e.g. a CD4007 array transistor or 2N7000) and extract Vth, μn and the transconductance.

Theory (Week 14). In the linear region at small VDS:

ID ≈ μnCox(W/L)[(VGS − VT)VDS − VDS2/2]

Where:

- ID = drain current (A)

- μn = channel electron mobility (cm2/V·s)

- Cox = gate-oxide capacitance per unit area (F/cm2)

- W/L = channel width-to-length ratio

- VGS, VDS = gate–source and drain–source voltages (V); VT = threshold voltage (V)

so ID against VGS is a straight line of slope gm = μnCox(W/L)VDS that meets ID = 0 at VGS = VT + VDS/2. In saturation, √ID = √(μnCoxW/2L)(VGS − VT).

Apparatus. Two DC supplies (or a semiconductor parameter analyser), ammeter, voltmeters. Cox, W and L from the datasheet or test structure.

Procedure.

- Transfer curve (linear): set VDS = 0.1 V. Step VGS from 0 to 2.5 V in 0.25 V steps; record ID.

- Transfer curve (saturation): set VDS = VGS (gate tied to drain) and repeat; plot √ID against VGS.

- Output curves: for VGS = 1.0, 1.5, 2.0 V, sweep VDS from 0 to 3 V; record ID.

- Find VT by linear extrapolation at the point of maximum slope; find μn from the slope.

Example readings (linear region, VDS = 0.1 V; device with Cox = 3.45×10−7 F/cm2, W/L = 10):

| VGS (V) | 0.5 | 1.0 | 1.5 | 2.0 | 2.5 |
| --- | --- | --- | --- | --- | --- |
| ID (μA) | 15 | 84 | 153 | 222 | 291 |

Analysis.

gm = ΔID/ΔVGS = (291 − 84) μA / 1.5 V = 1.38×10−4 S
Line through (1.0 V, 84 μA): ID = 0 at VGS = 1.0 − 84/138 = 0.39 V
VT = 0.39 − VDS/2 = 0.39 − 0.05 = 0.34 V
μn = gm L / (W Cox VDS) = 1.38×10−4 / (10 × 3.45×10−7 × 0.1) = 400 cm2/V·s

The channel mobility (400) is about a third of bulk electron mobility in Si (1350) because of surface scattering at the Si/SiO2 interface (Week 7). At high VGS the measured slope falls further (mobility degradation by the vertical field), so the extraction uses the maximum-slope point.

Discussion. Compare VT from the linear and saturation methods. Why does mobility degrade at high gate voltage? How would a thicker oxide change VT and gm?

## Report format

For each practical: title and aim; brief theory with the equations used; circuit diagram; apparatus; procedure; tables of readings with units; graphs (labelled axes, units, fitted lines); calculations; results with uncertainties; discussion of sources of error (lead resistance, stray capacitance, self-heating, meter resolution); conclusion.

Revision & Practicals

# Glossary — Key Terms, Symbols, Constants and Abbreviations

Every key term, symbol, constant and abbreviation used anywhere in the course. Each week also has its own Key terms section and symbols table near the top, listing what that week uses.

## Key terms A–Z

| Term | Meaning | Defined in |
| --- | --- | --- |
| Acceptor | A dopant atom with one fewer valence electron than silicon, such as boron or gallium (Group III). It takes an electron from a neighbouring bond, leaving behind a fixed negative ion and a mobile empty bond called a hole, which behaves like a positive charge carrier. | Week 3 |
| Accumulation | The state of a MOS capacitor on p-type silicon when the gate is negative: extra holes (majority carriers) are pulled to the surface. | Week 14 |
| Accumulation layer | A thin layer at the interface with extra majority carriers (the opposite of depletion). The bands bend downward in n-type, and there is no barrier. | Week 11 |
| Annealing | Heating a wafer after implantation to repair the crystal damage caused by the ions and to move dopant atoms onto proper lattice sites, where they become electrically active. | Week 3 |
| Arrhenius plot | A graph of the logarithm of a temperature-dependent quantity against 1/T. A process with an energy barrier gives a straight line whose slope gives the barrier energy. | Week 12 |
| Atomic packing factor (APF) | The fraction of the unit-cell volume filled by atoms, treated as hard spheres that touch their nearest neighbours. | Week 6 |
| Background doping (NB) | The doping the wafer already had before the new dopant was added, usually of the opposite type (cm−3). | Week 3 |
| Band bending | The upward or downward curving of Ec and Ev near the interface, caused by the voltage across the depletion (or accumulation) region. Upward bending in n-type = a barrier to electrons. | Week 11 |
| Band gap (Eg) | The range of energies between the top of the valence band and the bottom of the conduction band in which no electron states exist. It is the minimum energy needed to free an electron from a bond. | Week 1, Week 4, Week 5, Week 6, Week 7, Week 8, Week 9, Week 10, Week 11 |
| Base transport factor (αT) | The fraction of the carriers injected into the base that cross it without recombining and reach the collector. | Week 13 |
| Bipolar junction transistor (BJT) | A three-terminal device made of three alternately doped regions, emitter (E), base (B) and collector (C), forming two back-to-back p-n junctions. It is called bipolar because both electrons and holes carry current. It is built as NPN or PNP. | Week 13 |
| Bipolar junction transistor (BJT) and current gains (α, β) | A three-layer (n-p-n or p-n-p) device in which a small base current controls a much larger collector current. α = IC/IE is the common-base gain (just below 1); β = IC/IB = α/(1 − α) is the common-emitter gain (typically 50–500). | Week 15 |
| Body effect | The rise in threshold voltage that occurs when the source is at a higher voltage than the substrate (body), because a wider depletion region must then be supported before inversion. | Week 14 |
| Boltzmann (Maxwell–Boltzmann) approximation | The simpler form f(E) ≈ e−(E − EF)/kT, accurate to about 5 % or better when the state is more than about 3kT above EF. | Week 5 |
| Breakdown (VBR) | The sudden, large rise of reverse current at a high enough reverse voltage VBR, caused either by avalanche multiplication or by Zener tunnelling. It is not destructive if the current is limited. | Week 10 |
| Built-in potential (Vbi) | The voltage that appears across the depletion region in equilibrium, created by the fixed ion charges. It is the barrier that stops further diffusion of majority carriers. | Week 10, Week 11, Week 12, Week 15, Laboratory |
| Bulk Fermi potential (φF) | How far, in volts, the Fermi level lies below the intrinsic level deep inside a p-type substrate. | Week 14 |
| C-V characterisation | Measuring the small-signal capacitance of a reverse-biased junction, Schottky diode or MOS capacitor as the DC bias is stepped, to find the doping, its profile with depth and the built-in potential. | Week 12 |
| C-V profiling | Measuring a reverse-biased junction's capacitance C against voltage V. A plot of 1/C2 against V is a straight line whose slope gives the doping and whose voltage intercept gives Vbi. | Week 15 |
| C-V profiling and the Mott–Schottky plot | C-V profiling is measuring a junction's capacitance against reverse bias to find its doping. A Mott–Schottky plot is the graph of 1/C2 against V: its slope gives the doping N and its intercept gives Vbi. A straight line means uniform doping. | Laboratory |
| Channel (effective) mobility | The mobility of electrons in the thin MOSFET channel, worked out from the measured gm. It is well below the bulk mobility (1350 cm2/V·s in Si) because the electrons scatter off the Si/SiO2 interface, and it falls further at high gate voltage (mobility degradation). | Laboratory |
| Channelling | The unwanted travel of implanted ions far deeper than Rp along open "channels" between rows of atoms in the crystal. It is avoided by tilting the wafer about 7° or covering it with a thin non-crystalline layer. | Week 3 |
| Charge neutrality and compensation | Charge neutrality is the rule that a uniform piece of semiconductor has no net charge, so positive charges (holes, ionised donors) equal negative charges (electrons, ionised acceptors). Compensation is the partial cancelling of donors and acceptors when both are present; the material behaves as if doped with the difference, ND − NA or NA − ND. | Week 5 |
| Chemical vapour deposition (CVD) | Growing a solid film from gases that react or decompose on a hot surface, leaving the wanted atoms behind. The Siemens process and vapour-phase epitaxy are both CVD processes. | Week 2 |
| Common-base current gain (α) | The ratio of collector current to emitter current, α = IC/IE. It is just below 1 (typically 0.98–0.999). | Week 13 |
| Common-emitter current gain (β, hFE) | The ratio of collector current to base current, β = IC/IB; typically 50–500. | Week 13 |
| Compensated semiconductor | A semiconductor containing both donors and acceptors. They partly cancel, so the carriers are set by the difference ND − NA (or NA − ND), called the net doping. | Week 4 |
| Concentration gradient (dC/dx) | How fast the dopant concentration changes with depth. A steep gradient means a large change over a short distance. It is measured in atoms/cm4 (atoms per cm3, per cm). | Week 3 |
| Conduction band | The energy band just above the valence band, empty at 0 K. Electrons that reach it are free to move through the crystal and carry current. Its bottom edge is at energy Ec. | Week 4 |
| Conduction band edge (Ec) and valence band edge (Ev) | Ec is the lowest energy a free electron can have in the semiconductor. Ev is the highest energy of the (almost full) valence band, where holes live. | Week 11 |
| Conductivity (σ) and resistivity (ρ) | Conductivity measures how well a material carries current; resistivity is its inverse. In a semiconductor both electrons and holes contribute. | Week 1, Week 7, Week 15 |
| Continuity equation | The book-keeping equation for carriers: in any small volume, the rate of change of the carrier density equals the net inflow carried by current, plus generation, minus recombination. | Week 9 |
| Covalent bond | A bond in which two neighbouring atoms share a pair of valence electrons, one from each atom. In silicon each atom forms four covalent bonds with four neighbours, so every atom has a full outer shell of eight electrons. | Week 1 |
| Crystal lattice | A regular, repeating three-dimensional arrangement of atoms. A single crystal has the same arrangement and orientation throughout the whole piece. | Week 1, Week 6 |
| Current density (J) | The electric current flowing through each square centimetre of cross-section, in A/cm2. The current is I = JA, where A is the cross-sectional area. | Week 7 |
| Czochralski (CZ) growth | Making a large single crystal by dipping a small seed crystal into molten silicon in a quartz crucible and pulling it up slowly while rotating it. The melt freezes onto the seed and copies its crystal orientation. | Week 2 |
| Czochralski (CZ) growth and epitaxy | CZ growth pulls a large single-crystal ingot of silicon slowly out of a melt using a seed crystal. Epitaxy grows a thin new crystalline layer on top of a crystal wafer, continuing its lattice (VPE from a gas, LPE from a liquid, MBE from molecular beams in vacuum). | Week 15 |
| Dash necking | Pulling a thin neck (about 3 mm across) quickly at the start of CZ growth so that dislocations created by the thermal shock of dipping grow out of the sides, leaving the rest of the crystal dislocation-free. | Week 2 |
| Degenerate semiconductor | A very heavily doped semiconductor (above about 1018–1019 cm−3 in Si) whose Fermi level is within about 3kT of a band edge, or inside a band. The Boltzmann approximation fails and full Fermi–Dirac statistics must be used. A semiconductor with EF more than 3kT from both edges is non-degenerate. | Week 5 |
| Density of states (g(E)) | The number of allowed electron states per unit energy per unit volume at energy E, in states/(eV·cm3). It is zero inside the band gap and grows as the square root of the distance into each band. | Week 5 |
| Depletion (junction) capacitance (C, Cj) | The capacitance of a reverse-biased junction, which behaves like a parallel-plate capacitor with the depletion region as the gap between the plates. It falls as the reverse bias widens the depletion region. | Week 12, Laboratory |
| Depletion approximation | The simplifying assumption that the depletion region contains no mobile carriers at all and has sharp edges, while the regions outside it are exactly neutral. | Week 10 |
| Depletion region (W) | The thin layer on both sides of the junction that has lost almost all its mobile carriers, leaving only the fixed charged donor and acceptor ions. It is also called the space-charge region and is typically 0.1–10 μm wide. | Week 10, Week 11, Week 12, Week 14 |
| Diamond cubic structure | The crystal structure of Si and Ge: a cubic cell holding 8 atoms, each bonded covalently to 4 nearest neighbours (coordination number 4) at distance rnn = (√3/4)a. Zinc blende, the structure of GaAs, is the same arrangement with two kinds of atom alternating. | Week 6 |
| Diffusion | The net movement of atoms from where they are crowded (high concentration) to where they are sparse (low concentration), caused only by their random thermal jumping. In processing, dopants diffuse into a silicon wafer heated to about 900–1200 °C. | Week 3, Week 7, Week 13 |
| Diffusion coefficient (D) | A number that says how easily a dopant moves through the crystal. It rises steeply with temperature because each atomic jump needs a certain minimum energy, the activation energy Ea. | Week 3, Week 7, Week 9 |
| Diffusion current and the Einstein relation | Diffusion current flows when carriers spread from where they are concentrated to where they are scarce, even with no field. The diffusion coefficient D and the mobility are linked by the Einstein relation D/μ = kT/q (0.0259 V at 300 K). | Week 15 |
| Diffusion length (L) | The average distance an excess minority carrier diffuses before it recombines. | Week 9, Week 15 |
| Direct and indirect band gap | In a direct-gap material (GaAs, GaN, InP) an electron can drop from the conduction band to the valence band without changing its momentum, so it gives out its energy as light efficiently. In an indirect-gap material (Si, Ge) the drop also needs a lattice vibration (phonon), so light emission is very weak. | Week 1, Week 4, Week 6 |
| Dislocation | A line defect in a crystal, where a row of atoms is out of place. Dislocations carry leakage current and kill carriers, so device wafers must be dislocation-free. | Week 2 |
| Donor | A dopant atom with one more outer (valence) electron than the silicon atom it replaces, such as phosphorus, arsenic or antimony (Group V). The spare electron is easily set free to carry current, leaving behind a fixed positive ion. | Week 3 |
| Donor and acceptor | A donor is a dopant atom with five valence electrons (P, As, Sb in Si) that gives one free electron to the crystal and becomes a fixed positive ion. An acceptor is a dopant with three valence electrons (B, Al, Ga, In in Si) that takes an electron from a neighbouring bond, creating a hole, and becomes a fixed negative ion. | Week 1 |
| Dopant diffusion and ion implantation | The two ways of putting dopants into a wafer. In diffusion, dopant atoms spread in from the surface in a hot furnace, giving an erfc or Gaussian profile; in ion implantation, ions are fired into the wafer, giving a Gaussian profile centred at the projected range Rp. | Week 15 |
| Dopant: donor and acceptor | A donor is an impurity atom (e.g. phosphorus in Si) that gives a free electron to the conduction band; its concentration is ND. An acceptor (e.g. boron in Si) takes an electron from the valence band and so creates a hole; its concentration is NA. Both are in cm−3. | Week 4 |
| Doping | The deliberate addition of a small, controlled amount of an impurity element (the dopant) to a pure semiconductor, to set whether electrons or holes carry the current and to raise the conductivity. | Week 1, Week 3, Week 5, Week 7, Week 8, Week 9, Week 10, Week 12, Week 13, Week 14, Week 15 |
| Doping and compensation | Doping is adding a small, controlled amount of impurity: donors (e.g. P) give electrons and make the material n-type; acceptors (e.g. B) create holes and make it p-type. When both are present they partly cancel (compensation), and the material behaves as if doped with the difference, ND − NA or NA − ND. | Week 6 |
| Doping and dopant | Doping is the deliberate addition of a small, controlled amount of an impurity element (the dopant) to set the conductivity type and resistivity. Boron gives p-type silicon (holes carry the current); phosphorus, arsenic and antimony give n-type silicon (electrons carry the current). | Week 2 |
| Doping profile (N(x)) | The way the doping concentration changes with depth x below the surface, for example after diffusion or ion implantation. | Week 12 |
| Doping; n-type and p-type | Doping is adding a small, controlled amount of impurity atoms to a semiconductor. Donor atoms (e.g. phosphorus in Si, concentration ND) give free electrons and make it n-type. Acceptor atoms (e.g. boron, concentration NA) create holes and make it p-type. | Week 11 |
| Dose (Q) | The total number of dopant atoms put into the wafer under each square centimetre of surface, in atoms/cm2. It is the area under the concentration-against-depth curve. | Week 3 |
| Drift and diffusion | The two ways carriers move. Drift is motion pushed by an electric field; diffusion is the spreading of carriers from where there are many to where there are few, with no field needed. | Week 9, Week 10 |
| Drift and drift velocity (vd) | Drift is the movement of carriers caused by an electric field. The drift velocity vd is the small, steady average velocity in the field direction that is added on top of the random thermal motion. | Week 7 |
| Drift and mobility (μ) | Drift is the motion of carriers caused by an electric field. Mobility is the drift velocity per unit field, vd = μE, in cm2/(V·s); for lightly doped Si μn = 1350 and μp = 480. | Week 15 |
| Drift velocity and saturation velocity (vd, vsat) | The drift velocity is the average velocity carriers gain in an electric field; at low field it is vd = μE, where μ is the mobility (cm2/V·s). At high field it stops rising and levels off at the saturation velocity vsat, about 1×107 cm/s in silicon. | Week 8 |
| Drive-in (limited-source diffusion) | A second heating with the source removed, so the fixed dose already in the wafer spreads deeper and the surface concentration falls. It gives a Gaussian (bell-curve) profile and is used to reach the wanted depth. | Week 3 |
| Early effect and Early voltage (VA) | In the active mode, raising VCE widens the collector depletion region into the base and makes the neutral base thinner, so IC rises slightly. Extended backwards, the sloping output curves meet the VCE axis at −VA, the Early voltage. | Week 13 |
| Effective density of states (Nc, Nv) | The number of states which, if all placed exactly at the band edge (Ec or Ev), would give the same carrier concentration as the real, spread-out band. For Si at 300 K, Nc = 2.8×1019 cm−3 and Nv = 1.04×1019 cm−3. | Week 5 |
| Effective lifetime (τeff) | The lifetime actually measured in a sample, which includes losses both in the bulk and at the surfaces. It is always shorter than the bulk lifetime. | Week 9 |
| Effective mass (m∗) | The mass an electron or hole appears to have when it is pushed by a force inside a crystal. It differs from the free-electron mass because the crystal's atoms also act on the carrier; a smaller m∗ means a lighter, faster carrier. | Week 4, Week 7 |
| Effective Richardson constant (A∗∗) | The material constant in the thermionic-emission law that links a Schottky diode's saturation current density to its barrier height and temperature; about 110 A/(cm2·K2) for n-type Si. | Week 12 |
| Einstein relation | The rule that the diffusion coefficient and the mobility of a carrier are always in the same ratio, fixed only by temperature, because both are limited by the same collisions. | Week 7 |
| Electron affinity (χ) | The energy from the bottom of the conduction band up to the vacuum level. Unlike Φs, it does not change with doping, so it is a fixed property of the material: Si 4.05 eV, GaAs 4.07 eV, Ge 4.0 eV. | Week 11 |
| Electron and hole (carriers) | A free electron is an electron in the conduction band; a hole is an empty place left in the valence band, which behaves like a positive charge +q that can move. Together they are called carriers because they carry the current. | Week 7, Week 8, Week 9, Week 10, Week 14, Week 15 |
| Electron-volt (eV) | The energy an electron gains when it moves through a potential difference of one volt: 1 eV = 1.6×10−19 J. Energies of electrons in solids are almost always quoted in eV. | Week 4 |
| Electronic-grade silicon (EG-Si) | Polycrystalline silicon with no more than about one impurity atom in a billion (99.9999999 %, "9N", or better), made by distilling trichlorosilane and depositing silicon from it in the Siemens process. | Week 2 |
| Emitter injection efficiency (γ) | The fraction of the emitter current that is carried by the useful carriers injected from the emitter into the base (electrons in an NPN), rather than by carriers injected backwards from the base into the emitter. | Week 13 |
| Emitter, base and collector | The emitter is the heavily doped region that injects carriers; the base is the thin, lightly doped middle region they cross; the collector is the moderately doped region that gathers them. | Week 13 |
| Energy band | When many atoms join to form a solid, each sharp atomic energy level spreads into a wide range of closely spaced allowed energies, called a band. The valence band holds the electrons that form the bonds; the conduction band above it holds electrons that are free to move and carry current. | Week 1, Week 4 |
| Energy band and band gap (Eg) | In a crystal the allowed electron energies form bands. The valence band (top edge Ev) is normally full; the conduction band (bottom edge Ec) is normally nearly empty. The band gap Eg = Ec − Ev is the forbidden energy range between them: 1.12 eV for Si. | Week 15 |
| Enhancement and depletion mode | An enhancement-mode MOSFET has no channel at VGS = 0 and needs a gate voltage beyond VT to create one. A depletion-mode MOSFET is built with a channel already present at VGS = 0 and needs a gate voltage of the opposite sign to remove it. | Week 14 |
| Epitaxy | Growing a thin single-crystal layer on top of a single-crystal wafer so that the layer continues the wafer's crystal structure and orientation. The wafer underneath is called the substrate. Growing the same material (Si on Si) is homoepitaxy; growing a different material (AlGaAs on GaAs) is heteroepitaxy. | Week 2 |
| Excess carriers (Δn, Δp) | Electrons and holes present in addition to the equilibrium numbers, for example created by light or injected by a forward-biased junction: n = n0 + Δn and p = p0 + Δp. | Week 8, Week 9 |
| Extrinsic semiconductor (n-type, p-type) | A doped semiconductor whose carrier concentrations are set mainly by its dopants rather than by ni. n-type material has more electrons than holes; p-type has more holes than electrons. | Week 4 |
| E–k diagram (band structure) | A graph of the allowed electron energies E against the wave vector k. Its shape near the band edges sets how carriers move and whether the material emits light well. | Week 4 |
| Fermi level (EF) | The energy at which an electron state has exactly a 50 % chance of being occupied. It sits near the middle of the gap in intrinsic material, near the conduction band in n-type material and near the valence band in p-type material. | Week 1, Week 4, Week 5, Week 6, Week 7, Week 8, Week 10, Week 11, Week 15 |
| Fermi level (EF) and intrinsic level (Ei) | The Fermi level is the energy at which a state has a 50 % chance of being occupied by an electron; it is flat through a material in equilibrium. The intrinsic level Ei is where EF would sit in undoped material, close to the middle of the band gap. In p-type material EF lies below Ei; in n-type it lies above. | Week 14, Laboratory |
| Fermi-level pinning | At a real interface, defects and surface states hold ("pin") the Fermi level near a fixed energy, so the measured barrier height depends much less on the metal than the ideal rule predicts. | Week 11 |
| Fermi–Dirac distribution function (f(E)) | The probability that an allowed electron state at energy E is occupied in thermal equilibrium. | Week 5 |
| Fermi–Dirac function (f(E)) | The probability that an allowed state at energy E holds an electron in thermal equilibrium. When E − EF is more than about 3kT it can be replaced by the Boltzmann approximation f ≈ e−(E − EF)/kT. | Week 6 |
| Fick's first law | The rule that the flow of diffusing atoms is proportional to the concentration gradient, and runs from high to low concentration. | Week 3 |
| Flat-band voltage (VFB) | The gate voltage that makes the energy bands flat right up to the surface (no band bending, no surface charge). It is zero for an ideal MOS capacitor. | Week 14, Laboratory |
| Float-zone (FZ) growth | Making a single crystal by passing a narrow molten zone along a vertical polysilicon rod, without any crucible. It gives the purest, highest-resistivity silicon. | Week 2 |
| Forward and reverse bias (Va) | Forward bias makes the p side positive (Va > 0) and lowers the barrier to Vbi − Va; reverse bias makes the p side negative (Va < 0) and raises the barrier to Vbi + ¦Va¦. | Week 10, Week 13, Week 15 |
| Forward bias and reverse bias | For a metal on n-type: forward bias makes the metal positive with respect to the semiconductor (current flows easily); reverse bias makes the metal negative (only a small current flows). | Week 11 |
| Forward-active mode | The normal amplifying condition: emitter–base junction forward biased, collector–base junction reverse biased. The collector current is then set by VBE (or IB) and hardly depends on the collector voltage. | Week 13 |
| Free electron and hole | When a covalent bond breaks, the released electron can wander through the crystal (a free electron, in the conduction band), and the empty place it leaves in the bond (a hole, in the valence band) behaves as a mobile positive charge. Breaking one bond creates one electron–hole pair. | Week 1 |
| Gate-oxide capacitance (Cox) | The capacitance of the oxide layer per unit area: how much charge the gate induces in the silicon per volt. | Week 14 |
| Generation and recombination (G, R, U) | Generation is the creation of an electron–hole pair; recombination is the loss of one, when a conduction-band electron falls back into a hole. G and R are rates in pairs per cm3 per second; U = R − G is the net recombination rate. | Week 8, Week 9 |
| Hole | An empty electron state (a missing electron) in the valence band. Neighbouring electrons can move into it, so the empty state moves around and behaves like a positively charged particle that carries current. | Week 4, Week 5, Week 6 |
| Hot carriers | Carriers whose average energy, gained from a strong electric field, is far above the normal thermal energy of the crystal. Their energy is described by an electron temperature Te much higher than the lattice temperature T. | Week 8 |
| I-V characterisation | Measuring the current through a device as the applied voltage is stepped, and comparing the curve with theory to extract Is, η, Rs, leakage, breakdown and, for a Schottky diode, ΦB. | Week 12 |
| I-V characteristic | A graph of a device's current against the voltage across it. A semi-log plot shows ln I (or log10 I) against V, which turns an exponential law into a straight line. | Laboratory |
| Ideality factor (η) | A number between 1 and 2 that says how closely a real diode follows the ideal diode equation. η = 1 means the current is pure diffusion (or, in a Schottky diode, pure thermionic emission); η near 2 means recombination in the depletion region dominates. | Week 12, Laboratory |
| Impact ionisation | The process in which a hot carrier collides with the lattice hard enough to break a bond and create a new electron–hole pair. Repeated, it becomes an avalanche, which causes avalanche breakdown. | Week 8 |
| Intrinsic carrier concentration (ni) | The number of electrons (equal to the number of holes) per cm3 in pure, undoped material; about 1×1010 cm−3 in Si at 300 K. In thermal equilibrium (no light, no applied voltage, steady temperature) the electron and hole concentrations of any sample obey the mass-action law: | Week 8, Week 10, Week 15 |
| Intrinsic Fermi level (Ei) | The position of the Fermi level in an intrinsic semiconductor, where n = p. It lies very close to the middle of the band gap (13 meV below it in Si). | Week 5 |
| Intrinsic semiconductor | A pure semiconductor with no impurities deliberately added, in which every free electron comes from a broken bond and so is matched by a hole. The number of each per cm3 is the intrinsic carrier concentration, ni. | Week 1, Week 5, Week 6 |
| Intrinsic semiconductor and intrinsic carrier concentration (ni) | A pure, undoped semiconductor, in which every free electron comes from a broken bond that also leaves a hole, so the electron and hole concentrations are equal. Their common value is ni (cm−3), about 1×1010 cm−3 for Si at 300 K. Its Fermi level, the intrinsic level Ei, lies very close to the middle of the gap. | Week 4 |
| Intrinsic temperature | The temperature at which the thermally generated carrier concentration ni rises to equal the doping, so the material stops behaving as doped and EF falls back to mid-gap. Above it a device no longer works properly. | Laboratory |
| Inversion and strong inversion | Inversion is the state in which the gate has pulled so many minority electrons to the surface of p-type silicon that the surface behaves as n-type. Strong inversion is reached when the surface is as n-type as the bulk is p-type, which happens when ψs = 2φF. | Week 14 |
| Ion implantation | A doping method in which dopant atoms are turned into ions, accelerated by a high voltage and fired into the wafer, where they stop at a depth set by their energy. The dose is counted exactly from the beam current. | Week 3 |
| Junction capacitance (Cj) | The capacitance of the depletion region, which acts like a parallel-plate capacitor whose plate spacing W grows with reverse bias. | Week 10 |
| Junction depth (xj) | The depth below the surface at which the added dopant concentration has fallen to equal the background doping, so that a p-n junction forms there (μm). | Week 3, Week 15 |
| Lattice constant (a) | The edge length of the cubic unit cell, measured in ångströms (1 Å = 10−10 m). Si: 5.43 Å; Ge and GaAs: 5.65 Å. | Week 1, Week 2, Week 6 |
| Lattice mismatch (fm) | The fractional difference between the lattice constants of a grown layer and its substrate. | Week 2 |
| LCR meter | An instrument that measures inductance (L), capacitance (C) and resistance (R) by applying a small AC test signal (here 20–50 mV at 1 MHz), usually with an adjustable DC bias added. | Laboratory |
| Low-level injection | The condition in which the excess carrier concentration is much smaller than the equilibrium majority concentration (Δp ≪ n0 in n-type). The majority concentration is then almost unchanged. | Week 8, Week 9 |
| Majority and minority carriers | The carrier type present in larger numbers is the majority carrier (electrons in n-type, holes in p-type); the other type is the minority carrier. | Week 4, Week 6, Week 7, Week 8, Week 9, Week 10, Week 11, Week 12, Week 13, Week 14, Week 15 |
| Mass action law | In thermal equilibrium the product of the electron and hole concentrations is fixed at a given temperature, whatever the doping (for non-degenerate material). | Week 5, Week 6 |
| Mass-action law | In thermal equilibrium the product of the electron and hole concentrations equals ni2, whatever the doping. Raising one carrier type therefore lowers the other. | Week 4, Week 15 |
| Metal | A material with a very large number of free electrons (about 1022 cm−3), so it conducts electricity very easily. Its electron states are filled up to the Fermi level, and there are empty states immediately above it. Examples: aluminium, gold, platinum, titanium, tungsten. | Week 11 |
| Metallurgical-grade silicon (MG-Si) | Silicon about 98 % pure, made by reducing quartz with carbon in an arc furnace. Good enough for steel and aluminium alloys, far too impure for devices. | Week 2 |
| Metal–semiconductor contact (interface) | The boundary formed where a metal touches a semiconductor. Every device has several, because every device must be wired to the circuit with metal. | Week 11 |
| Miller indices (h k l) | Three whole numbers, found from the reciprocals of the points where a plane cuts the crystal axes, that name the orientation of a crystal plane. Wafers are described by them, e.g. (100) wafers for MOS chips. | Week 1, Week 6, Week 15 |
| Minority-carrier diffusion equation | The continuity equation written for minority carriers in a region with almost no electric field (a quasi-neutral region), using diffusion for the current and Δp/τ for the recombination. | Week 9 |
| Minority-carrier injection (law of the junction) | Under forward bias, majority carriers cross the lowered barrier and become minority carriers on the other side. The minority density at the edge of the depletion region rises exponentially with voltage. | Week 10 |
| Minority-carrier lifetime (τ) | The average time an excess minority carrier survives before it recombines. After the source of excess carriers is removed, the excess falls to 1/e (37 %) of its starting value in one lifetime. | Week 8, Week 9 |
| Minority-carrier lifetime and diffusion length (τ, L) | The lifetime τ is the average time an injected minority carrier survives before it recombines; the diffusion length L = √(Dτ) is the average distance it diffuses in that time (D is the diffusion coefficient, cm2/s). | Week 10, Week 13 |
| Mobility (μ) | How easily a carrier moves through the crystal: the average drift velocity it gains per unit electric field. | Week 1, Week 7 |
| Mobility and conductivity (μ, σ) | Mobility is the drift speed a carrier reaches per unit electric field, in cm2/(V·s). Conductivity measures how easily the material carries current; resistivity ρ = 1/σ is its inverse. | Week 6 |
| MOS capacitor | A metal (or polysilicon) plate on a thin oxide on a semiconductor: the gate structure of a MOSFET. Its C-V curve reveals the oxide thickness, the flat-band and threshold voltages and the quality of the oxide. | Week 12, Week 14 |
| MOS capacitor and inversion | A MOS capacitor is a gate, a thin oxide and a semiconductor stacked together. On p-type silicon a negative gate gives accumulation (more holes at the surface), a small positive gate gives depletion, and a large positive gate gives inversion: the surface fills with electrons and becomes n-type. | Week 15 |
| MOSFET (source, drain, gate, channel) | A metal–oxide–semiconductor field-effect transistor: a MOS capacitor with two heavily doped regions, the source and the drain, at either side of the gate. The inversion layer under the gate is the channel that carries current between them; the gate voltage controls it through an electric field, with no DC gate current. | Week 14 |
| MOSFET and its operating regions | A metal–oxide–semiconductor field-effect transistor: a MOS capacitor with a source and a drain on either side of the gate, whose inversion layer forms the conducting channel. It is cut off for VGS < VT, linear for VDS < VGS − VT, and saturated for VDS ≥ VGS − VT. | Week 15 |
| Mott–Schottky plot | A graph of 1/C2 against V for a one-sided junction or Schottky diode. Uniform doping gives a straight line: its slope gives the doping and its voltage-axis intercept gives Vbi. | Week 12 |
| n-type and p-type semiconductor | Silicon doped mainly with donors is n-type: most of its free carriers are electrons. Silicon doped mainly with acceptors is p-type: most of its free carriers are holes. | Week 3 |
| n-type and p-type semiconductor; majority and minority carriers | Silicon doped with donors is n-type: electrons are the majority carriers (the more numerous) and holes the minority carriers. Silicon doped with acceptors is p-type: holes are the majority and electrons the minority. In either case the product of the two concentrations is fixed (the mass-action law): | Week 1 |
| n-type and p-type; majority and minority carriers | Donor-doped material has many more electrons than holes and is n-type; acceptor-doped material has many more holes and is p-type. The more numerous carrier is the majority carrier and the less numerous one is the minority carrier. | Week 5 |
| Ohmic contact | A metal–semiconductor contact with no significant barrier, so current flows equally easily in both directions and the I-V graph is a straight line through the origin (V = IRc). Its job is to connect a device to the circuit while adding almost no resistance. | Week 11, Week 15 |
| One-sided junction | A p-n junction with one side much more heavily doped than the other (p+n or n+p). Almost all of the depletion region then lies in the lightly doped side, so measurements on it describe that side alone. A Schottky diode behaves the same way. | Week 12, Laboratory |
| Open-circuit correction (nulling) | Measuring the test fixture with no device in place and subtracting that stray capacitance from every later reading, so only the device's capacitance is recorded. | Laboratory |
| Output resistance (ro) | The small-signal resistance seen looking into the collector, ΔVCE/ΔIC, approximately VA/IC. A large ro means the transistor behaves like a good current source. | Week 13 |
| p-n junction | The boundary inside one crystal between a p-type region and an n-type region. It is the basic building block of diodes and transistors. | Week 3, Week 10 |
| p-n junction and depletion region | The boundary between a p-type and an n-type region. Around it lies a thin depletion region, emptied of mobile carriers and containing a strong electric field. | Week 13, Week 15 |
| Passivation | Treating a surface (for example growing an oxide or depositing a nitride film) so that its dangling bonds are tied up and S becomes small. | Week 9 |
| Phonon | A quantum (packet) of vibration of the crystal lattice. It carries very little energy but can carry a large momentum, so it can supply the momentum change an electron needs in an indirect-gap material. | Week 4 |
| Pinch-off and saturation | Pinch-off is the point, at VDS = VGS − VT, where the channel charge at the drain end falls to zero. For larger VDS the transistor is in saturation: the drain current stays almost constant, set by VGS alone. | Week 14 |
| Polycrystalline material (polysilicon) | A solid made of many small single-crystal grains pointing in different directions. The boundaries between grains scatter carriers and provide leakage paths, so polysilicon is used as a raw material (and for some thin films), not as the wafer. | Week 2 |
| Predeposition (constant-source diffusion) | A diffusion in which a dopant source is present at the surface the whole time, so the surface concentration Cs stays fixed while dopant creeps deeper. It gives a complementary-error-function (erfc) profile and is used as the first doping step. | Week 3 |
| Projected range (Rp) and straggle (ΔRp) | The average depth at which implanted ions stop (Rp), and the spread of stopping depths about that average (ΔRp, a standard deviation). Both are in μm and both increase with ion energy. | Week 3 |
| Quasi-Fermi levels (EFn, EFp) | When the material is out of equilibrium (np ≠ ni2), one Fermi level can no longer describe both carriers, so two are used: EFn gives the electron concentration and EFp the hole concentration. Their separation measures how far the material is from equilibrium. | Week 8 |
| Recombination and minority-carrier lifetime (τ) | Recombination is an electron falling back into a hole, removing both. The lifetime τ is the average time an extra (excess) minority carrier survives before it recombines; in Si it ranges from about 1 ns to 1 ms. | Week 15 |
| Rectifying | Conducting much better in one direction (forward bias) than the other (reverse bias). | Week 11 |
| Resistivity (ρ) | How strongly a material opposes current, the inverse of conductivity. In doped silicon it is set mainly by the dopant concentration. | Week 2 |
| Saturation current (Is) | The small, almost voltage-independent current that flows under reverse bias, carried by minority carriers that diffuse to the depletion region and are swept across. In small silicon diodes it is about 10−15–10−12 A. | Week 10, Week 12, Laboratory |
| Saturation current (Is, Js) and ideality factor (η) | Is is the small current that flows under reverse bias; Js is the same per unit area. The ideality factor η (1 for an ideal diode, 1.0–1.1 for a good Schottky diode) measures how closely a real diode follows the ideal equation. | Week 11 |
| Saturation current of a transistor (IS) | The scale factor in the collector-current law IC = IS eqVBE/kT. It is set by the base doping, base width and device area, and is typically 10−16–10−14 A. | Week 13 |
| Scattering and mean free time (τm) | Scattering is a collision of a carrier with a vibrating atom, an impurity ion or a defect, which randomises its direction. The mean free time τm is the average time between collisions, about 0.1–1 ps. | Week 7 |
| Schottky barrier height (ΦB) | The height of the barrier an electron in the metal must climb to enter the semiconductor. It is fixed by the interface and does not change with bias. | Week 11 |
| Schottky contact (Schottky barrier) | A metal–semiconductor contact that has an energy barrier to majority carriers, so it rectifies: current flows easily in one direction and hardly at all in the other. A diode made this way is a Schottky barrier diode (SBD). | Week 11 |
| Schottky contact and barrier height (ΦB) | A rectifying metal–semiconductor contact. Electrons crossing from the metal face a barrier of height ΦB = Φm − χ, where Φm is the metal's work function and χ the semiconductor's electron affinity. | Week 15 |
| Schottky diode and barrier height (ΦB) | A Schottky diode is a rectifying metal–semiconductor contact. Its barrier height ΦB is the energy step an electron in the metal must climb to enter the semiconductor; it fixes how much current the diode can leak. | Week 12, Laboratory |
| Seed, ingot and wafer | The seed is the small single crystal, cut to the wanted orientation, that starts the growth. The ingot (boule) is the large cylindrical single crystal that is pulled. Wafers are the thin discs, typically 0.5–0.8 mm thick, sliced from the ingot and polished. | Week 2 |
| Segregation coefficient (k0) | The ratio of the dopant concentration in the freezing solid to that in the liquid it is freezing from. When k0 < 1 the crystal rejects dopant into the melt. | Week 2 |
| Semi-log plot | A graph of the natural logarithm of a quantity (here ln I) against a linear quantity (here V). An exponential law becomes a straight line on it, so slope and intercept can be read off. | Week 12 |
| Semiconductor | A material whose ability to carry electric current lies between that of a metal (conductor) and that of an insulator, and can be changed enormously by temperature, light and, above all, by adding tiny amounts of selected impurities. Silicon, germanium and gallium arsenide are the main examples. | Week 1, Week 11, Week 15 |
| Series resistance (Rs) | The resistance of the bulk semiconductor, contacts and leads in series with the junction itself. It wastes part of the applied voltage, so at high current the diode needs more voltage than the ideal equation predicts. | Week 12, Laboratory |
| Sheet resistance (Rs) | The resistance of a thin doped layer measured between opposite edges of any square of it, in ohms per square (Ω/□). It shows how much dopant has been put in: more dopant, lower Rs. | Week 3 |
| Shockley (ideal diode) equation | The current–voltage law of an ideal p-n junction, obtained by adding up the minority-carrier diffusion currents on both sides. | Week 10 |
| Shockley diode equation (Is, η) | The current–voltage law of a diode, I = Is(eqV/ηkT − 1). The saturation current Is is the tiny reverse current; the ideality factor η is 1 for an ideal diode and up to 2 when recombination in the depletion region matters. | Week 15 |
| Shockley–Read–Hall (SRH) recombination | Recombination through traps. The energy is released as lattice vibrations (heat). It is the main recombination mechanism in silicon. | Week 8 |
| Single crystal | A solid in which the atoms are arranged in one regular, repeating pattern with the same orientation throughout the whole piece. Devices are built in single-crystal silicon because carriers move through it freely and leak little. | Week 2 |
| Source-measure unit (SMU) and parameter analyser | An SMU is a precision instrument that applies a chosen voltage (or current) and measures the resulting current (or voltage) at the same time. A semiconductor parameter analyser contains several SMUs and sweeps them automatically to record device characteristics. | Laboratory |
| Specific contact resistance (ρc) | The resistance of a contact multiplied by its area, in Ω·cm2. It lets contacts of different sizes be compared. Good ohmic contacts have ρc ≈ 10−6–10−8 Ω·cm2. | Week 11 |
| Surface potential (ψs) | The amount, in volts, by which the energy bands bend at the silicon surface compared with the bulk. The gate voltage controls it. | Week 14 |
| Surface recombination velocity (S) | A measure, in cm/s, of how fast a surface destroys excess carriers: the recombination per unit area equals S times the excess density at the surface. | Week 9 |
| Surface states (dangling bonds) | Energy levels inside the band gap located at a surface, caused mainly by surface atoms whose bonds point out into nothing (dangling bonds). They act as traps. | Week 9 |
| Thermal equilibrium | The steady condition of a material left alone at a fixed temperature, with no applied voltage, light or current. Carriers are still being created and lost, but at equal rates, so their numbers do not change. | Week 5 |
| Thermal velocity (vth) | The average speed of the random motion that carriers have because of heat, about 107 cm/s in silicon at 300 K. Because the directions are random, it gives no current on its own. | Week 7 |
| Thermal voltage (kT/q) | The thermal energy kT expressed as a voltage: 0.0259 V (about 26 mV) at 300 K. It sets the voltage scale of almost every semiconductor equation. | Week 7 |
| Thermionic emission | Current carried by carriers that have enough thermal energy to jump over a barrier. It is how current flows in a Schottky diode. | Week 11 |
| Threshold voltage (VT) | The gate-to-source voltage at which strong inversion starts, so that a conducting channel joins source and drain and the transistor begins to turn on. | Week 14, Week 15, Laboratory |
| Transconductance (gm) | The change in drain current per unit change in gate voltage, gm = ∂ID/∂VGS, in siemens (A/V). It measures how good the transistor is as an amplifier. | Week 14, Laboratory |
| Transfer and output characteristics | The transfer characteristic is ID plotted against VGS at fixed VDS; the output characteristics are ID against VDS for several fixed values of VGS. | Laboratory |
| Trap (recombination centre, Nt, Et) | A localised energy level Et inside the band gap, created by a crystal defect or an impurity atom such as gold or iron. It can capture an electron and then a hole, helping them recombine in two small steps. Nt is the density of traps (cm−3). | Week 8, Week 9 |
| Tunnelling (field emission) | A quantum effect: an electron passes through a barrier that is thin enough (a few nanometres) without having the energy to go over it. It is how most practical ohmic contacts work. | Week 11 |
| Turn-on voltage and reverse leakage current | The turn-on voltage is the forward voltage at which a diode's current becomes noticeable (about 0.6 V for a Si p-n diode, 0.2–0.3 V for a Schottky diode). The reverse leakage current is the small current that flows under reverse bias. | Laboratory |
| Unit cell | The smallest block of a crystal lattice that, repeated over and over in three directions, rebuilds the whole crystal. Silicon's unit cell is a cube containing 8 atoms (the diamond-cubic structure). | Week 1, Week 6 |
| Vacuum level (Evac) | The energy of an electron at rest just outside the material, free of it. Every other energy this week is measured down from this level. | Week 11 |
| Valence band | The highest energy band that is completely filled with electrons at absolute zero (0 K). Its electrons are the ones that hold the atoms together in chemical bonds. Its top edge is at energy Ev. | Week 4 |
| Valence band and conduction band (Ev, Ec) | The valence band is the highest range of electron energies that is normally full, holding the electrons that form the covalent bonds; its top edge is Ev. The conduction band is the next range of energies above it, normally almost empty; its bottom edge is Ec. Electrons in the conduction band are free to move and carry current. | Week 5, Week 6 |
| Valence electrons | The electrons in the outermost shell of an atom. They take part in chemical bonding and decide the electrical behaviour of the material: silicon and germanium have 4, gallium and boron 3, arsenic and phosphorus 5. | Week 1 |
| Wave function (ψ) | The mathematical wave that describes an electron in quantum mechanics. It cannot be measured directly, but its square, ¦ψ¦2, gives the probability of finding the electron at each point. | Week 4 |
| Wave vector (k) | A number that says how many wave cycles fit into each unit of length, k = 2π/λ. It measures the electron's momentum, p = ħk. | Week 4 |
| Work function (Φ) | The minimum energy needed to remove an electron from the Fermi level and take it to the vacuum level. Φm is the metal's work function, Φs the semiconductor's. | Week 11 |

## Constants and units

| Symbol | Meaning | Units / typical value |
| --- | --- | --- |
| q | Magnitude of the electronic charge | 1.6×10−19 C |
| k | Boltzmann constant | 8.617×10−5 eV/K = 1.381×10−23 J/K |
| kT | Thermal energy | 0.0259 eV (often 0.02585 eV) at 300 K |
| kT/q | Thermal voltage | 0.0259 V (about 26 mV) at 300 K |
| T | Absolute temperature | kelvin (K); room temperature = 300 K |
| h | Planck constant | 6.626×10−34 J·s |
| ħ | Reduced Planck constant, h/2π | 1.055×10−34 J·s |
| m0 | Free-electron mass | 9.11×10−31 kg |
| ε0 | Permittivity of free space | 8.854×10−14 F/cm |
| εs (εsi) | Permittivity of silicon, 11.7ε0 | 1.04×10−12 F/cm |
| εox | Permittivity of SiO2, 3.9ε0 | 3.45×10−13 F/cm |
| εr | Relative permittivity (dielectric constant) | Si 11.7, SiO2 3.9, GaAs 12.9 |
| eV | Electron-volt, a unit of energy | 1 eV = 1.6×10−19 J |
| Å | Ångström, a unit of length | 1 Å = 10−10 m = 0.1 nm |
| μm | Micrometre (micron) | 1 μm = 10−4 cm = 10−6 m |

## Symbols

| Symbol | Meaning | Units / typical value |
| --- | --- | --- |
| Ec (EC) | Energy of the bottom of the conduction band | eV |
| Ev (EV) | Energy of the top of the valence band | eV |
| Eg | Band-gap energy, Ec − Ev | eV; Si 1.12, Ge 0.66, GaAs 1.42 at 300 K |
| EF | Fermi level: the energy at which a state has a 50 % chance of being occupied | eV |
| Ei | Intrinsic Fermi level, close to mid-gap | eV |
| EFn, EFp | Quasi-Fermi levels for electrons and holes, used out of equilibrium | eV |
| ED | Donor energy level, just below Ec | eV; Ec − ED ≈ 0.045 eV for P in Si |
| EA | Acceptor energy level, just above Ev | eV; EA − Ev ≈ 0.045 eV for B in Si |
| Et | Energy level of a trap (recombination centre) in the gap | eV |
| Ea | Activation energy of dopant diffusion | eV; about 3–4 eV |
| En | Allowed energy of level n of a particle in a box | J or eV |
| f(E) | Fermi–Dirac function: probability that a state at energy E is occupied | dimensionless, 0 to 1 |
| g(E), gc, gv | Density of states: allowed states per unit energy per unit volume | states/(eV·cm3) |
| Nc | Effective density of states in the conduction band | cm−3; Si 2.8×1019 at 300 K |
| Nv | Effective density of states in the valence band | cm−3; Si 1.04×1019 at 300 K |
| n | Electron concentration (free electrons per cm3) | cm−3 |
| p | Hole concentration (holes per cm3) | cm−3 |
| ni | Intrinsic carrier concentration (n = p = ni in pure material) | cm−3; Si ≈ 1×1010 at 300 K |
| n0, p0 | Equilibrium electron and hole concentrations | cm−3 |
| pn0, np0 | Equilibrium minority concentrations: holes on the n side, electrons on the p side | cm−3; pn0 = ni2/ND |
| ND | Donor concentration | cm−3 |
| NA | Acceptor concentration | cm−3 |
| ND+, NA− | Concentrations of ionised donors and acceptors | cm−3 |
| Δn, Δp | Excess electron and hole concentrations above equilibrium | cm−3 |
| m∗, mn∗, mp∗ | Effective mass of electrons or holes | kg, or as a multiple of m0 |
| ψ | Wave function (¦ψ¦2 is the probability density) | — |
| V(x) | Potential energy in the Schrödinger equation | J or eV |
| k (wave vector) | Wave vector, 2π/λ; measures the electron's momentum, p = ħk | m−1 or cm−1 |
| α (Kronig–Penney) | √(2mE)/ħ, set by the electron energy | m−1 |
| P (Kronig–Penney) | Barrier strength mV0ba/ħ2 | dimensionless |
| V0 | Height of a potential barrier | J or eV |
| λ | Wavelength | μm or nm; λ(μm) = 1.24/E(eV) |
| ν, hν | Frequency of light, and photon energy | Hz; eV |
| a | Lattice constant: edge length of the cubic unit cell | Å; Si 5.43, Ge and GaAs 5.65 |
| (h k l), {h k l} | Miller indices of a plane; family of equivalent planes | integers |
| [u v w], ⟨u v w⟩ | A crystal direction; family of equivalent directions | integers |
| dhkl | Spacing between neighbouring (h k l) planes, a/√(h2 + k2 + l2) | Å |
| rnn | Nearest-neighbour distance | Å; Si 2.35 |
| k0 | Segregation coefficient, Cs/Cl at the freezing interface | dimensionless; B 0.8, P 0.35 |
| Cs | Surface concentration of a diffusion (or solid concentration when freezing) | cm−3 |
| Cl, C0 | Concentration in the melt (liquid); C0 at the start | cm−3 |
| f (growth) | Fraction of the melt already solidified | 0 to 1 |
| C(x, t) | Dopant concentration at depth x and time t | cm−3 |
| D | Diffusion coefficient (dopants in a furnace, or carriers) | cm2/s |
| D0 | Diffusion constant in D = D0e−Ea/kT | cm2/s |
| J (Fick) | Dopant flux: atoms crossing 1 cm2 per second | atoms/(cm2·s) |
| F | Particle flux in Fick's law | particles/(cm2·s) |
| Q | Dose: dopant atoms per unit area (in Weeks 13–14, Q also means charge) | atoms/cm2 (C or C/cm2 for charge) |
| Φ (dose) | Implanted dose (ions per cm2) | cm−2 |
| erfc | Complementary error function, erfc(u) = 1 − erf(u); read from a table | dimensionless |
| xj | Junction depth: where the dopant concentration equals the background | μm |
| NB (CB) | Background doping of the wafer (in Week 13, NB is the base doping) | cm−3 |
| Rp | Projected range: average depth at which implanted ions stop | μm |
| ΔRp | Straggle: spread of the implanted ions' stopping depths | μm |
| Np | Peak concentration of an implanted profile | cm−3 |
| Sn, Se | Nuclear and electronic stopping power of an implanted ion | eV·cm2 |
| NSi | Atom density of silicon | 5×1022 cm−3 |
| Rs | Sheet resistance (or diode series resistance in Week 12) | Ω/□ (ohms per square); Ω |
| xmask | Thickness of an implant mask | μm |
| E (field) | Electric field (on band diagrams, E is energy instead) | V/cm |
| μ, μn, μp | Mobility: drift velocity per unit field (electrons, holes) | cm2/(V·s); Si μn 1350, μp 480 |
| μL, μI | Mobility limited by lattice scattering, by ionised-impurity scattering | cm2/(V·s) |
| vd | Drift velocity | cm/s |
| vth | Thermal velocity of carriers | ≈ 107 cm/s at 300 K |
| vsat | Saturation velocity at high field | ≈ 107 cm/s in Si |
| τm | Mean free time between collisions | s; about 0.1–1 ps |
| σ | Conductivity, q(nμn + pμp) (in Week 8, σ is also a capture cross-section) | S/cm (siemens per cm) |
| ρ | Resistivity, 1/σ | Ω·cm |
| J, Jn, Jp | Current density (total, electrons, holes) | A/cm2 |
| Dn, Dp | Diffusion coefficients of electrons and holes | cm2/s; Si 35 and 12.4 |
| RH, VH, B | Hall coefficient, Hall voltage, magnetic flux density | cm3/C; V; T (Wb/m2) |
| Te | Electron temperature of hot carriers | K |
| G, GL | Generation rate of electron–hole pairs (GL: by light) | cm−3s−1 |
| R | Recombination rate | cm−3s−1 |
| U | Net recombination rate, R − G | cm−3s−1 |
| τ, τn, τp | Minority-carrier lifetime (τeff: effective, including surfaces) | s; Si 1 ns – 1 ms |
| Nt | Density of traps (recombination centres) | cm−3 |
| σn, σp | Capture cross-section of a trap for electrons, holes | cm2 |
| n1, p1 | SRH parameters nie(Et − Ei)/kT and nie(Ei − Et)/kT | cm−3 |
| L, Ln, Lp | Diffusion length √(Dτ): distance a minority carrier travels before recombining | μm or cm |
| S | Surface recombination velocity | cm/s |
| Nst | Density of surface traps | cm−2 |
| Us | Recombination rate per unit area at a surface | cm−2s−1 |
| Vbi | Built-in potential of a junction or Schottky contact | V; typically 0.5–1 V |
| V, Va | Applied voltage (positive for forward bias) | V |
| W | Depletion-region width (in Week 13 WB, WE are base and emitter widths; in Week 14 W is channel width) | μm or cm |
| xn, xp | Parts of the depletion region on the n side and on the p side | μm |
| Emax | Peak electric field, at the junction | V/cm |
| Is, Js (IS) | Saturation current (density) of a diode or transistor | A; A/cm2 |
| I | Current | A |
| A (area) | Device or contact area | cm2 |
| η | Ideality factor of a diode, 1 (ideal) to 2 | dimensionless |
| C, Cj | Capacitance (junction or depletion capacitance) | F (pF = 10−12 F) |
| VBR | Breakdown voltage | V |
| Φm | Work function of a metal | eV; Al 4.28, Au 5.1 |
| Φs | Work function of a semiconductor, χ + (Ec − EF) | eV |
| χ | Electron affinity: energy from Ec up to the vacuum level | eV; Si 4.05 |
| ΦB | Schottky barrier height seen from the metal | eV (or V) |
| A∗∗ | Effective Richardson constant | A/(cm2·K2); n-Si ≈ 110 |
| ρc | Specific contact resistance | Ω·cm2 |
| Evac | Vacuum level: energy of an electron just free of the material | eV |
| IE, IB, IC | Emitter, base and collector currents | A (mA) |
| VBE, VCE, VCB | Base–emitter, collector–emitter and collector–base voltages | V |
| α, β, γ (cell) | Angles between the edges of a unit cell | degrees; 90° for cubic |
| α | Common-base current gain, IC/IE | dimensionless; 0.98–0.999 |
| β | Common-emitter current gain, IC/IB (also hFE) | dimensionless; 50–500 |
| γ (BJT) | Emitter injection efficiency | dimensionless, close to 1 |
| αT | Base transport factor | dimensionless, close to 1 |
| NE, WE, DE; NB, WB, DB | Doping, width and minority diffusion coefficient of the emitter; of the base | cm−3; μm; cm2/s |
| VA | Early voltage | V |
| ro | Output resistance | Ω |
| τB | Base transit time, WB2/2Dn | s |
| fT | Transition (cut-off) frequency | Hz |
| Cox | Gate-oxide capacitance per unit area, εox/tox | F/cm2 |
| tox | Gate-oxide thickness | nm |
| φF, ψs (φs) | Bulk Fermi potential (kT/q)ln(NA/ni); surface potential (band bending) | V |
| Wd, Wdmax, Qdmax | MOS depletion width, its maximum at inversion, and the depletion charge then | μm; C/cm2 |
| VT (Vth) | Threshold voltage of a MOSFET | V |
| VFB | Flat-band voltage | V |
| Φms, Qf | Gate–substrate work-function difference; fixed oxide charge | V; C/cm2 |
| γ (MOSFET) | Body-effect coefficient √(2qεsiNA)/Cox | V1/2 |
| VGS, VDS, VSB, VG | Gate–source, drain–source, source–body and gate voltages | V |
| ID | Drain current | A (mA) |
| W/L | Channel width-to-length ratio | dimensionless |
| gm | Transconductance, ∂ID/∂VGS | S (A/V) |
| k (MOSFET) | Device parameter μnCox(W/L) | A/V2 (mA/V2) |
| λ (MOSFET) | Channel-length modulation parameter | V−1 |
| λmax | Longest wavelength a material absorbs, 1.24/Eg (μm, Eg in eV) | μm |
| σi, ρi | Conductivity and resistivity of intrinsic (undoped) material; σdoped after doping | S/cm; Ω·cm |
| alayer, asub | Lattice constants of the grown layer and of the substrate | Å |
| Ntotal | Total number of dopant atoms in a region | atoms |
| ψk(x), uk(x) | Bloch wavefunction of an electron, and its part that repeats with the lattice | — |
| Fn, Fp | Particle flux of electrons and holes (carriers crossing 1 cm2 per second) | cm−2s−1 |
| Bz, Ix, VH | Hall effect: magnetic field (z), current (x) and Hall voltage | T (tesla); A; V |
| RH | Hall coefficient, 1/qp (p-type) or −1/qn (n-type) | cm3/C |
| vdn, vdp | Drift velocity of electrons and holes | cm/s |
| μi, τi (μL, μI, NI) | Mobility and scattering time for one scattering mechanism (L: lattice, I: ionised impurity); NI = ionised-impurity density | cm2/(V·s); s; cm−3 |
| Jdrift, Jdiff | Drift and diffusion parts of the current density | A/cm2 |
| Esat | Field at which the drift velocity saturates, vsat/μ | V/cm |
| Gth, Rth | Thermal generation and recombination rates (equal in equilibrium) | cm−3s−1 |
| Gn, Gp, Rn, Rp | Generation and recombination rates of electrons and holes | cm−3s−1 |
| ft, en, ep | Probability a trap is occupied by an electron; emission rates of electrons and holes from traps | dimensionless; s−1 |
| ra, rb, rc, rd | SRH rates: electron capture, electron emission, hole capture, hole emission | cm−3s−1 |
| τSRH, τradiative, τAuger | Lifetimes set by trap (SRH), radiative and Auger recombination | s |
| τb (τbulk), τsurface | Lifetime from bulk recombination only; from surface recombination only | s |
| Us, ps, Δps | Surface recombination rate; hole density and excess at the surface | cm−2s−1; cm−3 |
| nn0, pp0, pn0, np0 | Equilibrium densities: majority (nn0, pp0) and minority (pn0 holes on n side, np0 electrons on p side) | cm−3 |
| Δpn, Δnp | Excess minority carriers at the depletion edges (holes on n side, electrons on p side) | cm−3 |
| Rc | Contact resistance | Ω (specific: Ω·cm2) |
| ΦBn, ΦBp | Schottky barrier height for electrons (n-type) and for holes (p-type) | eV |
| Vjunction | Part of the applied voltage that appears across the junction itself | V |
| IE,n, IE,p, IC,n | Electron and hole parts of the emitter and collector currents | A |
| nB(x) | Minority-electron density in the base of an NPN transistor | cm−3 |
| Igen, Jgen | Generation current (density) from carriers generated in the depletion region | A; A/cm2 |
| pn, np | Minority-carrier density: holes on the n side, electrons on the p side | cm−3 |
| ΔID, ΔVGS | Small changes in drain current and gate voltage (their ratio is gm) | A; V |
| Qcharge | Total charge delivered by the ion beam, I × t | C |
| B (recombination) | Radiative recombination coefficient, R = B np | cm3/s; GaAs ≈ 10−10, Si ≈ 10−14 |
| Cn, Cp (Auger) | Auger recombination coefficients | cm6/s; Si ≈ 10−31 |
| τ0 (τg) | Effective generation lifetime in a depletion region | s |
| fm | Lattice mismatch, (alayer − asub)/asub | dimensionless, usually in % |
| vpull | Pull rate of a Czochralski crystal | mm/min |
| λc | Cut-off wavelength of a detector, 1.24/Eg (μm, Eg in eV) | μm |
| c | Speed of light in vacuum | 3×108 m/s |
| erfc(u), erfc−1 | Complementary error function, 1 − erf(u), and its inverse (read from a table) | dimensionless |
| N(x), N(W) | Doping concentration at depth x (or at the depletion edge W), from C-V profiling | cm−3 |
| VEB, VBC (VCB) | Emitter–base and base–collector voltages | V |
| ΔV, ΔVBE | A small change in a voltage | V |
| IC1, IC2 | Collector currents at two operating points | A |
| r (atom) | Atomic radius (hard-sphere model), half the nearest-neighbour distance | Å |
| t | Time (or a thickness, where the text says so) | s (or cm) |
| ΔVT | Shift in threshold voltage (e.g. from body bias) | V |

## Abbreviations

| Abbreviation | Meaning |
| --- | --- |
| Si | Silicon |
| Ge | Germanium |
| GaAs | Gallium arsenide |
| GaN | Gallium nitride |
| SiC | Silicon carbide |
| InP | Indium phosphide |
| GaP | Gallium phosphide |
| SiO2 | Silicon dioxide (silica), the oxide insulator |
| CB | Conduction band |
| VB | Valence band |
| FCC | Face-centred cubic lattice |
| BCC | Body-centred cubic lattice |
| SC | Simple cubic lattice |
| APF | Atomic packing factor |
| III–V | Compound of Group III and Group V elements (e.g. GaAs) |
| MG-Si | Metallurgical-grade silicon (≈ 98 % pure) |
| EG-Si | Electronic-grade silicon (99.9999999 % or better) |
| CZ | Czochralski crystal growth |
| FZ | Float-zone crystal growth |
| CVD | Chemical vapour deposition |
| VPE | Vapour-phase epitaxy |
| LPE | Liquid-phase epitaxy |
| MBE | Molecular-beam epitaxy |
| MOCVD | Metal-organic chemical vapour deposition |
| UHV | Ultra-high vacuum (≈ 10−10 Torr) |
| RHEED | Reflection high-energy electron diffraction (counts atomic layers during MBE) |
| RTA | Rapid thermal annealing |
| SIMS | Secondary-ion mass spectrometry |
| TLM | Transmission-line method (contact resistance) |
| SRH | Shockley–Read–Hall (trap-assisted) recombination |
| LDD | Lightly doped drain |
| I-V | Current–voltage (measurement or characteristic) |
| C-V | Capacitance–voltage (measurement or characteristic) |
| LCR | Inductance–capacitance–resistance meter |
| SMU | Source-measure unit |
| MOS | Metal–oxide–semiconductor |
| MOSFET | Metal–oxide–semiconductor field-effect transistor |
| CMOS | Complementary MOS (n- and p-channel MOSFETs together) |
| FET | Field-effect transistor |
| JFET | Junction field-effect transistor |
| MESFET | Metal–semiconductor field-effect transistor |
| HEMT | High-electron-mobility transistor |
| BJT | Bipolar junction transistor |
| HBT | Heterojunction bipolar transistor |
| NPN | BJT with n-type emitter, p-type base, n-type collector |
| PNP | BJT with p-type emitter, n-type base, p-type collector |
| E–B | Emitter–base (junction) |
| C–B | Collector–base (junction) |
| IC | Integrated circuit |
| VLSI | Very-large-scale integration |
| LED | Light-emitting diode |
| RF | Radio frequency |
| IGBT | Insulated-gate bipolar transistor |
| MEMS | Micro-electro-mechanical systems |
| CAT | Continuous Assessment Test |
| PGD | Postgraduate Diploma |
| DC | Direct current (steady) |
| AC | Alternating current (small signal) |
| n+ | Very heavily doped n-type (similarly p+) |
| LCM | Lowest common multiple |
| LHS | Left-hand side (of an equation) |
| MATLAB | A numerical computing program (alternative to Python) |
| KOH | Potassium hydroxide (an anisotropic silicon etchant) |
| UV | Ultraviolet |
| IR | Infrared |
| VCSEL | Vertical-cavity surface-emitting laser |
| PCD | Photoconductive decay (lifetime measurement) |
| TCAD | Technology computer-aided design (device simulation software) |
| FD | Fermi–Dirac (distribution) |